PEALD Ru Process with Novel Carbonyl Cyclohexadiene Ruthenium Precursor and Low Oxygen Incorporation based on Hydrogen Plasma

Geonwoo Park*, ‡, Keunhoi Kim*, ‡, Jeong Woo Shin**, ***, Geongu Han*, Dohyun Go****, †, and Jihwan An **, *****, †

*Department of Manufacturing Systems and Design Engineering (MSDE), Seoul National University of Science and Technology, Seoul, Republic of Korea
**Energy & Environment Research Institute, Seoul National University of Science and Technology, Seoul, Republic of Korea

***Department of Mechanical and Aerospace Engineering, Nanyang Technological University, Singapore

****Department of Chemistry and Biochemistry, University of California San Diego, La Jolla, USA

*****Department of Mechanical Engineering, Pohang University of Science and Technology (POSTECH), Pohang, Republic of Korea

‡These authors contributed equally to this work

†Corresponding authors

Dohyun Go, Ph.D.

Post-doctoral scholar, Department of Chemistry and Biochemistry

University of California San Diego

9500 Gilman Dr, La Jolla, CA 92093

E-mail: dogo@ucsd.edu

Jihwan An, Ph.D.

Associate Professor, Department of Mechanical Engineering

Pohang University of Science and Technology (POSTECH)

77 Cheongam-ro, Nam-gu, Pohang, Gyeongbuk, 37673 Republic of Korea

E-mail: jihwanan@postech.ac.kr, Tel: +82-54-279-2177

Fig. S1. Schematic figure of ICP-type PE-ALD system used in this study.

Fig. S2. X-ray reflectivity spectra of PE-ALD Ru films on Si depending on the (a) precursor pulse time, (b) H2 plasma pulse time, (c) purge time, and (d) deposition temperature.

Table S1. Detailed GPC data according to the variation of process parameters, 1) precursor pulse time (0.5, 1, and 2 s), 2) H2 plasma pulse time (5, 10, and 20 s), 3) purge time (10, 30, and 60 s), and 4) deposition temperature (150, 200, 250, and 275 ℃).

| Parameter | The number of PEALD cycle | Precursor pulse time (s) | H2 plasma pulse time (s) | Purge time (s) | Deposition temperature (℃) | GPC (Å /cycle) |
| --- | --- | --- | --- | --- | --- | --- |
| Precursor pulse | 100 | 0.5 | 10 | 30 | 250 | 1.2 ± 0.1 |
|  |  | 1 |  |  |  | 1.2 ± 0.1 |
|  |  | 2 |  |  |  | 1.5 ± 0.1 |
| H2 plasma pulse |  | 1 | 5 | 30 | 250 | 1.3 ± 0.1 |
|  |  |  | 10 |  |  | 1.2 ± 0.1 |
|  |  |  | 20 |  |  | 1.2 ± 0.1 |
| Purge |  | 1 | 10 | 15 | 250 | 1.1 ± 0.1 |
|  |  |  |  | 30 |  | 1.2 ± 0.1 |
|  |  |  |  | 60 |  | 1.2 ± 0.1 |
| Deposition temperature |  | 1 | 10 | 30 | 150 | 1.7 ± 0.4 |
|  |  |  |  |  | 200 | 2.3 ± 0.4 |
|  |  |  |  |  | 250 | 1.2 ± 0.1 |
|  |  |  |  |  | 275 | 2.9 ± 0.7 |

Fig. S3. XPS survey scan of PE-ALD Ru thin films which is deposited in standards recipe (1 s Ru precursor pulse – 10 s exposure time – 30 s Ar purge time – 10 s H2 plasma pulse time – 30 s Ar purge time at a temperature of 250 ℃).

Table S2. Detailed single components of high-resolution XPS spectra of Ru 3d peak of PE-ALD Ru films on Si.

| Peak | Position (eV) | Area | FWHM (eV) | % GL (%) | at. % |
| --- | --- | --- | --- | --- | --- |
| Ru 3d (5/2) | 280.23 | 343181.6 | 0.71 | 36 | 95.54302 |
| Ru 3d (3/2) | 284.4 | 227516.3 | 1.07 | 49 |  |
| RuOx (5/2) | 281.07 | 36927.18 | 0.79 | 72 |  |
| RuOx (3/2) | 285.24 | 24618.12 | 1.2 | 76 |  |
| C 1s | 283.13 | 5750.692 | 0.75 | 100 | 3.713366 |
| O 1s | 530.541 | 3374.168 | 1.756 | 32 | 0.743613 |