Supplementary Information

Quantum spin liquid signatures in monolayer 1T-NbSe2

Quanzhen Zhang1,#, Wen-Yu He2,#, Yu Zhang1,3,#,*,Yaoyao Chen1,#, Liangguang Jia1, Yanhui Hou1, Hongyan Ji1, Huixia Yang1, Teng Zhang1, Liwei Liu1, Hong-Jun Gao4, Thomas A Jung5, and Yeliang Wang1,*

1School of Integrated Circuits and Electronics, MIIT Key Laboratory for Low-Dimensional Quantum Structure and Devices, Beijing Institute of Technology, Beijing 100081, China.

2School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China.

3Advanced Research Institute of Multidisciplinary Sciences, Beijing Institute of Technology, Beijing 100081, China.

4Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China.

5Laboratory for X-ray Nanoscience and Technologies, Paul Scherrer Institut (PSI), 5232 Villigen, Switzerland.

*Correspondence and requests for materials should be addressed to Yu Zhang (e-mail: yzhang@bit.edu.cn) and Yeliang Wang (e-mail: yeliang.wang@bit.edu.cn).

Supplementary Fig. 1 | Large-scale topographic STM image of monolayer 1H-NbSe2, 1T-NbSe2, and their vertical heterostructure on BLG/SiC(0001) substrate (Vb = -1.5 V, It = 10 pA).

Supplementary Fig. 2 | Atomic structure of 1H-NbSe2. a, Atomic resolution STM image of monolayer 1H-NbSe2 on BLG/SiC(0001) substrate recorded at the sample bias of -0.1 V. b, The corresponding FFT image of the atomic STM image of monolayer 1H-NbSe2. The six bright spots enclosed by the dashed red circles and the six bright spots enclosed by the dashed yellow circles indicate the atomic and CDW wavevectors of monolayer 1H-NbSe2 with 1 × 1 and 3 × 3 patterns, respectively. The basis vectors of the atomic and CDW pattern are indicated as a1*/a2* and b1*/b2*, respectively.

Supplementary Fig. 3 | FFT images of the STS maps at the sample bias of 0.6 V, 0.7 V, and 0.8 V, from left to right, respectively. The six bright spots enclosed by the red circles indicate the CDW wavevectors of monolayer 1T-NbSe2, while the spots enclosed by the yellow circles are related to the charge modulation with their real-space wavelength being √3 times larger (correspondingly smaller in momentum space) of the CDW wavevectors. The white hexagon represents the CDW Brillouin zone (BZ).

Supplementary Fig. 4 | MnPc molecules with two topographic configurations via an STM tip manipulation technique. a, Topographic STM image of MnPc molecules adsorbed off the SOD motifs. b, After the STM tip manipulation, the molecule adsorbed on the SOD motifs. The four lobes of the MnPc molecules are roughly classified into Pc-1 and Pc-2, given the lobe locating on and off a SOD motif, respectively.

Supplementary Note

The MnPc molecule with S = 3/2 is treated as an idealized local magnetic impurity in the theoretical calculation. In the underscreened Kondo regime, a local spin of S = 1 is expected to remain in the magnetic impurity, while the spin S = 1/2 undergoes Kondo spin exchange with the itinerant spinons1. For the magnetic impurity deposited on the U(1) quantum spin liquid (QSL) with spinon Fermi surface (SFS), the magnetic impurity couples to the QSL electronic states individually in the spin and charge channels. In the slave rotor mean field description, the Matsubara Green’s functions for the auxiliary fermion and the charged boson at the impurity take the form

Ga, σiωn=1iωn-ϵ0+h-w2Gf,σiωn, R, R,

GXdiνn=1νn2U-2iνnhU+λ-u2GXiνn, R,R,

with the imaginary-time Green’s function Gf, σiωn,R,R=k1iωn-ξk for the spinon and GXiνn,R,R=k1iνn+ϵk-1iνn-ϵk for the chargon, respectively. Here the coupling fields w, u and the Lagrangian multipliers λ, h take the value at the saddle point with the minimal free energy, based on the mean-field theory. ϵ0 is the impurity on-site energy, U is the onsite repulsion, and σ = ↑/↓ is the spin index. ωn and νn are the fermionic and bosonic Matsubara frequencies, respectively. The spinon and chargon states in the U(1) QSL with SFS have the Matsubara Green’s function as

Gf, σ0iωn, R, R=1Gf, σ-1iωn, R,R-w2iωn-ϵ0+h,

GX0iνn, R,R=1GX-1iνn,R,R-u2νn2U-2iνnhU+λ.

Given the mean field parameters w=-0.03 eV, u=0.16 eV, h=0.002 eV, λ=1.28 eV, and the onsite repulsion U=5 eV at the impurity, we obtain the auxiliary fermion density of states (DOS)

ρa, σ0ω=-1πImGa,σ0iωn→ω+i0+,

the charged boson DOS

ρXd0ω=-1πImGXdiνn→ω+i0+,

the QSL spinon DOS

ρf, σ0ω=-1πImGf, σ0iωn→ω+i0+,

and the QSL chargon DOS

ρX0ω=-1πImGXiνn→ω+i0+.

The Matsubara Green’s functions for the electronic state at the impurity and QSL electronic states are obtained through the convolution

Gd, σ0iωn=1βνnGa, σiωn+iνnGXdiνn,

Gc, σiωn, R,R=1βνnGf, σ0iωn+iνn, R, RGX0iνn, R,R.

Here β-1=kbT is the Boltzmann constant. The corresponding DOS spectra are plotted in Supplementary Fig. 6 as well. Here the band dispersions of the spinon and chargon in the QSL are

ξk=2tf2cos12kxacos32kya+coskxa-μf

ϵk=2tX2cos12kxacos32kya+coskxa-3+Δ.

The longitudinal gauge field fluctuations in the QSL gives rise to the gauge binding interaction

HUb=Ubσfσ, R†fσ, RaR†aR-fσ, R†fσ, RbR†bR,

with fσ, R†, aR†, bR† being the annihilation (creation) operators for the spinon, holon, and doublon states in the QSL. Taking the gauge binding UR into account, the Matsubara Green’s function for the impurity electronic state reads

Gd, σiωn=i,j=1,2G0,σ11iωn+G0,σ12iωnURσz1-G0,σ22iωnURσz-1G0,σ21iωnij,

with the form of G0, σiωn given in the method section. The local electronic DOS of the impurity is then ρd,σω=-1πImGd, σiωn→ω+i0+. As the gauge binding interaction increases, a pair of band edge resonance peaks in ρd,σω gradually emerge as is plotted in Supplementary Fig. 7.

In the case that the holon-spinon hole binding interaction is effectively suppressed:

HUb'=-URσfσ, R†fσ, RbR†bR,

the Matsubara Green’s function for the impurity electronic state takes the form

Gd, σ'iωn=i,j=1,2G0,σ11iωn+G0,σ12iωnURσ'1-G0,σ22iωnURσz-1G0,σ21iωnij with σ'=000-1.

The corresponding impurity electronic DOS is ρd,σ'ω=-1πImGd, σ'iωn→ω+i0+, which has only one single resonance peak at the bottom of the UHB as plotted in Fig. 4d (green line).

Supplementary Fig. 5 | The DOS in the pristine QSL and at the position of the adsorbate acting like a Kondo-impurity. a, Energy diagram of the QSL state. b, Schematic diagram of the QSL state detected via STM. c, Energy diagram of the band edge resonance states. d, Physical mechanism of the interaction between a QSL state and a local magnetic moment. A magnetic impurity in a QSL candidate can result in a spinon Kondo screening cloud (brown shadow). Such a cloud attracts a chargon in QSL under the spin-charge binding interaction.

Supplementary Fig. 6 | The DOS in the pristine QSL and at the position of the adsorbate acting like a Kondo-impurity. a-c, The DOS of the spinon, chargon, and the electronic states in the pristine QSL, respectively. In the case of the pristine QSL, there is no magnetic impurity present. The DOS can be obtained from the Green’s functions through setting the coupling parameters u=w=0 eV. d-f, The DOS of the auxiliary fermion, charged boson and electronic state at the adsorbate position acting like an impurity, respectively. Here, the spin exchange between the impurity and the QSL gives rise to the spinon Kondo resonance in the spin channel.

Supplementary Fig. 7 | The emergence of a pair of band edge resonance peaks in the local electronic DOS of the local magnetic impurity. The gauge binding is considered in both the doublon-spinon channel and the holon-spinon hole channel. The spinon-chargon binding interaction UR modifies the impurity electronic Green’s function, which is expected to induce the spectral weight to transfer from the bulk Hubbard bands to the band edges. Experimentally, UR depends on the location of a magnetic molecular related to the SOD motif.

References

- Nagaosa, N. Quantum Field Theory in Strongly Correlated Electronic Systems (Springer, 1999).