Supporting Information

for

Automotive urban minerals formation in China and Japan

Guochang Xua,c, Fei Liua, Youping Miaoa, Binze Wangb, Zhengyang Zhangb*, Jinhui Lia, Kazuyo Matsubaeb, Xianlai Zenga*

a State Key Joint Laboratory of Environment Simulation and Pollution Control, School of Environment, Tsinghua University, 100084, Beijing, China

b Graduate School of Environmental Studies, Tohoku University, Aoba 468-1, Aramaki, Aoba-ku, Sendai, 980-8574, Japan

c Material Cycles Division, National Institute for Environmental Studies, Onogawa 16-2, Tsukuba 305-8506, Japan

* Corresponding author: xlzeng@tsinghua.edu.cn (X.Z.); zhengyang.zhang.a8@tohoku.ac.jp (Z.Z.)

This document (53 pages) includes:

- Tables S1−S38

- Figures S1

- References

Contents

Abbreviations and Acronyms	S1

Definition of key terms	S2

Supplementary Methods	S3

Table S1. Material content in vehicles reviewed from literature of Castro et al.	S3

Table S2. Material content in vehicles reviewed from literature of Elgowainy  et al.	S4

Table S3. Material content in vehicles reviewed from literature of Field et al.	S5

Table S4. Material content in vehicles reviewed from literature of Yano et al.	S6

Table S5. Material content in vehicles reviewed from literature of Kosai et al.	S7

Table S6. Material content in vehicles reviewed from literature of Bhuwalka et al.	S8

Table S7. Metal price in global markets from 2016 to 2022.	S9

Table S8. Number of vehicle sales in China between 1990 and 2022	S10

Table S9. Number of vehicle sales in Japan between 1990 and 2022	S11

Table S10. Shape and scale parameters (Weibull distribution) of vehicles in China and Japan	S12

Fig. S1. Remaining rate of vehicles. a) China; b) Japan.	S13

Table S11. ELV collection ratios and metal separation-recycling ratios in China and Japan	S14

Supplementary Results	S16

Table S12. Estimated average material content per vehicle summarized from literature review	S16

Table S13. Estimated average material value per vehicle	S17

Table S14. Estimated number of vehicle sales in China in 2022−2050 in standard scenario	S18

Table S15. Estimated number of vehicle sales in China in 2022−2050 in low scenario	S19

Table S16. Estimated number of vehicle sales in China in 2022−2050 in high scenario	S20

Table S17. Estimated number of vehicle sales in Japan in 2022−2050 in standard scenario	S21

Table S18. Estimated number of vehicle sales in Japan in 2022−2050 in low scenario	S22

Table S19. Estimated number of vehicle sales in Japan in 2022−2050 in high scenario	S23

Table S20. Estimated number of in-use vehicles in China in 2022−2050 in standard scenario	S24

Table S21. Estimated number of in-use vehicles in China in 2022−2050 in low scenario	S25

Table S22. Estimated number of in-use vehicles in China in 2022−2050 in high scenario	S26

Table S23. Estimated number of in-use vehicles in Japan in 2022−2050 in standard scenario	S27

Table S24. Estimated number of in-use vehicles in Japan in 2022−2050 in low scenario	S28

Table S25. Estimated number of in-use vehicles in Japan in 2022−2050 in high scenario	S29

Table S26. Estimated number of ELVs in China in 2022−2050 in standard scenario	S30

Table S27. Estimated number of ELVs in China in 2022−2050 in low scenario	S31

Table S28. Estimated number of ELVs in China in 2022−2050 in high scenario	S32

Table S29. Estimated number of ELVs in Japan in 2022−2050 in standard scenario	S33

Table S30. Estimated number of ELVs in Japan in 2022−2050 in low scenario	S34

Table S31. Estimated number of ELVs in Japan in 2022−2050 in high scenario	S35

Table S32a. Estimated material demand for producing vehicles in China in 2022−2050 following standard scenario (Fe−Ag)	S36

Table S32b. Estimated material demand for producing vehicles in China in 2022−2050 following standard scenario (Pd−Nb)	S37

Table S33a. Estimated material demand for producing vehicles in Japan in 2022−2050 following standard scenario (Fe−Ag)	S38

Table S33b. Estimated material demand for producing vehicles in Japan in 2022−2050 following standard scenario (Pd−Nb)	S39

Table S34a. Estimated automotive urban mineral formation in China in 2022−2050 following standard scenario (Fe−Ag)	S40

Table S34b. Estimated automotive urban mineral formation in China in 2022−2050 following standard scenario (Pd−Nb)	S41

Table S35a. Estimated automotive urban mineral formation in Japan in 2022−2050 following standard scenario (Fe−Ag)	S42

Table S35b. Estimated automotive urban mineral formation in Japan in 2022−2050 following standard scenario (Pd−Nb)	S43

Table S36a. Estimated UMS of vehicles in China in 2022−2050 following standard scenario (Fe−Ag)	S44

Table S36b. Estimated UMS of vehicles in China in 2022−2050 following standard scenario (Pd−Nb)	S45

Table S37a. Estimated UMS of vehicles in Japan in 2022−2050 following standard scenario (Fe−Ag)	S46

Table S37b.Estimated UMS of vehicles in Japan in 2022−2050 following standard scenario (Pd−Nb)	S47

Table S38. Sensitivity of parameters	S48

References	S49

# Abbreviations and Acronyms

AUM			Automotive urban mineral

BEV			Battery electric vehicle

ELV			End-of-life vehicle

EV			Electric vehicle

FCV			Fuel cell vehicle

GHG			Greenhouse gas

HEV			Hybrid electric vehicle

ICEV			Internal combustion engine vehicle

PGM			Platinum group metal

PHEV			Plug-in hybrid electric vehicles

REE			Rear earth element

UM			Urban mineral

UMS			Urban material stock

# Definition of key terms

BEV is a type of EVs that exclusively uses chemical energy stored in rechargeable battery packs, with no secondary source of propulsion. BEVs do not use gasoline or diesel and do not produce tailpipe emissions, making them more environmentally friendly than conventional vehicles1. Some examples of the most popular BEVs are Wuling Hongguang Mini EV, Leaf, and Tesla Model 3.

Both HEV and PHEV are hybrid electric vehicles that use a combination of an internal combustion engine and an electric motor to power the vehicle. The primary difference between them is that a PHEV has a charging port and a larger battery that can be plugged into the grid, while an HEV does not. A PHEV can operate more like an EV, driving off the battery for longer distances before the ICE kicks in, while an HEV only uses the battery for short distances2. A typical HEV is Toyota Prius.

FCV is an electric vehicle that uses a fuel cell to power its onboard electric motor. A fuel cell is a device that generates electricity through a chemical reaction of hydrogen and oxygen. FCV can run on hydrogen alone without emitting carbon dioxide or other pollutants, making it a zero-emission vehicle3. A typical FCV is Toyota Mirai.

ELV is a vehicle that has reached the end of its useful life and is considered as waste. ELVs can cause environmental problems if they are improperly managed, such as releasing hazardous substances or wasting valuable materials. ELVs can be a secondary resource if they are properly managed and recycled. ELV management can reduce GHG emissions, save energy and materials, and create economic benefits4.

UM refers to the resources of metals, plastics, rubber, etc., that can be recycled from waste mechanical and electrical equipment, wires and cables, communication tools, automobiles, household appliances, electronic products, and other scraps generated and accumulated during industrialization and urbanization; their utilization is equivalent to primary mineral resources5.

UMS is the amount of materials contained in cities' products, buildings, and infrastructure. UMS reflects the historical accumulation of natural resources consumed in urban development. It can help understand cities' urban metabolism, material efficiency, and circular economy potential6.

# Supplementary Methods

## Table S1. Material content in vehicles reviewed from literature of Castro et al.7

In this study, an average passenger vehicle in Netherlands is defined with average weight and material composition.

| Material | ICEV (kg) |
| --- | --- |
| Entire sample vehicle | 880 |
| Fe | 581 |
| Al | 30 |
| Cu | 15 |
| Co | - |
| Pb | - |
| Ni | - |
| Sn | - |
| Zn | - |
| Mn | - |
| Mg | - |
| Sb | - |
| Cr | - |
| Ba | - |
| W | - |
| Au | - |
| Ag | - |
| Pd | - |
| Pt | - |
| Rh | - |
| Nd | - |
| Y | - |
| Pr | - |
| Sm | - |
| Dy | - |
| La | - |
| Ce | - |
| Li | - |
| In | - |
| Ta | - |
| Ti | - |
| Mo | - |
| Nb | - |
| V | - |
| Other metals | 37 |
| Non-metals | 217 |

-: no data

## Table S2. Material content in vehicles reviewed from literature of Elgowainy  et al.8

This study spans a full portfolio of midsize light-duty vehicles, including ICEV, HEV, PHEV, BEV, and FCV.

| Material | ICEV (kg) | HEV (kg) | PHEV (kg) | BEV (kg) | FCV (kg) |
| --- | --- | --- | --- | --- | --- |
| Entire sample vehicle | 1483 | 1548 | 1694 | 1735 | 1643 |
| Fe | 1088 | 1073 | 1158 | 1163 | 1041 |
| Al | 97 | 123 | 153 | 148 | 130 |
| Cu | 30 | 92 | 111 | 113 | 98 |
| Co | - | - | - | - | - |
| Pb | - | - | - | - | - |
| Ni | - | - | - | - | - |
| Sn | - | - | - | - | - |
| Zn | - | - | - | - | - |
| Mn | - | - | - | - | - |
| Mg | - | - | - | - | - |
| Sb | - | - | - | - | - |
| Cr | - | - | - | - | - |
| Ba | - | - | - | - | - |
| W | - | - | - | - | - |
| Au | - | - | - | - | - |
| Ag | - | - | - | - | - |
| Pd | - | - | - | - | - |
| Pt | - | - | - | - | - |
| Rh | - | - | - | - | - |
| Nd | - | - | - | - | - |
| Y | - | - | - | - | - |
| Pr | - | - | - | - | - |
| Sm | - | - | - | - | - |
| Dy | - | - | - | - | - |
| La | - | - | - | - | - |
| Ce | - | - | - | - | - |
| Li | - | - | - | - | - |
| In | - | - | - | - | - |
| Ta | - | - | - | - | - |
| Ti | - | - | - | - | - |
| Mo | - | - | - | - | - |
| Nb | - | - | - | - | - |
| V | - | - | - | - | - |
| Other metals | - | - | - | - | - |
| Non-metals | 268 | 261 | 272 | 312 | 374 |

-: no data

## Table S3. Material content in vehicles reviewed from literature of Field et al.9

This study includes cars and light-duty trucks using comprehensive, component-level data reported by suppliers, and samples are Ford Fiesta, Focus, Fusion, and F-150.

| Material | ICEV (kg) |
| --- | --- |
| Entire sample vehicle | 1356 |
| Fe | 806 |
| Al | 149 |
| Cu | 30 |
| Co | 0.030 |
| Pb | - |
| Ni | 1.6 |
| Sn | - |
| Zn | - |
| Mn | 5.5 |
| Mg | 4.0 |
| Sb | - |
| Cr | - |
| Ba | - |
| W | 0.0068 |
| Au | 0.0016 |
| Ag | 0.013 |
| Pd | - |
| Pt | - |
| Rh | - |
| Nd | - |
| Y | - |
| Pr | - |
| Sm | - |
| Dy | - |
| La | - |
| Ce | - |
| Li | - |
| In | - |
| Ta | 0.0044 |
| Ti | 0.39 |
| Mo | - |
| Nb | 0.076 |
| V | - |
| Other metals | 36 |
| Non-metals | 323 |

-: no data

## Table S4. Material content in vehicles reviewed from literature of Yano et al.10

This study surveyed six vehicle models in Japan, comprising conventional vehicles and next-generation vehicles (e.g., HEV and EV) by an on-site dismantling and chemical analysis.

| Material | ICEV (kg) | HEV (kg) | PHEV (kg) |
| --- | --- | --- | --- |
| Entire sample vehicle | 1040 | 1240 | 1520 |
| Fe | 724 | 822 | 892 |
| Al | 28 | 36 | 56 |
| Cu | 9.1 | 36 | 65 |
| Co | - | - | - |
| Pb | - | - | - |
| Ni | - | - | - |
| Sn | - | - | - |
| Zn | - | - | - |
| Mn | - | - | - |
| Mg | - | - | - |
| Sb | - | - | - |
| Cr | - | - | - |
| Ba | - | - | - |
| W | - | - | - |
| Au | - | - | - |
| Ag | - | - | - |
| Pd | - | - | - |
| Pt | - | - | - |
| Rh | - | - | - |
| Nd | - | - | - |
| Y | - | - | - |
| Pr | - | - | - |
| Sm | - | - | - |
| Dy | - | - | - |
| La | - | - | - |
| Ce | - | - | - |
| Li | - | - | - |
| In | - | 0.00031 | - |
| Ta | - | - | - |
| Ti | - | - | - |
| Mo | - | - | - |
| Nb | - | - | - |
| V | - | - | - |
| Other metals | 60 | 77 | 43 |
| Non-metals | 219 | 269 | 464 |

-: no data

## Table S5. Material content in vehicles reviewed from literature of Kosai et al.11

This study includes four vehicle type which are gasoline vehicle, BEV, HEV, and FCV.

| Material | ICEV (kg) | HEV (kg) | BEV (kg) | FCV (kg) |
| --- | --- | --- | --- | --- |
| Entire sample vehicle | 1079 | 1379 | 1368 | 1286 |
| Fe | 623 | 694 | 721 | 751 |
| Al | 143 | 186 | 66 | 43 |
| Cu | 13 | 61 | 90 | 62 |
| Co | 0.0016 | 0.84 | 0.83 | 2.2 |
| Pb | 6.9 | 6.9 | - | - |
| Ni | 4.1 | 38 | 54 | 21 |
| Sn | 0.021 | 0.021 | 0.021 | 0.021 |
| Zn | 0.058 | 0.058 | 0.058 | 0.058 |
| Mn | 12 | 12 | 4.7 | 4.7 |
| Mg | 3.2 | 3.2 | 0.015 | 0.76 |
| Sb | - | - | - | - |
| Cr | 29 | 29 | 19 | 19 |
| Ba | - | - | - | - |
| W | 0.13 | 0.13 | - | - |
| Au | - | - | - | - |
| Ag | - | - | - | - |
| Pd | 0.0015 | 0.0015 | - | - |
| Pt | 0.0011 | 0.0011 | - | 0.045 |
| Rh | 0.00036 | 0.00036 | - | - |
| Nd | - | 0.34 | 0.33 | 0.33 |
| Y | 0.0013 | 0.0013 | - | 0.020 |
| Pr | - | - | - | - |
| Sm | - | - | - | - |
| Dy | - | 0.078 | 0.078 | 0.078 |
| La | 0.0032 | 0.0032 | - | 0.065 |
| Ce | - | - | - | - |
| Li | - | 3.9 | 6.3 | - |
| In | - | - | - | - |
| Ta | - | - | - | - |
| Ti | 0.66 | 0.66 | - | - |
| Mo | 0.73 | 0.81 | 0.083 | - |
| Nb | 0.17 | 0.17 | - | - |
| V | 0.19 | 0.19 | - | - |
| Other metals | 2.0 | 7.2 | 7.6 | 2.9 |
| Non-metals | 241 | 336 | 398 | 377 |

-: no data

## Table S6. Material content in vehicles reviewed from literature of Bhuwalka et al.12

This study analyzed part-level data of material use for seven current year models, ranging between ICEV, HEV, and PHEV.

| Material | ICEV (kg) | HEV (kg) | PHEV (kg) |
| --- | --- | --- | --- |
| Entire sample vehicle | 1764 | 1801 | 1869 |
| Fe | 1031 | 1108 | 1092 |
| Al | 208 | 150 | 173 |
| Cu | 31 | 53 | 54 |
| Co | 0.068 | 0.69 | 3.5 |
| Pb | 13 | 8.9 | 8.9 |
| Ni | 3.0 | 2.7 | 5.5 |
| Sn | 0.55 | 0.59 | 0.58 |
| Zn | 20 | 24 | 24 |
| Mn | 7.3 | 7.8 | 10 |
| Mg | 5.0 | 4.3 | 5.2 |
| Sb | 0.082 | 0.15 | 0.28 |
| Cr | 8.3 | 7.2 | 6.7 |
| Ba | 0.30 | 1.0 | 1.2 |
| W | - | - | - |
| Au | 0.0026 | 0.0053 | 0.0047 |
| Ag | 0.028 | 0.030 | 0.036 |
| Pd | 0.0041 | 0.0021 | 0.0022 |
| Pt | 0.00021 | 0.00027 | 0.00022 |
| Rh | 0.00026 | 0.00022 | 0.00022 |
| Nd | 0.11 | 1.1 | 0.63 |
| Y | 0.0021 | 0.00012 | 0.00012 |
| Pr | 0.0063 | 0.0051 | 0.0060 |
| Sm | 0.0056 | 0.0049 | 0.0045 |
| Dy | 0.0045 | 0.011 | 0.010 |
| La | 0.0090 | 0.0029 | 0.00014 |
| Ce | 0.020 | 0.0051 | 0.0052 |
| Li | 0.012 | 0.25 | 1.3 |
| In | - | - | - |
| Ta | - | - | - |
| Ti | - | - | - |
| Mo | - | - | - |
| Nb | - | - | - |
| V | - | - | - |
| Other metals | 0.18 | 0.17 | 0.14 |
| Non-metals | 437 | 431 | 481 |

-: no data

## Table S7. Metal price in global markets from 2016 to 202213. -: no data.

| Metal | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | Note and unit (in USD) | Average price USD/kg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Li | 8650 | 15000 | 17000 | 12700 | 8000 | 12600 | 37000 | Price, annual average, battery-grade lithium carbonate, dollars per metric ton | 16 |
| Mg | 2190 | 2265 | 2550 | 2425 | 2100 | 5008 | 5500 | Price, annual average, European free market, dollars per metric ton | 3.1 |
| Al | 80.4 | 98.3 | 114.7 | 99.5 | 89 | 138.5 | 150 | Price, ingot, average U.S. market (spot), cents per pound | 2.4 |
| Ti | 740 | 740 | 1025 | 1125 | 1200 | 1450 | 1500 | Price, dollars per metric ton, rutile, bulk, minimum 95% TiO2, f.o.b. Australia | 1.1 |
| V | 3.38 | 7.61 | 16.40 | 12.20 | 6.70 | 8.17 | 9.20 | Price, average, vanadium pentoxide, dollars per pound | 20 |
| Cr | 9939 | 9675 | 11344 | 10393 | 7900 | 8757 | 21000 | Price, average annual value of imports, dollars per ton, chromium metal | 10 |
| Mn | 4.34 | 5.97 | 7.16 | 5.63 | 4.72 | 5.27 | 6.50 | Price, average, Mn metallurgical ore, contained Mn, dollars per ton unit | 0.01 |
| Fe | 168 | 187 | 211 | 204 | 180 | 351 | 400 | Iron and steel, producer price index for steel mill products, dollars per ton | 0.2 |
| Co | 11.57 | 25.28 | 32.94 | 14.88 | 14.00 | 23.17 | 29.00 | Price, average, dollars per pound, London Metal Exchange, cash | 48 |
| Ni | 9594 | 10403 | 13114 | 13903 | 14000 | 18476 | 25000 | Price, average annual, London Metal Exchange, cash, dollars per ton | 15 |
| Cu | 220.6 | 279.5 | 296.0 | 272.4 | 270.0 | 432.3 | 410.0 | Price, annual average, cents per pound, London Metal Exchange, high-grade | 6.9 |
| Zn | 94.8 | 131.2 | 132.7 | 115.6 | 101.0 | 145.8 | 190.0 | Price, average, cents per pound, London Metal Exchange, cash | 2.9 |
| Y | 35 | 35 | 36 | 34 | 34 | 39 | 43 | Price, average, dollars per kilogram, Yttrium metal, minimum 99.9% purity | 37 |
| Nb | 21 | 20 | 21 | 23 | 24 | 20 | 24 | Price, unit value, ferroniobium, dollars per kilogram | 22 |
| Mo | 14.40 | 18.06 | 27.04 | 26.50 | 20.00 | 35.3 | 39.25 | Price, average value, dollars per kilogram | 26 |
| Rh | 697 | 1113 | 2225 | 3919 | 9200 | 20254 | 17000 | Price, dollars per troy ounce | 274168 |
| Pd | 617 | 874 | 1036 | 1544 | 2100 | 2419 | 2200 | Price, dollars per troy ounce | 54380 |
| Ag | 17.20 | 17.07 | 15.75 | 17.17 | 20.00 | 25.23 | 21.00 | Price, bullion, average, dollars per troy ounce | 672 |
| In | 240 | 225 | 291 | 185 | 150 | 215 | 250 | Price, annual average, dollars per kilogram, Rotterdam | 222 |
| Sn | 815 | 911 | 914 | 846 | 770 | 1478 | 1500 | Price, average, cents per pound, London Metal Exchange, cash | 23 |
| Sb | 3.35 | 3.98 | 3.88 | 3.90 | 3.98 | 5.31 | 6.30 | Price, metal, average, dollars per pound | 9.7 |
| Ba | 187 | 179 | 176 | 179 | 180 | 167 | 170 | Price, average value, ground, ex-works, dollars per ton, barium-based mineral | 0.2 |
| Ta | 21.00 | 20.00 | 21.00 | 23.00 | 24.00 | 20.00 | 24.00 | Price, unit value, ferroniobium, dollars per kilogram | 22 |
| W | 148.00 | 245.00 | 326.00 | 270.00 | 270.00 | 225.00 | 270.00 | Price, concentrate, dollars per ton unit of tungsten trioxide | 0.3 |
| Pt | 990 | 951 | 883 | 867 | 850 | 1094 | 980 | Price, dollars per troy ounce | 33332 |
| Au | 1252 | 1261 | 1272 | 1395 | 1770 | 1801 | 1800 | Price, dollars per troy ounce | 53168 |
| Pb | 85 | 105 | 102 | 91 | 82 | 113 | 115 | Price, average, cents per pound, London Metal Exchange, cash | 2.2 |
| La | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 1.00 | Price, average, dollars per kilogram, lanthanum oxide, 99.5% minimum | 1.9 |
| Ce | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 2.00 | 1.00 | Price, average, dollars per kilogram, cerium oxide, 99.5% minimum | 1.9 |
| Pr | 52.00 | 65.00 | - | - | - | - | - | Price, average, dollars per kilogram, praseodymium oxide, 99.5% minimum | 59 |
| Nd | 40 | 50 | 50 | 45 | 47 | 49 | 130 | Price, average, dollars per kilogram, neodymium oxide, 99.5% minimum | 59 |
| Sm | 2.00 | 2.00 | - | - | - | - | - | Price, average, dollars per kilogram, samarium oxide, 99.5% minimum | 2.0 |
| Dy | 198 | 187 | 179 | 239 | 258 | 400 | 390 | Price, average, dollars per kilogram, dysprosium oxide, 99.5% minimum | 264 |

## Table S8. Number of vehicle sales in China between 1990 and 202214

The national-level initiation of scientific research and industrialization of electric vehicles in China started in 2000, when they were included as one of the 12 major projects of the “863” plan. The “New Energy Vehicle Production Access Management Rules”, issued by the National Development and Reform Commission in 2007, provided the definition and regulation of new energy vehicles. China surpassed the United States as the world’s largest new energy vehicle market in 2015. However, due to the data accessibility, the starting year of HEV, PHEV, and BEV was set from 2010, and for FCV is 2021.

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 1990 | 1.57E+05 | - | - | - | - |
| 1991 | 1.58E+05 | - | - | - | - |
| 1992 | 1.54E+05 | - | - | - | - |
| 1993 | 1.45E+05 | - | - | - | - |
| 1994 | 1.40E+05 | - | - | - | - |
| 1995 | 1.37E+05 | - | - | - | - |
| 1996 | 1.44E+05 | - | - | - | - |
| 1997 | 1.49E+05 | - | - | - | - |
| 1998 | 1.59E+05 | - | - | - | - |
| 1999 | 2.51E+06 | - | - | - | - |
| 2000 | 3.51E+06 | - | - | - | - |
| 2001 | 3.82E+06 | - | - | - | - |
| 2002 | 3.37E+06 | - | - | - | - |
| 2003 | 4.34E+06 | - | - | - | - |
| 2004 | 4.51E+06 | - | - | - | - |
| 2005 | 5.29E+06 | - | - | - | - |
| 2006 | 6.73E+06 | - | - | - | - |
| 2007 | 6.08E+06 | - | - | - | - |
| 2008 | 7.63E+06 | - | - | - | - |
| 2009 | 1.25E+07 | - | - | - | - |
| 2010 | 1.53E+07 | 3.29E+03 | 1.04E+03 | 6.66E+02 | - |
| 2011 | 1.62E+07 | 5.54E+03 | 1.75E+03 | 1.12E+03 | - |
| 2012 | 1.77E+07 | 8.30E+03 | 2.62E+03 | 1.68E+03 | - |
| 2013 | 2.03E+07 | 1.15E+04 | 3.64E+03 | 2.33E+03 | - |
| 2014 | 2.21E+07 | 5.17E+04 | 1.63E+04 | 1.05E+04 | - |
| 2015 | 2.33E+07 | 2.18E+05 | 6.88E+04 | 4.41E+04 | - |
| 2016 | 2.72E+07 | 3.36E+05 | 1.06E+05 | 6.79E+04 | - |
| 2017 | 2.80E+07 | 5.14E+05 | 1.62E+05 | 1.04E+05 | - |
| 2018 | 2.65E+07 | 8.37E+05 | 2.64E+05 | 1.69E+05 | - |
| 2019 | 2.54E+07 | 7.91E+05 | 2.49E+05 | 1.60E+05 | - |
| 2020 | 2.40E+07 | 7.18E+05 | 2.27E+05 | 1.45E+05 | - |
| 2021 | 2.39E+07 | 1.47E+06 | 4.58E+05 | 2.92E+05 | 2.22E+03 |
| 2022 | 2.39E+07 | 2.09E+06 | 6.42E+05 | 4.06E+05 | 6.30E+03 |

-: no data

## Table S9. Number of vehicle sales in Japan between 1990 and 202215

Japan has been a leader in the development of EVs. In 1997, Toyota launched the Prius, the first HEV to be mass-produced globally, initiating Japan’s HEV industry. Nissan followed with the introduction of the Leaf in 2009, the first BEV to be mass-produced worldwide, marking Japan’s pioneering role in EVs. In recent years, Japan ranked second globally in the field of electromobility, only behind China. Japan also excelled in FCVs.

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 1990 | 5.10E+06 | - | - | - | - |
| 1991 | 4.87E+06 | - | - | - | - |
| 1992 | 4.45E+06 | - | - | - | - |
| 1993 | 4.20E+06 | - | - | - | - |
| 1994 | 4.21E+06 | - | - | - | - |
| 1995 | 4.44E+06 | - | - | - | - |
| 1996 | 4.67E+06 | - | - | - | - |
| 1997 | 4.49E+06 | - | - | - | - |
| 1998 | 4.09E+06 | - | - | - | - |
| 1999 | 4.15E+06 | - | - | - | - |
| 2000 | 4.26E+06 | - | - | - | - |
| 2001 | 4.29E+06 | - | - | - | - |
| 2002 | 4.44E+06 | - | - | - | - |
| 2003 | 4.72E+06 | - | - | - | - |
| 2004 | 4.77E+06 | - | - | - | - |
| 2005 | 4.75E+06 | - | - | - | - |
| 2006 | 4.64E+06 | - | - | - | - |
| 2007 | 4.40E+06 | - | - | - | - |
| 2008 | 4.12E+06 | - | - | 1.09E+05 | - |
| 2009 | 3.57E+06 | 1.08E+03 | - | 3.48E+05 | - |
| 2010 | 3.73E+06 | 2.44E+03 | - | 4.81E+05 | - |
| 2011 | 3.06E+06 | 1.26E+04 | 1.50E+01 | 4.51E+05 | - |
| 2012 | 3.66E+06 | 1.35E+04 | 1.10E+04 | 8.88E+05 | - |
| 2013 | 3.61E+06 | 1.48E+04 | 1.41E+04 | 9.21E+05 | - |
| 2014 | 3.61E+06 | 1.61E+04 | 1.62E+04 | 1.06E+06 | 7.00E+00 |
| 2015 | 3.12E+06 | 1.05E+04 | 1.42E+04 | 1.07E+06 | 4.11E+02 |
| 2016 | 2.85E+06 | 1.53E+04 | 9.39E+03 | 1.28E+06 | 1.05E+03 |
| 2017 | 2.95E+06 | 1.81E+04 | 3.60E+04 | 1.39E+06 | 8.49E+02 |
| 2018 | 2.91E+06 | 2.65E+04 | 2.32E+04 | 1.43E+06 | 6.12E+02 |
| 2019 | 2.79E+06 | 2.13E+04 | 1.76E+04 | 1.47E+06 | 6.85E+02 |
| 2020 | 2.46E+06 | 1.46E+04 | 1.47E+04 | 1.32E+06 | 7.61E+02 |
| 2021 | 2.38E+06 | 4.75E+04 | 6.48E+04 | 1.35E+06 | 1.36E+04 |
| 2022 | 2.31E+06 | 8.05E+04 | 1.15E+05 | 1.38E+06 | 2.64E+04 |

-: no data

## Table S10. Shape and scale parameters (Weibull distribution) of vehicles in China and Japan16, 17

The Weibull distribution is a probability distribution that can be used to model the lifetime of products or systems. It has two parameters: the shape parameter and the scale parameter. The shape parameter determines the shape of the distribution curve, while the scale parameter determines the spread of the distribution18.

| Country | Vehicle | Shape (μ) | Scale (η) | Lifespan (year) |
| --- | --- | --- | --- | --- |
| China | ICEV | 2.75 | 12.8 | 11.2 |
|  | HEV* | 5.08 | 13.11 | 12.2 |
|  | PHEV* | 5.08 | 13.11 | 12.2 |
|  | BEV | 5.08 | 13.11 | 12.2 |
|  | FCV* | 2.20 | 15.69 | 13.3 |
| Japan | ICEV | 4.79 | 14.46 | 13.4 |
|  | HEV | 2.51 | 17.69 | 15.3 |
|  | PHEV* | 2.51 | 17.69 | 15.3 |
|  | BEV | 5.55 | 14.13 | 13.2 |
|  | FCV | 2.20 | 15.69 | 13.3 |

*: assumed value

## Fig. S1. Remaining rate of vehicles. a) China; b) Japan16, 17.

In general, Japanese passenger vehicles tend to have a longer use lifespan than vehicles in China. Because Chinese passenger vehicles have a general use lifespan of 15 years or 600,000 kilometers19, while there is no mandatory retirement age for Japanese passenger vehicles as long as they pass the annual inspection.

## Table S11. ELV collection ratios and metal separation-recycling ratios in China and Japan20, 21

| Country | ELV collection ratio | Metal | Metal collection-separation-recycling ratio |
| --- | --- | --- | --- |
| China | 90.0% | Fe | 68% |
|  |  | Al | 55% |
|  |  | Cu | 44% |
|  |  | Co | 35% |
|  |  | Pb | 85% |
|  |  | Ni | 53% |
|  |  | Zn | 49% |
|  |  | Cr | 42% |
|  |  | Au | 62% |
|  |  | Ag | 52% |
|  |  | Pd | 56% |
|  |  | Pt | 56% |
|  |  | Rh | 50% |
|  |  | Nd | 0.5% |
|  |  | Y | 0.5% |
|  |  | Pr | 0.5% |
|  |  | Dy | 0.5% |
|  |  | La | 0.5% |
|  |  | Ce | 0.5% |
|  |  | Li | 0.7% |
|  |  | In | 0.9% |
| Japan | 99.5% | Fe | 76% |
|  |  | Al | 61% |
|  |  | Cu | 49% |
|  |  | Co | 38% |
|  |  | Pb | 94% |
|  |  | Ni | 59% |
|  |  | Zn | 55% |
|  |  | Cr | 47% |
|  |  | Au | 68% |
|  |  | Ag | 57% |
|  |  | Pd | 62% |
|  |  | Pt | 62% |
|  |  | Rh | 55% |
|  |  | Nd | 0.6% |
|  |  | Y | 0.6% |
|  |  | Pr | 0.6% |
|  |  | Dy | 0.6% |
|  |  | La | 0.6% |
|  |  | Ce | 0.6% |
|  |  | Li | 0.7% |
|  |  | In | 1.0% |

The Chinese government enacted the Regulation on the Administration of the Recovery and Disposal of Waste Motor Vehicles in 2001, which created a system for the recycling of scrap vehicles, with the objective of avoiding accidents resulting from the utilization of renovated or outdated vehicles. To achieve this objective, the regulation requires the restructuring and enhancement of the capabilities of dismantling enterprises. The regulation also bans the repeated use of the five major components of engine, steering, transmission, axle, and frame, in order to prevent traffic accidents due to inappropriate use. In 2006, the Technical Policy for the Recycling of Automobile Products was issued, which specifies the roles of manufacturers and importers in facilitating the recycling of scrap vehicles, and regulates the substances that should be restricted or eliminated in automobile manufacturing for environmental protection purposes. The technical policy sets differentiated recycling targets for ELVs: 85−95% by 20174.

In 2005, Japan enacted the Automobile Recycling Law, which responds to the challenges of reducing automobile shredding residue due to the limited capacity of landfills, and of avoiding the unlawful disposal and treatment of ELVs resulting from the instability of the scrap steel market. The law specifies the components/materials subject to recycling, the allocation of recycling costs among the stakeholders, and the creation of an information management system. The law sets differentiated recycling targets for airbags, refrigerant gases, and automobile shredding residue, instead of applying a uniform target to the whole ELV. Moreover, the law mandates the safe disposal of chlorofluorocarbons. With respect to the recycling of automobile shredding residue, the law permits thermal recycling and does not impose any recycling rate requirement4.

# Supplementary Results

## Table S12. Estimated average material content per vehicle summarized from literature review

| Material | ICEV (kg) | BEV (kg) | PHEV (kg) | HEV (kg) | FCV (kg) |
| --- | --- | --- | --- | --- | --- |
| Entire sample vehicle | 942 | 1158 | 1221 | 1128 | 1084 |
| Fe | 809 | 925 | 978 | 924 | 896 |
| Al | 109 | 90 | 142 | 123 | 87 |
| Cu | 21 | 89 | 72 | 61 | 80 |
| Co | 0.033 | 0.83 | 0.78 | 0.76 | 2.2 |
| Pb | 10 | 9.0 | 7.8 | 7.9 | 9.0 |
| Ni | 2.9 | 54 | 30 | 20 | 21 |
| Sn | 0.29 | 0.021 | 0.51 | 0.31 | 0.021 |
| Zn | 10.019 | 0.058 | 21.035 | 12.179 | 0.058 |
| Mn | 8.3 | 4.7 | 8.9 | 10 | 4.7 |
| Mg | 4.1 | 0.015 | 4.5 | 3.8 | 0.76 |
| Sb | 0.082 | 0.17 | 0.24 | 0.15 | 0.17 |
| Cr | 18 | 19 | 5.8 | 18 | 19 |
| Ba | 0.30 | 0.83 | 1.0 | 1.0 | 0.83 |
| W | 0.067 | 0.098 | 0.085 | 0.13 | 0.098 |
| Au | 0.0020 | 0.0040 | 0.0040 | 0.0050 | 0.0040 |
| Ag | 0.020 | 0.029 | 0.031 | 0.030 | 0.029 |
| Pd | 0.0030 | - | 0.0020 | 0.0020 | - |
| Pt | 0.001 | - | - | 0.0010 | 0.045 |
| Rh | 0.00030 | - | 0.00020 | 0.00030 | - |
| Nd | 0.11 | 0.33 | 0.55 | 0.73 | 0.3 |
| Y | 0.0020 | 0.0060 | - | 0.0010 | 0.020 |
| Pr | 0.0060 | 0.0060 | 0.0050 | 0.0050 | 0.0060 |
| Sm | 0.0060 | 0.0050 | 0.0040 | 0.0050 | 0.0050 |
| Dy | 0.0040 | 0.078 | 0.0090 | 0.045 | 0.078 |
| La | 0.0060 | 0.019 | - | 0.0030 | 0.065 |
| Ce | 0.020 | 0.010 | 0.0040 | 0.0050 | 0.010 |
| Li | 0.012 | 6.3 | 3.0 | 2.1 | - |
| In | 0.00031 | 0.00031 | 0.00027 | 0.00031 | 0.00031 |
| Ta | 0.0040 | 0.0040 | 0.0040 | 0.0040 | 0.0040 |
| Ti | 0.53 | 0.59 | 0.52 | 0.66 | 0.59 |
| Mo | 0.73 | 0.083 | 0.47 | 0.81 | 0.54 |
| Nb | 0.12 | 0.14 | 0.12 | 0.17 | 0.14 |
| V | 0.19 | 0.19 | 0.17 | 0.19 | 0.19 |
| Other metals | 29 | 34 | 6.1 | 34 | 7.4 |
| Non-metals | 244.442 | 314.728 | 276.024 | 276.916 | 338.068 |

-: no data

## Table S13. Estimated average material value equivalent per vehicle

| Material | ICEV (USD/kg) | BEV (USD/kg) | PHEV (USD/kg) | HEV (USD/kg) | FCV (USD/kg) |
| --- | --- | --- | --- | --- | --- |
| Entire sample vehicle | 1505 | 2906 | 2576 | 2502 | 3844 |
| Fe | 197 | 225 | 238 | 225 | 218 |
| Al | 265 | 218 | 344 | 300 | 210 |
| Cu | 146 | 613 | 491 | 416 | 548 |
| Co | 1.6 | 40 | 37 | 36 | 105 |
| Pb | 22 | 20 | 17 | 17 | 20 |
| Ni | 43 | 806 | 448 | 300 | 321 |
| Sn | 6.5 | 0.49 | 12 | 6.9 | 0.49 |
| Zn | 29 | 0.17 | 60 | 35 | 0.17 |
| Mn | 0.047 | 0.027 | 0.050 | 0.057 | 0.027 |
| Mg | 13 | 0.048 | 14 | 12 | 2.4 |
| Sb | 0.80 | 1.7 | 2.4 | 1.5 | 1.7 |
| Cr | 45 | 188 | 56 | 173 | 188 |
| Ba | 0.054 | 0.15 | 0.18 | 0.18 | 0.15 |
| W | 0.017 | 0.024 | 0.021 | 0.032 | 0.024 |
| Au | 110 | 212 | 215 | 279 | 212 |
| Ag | 14 | 19 | 21 | 20 | 19 |
| Pd | 152 | - | 104 | 98 | - |
| Pt | 21 | - | 6.4 | 22 | 1500 |
| Rh | 85 | - | 52 | 80 | - |
| Nd | 6.2 | 20 | 32 | 43 | 20 |
| Y | 0.0050 | 0.016 | - | 0.0020 | 0.057 |
| Pr | 0.37 | 0.34 | 0.31 | 0.30 | 0.34 |
| Sm | 0.011 | 0.010 | 0.0080 | 0.010 | 0.010 |
| Dy | 1.2 | 21 | 2.3 | 12 | 21 |
| La | 0.011 | 0.034 | - | 0.0060 | 0.12 |
| Ce | 0.037 | 0.019 | 0.0080 | 0.0090 | 0.019 |
| Li | 0.19 | 100 | 48 | 33 | - |
| In | 0.069 | 0.069 | 0.060 | 0.069 | 0.069 |
| Ta | 0.096 | 0.096 | 0.084 | 0.096 | 0.096 |
| Ti | 0.58 | 0.66 | 0.57 | 0.73 | 0.66 |
| Mo | 19 | 2.1 | 12 | 21 | 14 |
| Nb | 2.6 | 3.1 | 2.7 | 3.6 | 3.1 |
| V | 3.9 | 3.9 | 3.4 | 3.9 | 3.9 |
| Other metals* | 7.0 | 8.3 | 1.5 | 8.2 | 1.8 |
| Non-metals* | 314 | 404 | 355 | 356 | 434 |

-: no data; *: assumed value

## Table S14. Estimated number of vehicle sales in China in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.39E+07 | 2.09E+06 | 6.42E+05 | 4.06E+05 | 6.30E+03 |
| 2023 | 2.38E+07 | 2.72E+06 | 8.23E+05 | 5.17E+05 | 1.22E+04 |
| 2024 | 2.38E+07 | 3.35E+06 | 1.00E+06 | 6.24E+05 | 2.00E+04 |
| 2025 | 2.37E+07 | 3.99E+06 | 1.17E+06 | 7.27E+05 | 2.96E+04 |
| 2026 | 2.32E+07 | 4.95E+06 | 1.44E+06 | 8.82E+05 | 4.39E+04 |
| 2027 | 2.26E+07 | 5.97E+06 | 1.71E+06 | 1.04E+06 | 6.14E+04 |
| 2028 | 2.19E+07 | 7.04E+06 | 1.98E+06 | 1.20E+06 | 8.24E+04 |
| 2029 | 2.12E+07 | 8.17E+06 | 2.27E+06 | 1.36E+06 | 1.07E+05 |
| 2030 | 2.04E+07 | 9.35E+06 | 2.56E+06 | 1.52E+06 | 1.36E+05 |
| 2031 | 2.02E+07 | 1.01E+07 | 2.73E+06 | 1.61E+06 | 1.61E+05 |
| 2032 | 2.00E+07 | 1.09E+07 | 2.90E+06 | 1.69E+06 | 1.88E+05 |
| 2033 | 1.97E+07 | 1.17E+07 | 3.07E+06 | 1.78E+06 | 2.18E+05 |
| 2034 | 1.94E+07 | 1.26E+07 | 3.24E+06 | 1.86E+06 | 2.51E+05 |
| 2035 | 1.91E+07 | 1.35E+07 | 3.42E+06 | 1.94E+06 | 2.87E+05 |
| 2036 | 1.88E+07 | 1.44E+07 | 3.60E+06 | 2.02E+06 | 3.25E+05 |
| 2037 | 1.84E+07 | 1.53E+07 | 3.78E+06 | 2.10E+06 | 3.67E+05 |
| 2038 | 1.80E+07 | 1.63E+07 | 3.96E+06 | 2.18E+06 | 4.11E+05 |
| 2039 | 1.75E+07 | 1.73E+07 | 4.14E+06 | 2.25E+06 | 4.59E+05 |
| 2040 | 1.70E+07 | 1.84E+07 | 4.32E+06 | 2.32E+06 | 5.11E+05 |
| 2041 | 1.65E+07 | 1.94E+07 | 4.50E+06 | 2.39E+06 | 5.65E+05 |
| 2042 | 1.59E+07 | 2.06E+07 | 4.69E+06 | 2.46E+06 | 6.23E+05 |
| 2043 | 1.53E+07 | 2.17E+07 | 4.87E+06 | 2.52E+06 | 6.85E+05 |
| 2044 | 1.47E+07 | 2.29E+07 | 5.05E+06 | 2.58E+06 | 7.51E+05 |
| 2045 | 1.41E+07 | 2.41E+07 | 5.24E+06 | 2.64E+06 | 8.20E+05 |
| 2046 | 1.34E+07 | 2.53E+07 | 5.42E+06 | 2.69E+06 | 8.93E+05 |
| 2047 | 1.26E+07 | 2.66E+07 | 5.60E+06 | 2.74E+06 | 9.71E+05 |
| 2048 | 1.19E+07 | 2.80E+07 | 5.78E+06 | 2.79E+06 | 1.05E+06 |
| 2049 | 1.11E+07 | 2.93E+07 | 5.96E+06 | 2.83E+06 | 1.14E+06 |
| 2050 | 1.02E+07 | 3.07E+07 | 6.14E+06 | 2.87E+06 | 1.23E+06 |

## Table S15. Estimated number of vehicle sales in China in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.48E+07 | 1.48E+06 | 4.52E+05 | 2.86E+05 | 4.44E+03 |
| 2023 | 2.51E+07 | 1.89E+06 | 5.71E+05 | 3.59E+05 | 8.48E+03 |
| 2024 | 2.53E+07 | 2.33E+06 | 6.95E+05 | 4.33E+05 | 1.39E+04 |
| 2025 | 2.55E+07 | 2.80E+06 | 8.22E+05 | 5.09E+05 | 2.07E+04 |
| 2026 | 2.54E+07 | 3.47E+06 | 1.00E+06 | 6.17E+05 | 3.07E+04 |
| 2027 | 2.52E+07 | 4.18E+06 | 1.19E+06 | 7.28E+05 | 4.30E+04 |
| 2028 | 2.50E+07 | 4.93E+06 | 1.39E+06 | 8.39E+05 | 5.77E+04 |
| 2029 | 2.47E+07 | 5.72E+06 | 1.59E+06 | 9.52E+05 | 7.50E+04 |
| 2030 | 2.44E+07 | 6.55E+06 | 1.79E+06 | 1.07E+06 | 9.50E+04 |
| 2031 | 2.46E+07 | 7.08E+06 | 1.91E+06 | 1.13E+06 | 1.13E+05 |
| 2032 | 2.47E+07 | 7.64E+06 | 2.03E+06 | 1.19E+06 | 1.32E+05 |
| 2033 | 2.48E+07 | 8.21E+06 | 2.15E+06 | 1.24E+06 | 1.53E+05 |
| 2034 | 2.48E+07 | 8.81E+06 | 2.27E+06 | 1.30E+06 | 1.76E+05 |
| 2035 | 2.49E+07 | 9.43E+06 | 2.39E+06 | 1.36E+06 | 2.01E+05 |
| 2036 | 2.49E+07 | 1.01E+07 | 2.52E+06 | 1.42E+06 | 2.28E+05 |
| 2037 | 2.49E+07 | 1.07E+07 | 2.64E+06 | 1.47E+06 | 2.57E+05 |
| 2038 | 2.48E+07 | 1.14E+07 | 2.77E+06 | 1.52E+06 | 2.88E+05 |
| 2039 | 2.48E+07 | 1.21E+07 | 2.90E+06 | 1.58E+06 | 3.22E+05 |
| 2040 | 2.47E+07 | 1.29E+07 | 3.02E+06 | 1.63E+06 | 3.57E+05 |
| 2041 | 2.46E+07 | 1.36E+07 | 3.15E+06 | 1.68E+06 | 3.96E+05 |
| 2042 | 2.44E+07 | 1.44E+07 | 3.28E+06 | 1.72E+06 | 4.36E+05 |
| 2043 | 2.43E+07 | 1.52E+07 | 3.41E+06 | 1.77E+06 | 4.80E+05 |
| 2044 | 2.41E+07 | 1.60E+07 | 3.54E+06 | 1.81E+06 | 5.25E+05 |
| 2045 | 2.39E+07 | 1.69E+07 | 3.66E+06 | 1.85E+06 | 5.74E+05 |
| 2046 | 2.37E+07 | 1.77E+07 | 3.79E+06 | 1.89E+06 | 6.25E+05 |
| 2047 | 2.34E+07 | 1.86E+07 | 3.92E+06 | 1.92E+06 | 6.79E+05 |
| 2048 | 2.31E+07 | 1.96E+07 | 4.05E+06 | 1.95E+06 | 7.36E+05 |
| 2049 | 2.28E+07 | 2.05E+07 | 4.17E+06 | 1.98E+06 | 7.96E+05 |
| 2050 | 2.25E+07 | 2.15E+07 | 4.30E+06 | 2.01E+06 | 8.60E+05 |

## Table S16. Estimated number of vehicle sales in China in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.35E+07 | 2.34E+06 | 7.17E+05 | 4.54E+05 | 7.03E+03 |
| 2023 | 2.31E+07 | 3.23E+06 | 9.77E+05 | 6.14E+05 | 1.45E+04 |
| 2024 | 2.25E+07 | 4.18E+06 | 1.25E+06 | 7.78E+05 | 2.49E+04 |
| 2025 | 2.19E+07 | 5.19E+06 | 1.53E+06 | 9.45E+05 | 3.85E+04 |
| 2026 | 2.10E+07 | 6.44E+06 | 1.87E+06 | 1.15E+06 | 5.71E+04 |
| 2027 | 1.99E+07 | 7.76E+06 | 2.22E+06 | 1.35E+06 | 7.99E+04 |
| 2028 | 1.88E+07 | 9.15E+06 | 2.58E+06 | 1.56E+06 | 1.07E+05 |
| 2029 | 1.76E+07 | 1.06E+07 | 2.95E+06 | 1.77E+06 | 1.39E+05 |
| 2030 | 1.63E+07 | 1.22E+07 | 3.33E+06 | 1.98E+06 | 1.76E+05 |
| 2031 | 1.58E+07 | 1.32E+07 | 3.54E+06 | 2.09E+06 | 2.09E+05 |
| 2032 | 1.53E+07 | 1.42E+07 | 3.77E+06 | 2.20E+06 | 2.45E+05 |
| 2033 | 1.47E+07 | 1.52E+07 | 3.99E+06 | 2.31E+06 | 2.84E+05 |
| 2034 | 1.41E+07 | 1.64E+07 | 4.22E+06 | 2.42E+06 | 3.27E+05 |
| 2035 | 1.34E+07 | 1.75E+07 | 4.45E+06 | 2.53E+06 | 3.73E+05 |
| 2036 | 1.27E+07 | 1.87E+07 | 4.68E+06 | 2.63E+06 | 4.23E+05 |
| 2037 | 1.19E+07 | 1.99E+07 | 4.91E+06 | 2.73E+06 | 4.77E+05 |
| 2038 | 1.11E+07 | 2.12E+07 | 5.14E+06 | 2.83E+06 | 5.35E+05 |
| 2039 | 1.03E+07 | 2.25E+07 | 5.38E+06 | 2.93E+06 | 5.97E+05 |
| 2040 | 9.36E+06 | 2.39E+07 | 5.62E+06 | 3.02E+06 | 6.64E+05 |
| 2041 | 8.42E+06 | 2.53E+07 | 5.85E+06 | 3.11E+06 | 7.35E+05 |
| 2042 | 7.44E+06 | 2.67E+07 | 6.09E+06 | 3.20E+06 | 8.10E+05 |
| 2043 | 6.41E+06 | 2.82E+07 | 6.33E+06 | 3.28E+06 | 8.91E+05 |
| 2044 | 5.34E+06 | 2.98E+07 | 6.57E+06 | 3.36E+06 | 9.76E+05 |
| 2045 | 4.22E+06 | 3.13E+07 | 6.81E+06 | 3.43E+06 | 1.07E+06 |
| 2046 | 3.44E+06 | 3.27E+07 | 6.98E+06 | 3.47E+06 | 1.15E+06 |
| 2047 | 2.62E+06 | 3.40E+07 | 7.16E+06 | 3.51E+06 | 1.24E+06 |
| 2048 | 1.78E+06 | 3.55E+07 | 7.33E+06 | 3.54E+06 | 1.33E+06 |
| 2049 | 9.05E+05 | 3.69E+07 | 7.50E+06 | 3.56E+06 | 1.43E+06 |
| 2050 | 0.00E+00 | 3.84E+07 | 7.67E+06 | 3.58E+06 | 1.53E+06 |

## Table S17. Estimated number of vehicle sales in Japan in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.31E+06 | 8.05E+04 | 1.15E+05 | 1.38E+06 | 2.64E+04 |
| 2023 | 2.23E+06 | 1.13E+05 | 1.65E+05 | 1.40E+06 | 3.92E+04 |
| 2024 | 2.16E+06 | 1.46E+05 | 2.15E+05 | 1.43E+06 | 5.21E+04 |
| 2025 | 2.09E+06 | 1.79E+05 | 2.65E+05 | 1.46E+06 | 6.49E+04 |
| 2026 | 2.01E+06 | 2.12E+05 | 3.15E+05 | 1.48E+06 | 7.77E+04 |
| 2027 | 1.94E+06 | 2.45E+05 | 3.66E+05 | 1.51E+06 | 9.05E+04 |
| 2028 | 1.87E+06 | 2.78E+05 | 4.16E+05 | 1.54E+06 | 1.03E+05 |
| 2029 | 1.79E+06 | 3.11E+05 | 4.66E+05 | 1.56E+06 | 1.16E+05 |
| 2030 | 1.72E+06 | 3.44E+05 | 5.16E+05 | 1.59E+06 | 1.29E+05 |
| 2031 | 1.68E+06 | 3.66E+05 | 5.38E+05 | 1.57E+06 | 1.46E+05 |
| 2032 | 1.63E+06 | 3.87E+05 | 5.59E+05 | 1.56E+06 | 1.63E+05 |
| 2033 | 1.59E+06 | 4.09E+05 | 5.81E+05 | 1.54E+06 | 1.81E+05 |
| 2034 | 1.55E+06 | 4.30E+05 | 6.02E+05 | 1.52E+06 | 1.98E+05 |
| 2035 | 1.51E+06 | 4.52E+05 | 6.24E+05 | 1.51E+06 | 2.15E+05 |
| 2036 | 1.46E+06 | 4.73E+05 | 6.45E+05 | 1.49E+06 | 2.32E+05 |
| 2037 | 1.42E+06 | 4.95E+05 | 6.67E+05 | 1.47E+06 | 2.49E+05 |
| 2038 | 1.38E+06 | 5.16E+05 | 6.88E+05 | 1.45E+06 | 2.67E+05 |
| 2039 | 1.33E+06 | 5.38E+05 | 7.10E+05 | 1.44E+06 | 2.84E+05 |
| 2040 | 1.29E+06 | 5.59E+05 | 7.31E+05 | 1.42E+06 | 3.01E+05 |
| 2041 | 1.25E+06 | 5.81E+05 | 7.53E+05 | 1.41E+06 | 3.14E+05 |
| 2042 | 1.20E+06 | 6.02E+05 | 7.74E+05 | 1.39E+06 | 3.27E+05 |
| 2043 | 1.16E+06 | 6.24E+05 | 7.96E+05 | 1.38E+06 | 3.40E+05 |
| 2044 | 1.12E+06 | 6.45E+05 | 8.17E+05 | 1.37E+06 | 3.53E+05 |
| 2045 | 1.08E+06 | 6.67E+05 | 8.39E+05 | 1.35E+06 | 3.66E+05 |
| 2046 | 1.03E+06 | 6.88E+05 | 8.60E+05 | 1.34E+06 | 3.78E+05 |
| 2047 | 9.89E+05 | 7.10E+05 | 8.82E+05 | 1.33E+06 | 3.91E+05 |
| 2048 | 9.46E+05 | 7.31E+05 | 9.03E+05 | 1.32E+06 | 4.04E+05 |
| 2049 | 9.03E+05 | 7.53E+05 | 9.25E+05 | 1.30E+06 | 4.17E+05 |
| 2050 | 8.60E+05 | 7.74E+05 | 9.46E+05 | 1.29E+06 | 4.30E+05 |

## Table S18. Estimated number of vehicle sales in Japan in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.46E+06 | 5.98E+04 | 8.40E+04 | 1.28E+06 | 1.87E+04 |
| 2023 | 2.47E+06 | 8.24E+04 | 1.19E+05 | 1.26E+06 | 2.76E+04 |
| 2024 | 2.47E+06 | 1.05E+05 | 1.53E+05 | 1.24E+06 | 3.66E+04 |
| 2025 | 2.47E+06 | 1.28E+05 | 1.88E+05 | 1.22E+06 | 4.55E+04 |
| 2026 | 2.48E+06 | 1.50E+05 | 2.23E+05 | 1.20E+06 | 5.45E+04 |
| 2027 | 2.48E+06 | 1.73E+05 | 2.57E+05 | 1.18E+06 | 6.34E+04 |
| 2028 | 2.49E+06 | 1.96E+05 | 2.92E+05 | 1.16E+06 | 7.24E+04 |
| 2029 | 2.49E+06 | 2.18E+05 | 3.27E+05 | 1.13E+06 | 8.13E+04 |
| 2030 | 2.49E+06 | 2.41E+05 | 3.61E+05 | 1.11E+06 | 9.03E+04 |
| 2031 | 2.46E+06 | 2.56E+05 | 3.76E+05 | 1.10E+06 | 1.02E+05 |
| 2032 | 2.43E+06 | 2.71E+05 | 3.91E+05 | 1.09E+06 | 1.14E+05 |
| 2033 | 2.40E+06 | 2.86E+05 | 4.06E+05 | 1.08E+06 | 1.26E+05 |
| 2034 | 2.37E+06 | 3.01E+05 | 4.21E+05 | 1.07E+06 | 1.38E+05 |
| 2035 | 2.34E+06 | 3.16E+05 | 4.36E+05 | 1.05E+06 | 1.51E+05 |
| 2036 | 2.31E+06 | 3.31E+05 | 4.52E+05 | 1.04E+06 | 1.63E+05 |
| 2037 | 2.28E+06 | 3.46E+05 | 4.67E+05 | 1.03E+06 | 1.75E+05 |
| 2038 | 2.25E+06 | 3.61E+05 | 4.82E+05 | 1.02E+06 | 1.87E+05 |
| 2039 | 2.22E+06 | 3.76E+05 | 4.97E+05 | 1.01E+06 | 1.99E+05 |
| 2040 | 2.19E+06 | 3.91E+05 | 5.12E+05 | 9.93E+05 | 2.11E+05 |
| 2041 | 2.16E+06 | 4.06E+05 | 5.27E+05 | 9.84E+05 | 2.20E+05 |
| 2042 | 2.13E+06 | 4.21E+05 | 5.42E+05 | 9.75E+05 | 2.29E+05 |
| 2043 | 2.10E+06 | 4.36E+05 | 5.57E+05 | 9.66E+05 | 2.38E+05 |
| 2044 | 2.07E+06 | 4.52E+05 | 5.72E+05 | 9.57E+05 | 2.47E+05 |
| 2045 | 2.04E+06 | 4.67E+05 | 5.87E+05 | 9.48E+05 | 2.56E+05 |
| 2046 | 2.01E+06 | 4.82E+05 | 6.02E+05 | 9.39E+05 | 2.65E+05 |
| 2047 | 1.98E+06 | 4.97E+05 | 6.17E+05 | 9.30E+05 | 2.74E+05 |
| 2048 | 1.95E+06 | 5.12E+05 | 6.32E+05 | 9.21E+05 | 2.83E+05 |
| 2049 | 1.92E+06 | 5.27E+05 | 6.47E+05 | 9.12E+05 | 2.92E+05 |
| 2050 | 1.89E+06 | 5.42E+05 | 6.62E+05 | 9.03E+05 | 3.01E+05 |

## Table S19. Estimated number of vehicle sales in Japan in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.15E+06 | 1.01E+05 | 1.46E+05 | 1.47E+06 | 3.41E+04 |
| 2023 | 2.00E+06 | 1.44E+05 | 2.12E+05 | 1.55E+06 | 5.08E+04 |
| 2024 | 1.85E+06 | 1.88E+05 | 2.77E+05 | 1.62E+06 | 6.75E+04 |
| 2025 | 1.70E+06 | 2.31E+05 | 3.43E+05 | 1.70E+06 | 8.42E+04 |
| 2026 | 1.55E+06 | 2.74E+05 | 4.08E+05 | 1.77E+06 | 1.01E+05 |
| 2027 | 1.40E+06 | 3.17E+05 | 4.74E+05 | 1.85E+06 | 1.18E+05 |
| 2028 | 1.25E+06 | 3.61E+05 | 5.40E+05 | 1.92E+06 | 1.34E+05 |
| 2029 | 1.10E+06 | 4.04E+05 | 6.05E+05 | 1.99E+06 | 1.51E+05 |
| 2030 | 9.46E+05 | 4.47E+05 | 6.71E+05 | 2.07E+06 | 1.68E+05 |
| 2031 | 8.96E+05 | 4.70E+05 | 6.99E+05 | 2.05E+06 | 1.90E+05 |
| 2032 | 8.45E+05 | 4.92E+05 | 7.27E+05 | 2.02E+06 | 2.12E+05 |
| 2033 | 7.95E+05 | 5.14E+05 | 7.55E+05 | 2.00E+06 | 2.35E+05 |
| 2034 | 7.45E+05 | 5.37E+05 | 7.83E+05 | 1.98E+06 | 2.57E+05 |
| 2035 | 6.94E+05 | 5.59E+05 | 8.11E+05 | 1.96E+06 | 2.80E+05 |
| 2036 | 6.44E+05 | 5.81E+05 | 8.39E+05 | 1.93E+06 | 3.02E+05 |
| 2037 | 5.94E+05 | 6.04E+05 | 8.66E+05 | 1.91E+06 | 3.24E+05 |
| 2038 | 5.44E+05 | 6.26E+05 | 8.94E+05 | 1.89E+06 | 3.47E+05 |
| 2039 | 4.93E+05 | 6.48E+05 | 9.22E+05 | 1.87E+06 | 3.69E+05 |
| 2040 | 4.43E+05 | 6.71E+05 | 9.50E+05 | 1.84E+06 | 3.91E+05 |
| 2041 | 3.99E+05 | 7.04E+05 | 9.70E+05 | 1.82E+06 | 4.08E+05 |
| 2042 | 3.54E+05 | 7.38E+05 | 9.89E+05 | 1.79E+06 | 4.25E+05 |
| 2043 | 3.10E+05 | 7.71E+05 | 1.01E+06 | 1.77E+06 | 4.42E+05 |
| 2044 | 2.66E+05 | 8.05E+05 | 1.03E+06 | 1.74E+06 | 4.58E+05 |
| 2045 | 2.21E+05 | 8.39E+05 | 1.05E+06 | 1.72E+06 | 4.75E+05 |
| 2046 | 1.77E+05 | 8.72E+05 | 1.07E+06 | 1.69E+06 | 4.92E+05 |
| 2047 | 1.33E+05 | 9.06E+05 | 1.09E+06 | 1.67E+06 | 5.09E+05 |
| 2048 | 8.86E+04 | 9.39E+05 | 1.11E+06 | 1.64E+06 | 5.25E+05 |
| 2049 | 4.43E+04 | 9.73E+05 | 1.12E+06 | 1.62E+06 | 5.42E+05 |
| 2050 | 0.00E+00 | 1.01E+06 | 1.14E+06 | 1.59E+06 | 5.59E+05 |

## Table S20. Estimated number of in-use vehicles in China in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.86E+08 | 7.02E+06 | 2.19E+06 | 1.40E+06 | 8.51E+03 |
| 2023 | 2.96E+08 | 9.69E+06 | 3.00E+06 | 1.90E+06 | 2.07E+04 |
| 2024 | 3.05E+08 | 1.30E+07 | 3.97E+06 | 2.51E+06 | 4.05E+04 |
| 2025 | 3.11E+08 | 1.68E+07 | 5.10E+06 | 3.21E+06 | 6.97E+04 |
| 2026 | 3.15E+08 | 2.16E+07 | 6.48E+06 | 4.05E+06 | 1.13E+05 |
| 2027 | 3.17E+08 | 2.72E+07 | 8.09E+06 | 5.03E+06 | 1.73E+05 |
| 2028 | 3.17E+08 | 3.38E+07 | 9.93E+06 | 6.14E+06 | 2.52E+05 |
| 2029 | 3.14E+08 | 4.14E+07 | 1.20E+07 | 7.38E+06 | 3.55E+05 |
| 2030 | 3.11E+08 | 4.99E+07 | 1.43E+07 | 8.74E+06 | 4.84E+05 |
| 2031 | 3.06E+08 | 5.90E+07 | 1.67E+07 | 1.01E+07 | 6.35E+05 |
| 2032 | 3.01E+08 | 6.85E+07 | 1.92E+07 | 1.16E+07 | 8.10E+05 |
| 2033 | 2.96E+08 | 7.84E+07 | 2.17E+07 | 1.30E+07 | 1.01E+06 |
| 2034 | 2.91E+08 | 8.86E+07 | 2.42E+07 | 1.44E+07 | 1.23E+06 |
| 2035 | 2.86E+08 | 9.92E+07 | 2.68E+07 | 1.58E+07 | 1.49E+06 |
| 2036 | 2.81E+08 | 1.10E+08 | 2.93E+07 | 1.72E+07 | 1.77E+06 |
| 2037 | 2.76E+08 | 1.21E+08 | 3.19E+07 | 1.85E+07 | 2.08E+06 |
| 2038 | 2.70E+08 | 1.32E+08 | 3.43E+07 | 1.98E+07 | 2.43E+06 |
| 2039 | 2.65E+08 | 1.43E+08 | 3.68E+07 | 2.10E+07 | 2.81E+06 |
| 2040 | 2.60E+08 | 1.55E+08 | 3.91E+07 | 2.22E+07 | 3.22E+06 |
| 2041 | 2.54E+08 | 1.66E+08 | 4.14E+07 | 2.33E+07 | 3.67E+06 |
| 2042 | 2.49E+08 | 1.78E+08 | 4.37E+07 | 2.43E+07 | 4.15E+06 |
| 2043 | 2.43E+08 | 1.89E+08 | 4.59E+07 | 2.53E+07 | 4.68E+06 |
| 2044 | 2.37E+08 | 2.01E+08 | 4.81E+07 | 2.62E+07 | 5.24E+06 |
| 2045 | 2.31E+08 | 2.14E+08 | 5.03E+07 | 2.71E+07 | 5.85E+06 |
| 2046 | 2.24E+08 | 2.27E+08 | 5.25E+07 | 2.79E+07 | 6.50E+06 |
| 2047 | 2.18E+08 | 2.40E+08 | 5.47E+07 | 2.87E+07 | 7.19E+06 |
| 2048 | 2.10E+08 | 2.53E+08 | 5.68E+07 | 2.95E+07 | 7.93E+06 |
| 2049 | 2.03E+08 | 2.67E+08 | 5.90E+07 | 3.02E+07 | 8.72E+06 |
| 2050 | 1.95E+08 | 2.81E+08 | 6.12E+07 | 3.09E+07 | 9.55E+06 |

## Table S21. Estimated number of in-use vehicles in China in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.87E+08 | 6.01E+06 | 1.88E+06 | 1.20E+06 | 6.07E+03 |
| 2023 | 2.99E+08 | 7.85E+06 | 2.44E+06 | 1.55E+06 | 1.45E+04 |
| 2024 | 3.09E+08 | 1.01E+07 | 3.10E+06 | 1.97E+06 | 2.83E+04 |
| 2025 | 3.17E+08 | 1.28E+07 | 3.89E+06 | 2.45E+06 | 4.87E+04 |
| 2026 | 3.23E+08 | 1.60E+07 | 4.83E+06 | 3.03E+06 | 7.88E+04 |
| 2027 | 3.28E+08 | 1.99E+07 | 5.93E+06 | 3.70E+06 | 1.21E+05 |
| 2028 | 3.30E+08 | 2.45E+07 | 7.19E+06 | 4.45E+06 | 1.77E+05 |
| 2029 | 3.32E+08 | 2.96E+07 | 8.61E+06 | 5.30E+06 | 2.48E+05 |
| 2030 | 3.32E+08 | 3.55E+07 | 1.02E+07 | 6.22E+06 | 3.39E+05 |
| 2031 | 3.32E+08 | 4.17E+07 | 1.18E+07 | 7.17E+06 | 4.45E+05 |
| 2032 | 3.31E+08 | 4.82E+07 | 1.35E+07 | 8.14E+06 | 5.67E+05 |
| 2033 | 3.31E+08 | 5.50E+07 | 1.52E+07 | 9.12E+06 | 7.06E+05 |
| 2034 | 3.30E+08 | 6.21E+07 | 1.70E+07 | 1.01E+07 | 8.64E+05 |
| 2035 | 3.30E+08 | 6.95E+07 | 1.88E+07 | 1.11E+07 | 1.04E+06 |
| 2036 | 3.30E+08 | 7.70E+07 | 2.05E+07 | 1.20E+07 | 1.24E+06 |
| 2037 | 3.29E+08 | 8.46E+07 | 2.23E+07 | 1.30E+07 | 1.46E+06 |
| 2038 | 3.29E+08 | 9.24E+07 | 2.40E+07 | 1.39E+07 | 1.70E+06 |
| 2039 | 3.29E+08 | 1.00E+08 | 2.57E+07 | 1.47E+07 | 1.96E+06 |
| 2040 | 3.29E+08 | 1.08E+08 | 2.74E+07 | 1.55E+07 | 2.25E+06 |
| 2041 | 3.28E+08 | 1.16E+08 | 2.90E+07 | 1.63E+07 | 2.57E+06 |
| 2042 | 3.28E+08 | 1.24E+08 | 3.06E+07 | 1.70E+07 | 2.91E+06 |
| 2043 | 3.27E+08 | 1.33E+08 | 3.21E+07 | 1.77E+07 | 3.27E+06 |
| 2044 | 3.26E+08 | 1.41E+08 | 3.37E+07 | 1.83E+07 | 3.67E+06 |
| 2045 | 3.26E+08 | 1.50E+08 | 3.52E+07 | 1.89E+07 | 4.09E+06 |
| 2046 | 3.24E+08 | 1.59E+08 | 3.67E+07 | 1.95E+07 | 4.55E+06 |
| 2047 | 3.23E+08 | 1.68E+08 | 3.83E+07 | 2.01E+07 | 5.03E+06 |
| 2048 | 3.21E+08 | 1.77E+08 | 3.98E+07 | 2.06E+07 | 5.55E+06 |
| 2049 | 3.20E+08 | 1.87E+08 | 4.13E+07 | 2.12E+07 | 6.10E+06 |
| 2050 | 3.17E+08 | 1.97E+08 | 4.29E+07 | 2.17E+07 | 6.69E+06 |

## Table S22. Estimated number of in-use vehicles in China in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 2.85E+08 | 7.29E+06 | 2.27E+06 | 1.45E+06 | 9.29E+03 |
| 2023 | 2.95E+08 | 1.05E+07 | 3.23E+06 | 2.05E+06 | 2.37E+04 |
| 2024 | 3.02E+08 | 1.46E+07 | 4.46E+06 | 2.81E+06 | 4.84E+04 |
| 2025 | 3.07E+08 | 1.96E+07 | 5.94E+06 | 3.73E+06 | 8.64E+04 |
| 2026 | 3.09E+08 | 2.59E+07 | 7.74E+06 | 4.84E+06 | 1.42E+05 |
| 2027 | 3.08E+08 | 3.33E+07 | 9.86E+06 | 6.13E+06 | 2.20E+05 |
| 2028 | 3.04E+08 | 4.20E+07 | 1.23E+07 | 7.60E+06 | 3.24E+05 |
| 2029 | 2.99E+08 | 5.20E+07 | 1.50E+07 | 9.24E+06 | 4.58E+05 |
| 2030 | 2.91E+08 | 6.33E+07 | 1.81E+07 | 1.10E+07 | 6.26E+05 |
| 2031 | 2.82E+08 | 7.52E+07 | 2.13E+07 | 1.29E+07 | 8.23E+05 |
| 2032 | 2.73E+08 | 8.78E+07 | 2.46E+07 | 1.48E+07 | 1.05E+06 |
| 2033 | 2.63E+08 | 1.01E+08 | 2.79E+07 | 1.67E+07 | 1.31E+06 |
| 2034 | 2.53E+08 | 1.15E+08 | 3.13E+07 | 1.86E+07 | 1.60E+06 |
| 2035 | 2.43E+08 | 1.28E+08 | 3.47E+07 | 2.05E+07 | 1.93E+06 |
| 2036 | 2.33E+08 | 1.43E+08 | 3.81E+07 | 2.23E+07 | 2.30E+06 |
| 2037 | 2.22E+08 | 1.57E+08 | 4.14E+07 | 2.41E+07 | 2.71E+06 |
| 2038 | 2.12E+08 | 1.72E+08 | 4.46E+07 | 2.57E+07 | 3.15E+06 |
| 2039 | 2.01E+08 | 1.86E+08 | 4.78E+07 | 2.73E+07 | 3.65E+06 |
| 2040 | 1.91E+08 | 2.01E+08 | 5.09E+07 | 2.88E+07 | 4.18E+06 |
| 2041 | 1.80E+08 | 2.16E+08 | 5.39E+07 | 3.02E+07 | 4.77E+06 |
| 2042 | 1.70E+08 | 2.31E+08 | 5.68E+07 | 3.16E+07 | 5.40E+06 |
| 2043 | 1.59E+08 | 2.46E+08 | 5.97E+07 | 3.28E+07 | 6.08E+06 |
| 2044 | 1.48E+08 | 2.62E+08 | 6.25E+07 | 3.40E+07 | 6.81E+06 |
| 2045 | 1.36E+08 | 2.78E+08 | 6.54E+07 | 3.52E+07 | 7.60E+06 |
| 2046 | 1.25E+08 | 2.94E+08 | 6.82E+07 | 3.63E+07 | 8.44E+06 |
| 2047 | 1.13E+08 | 3.11E+08 | 7.09E+07 | 3.72E+07 | 9.32E+06 |
| 2048 | 1.02E+08 | 3.27E+08 | 7.35E+07 | 3.82E+07 | 1.02E+07 |
| 2049 | 9.00E+07 | 3.44E+08 | 7.61E+07 | 3.90E+07 | 1.12E+07 |
| 2050 | 7.81E+07 | 3.61E+08 | 7.87E+07 | 3.98E+07 | 1.22E+07 |

## Table S23. Estimated number of in-use vehicles in Japan in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.48E+07 | 2.67E+05 | 3.15E+05 | 1.28E+07 | 4.39E+04 |
| 2023 | 3.35E+07 | 3.72E+05 | 4.72E+05 | 1.37E+07 | 8.27E+04 |
| 2024 | 3.22E+07 | 5.08E+05 | 6.77E+05 | 1.45E+07 | 1.34E+05 |
| 2025 | 3.09E+07 | 6.75E+05 | 9.27E+05 | 1.53E+07 | 1.97E+05 |
| 2026 | 2.97E+07 | 8.70E+05 | 1.22E+06 | 1.60E+07 | 2.71E+05 |
| 2027 | 2.85E+07 | 1.09E+06 | 1.56E+06 | 1.67E+07 | 3.57E+05 |
| 2028 | 2.74E+07 | 1.34E+06 | 1.94E+06 | 1.73E+07 | 4.53E+05 |
| 2029 | 2.64E+07 | 1.62E+06 | 2.35E+06 | 1.79E+07 | 5.59E+05 |
| 2030 | 2.53E+07 | 1.91E+06 | 2.80E+06 | 1.85E+07 | 6.75E+05 |
| 2031 | 2.43E+07 | 2.22E+06 | 3.26E+06 | 1.90E+07 | 8.03E+05 |
| 2032 | 2.34E+07 | 2.53E+06 | 3.72E+06 | 1.94E+07 | 9.43E+05 |
| 2033 | 2.26E+07 | 2.85E+06 | 4.17E+06 | 1.97E+07 | 1.09E+06 |
| 2034 | 2.18E+07 | 3.18E+06 | 4.62E+06 | 2.00E+07 | 1.26E+06 |
| 2035 | 2.11E+07 | 3.51E+06 | 5.07E+06 | 2.02E+07 | 1.43E+06 |
| 2036 | 2.04E+07 | 3.84E+06 | 5.51E+06 | 2.03E+07 | 1.61E+06 |
| 2037 | 1.97E+07 | 4.17E+06 | 5.94E+06 | 2.05E+07 | 1.80E+06 |
| 2038 | 1.91E+07 | 4.51E+06 | 6.36E+06 | 2.05E+07 | 1.99E+06 |
| 2039 | 1.85E+07 | 4.84E+06 | 6.77E+06 | 2.06E+07 | 2.19E+06 |
| 2040 | 1.79E+07 | 5.16E+06 | 7.17E+06 | 2.05E+07 | 2.40E+06 |
| 2041 | 1.73E+07 | 5.49E+06 | 7.56E+06 | 2.05E+07 | 2.61E+06 |
| 2042 | 1.68E+07 | 5.82E+06 | 7.94E+06 | 2.04E+07 | 2.82E+06 |
| 2043 | 1.63E+07 | 6.14E+06 | 8.31E+06 | 2.04E+07 | 3.02E+06 |
| 2044 | 1.58E+07 | 6.46E+06 | 8.67E+06 | 2.02E+07 | 3.23E+06 |
| 2045 | 1.53E+07 | 6.77E+06 | 9.02E+06 | 2.01E+07 | 3.44E+06 |
| 2046 | 1.48E+07 | 7.09E+06 | 9.36E+06 | 2.00E+07 | 3.64E+06 |
| 2047 | 1.43E+07 | 7.40E+06 | 9.70E+06 | 1.98E+07 | 3.84E+06 |
| 2048 | 1.38E+07 | 7.71E+06 | 1.00E+07 | 1.97E+07 | 4.04E+06 |
| 2049 | 1.33E+07 | 8.02E+06 | 1.04E+07 | 1.95E+07 | 4.24E+06 |
| 2050 | 1.28E+07 | 8.32E+06 | 1.07E+07 | 1.94E+07 | 4.44E+06 |

## Table S24. Estimated number of in-use vehicles in Japan in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.51E+07 | 2.36E+05 | 2.68E+05 | 1.27E+07 | 3.23E+04 |
| 2023 | 3.39E+07 | 3.11E+05 | 3.80E+05 | 1.34E+07 | 5.96E+04 |
| 2024 | 3.29E+07 | 4.06E+05 | 5.23E+05 | 1.41E+07 | 9.54E+04 |
| 2025 | 3.21E+07 | 5.22E+05 | 6.98E+05 | 1.46E+07 | 1.40E+05 |
| 2026 | 3.13E+07 | 6.57E+05 | 9.04E+05 | 1.50E+07 | 1.92E+05 |
| 2027 | 3.07E+07 | 8.11E+05 | 1.14E+06 | 1.54E+07 | 2.52E+05 |
| 2028 | 3.01E+07 | 9.83E+05 | 1.40E+06 | 1.57E+07 | 3.19E+05 |
| 2029 | 2.97E+07 | 1.17E+06 | 1.69E+06 | 1.59E+07 | 3.93E+05 |
| 2030 | 2.93E+07 | 1.38E+06 | 2.00E+06 | 1.60E+07 | 4.74E+05 |
| 2031 | 2.90E+07 | 1.59E+06 | 2.32E+06 | 1.61E+07 | 5.63E+05 |
| 2032 | 2.87E+07 | 1.80E+06 | 2.63E+06 | 1.61E+07 | 6.61E+05 |
| 2033 | 2.85E+07 | 2.03E+06 | 2.95E+06 | 1.61E+07 | 7.67E+05 |
| 2034 | 2.83E+07 | 2.25E+06 | 3.26E+06 | 1.60E+07 | 8.80E+05 |
| 2035 | 2.81E+07 | 2.48E+06 | 3.57E+06 | 1.59E+07 | 1.00E+06 |
| 2036 | 2.78E+07 | 2.71E+06 | 3.88E+06 | 1.58E+07 | 1.13E+06 |
| 2037 | 2.76E+07 | 2.94E+06 | 4.17E+06 | 1.57E+07 | 1.26E+06 |
| 2038 | 2.74E+07 | 3.17E+06 | 4.47E+06 | 1.56E+07 | 1.39E+06 |
| 2039 | 2.71E+07 | 3.40E+06 | 4.75E+06 | 1.54E+07 | 1.54E+06 |
| 2040 | 2.68E+07 | 3.63E+06 | 5.03E+06 | 1.52E+07 | 1.68E+06 |
| 2041 | 2.66E+07 | 3.85E+06 | 5.30E+06 | 1.51E+07 | 1.83E+06 |
| 2042 | 2.63E+07 | 4.08E+06 | 5.57E+06 | 1.49E+07 | 1.97E+06 |
| 2043 | 2.60E+07 | 4.30E+06 | 5.82E+06 | 1.47E+07 | 2.12E+06 |
| 2044 | 2.56E+07 | 4.53E+06 | 6.07E+06 | 1.46E+07 | 2.26E+06 |
| 2045 | 2.53E+07 | 4.75E+06 | 6.32E+06 | 1.44E+07 | 2.41E+06 |
| 2046 | 2.50E+07 | 4.97E+06 | 6.56E+06 | 1.43E+07 | 2.55E+06 |
| 2047 | 2.46E+07 | 5.18E+06 | 6.79E+06 | 1.41E+07 | 2.69E+06 |
| 2048 | 2.43E+07 | 5.40E+06 | 7.02E+06 | 1.39E+07 | 2.83E+06 |
| 2049 | 2.40E+07 | 5.61E+06 | 7.25E+06 | 1.38E+07 | 2.97E+06 |
| 2050 | 2.36E+07 | 5.83E+06 | 7.47E+06 | 1.37E+07 | 3.11E+06 |

## Table S25. Estimated number of in-use vehicles in Japan in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.46E+07 | 2.98E+05 | 3.61E+05 | 1.30E+07 | 5.55E+04 |
| 2023 | 3.30E+07 | 4.34E+05 | 5.64E+05 | 1.40E+07 | 1.06E+05 |
| 2024 | 3.14E+07 | 6.11E+05 | 8.30E+05 | 1.50E+07 | 1.72E+05 |
| 2025 | 2.98E+07 | 8.27E+05 | 1.16E+06 | 1.60E+07 | 2.54E+05 |
| 2026 | 2.81E+07 | 1.08E+06 | 1.54E+06 | 1.70E+07 | 3.51E+05 |
| 2027 | 2.64E+07 | 1.37E+06 | 1.98E+06 | 1.80E+07 | 4.62E+05 |
| 2028 | 2.47E+07 | 1.70E+06 | 2.47E+06 | 1.90E+07 | 5.88E+05 |
| 2029 | 2.30E+07 | 2.06E+06 | 3.02E+06 | 2.00E+07 | 7.26E+05 |
| 2030 | 2.13E+07 | 2.45E+06 | 3.61E+06 | 2.09E+07 | 8.75E+05 |
| 2031 | 1.97E+07 | 2.84E+06 | 4.20E+06 | 2.18E+07 | 1.04E+06 |
| 2032 | 1.82E+07 | 3.25E+06 | 4.80E+06 | 2.26E+07 | 1.22E+06 |
| 2033 | 1.67E+07 | 3.65E+06 | 5.40E+06 | 2.33E+07 | 1.42E+06 |
| 2034 | 1.54E+07 | 4.05E+06 | 5.99E+06 | 2.39E+07 | 1.63E+06 |
| 2035 | 1.42E+07 | 4.46E+06 | 6.57E+06 | 2.44E+07 | 1.85E+06 |
| 2036 | 1.30E+07 | 4.86E+06 | 7.14E+06 | 2.49E+07 | 2.09E+06 |
| 2037 | 1.20E+07 | 5.26E+06 | 7.71E+06 | 2.52E+07 | 2.33E+06 |
| 2038 | 1.10E+07 | 5.65E+06 | 8.26E+06 | 2.55E+07 | 2.59E+06 |
| 2039 | 1.01E+07 | 6.03E+06 | 8.79E+06 | 2.57E+07 | 2.85E+06 |
| 2040 | 9.25E+06 | 6.41E+06 | 9.31E+06 | 2.58E+07 | 3.12E+06 |
| 2041 | 8.48E+06 | 6.80E+06 | 9.81E+06 | 2.59E+07 | 3.39E+06 |
| 2042 | 7.76E+06 | 7.19E+06 | 1.03E+07 | 2.59E+07 | 3.66E+06 |
| 2043 | 7.09E+06 | 7.58E+06 | 1.07E+07 | 2.59E+07 | 3.93E+06 |
| 2044 | 6.46E+06 | 7.98E+06 | 1.12E+07 | 2.58E+07 | 4.20E+06 |
| 2045 | 5.86E+06 | 8.38E+06 | 1.16E+07 | 2.57E+07 | 4.47E+06 |
| 2046 | 5.28E+06 | 8.79E+06 | 1.20E+07 | 2.55E+07 | 4.73E+06 |
| 2047 | 4.72E+06 | 9.20E+06 | 1.24E+07 | 2.54E+07 | 5.00E+06 |
| 2048 | 4.18E+06 | 9.61E+06 | 1.27E+07 | 2.51E+07 | 5.26E+06 |
| 2049 | 3.64E+06 | 1.00E+07 | 1.31E+07 | 2.49E+07 | 5.51E+06 |
| 2050 | 3.12E+06 | 1.05E+07 | 1.34E+07 | 2.46E+07 | 5.77E+06 |

## Table S26. Estimated number of ELVs in China in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 1.17E+07 | 2.45E+04 | 7.73E+03 | 4.95E+03 | 1.48E+01 |
| 2023 | 1.35E+07 | 4.55E+04 | 1.43E+04 | 9.20E+03 | 6.50E+01 |
| 2024 | 1.54E+07 | 7.93E+04 | 2.50E+04 | 1.60E+04 | 1.89E+02 |
| 2025 | 1.73E+07 | 1.31E+05 | 4.11E+04 | 2.64E+04 | 4.38E+02 |
| 2026 | 1.91E+07 | 2.04E+05 | 6.43E+04 | 4.12E+04 | 8.76E+02 |
| 2027 | 2.07E+07 | 3.06E+05 | 9.60E+04 | 6.14E+04 | 1.59E+03 |
| 2028 | 2.22E+07 | 4.39E+05 | 1.37E+05 | 8.77E+04 | 2.70E+03 |
| 2029 | 2.33E+07 | 6.08E+05 | 1.90E+05 | 1.21E+05 | 4.32E+03 |
| 2030 | 2.41E+07 | 8.21E+05 | 2.54E+05 | 1.62E+05 | 6.62E+03 |
| 2031 | 2.47E+07 | 1.09E+06 | 3.34E+05 | 2.11E+05 | 9.75E+03 |
| 2032 | 2.49E+07 | 1.41E+06 | 4.31E+05 | 2.72E+05 | 1.39E+04 |
| 2033 | 2.48E+07 | 1.82E+06 | 5.51E+05 | 3.46E+05 | 1.91E+04 |
| 2034 | 2.46E+07 | 2.33E+06 | 6.94E+05 | 4.33E+05 | 2.56E+04 |
| 2035 | 2.43E+07 | 2.92E+06 | 8.63E+05 | 5.35E+05 | 3.35E+04 |
| 2036 | 2.39E+07 | 3.61E+06 | 1.05E+06 | 6.49E+05 | 4.29E+04 |
| 2037 | 2.35E+07 | 4.37E+06 | 1.26E+06 | 7.73E+05 | 5.39E+04 |
| 2038 | 2.32E+07 | 5.21E+06 | 1.48E+06 | 9.03E+05 | 6.67E+04 |
| 2039 | 2.28E+07 | 6.10E+06 | 1.72E+06 | 1.04E+06 | 8.14E+04 |
| 2040 | 2.24E+07 | 7.04E+06 | 1.96E+06 | 1.17E+06 | 9.80E+04 |
| 2041 | 2.20E+07 | 8.00E+06 | 2.19E+06 | 1.31E+06 | 1.17E+05 |
| 2042 | 2.15E+07 | 8.96E+06 | 2.43E+06 | 1.43E+06 | 1.37E+05 |
| 2043 | 2.11E+07 | 9.91E+06 | 2.65E+06 | 1.55E+06 | 1.61E+05 |
| 2044 | 2.06E+07 | 1.08E+07 | 2.85E+06 | 1.66E+06 | 1.86E+05 |
| 2045 | 2.02E+07 | 1.17E+07 | 3.05E+06 | 1.76E+06 | 2.14E+05 |
| 2046 | 1.98E+07 | 1.26E+07 | 3.24E+06 | 1.85E+06 | 2.44E+05 |
| 2047 | 1.94E+07 | 1.35E+07 | 3.42E+06 | 1.93E+06 | 2.77E+05 |
| 2048 | 1.91E+07 | 1.45E+07 | 3.59E+06 | 2.01E+06 | 3.13E+05 |
| 2049 | 1.87E+07 | 1.54E+07 | 3.77E+06 | 2.09E+06 | 3.51E+05 |
| 2050 | 1.83E+07 | 1.64E+07 | 3.95E+06 | 2.17E+06 | 3.93E+05 |

## Table S27. Estimated number of ELVs in China in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 1.17E+07 | 2.45E+04 | 7.72E+03 | 4.95E+03 | 1.08E+01 |
| 2023 | 1.35E+07 | 4.54E+04 | 1.43E+04 | 9.18E+03 | 4.66E+01 |
| 2024 | 1.54E+07 | 7.87E+04 | 2.48E+04 | 1.59E+04 | 1.34E+02 |
| 2025 | 1.73E+07 | 1.29E+05 | 4.05E+04 | 2.60E+04 | 3.08E+02 |
| 2026 | 1.91E+07 | 1.98E+05 | 6.25E+04 | 4.00E+04 | 6.14E+02 |
| 2027 | 2.08E+07 | 2.91E+05 | 9.14E+04 | 5.85E+04 | 1.11E+03 |
| 2028 | 2.22E+07 | 4.07E+05 | 1.28E+05 | 8.15E+04 | 1.89E+03 |
| 2029 | 2.34E+07 | 5.45E+05 | 1.70E+05 | 1.09E+05 | 3.02E+03 |
| 2030 | 2.43E+07 | 7.07E+05 | 2.20E+05 | 1.40E+05 | 4.63E+03 |
| 2031 | 2.49E+07 | 8.94E+05 | 2.76E+05 | 1.75E+05 | 6.82E+03 |
| 2032 | 2.52E+07 | 1.11E+06 | 3.41E+05 | 2.15E+05 | 9.70E+03 |
| 2033 | 2.53E+07 | 1.38E+06 | 4.18E+05 | 2.62E+05 | 1.34E+04 |
| 2034 | 2.53E+07 | 1.70E+06 | 5.09E+05 | 3.18E+05 | 1.79E+04 |
| 2035 | 2.52E+07 | 2.09E+06 | 6.18E+05 | 3.84E+05 | 2.34E+04 |
| 2036 | 2.51E+07 | 2.55E+06 | 7.44E+05 | 4.59E+05 | 3.00E+04 |
| 2037 | 2.51E+07 | 3.07E+06 | 8.86E+05 | 5.43E+05 | 3.77E+04 |
| 2038 | 2.51E+07 | 3.65E+06 | 1.04E+06 | 6.33E+05 | 4.67E+04 |
| 2039 | 2.50E+07 | 4.27E+06 | 1.20E+06 | 7.26E+05 | 5.69E+04 |
| 2040 | 2.50E+07 | 4.93E+06 | 1.37E+06 | 8.22E+05 | 6.86E+04 |
| 2041 | 2.50E+07 | 5.60E+06 | 1.54E+06 | 9.15E+05 | 8.16E+04 |
| 2042 | 2.49E+07 | 6.28E+06 | 1.70E+06 | 1.00E+06 | 9.62E+04 |
| 2043 | 2.49E+07 | 6.94E+06 | 1.85E+06 | 1.09E+06 | 1.12E+05 |
| 2044 | 2.48E+07 | 7.58E+06 | 2.00E+06 | 1.16E+06 | 1.30E+05 |
| 2045 | 2.48E+07 | 8.22E+06 | 2.13E+06 | 1.23E+06 | 1.50E+05 |
| 2046 | 2.47E+07 | 8.84E+06 | 2.26E+06 | 1.29E+06 | 1.71E+05 |
| 2047 | 2.47E+07 | 9.48E+06 | 2.39E+06 | 1.35E+06 | 1.94E+05 |
| 2048 | 2.48E+07 | 1.01E+07 | 2.52E+06 | 1.41E+06 | 2.19E+05 |
| 2049 | 2.48E+07 | 1.08E+07 | 2.64E+06 | 1.46E+06 | 2.46E+05 |
| 2050 | 2.47E+07 | 1.15E+07 | 2.77E+06 | 1.52E+06 | 2.75E+05 |

## Table S28. Estimated number of ELVs in China in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 1.17E+07 | 2.45E+04 | 7.73E+03 | 4.95E+03 | 1.54E+01 |
| 2023 | 1.35E+07 | 4.55E+04 | 1.43E+04 | 9.20E+03 | 7.05E+01 |
| 2024 | 1.54E+07 | 7.94E+04 | 2.50E+04 | 1.60E+04 | 2.13E+02 |
| 2025 | 1.73E+07 | 1.31E+05 | 4.13E+04 | 2.64E+04 | 5.10E+02 |
| 2026 | 1.91E+07 | 2.06E+05 | 6.48E+04 | 4.15E+04 | 1.05E+03 |
| 2027 | 2.07E+07 | 3.11E+05 | 9.75E+04 | 6.24E+04 | 1.95E+03 |
| 2028 | 2.21E+07 | 4.52E+05 | 1.41E+05 | 9.02E+04 | 3.36E+03 |
| 2029 | 2.33E+07 | 6.37E+05 | 1.98E+05 | 1.26E+05 | 5.44E+03 |
| 2030 | 2.41E+07 | 8.79E+05 | 2.72E+05 | 1.72E+05 | 8.41E+03 |
| 2031 | 2.45E+07 | 1.19E+06 | 3.66E+05 | 2.31E+05 | 1.25E+04 |
| 2032 | 2.47E+07 | 1.60E+06 | 4.87E+05 | 3.06E+05 | 1.78E+04 |
| 2033 | 2.45E+07 | 2.13E+06 | 6.40E+05 | 4.01E+05 | 2.46E+04 |
| 2034 | 2.41E+07 | 2.78E+06 | 8.29E+05 | 5.17E+05 | 3.30E+04 |
| 2035 | 2.36E+07 | 3.58E+06 | 1.06E+06 | 6.54E+05 | 4.33E+04 |
| 2036 | 2.29E+07 | 4.51E+06 | 1.31E+06 | 8.10E+05 | 5.55E+04 |
| 2037 | 2.22E+07 | 5.56E+06 | 1.60E+06 | 9.80E+05 | 6.99E+04 |
| 2038 | 2.15E+07 | 6.69E+06 | 1.90E+06 | 1.16E+06 | 8.65E+04 |
| 2039 | 2.07E+07 | 7.89E+06 | 2.22E+06 | 1.34E+06 | 1.06E+05 |
| 2040 | 1.99E+07 | 9.13E+06 | 2.54E+06 | 1.52E+06 | 1.27E+05 |
| 2041 | 1.90E+07 | 1.04E+07 | 2.85E+06 | 1.70E+06 | 1.51E+05 |
| 2042 | 1.81E+07 | 1.17E+07 | 3.15E+06 | 1.86E+06 | 1.79E+05 |
| 2043 | 1.73E+07 | 1.29E+07 | 3.44E+06 | 2.02E+06 | 2.09E+05 |
| 2044 | 1.64E+07 | 1.41E+07 | 3.71E+06 | 2.16E+06 | 2.42E+05 |
| 2045 | 1.56E+07 | 1.53E+07 | 3.96E+06 | 2.29E+06 | 2.78E+05 |
| 2046 | 1.48E+07 | 1.64E+07 | 4.21E+06 | 2.40E+06 | 3.17E+05 |
| 2047 | 1.41E+07 | 1.76E+07 | 4.44E+06 | 2.51E+06 | 3.60E+05 |
| 2048 | 1.34E+07 | 1.88E+07 | 4.67E+06 | 2.62E+06 | 4.06E+05 |
| 2049 | 1.26E+07 | 2.00E+07 | 4.90E+06 | 2.72E+06 | 4.56E+05 |
| 2050 | 1.19E+07 | 2.13E+07 | 5.14E+06 | 2.82E+06 | 5.09E+05 |

## Table S29. Estimated number of ELVs in Japan in 2022−2050 in standard scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.70E+06 | 6.49E+03 | 5.86E+03 | 4.64E+05 | 2.09E+02 |
| 2023 | 3.58E+06 | 8.05E+03 | 7.77E+03 | 5.38E+05 | 4.70E+02 |
| 2024 | 3.46E+06 | 1.02E+04 | 1.06E+04 | 6.13E+05 | 9.74E+02 |
| 2025 | 3.34E+06 | 1.32E+04 | 1.47E+04 | 6.89E+05 | 1.81E+03 |
| 2026 | 3.22E+06 | 1.72E+04 | 2.04E+04 | 7.63E+05 | 3.07E+03 |
| 2027 | 3.10E+06 | 2.24E+04 | 2.80E+04 | 8.36E+05 | 4.83E+03 |
| 2028 | 2.98E+06 | 2.91E+04 | 3.78E+04 | 9.06E+05 | 7.17E+03 |
| 2029 | 2.87E+06 | 3.73E+04 | 5.00E+04 | 9.72E+05 | 1.01E+04 |
| 2030 | 2.76E+06 | 4.71E+04 | 6.48E+04 | 1.04E+06 | 1.38E+04 |
| 2031 | 2.65E+06 | 5.88E+04 | 8.23E+04 | 1.09E+06 | 1.82E+04 |
| 2032 | 2.54E+06 | 7.22E+04 | 1.03E+05 | 1.15E+06 | 2.33E+04 |
| 2033 | 2.44E+06 | 8.73E+04 | 1.25E+05 | 1.20E+06 | 2.93E+04 |
| 2034 | 2.34E+06 | 1.04E+05 | 1.50E+05 | 1.25E+06 | 3.60E+04 |
| 2035 | 2.25E+06 | 1.22E+05 | 1.77E+05 | 1.29E+06 | 4.36E+04 |
| 2036 | 2.16E+06 | 1.42E+05 | 2.06E+05 | 1.33E+06 | 5.20E+04 |
| 2037 | 2.08E+06 | 1.63E+05 | 2.36E+05 | 1.36E+06 | 6.13E+04 |
| 2038 | 2.00E+06 | 1.84E+05 | 2.67E+05 | 1.39E+06 | 7.13E+04 |
| 2039 | 1.93E+06 | 2.07E+05 | 2.98E+05 | 1.41E+06 | 8.21E+04 |
| 2040 | 1.87E+06 | 2.30E+05 | 3.31E+05 | 1.43E+06 | 9.36E+04 |
| 2041 | 1.80E+06 | 2.54E+05 | 3.63E+05 | 1.45E+06 | 1.06E+05 |
| 2042 | 1.74E+06 | 2.77E+05 | 3.95E+05 | 1.46E+06 | 1.19E+05 |
| 2043 | 1.69E+06 | 3.02E+05 | 4.26E+05 | 1.47E+06 | 1.32E+05 |
| 2044 | 1.63E+06 | 3.26E+05 | 4.57E+05 | 1.47E+06 | 1.46E+05 |
| 2045 | 1.58E+06 | 3.50E+05 | 4.88E+05 | 1.48E+06 | 1.60E+05 |
| 2046 | 1.53E+06 | 3.74E+05 | 5.17E+05 | 1.48E+06 | 1.74E+05 |
| 2047 | 1.49E+06 | 3.98E+05 | 5.46E+05 | 1.47E+06 | 1.89E+05 |
| 2048 | 1.44E+06 | 4.21E+05 | 5.74E+05 | 1.47E+06 | 2.04E+05 |
| 2049 | 1.40E+06 | 4.45E+05 | 6.01E+05 | 1.46E+06 | 2.19E+05 |
| 2050 | 1.35E+06 | 4.68E+05 | 6.27E+05 | 1.46E+06 | 2.34E+05 |

## Table S30. Estimated number of ELVs in Japan in 2022−2050 in low scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.70E+06 | 6.43E+03 | 5.77E+03 | 4.64E+05 | 1.85E+02 |
| 2023 | 3.59E+06 | 7.81E+03 | 7.40E+03 | 5.37E+05 | 3.78E+02 |
| 2024 | 3.47E+06 | 9.60E+03 | 9.68E+03 | 6.10E+05 | 7.42E+02 |
| 2025 | 3.35E+06 | 1.19E+04 | 1.28E+04 | 6.83E+05 | 1.34E+03 |
| 2026 | 3.24E+06 | 1.50E+04 | 1.71E+04 | 7.53E+05 | 2.23E+03 |
| 2027 | 3.13E+06 | 1.88E+04 | 2.26E+04 | 8.19E+05 | 3.48E+03 |
| 2028 | 3.03E+06 | 2.36E+04 | 2.96E+04 | 8.80E+05 | 5.12E+03 |
| 2029 | 2.93E+06 | 2.94E+04 | 3.83E+04 | 9.36E+05 | 7.21E+03 |
| 2030 | 2.85E+06 | 3.64E+04 | 4.87E+04 | 9.86E+05 | 9.78E+03 |
| 2031 | 2.77E+06 | 4.45E+04 | 6.10E+04 | 1.03E+06 | 1.29E+04 |
| 2032 | 2.70E+06 | 5.39E+04 | 7.51E+04 | 1.07E+06 | 1.65E+04 |
| 2033 | 2.65E+06 | 6.44E+04 | 9.09E+04 | 1.10E+06 | 2.06E+04 |
| 2034 | 2.60E+06 | 7.59E+04 | 1.08E+05 | 1.12E+06 | 2.53E+04 |
| 2035 | 2.57E+06 | 8.85E+04 | 1.27E+05 | 1.14E+06 | 3.07E+04 |
| 2036 | 2.54E+06 | 1.02E+05 | 1.47E+05 | 1.15E+06 | 3.65E+04 |
| 2037 | 2.51E+06 | 1.16E+05 | 1.68E+05 | 1.16E+06 | 4.30E+04 |
| 2038 | 2.49E+06 | 1.31E+05 | 1.89E+05 | 1.16E+06 | 5.00E+04 |
| 2039 | 2.48E+06 | 1.47E+05 | 2.11E+05 | 1.16E+06 | 5.76E+04 |
| 2040 | 2.46E+06 | 1.63E+05 | 2.33E+05 | 1.16E+06 | 6.56E+04 |
| 2041 | 2.44E+06 | 1.79E+05 | 2.56E+05 | 1.15E+06 | 7.41E+04 |
| 2042 | 2.43E+06 | 1.96E+05 | 2.78E+05 | 1.14E+06 | 8.31E+04 |
| 2043 | 2.41E+06 | 2.12E+05 | 3.00E+05 | 1.13E+06 | 9.24E+04 |
| 2044 | 2.39E+06 | 2.29E+05 | 3.21E+05 | 1.12E+06 | 1.02E+05 |
| 2045 | 2.37E+06 | 2.46E+05 | 3.42E+05 | 1.11E+06 | 1.12E+05 |
| 2046 | 2.34E+06 | 2.62E+05 | 3.63E+05 | 1.10E+06 | 1.22E+05 |
| 2047 | 2.32E+06 | 2.79E+05 | 3.83E+05 | 1.09E+06 | 1.32E+05 |
| 2048 | 2.29E+06 | 2.95E+05 | 4.02E+05 | 1.07E+06 | 1.43E+05 |
| 2049 | 2.26E+06 | 3.12E+05 | 4.21E+05 | 1.06E+06 | 1.53E+05 |
| 2050 | 2.23E+06 | 3.28E+05 | 4.39E+05 | 1.05E+06 | 1.63E+05 |

## Table S31. Estimated number of ELVs in Japan in 2022−2050 in high scenario

| Yea | ICEV (unit) | BEV (unit) | PHEV (unit) | HEV (unit) | FCV (unit) |
| --- | --- | --- | --- | --- | --- |
| 2022 | 3.70E+06 | 6.56E+03 | 5.96E+03 | 4.64E+05 | 2.34E+02 |
| 2023 | 3.58E+06 | 8.30E+03 | 8.13E+03 | 5.39E+05 | 5.61E+02 |
| 2024 | 3.46E+06 | 1.08E+04 | 1.15E+04 | 6.16E+05 | 1.21E+03 |
| 2025 | 3.34E+06 | 1.45E+04 | 1.66E+04 | 6.94E+05 | 2.28E+03 |
| 2026 | 3.21E+06 | 1.94E+04 | 2.38E+04 | 7.73E+05 | 3.91E+03 |
| 2027 | 3.08E+06 | 2.61E+04 | 3.35E+04 | 8.52E+05 | 6.19E+03 |
| 2028 | 2.94E+06 | 3.45E+04 | 4.60E+04 | 9.31E+05 | 9.22E+03 |
| 2029 | 2.81E+06 | 4.51E+04 | 6.18E+04 | 1.01E+06 | 1.31E+04 |
| 2030 | 2.66E+06 | 5.79E+04 | 8.09E+04 | 1.09E+06 | 1.78E+04 |
| 2031 | 2.52E+06 | 7.30E+04 | 1.04E+05 | 1.16E+06 | 2.35E+04 |
| 2032 | 2.37E+06 | 9.04E+04 | 1.30E+05 | 1.23E+06 | 3.02E+04 |
| 2033 | 2.23E+06 | 1.10E+05 | 1.59E+05 | 1.31E+06 | 3.79E+04 |
| 2034 | 2.08E+06 | 1.32E+05 | 1.92E+05 | 1.38E+06 | 4.67E+04 |
| 2035 | 1.93E+06 | 1.55E+05 | 2.27E+05 | 1.44E+06 | 5.66E+04 |
| 2036 | 1.79E+06 | 1.80E+05 | 2.65E+05 | 1.50E+06 | 6.75E+04 |
| 2037 | 1.65E+06 | 2.07E+05 | 3.04E+05 | 1.56E+06 | 7.96E+04 |
| 2038 | 1.52E+06 | 2.34E+05 | 3.44E+05 | 1.61E+06 | 9.26E+04 |
| 2039 | 1.39E+06 | 2.62E+05 | 3.86E+05 | 1.66E+06 | 1.07E+05 |
| 2040 | 1.28E+06 | 2.91E+05 | 4.28E+05 | 1.70E+06 | 1.22E+05 |
| 2041 | 1.17E+06 | 3.20E+05 | 4.70E+05 | 1.74E+06 | 1.37E+05 |
| 2042 | 1.07E+06 | 3.49E+05 | 5.12E+05 | 1.77E+06 | 1.54E+05 |
| 2043 | 9.80E+05 | 3.79E+05 | 5.53E+05 | 1.80E+06 | 1.71E+05 |
| 2044 | 8.98E+05 | 4.08E+05 | 5.93E+05 | 1.82E+06 | 1.89E+05 |
| 2045 | 8.23E+05 | 4.37E+05 | 6.32E+05 | 1.84E+06 | 2.08E+05 |
| 2046 | 7.55E+05 | 4.66E+05 | 6.70E+05 | 1.85E+06 | 2.27E+05 |
| 2047 | 6.92E+05 | 4.94E+05 | 7.06E+05 | 1.86E+06 | 2.46E+05 |
| 2048 | 6.33E+05 | 5.23E+05 | 7.41E+05 | 1.86E+06 | 2.65E+05 |
| 2049 | 5.78E+05 | 5.52E+05 | 7.74E+05 | 1.86E+06 | 2.84E+05 |
| 2050 | 5.26E+05 | 5.81E+05 | 8.06E+05 | 1.85E+06 | 3.04E+05 |

## Table S32a. Estimated material demand for producing vehicles in China in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 2.04E+07 | 2.73E+06 | 5.98E+05 | 1.68E+03 | 2.50E+05 | 1.18E+05 | 7.06E+03 | 2.47E+05 | 2.07E+05 | 9.98E+04 | 2.17E+03 | 4.61E+05 | 8.25E+03 | 1.72E+03 | 5.41E+01 | 5.23E+02 |
| 2021 | 2.14E+07 | 2.85E+06 | 6.90E+05 | 2.60E+03 | 2.60E+05 | 1.69E+05 | 7.22E+03 | 2.53E+05 | 2.14E+05 | 1.01E+05 | 2.38E+03 | 4.78E+05 | 9.24E+03 | 1.83E+03 | 5.87E+01 | 5.55E+02 |
| 2022 | 2.23E+07 | 2.94E+06 | 7.65E+05 | 3.36E+03 | 2.67E+05 | 2.10E+05 | 7.34E+03 | 2.58E+05 | 2.19E+05 | 1.02E+05 | 2.54E+03 | 4.93E+05 | 1.00E+04 | 1.92E+03 | 6.24E+01 | 5.81E+02 |
| 2023 | 2.31E+07 | 3.03E+06 | 8.40E+05 | 4.12E+03 | 2.74E+05 | 2.51E+05 | 7.46E+03 | 2.62E+05 | 2.24E+05 | 1.03E+05 | 2.71E+03 | 5.07E+05 | 1.09E+04 | 2.01E+03 | 6.61E+01 | 6.07E+02 |
| 2024 | 2.39E+07 | 3.12E+06 | 9.15E+05 | 4.88E+03 | 2.82E+05 | 2.93E+05 | 7.58E+03 | 2.67E+05 | 2.29E+05 | 1.04E+05 | 2.87E+03 | 5.21E+05 | 1.17E+04 | 2.09E+03 | 6.98E+01 | 6.33E+02 |
| 2025 | 2.47E+07 | 3.20E+06 | 9.90E+05 | 5.65E+03 | 2.89E+05 | 3.35E+05 | 7.69E+03 | 2.71E+05 | 2.34E+05 | 1.05E+05 | 3.04E+03 | 5.35E+05 | 1.25E+04 | 2.18E+03 | 7.35E+01 | 6.59E+02 |
| 2026 | 2.56E+07 | 3.29E+06 | 1.09E+06 | 6.78E+03 | 2.96E+05 | 3.96E+05 | 7.74E+03 | 2.73E+05 | 2.38E+05 | 1.05E+05 | 3.25E+03 | 5.49E+05 | 1.35E+04 | 2.28E+03 | 7.82E+01 | 6.89E+02 |
| 2027 | 2.65E+07 | 3.38E+06 | 1.20E+06 | 7.98E+03 | 3.02E+05 | 4.61E+05 | 7.78E+03 | 2.75E+05 | 2.42E+05 | 1.04E+05 | 3.47E+03 | 5.62E+05 | 1.46E+04 | 2.38E+03 | 8.30E+01 | 7.20E+02 |
| 2028 | 2.73E+07 | 3.46E+06 | 1.31E+06 | 9.24E+03 | 3.09E+05 | 5.29E+05 | 7.80E+03 | 2.76E+05 | 2.46E+05 | 1.03E+05 | 3.69E+03 | 5.76E+05 | 1.58E+04 | 2.49E+03 | 8.79E+01 | 7.52E+02 |
| 2029 | 2.82E+07 | 3.54E+06 | 1.43E+06 | 1.06E+04 | 3.15E+05 | 6.00E+05 | 7.80E+03 | 2.77E+05 | 2.49E+05 | 1.02E+05 | 3.92E+03 | 5.89E+05 | 1.70E+04 | 2.60E+03 | 9.30E+01 | 7.84E+02 |
| 2030 | 2.91E+07 | 3.63E+06 | 1.55E+06 | 1.19E+04 | 3.21E+05 | 6.74E+05 | 7.80E+03 | 2.77E+05 | 2.53E+05 | 1.01E+05 | 4.16E+03 | 6.02E+05 | 1.82E+04 | 2.71E+03 | 9.82E+01 | 8.16E+02 |
| 2031 | 3.00E+07 | 3.71E+06 | 1.64E+06 | 1.28E+04 | 3.29E+05 | 7.22E+05 | 7.87E+03 | 2.80E+05 | 2.57E+05 | 1.01E+05 | 4.34E+03 | 6.17E+05 | 1.91E+04 | 2.80E+03 | 1.02E+02 | 8.43E+02 |
| 2032 | 3.08E+07 | 3.80E+06 | 1.72E+06 | 1.37E+04 | 3.36E+05 | 7.72E+05 | 7.94E+03 | 2.82E+05 | 2.62E+05 | 1.02E+05 | 4.52E+03 | 6.31E+05 | 1.99E+04 | 2.89E+03 | 1.06E+02 | 8.70E+02 |
| 2033 | 3.16E+07 | 3.88E+06 | 1.81E+06 | 1.47E+04 | 3.43E+05 | 8.23E+05 | 8.00E+03 | 2.84E+05 | 2.66E+05 | 1.02E+05 | 4.70E+03 | 6.46E+05 | 2.08E+04 | 2.98E+03 | 1.10E+02 | 8.98E+02 |
| 2034 | 3.25E+07 | 3.96E+06 | 1.90E+06 | 1.56E+04 | 3.50E+05 | 8.76E+05 | 8.05E+03 | 2.86E+05 | 2.70E+05 | 1.02E+05 | 4.88E+03 | 6.60E+05 | 2.18E+04 | 3.07E+03 | 1.14E+02 | 9.26E+02 |
| 2035 | 3.33E+07 | 4.05E+06 | 1.99E+06 | 1.66E+04 | 3.57E+05 | 9.30E+05 | 8.09E+03 | 2.88E+05 | 2.74E+05 | 1.02E+05 | 5.07E+03 | 6.75E+05 | 2.27E+04 | 3.17E+03 | 1.18E+02 | 9.54E+02 |
| 2036 | 3.42E+07 | 4.13E+06 | 2.09E+06 | 1.77E+04 | 3.64E+05 | 9.87E+05 | 8.13E+03 | 2.89E+05 | 2.78E+05 | 1.01E+05 | 5.26E+03 | 6.89E+05 | 2.36E+04 | 3.26E+03 | 1.23E+02 | 9.82E+02 |
| 2037 | 3.50E+07 | 4.21E+06 | 2.19E+06 | 1.88E+04 | 3.71E+05 | 1.04E+06 | 8.15E+03 | 2.90E+05 | 2.82E+05 | 1.01E+05 | 5.45E+03 | 7.04E+05 | 2.46E+04 | 3.36E+03 | 1.27E+02 | 1.01E+03 |
| 2038 | 3.59E+07 | 4.29E+06 | 2.29E+06 | 1.99E+04 | 3.78E+05 | 1.10E+06 | 8.17E+03 | 2.91E+05 | 2.86E+05 | 1.00E+05 | 5.65E+03 | 7.19E+05 | 2.56E+04 | 3.45E+03 | 1.31E+02 | 1.04E+03 |
| 2039 | 3.67E+07 | 4.37E+06 | 2.39E+06 | 2.10E+04 | 3.85E+05 | 1.17E+06 | 8.18E+03 | 2.91E+05 | 2.89E+05 | 9.96E+04 | 5.85E+03 | 7.33E+05 | 2.66E+04 | 3.55E+03 | 1.36E+02 | 1.07E+03 |
| 2040 | 3.76E+07 | 4.45E+06 | 2.49E+06 | 2.22E+04 | 3.92E+05 | 1.23E+06 | 8.17E+03 | 2.91E+05 | 2.93E+05 | 9.87E+04 | 6.06E+03 | 7.48E+05 | 2.76E+04 | 3.65E+03 | 1.40E+02 | 1.10E+03 |
| 2041 | 3.85E+07 | 4.53E+06 | 2.60E+06 | 2.34E+04 | 3.99E+05 | 1.29E+06 | 8.16E+03 | 2.90E+05 | 2.96E+05 | 9.77E+04 | 6.26E+03 | 7.63E+05 | 2.87E+04 | 3.75E+03 | 1.45E+02 | 1.13E+03 |
| 2042 | 3.93E+07 | 4.61E+06 | 2.71E+06 | 2.46E+04 | 4.06E+05 | 1.36E+06 | 8.14E+03 | 2.89E+05 | 2.99E+05 | 9.66E+04 | 6.47E+03 | 7.77E+05 | 2.97E+04 | 3.85E+03 | 1.49E+02 | 1.16E+03 |
| 2043 | 4.02E+07 | 4.69E+06 | 2.82E+06 | 2.58E+04 | 4.12E+05 | 1.43E+06 | 8.11E+03 | 2.88E+05 | 3.02E+05 | 9.53E+04 | 6.69E+03 | 7.92E+05 | 3.08E+04 | 3.95E+03 | 1.54E+02 | 1.19E+03 |
| 2044 | 4.11E+07 | 4.77E+06 | 2.93E+06 | 2.71E+04 | 4.19E+05 | 1.50E+06 | 8.06E+03 | 2.87E+05 | 3.05E+05 | 9.39E+04 | 6.90E+03 | 8.07E+05 | 3.19E+04 | 4.05E+03 | 1.59E+02 | 1.22E+03 |
| 2045 | 4.20E+07 | 4.84E+06 | 3.05E+06 | 2.85E+04 | 4.26E+05 | 1.57E+06 | 8.01E+03 | 2.85E+05 | 3.08E+05 | 9.23E+04 | 7.12E+03 | 8.22E+05 | 3.30E+04 | 4.16E+03 | 1.63E+02 | 1.25E+03 |
| 2046 | 4.28E+07 | 4.92E+06 | 3.17E+06 | 2.98E+04 | 4.33E+05 | 1.64E+06 | 7.95E+03 | 2.82E+05 | 3.11E+05 | 9.05E+04 | 7.35E+03 | 8.36E+05 | 3.41E+04 | 4.26E+03 | 1.68E+02 | 1.28E+03 |
| 2047 | 4.37E+07 | 4.99E+06 | 3.29E+06 | 3.12E+04 | 4.39E+05 | 1.72E+06 | 7.87E+03 | 2.79E+05 | 3.13E+05 | 8.86E+04 | 7.57E+03 | 8.51E+05 | 3.53E+04 | 4.37E+03 | 1.73E+02 | 1.31E+03 |
| 2048 | 4.46E+07 | 5.06E+06 | 3.41E+06 | 3.27E+04 | 4.46E+05 | 1.80E+06 | 7.79E+03 | 2.76E+05 | 3.15E+05 | 8.66E+04 | 7.80E+03 | 8.66E+05 | 3.64E+04 | 4.47E+03 | 1.78E+02 | 1.35E+03 |
| 2049 | 4.55E+07 | 5.14E+06 | 3.54E+06 | 3.41E+04 | 4.52E+05 | 1.87E+06 | 7.70E+03 | 2.72E+05 | 3.18E+05 | 8.44E+04 | 8.03E+03 | 8.81E+05 | 3.76E+04 | 4.58E+03 | 1.83E+02 | 1.38E+03 |
| 2050 | 4.64E+07 | 5.21E+06 | 3.67E+06 | 3.56E+04 | 4.59E+05 | 1.96E+06 | 7.59E+03 | 2.68E+05 | 3.20E+05 | 8.20E+04 | 8.27E+03 | 8.96E+05 | 3.88E+04 | 4.69E+03 | 1.88E+02 | 1.41E+03 |

## Table S32b. Estimated material demand for producing vehicles in China in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 6.78E+01 | 1.53E+01 | 7.53E+00 | 2.99E+03 | 4.51E+01 | 1.58E+02 | 1.39E+02 | 1.72E+02 | 1.60E+02 | 4.92E+02 | 5.78E+03 | 7.79E+00 | 1.10E+02 | 1.32E+04 | 1.78E+04 | 3.04E+03 |
| 2021 | 6.84E+01 | 1.55E+01 | 7.60E+00 | 3.47E+03 | 4.94E+01 | 1.64E+02 | 1.45E+02 | 2.39E+02 | 1.75E+02 | 5.01E+02 | 1.15E+04 | 8.11E+00 | 1.15E+02 | 1.39E+04 | 1.81E+04 | 3.20E+03 |
| 2022 | 6.88E+01 | 1.58E+01 | 7.64E+00 | 3.86E+03 | 5.30E+01 | 1.69E+02 | 1.49E+02 | 2.95E+02 | 1.87E+02 | 5.07E+02 | 1.62E+04 | 8.37E+00 | 1.19E+02 | 1.44E+04 | 1.83E+04 | 3.32E+03 |
| 2023 | 6.91E+01 | 1.61E+01 | 7.69E+00 | 4.24E+03 | 5.66E+01 | 1.73E+02 | 1.53E+02 | 3.51E+02 | 1.99E+02 | 5.14E+02 | 2.09E+04 | 8.63E+00 | 1.22E+02 | 1.49E+04 | 1.85E+04 | 3.44E+03 |
| 2024 | 6.95E+01 | 1.65E+01 | 7.74E+00 | 4.62E+03 | 6.03E+01 | 1.78E+02 | 1.57E+02 | 4.07E+02 | 2.11E+02 | 5.20E+02 | 2.57E+04 | 8.89E+00 | 1.26E+02 | 1.54E+04 | 1.86E+04 | 3.57E+03 |
| 2025 | 6.98E+01 | 1.70E+01 | 7.78E+00 | 5.00E+03 | 6.41E+01 | 1.83E+02 | 1.61E+02 | 4.64E+02 | 2.23E+02 | 5.27E+02 | 3.04E+04 | 9.15E+00 | 1.30E+02 | 1.59E+04 | 1.88E+04 | 3.69E+03 |
| 2026 | 6.91E+01 | 1.75E+01 | 7.71E+00 | 5.53E+03 | 6.91E+01 | 1.88E+02 | 1.64E+02 | 5.47E+02 | 2.39E+02 | 5.28E+02 | 3.76E+04 | 9.41E+00 | 1.33E+02 | 1.64E+04 | 1.88E+04 | 3.82E+03 |
| 2027 | 6.83E+01 | 1.81E+01 | 7.62E+00 | 6.07E+03 | 7.43E+01 | 1.92E+02 | 1.68E+02 | 6.34E+02 | 2.56E+02 | 5.28E+02 | 4.51E+04 | 9.67E+00 | 1.37E+02 | 1.70E+04 | 1.87E+04 | 3.96E+03 |
| 2028 | 6.72E+01 | 1.87E+01 | 7.52E+00 | 6.64E+03 | 7.97E+01 | 1.96E+02 | 1.72E+02 | 7.26E+02 | 2.74E+02 | 5.28E+02 | 5.30E+04 | 9.92E+00 | 1.41E+02 | 1.75E+04 | 1.85E+04 | 4.09E+03 |
| 2029 | 6.60E+01 | 1.95E+01 | 7.39E+00 | 7.22E+03 | 8.55E+01 | 2.01E+02 | 1.75E+02 | 8.23E+02 | 2.92E+02 | 5.27E+02 | 6.12E+04 | 1.02E+01 | 1.44E+02 | 1.81E+04 | 1.84E+04 | 4.23E+03 |
| 2030 | 6.46E+01 | 2.05E+01 | 7.24E+00 | 7.81E+03 | 9.15E+01 | 2.05E+02 | 1.79E+02 | 9.24E+02 | 3.12E+02 | 5.25E+02 | 6.99E+04 | 1.04E+01 | 1.48E+02 | 1.86E+04 | 1.82E+04 | 4.37E+03 |
| 2031 | 6.45E+01 | 2.16E+01 | 7.24E+00 | 8.21E+03 | 9.61E+01 | 2.10E+02 | 1.83E+02 | 9.91E+02 | 3.27E+02 | 5.31E+02 | 7.54E+04 | 1.07E+01 | 1.52E+02 | 1.91E+04 | 1.83E+04 | 4.50E+03 |
| 2032 | 6.44E+01 | 2.28E+01 | 7.23E+00 | 8.62E+03 | 1.01E+02 | 2.14E+02 | 1.86E+02 | 1.06E+03 | 3.42E+02 | 5.36E+02 | 8.10E+04 | 1.10E+01 | 1.55E+02 | 1.97E+04 | 1.83E+04 | 4.62E+03 |
| 2033 | 6.42E+01 | 2.41E+01 | 7.21E+00 | 9.03E+03 | 1.06E+02 | 2.19E+02 | 1.90E+02 | 1.13E+03 | 3.58E+02 | 5.41E+02 | 8.69E+04 | 1.12E+01 | 1.59E+02 | 2.02E+04 | 1.84E+04 | 4.75E+03 |
| 2034 | 6.39E+01 | 2.55E+01 | 7.18E+00 | 9.45E+03 | 1.11E+02 | 2.24E+02 | 1.94E+02 | 1.20E+03 | 3.75E+02 | 5.45E+02 | 9.29E+04 | 1.15E+01 | 1.63E+02 | 2.07E+04 | 1.84E+04 | 4.88E+03 |
| 2035 | 6.35E+01 | 2.69E+01 | 7.14E+00 | 9.88E+03 | 1.16E+02 | 2.29E+02 | 1.98E+02 | 1.28E+03 | 3.92E+02 | 5.49E+02 | 9.92E+04 | 1.17E+01 | 1.66E+02 | 2.12E+04 | 1.84E+04 | 5.01E+03 |
| 2036 | 6.30E+01 | 2.85E+01 | 7.09E+00 | 1.03E+04 | 1.21E+02 | 2.33E+02 | 2.02E+02 | 1.36E+03 | 4.10E+02 | 5.53E+02 | 1.06E+05 | 1.20E+01 | 1.70E+02 | 2.18E+04 | 1.84E+04 | 5.13E+03 |
| 2037 | 6.24E+01 | 3.03E+01 | 7.03E+00 | 1.08E+04 | 1.27E+02 | 2.38E+02 | 2.06E+02 | 1.44E+03 | 4.28E+02 | 5.57E+02 | 1.12E+05 | 1.23E+01 | 1.74E+02 | 2.23E+04 | 1.84E+04 | 5.26E+03 |
| 2038 | 6.17E+01 | 3.21E+01 | 6.96E+00 | 1.12E+04 | 1.33E+02 | 2.42E+02 | 2.10E+02 | 1.52E+03 | 4.47E+02 | 5.60E+02 | 1.19E+05 | 1.25E+01 | 1.77E+02 | 2.28E+04 | 1.83E+04 | 5.40E+03 |
| 2039 | 6.09E+01 | 3.40E+01 | 6.87E+00 | 1.17E+04 | 1.39E+02 | 2.47E+02 | 2.14E+02 | 1.61E+03 | 4.66E+02 | 5.63E+02 | 1.26E+05 | 1.28E+01 | 1.81E+02 | 2.33E+04 | 1.83E+04 | 5.53E+03 |
| 2040 | 6.00E+01 | 3.61E+01 | 6.78E+00 | 1.21E+04 | 1.45E+02 | 2.52E+02 | 2.17E+02 | 1.70E+03 | 4.86E+02 | 5.65E+02 | 1.33E+05 | 1.30E+01 | 1.85E+02 | 2.39E+04 | 1.82E+04 | 5.66E+03 |
| 2041 | 5.91E+01 | 3.83E+01 | 6.67E+00 | 1.26E+04 | 1.51E+02 | 2.56E+02 | 2.21E+02 | 1.79E+03 | 5.07E+02 | 5.67E+02 | 1.41E+05 | 1.33E+01 | 1.88E+02 | 2.44E+04 | 1.81E+04 | 5.79E+03 |
| 2042 | 5.80E+01 | 4.07E+01 | 6.55E+00 | 1.31E+04 | 1.58E+02 | 2.61E+02 | 2.25E+02 | 1.88E+03 | 5.28E+02 | 5.69E+02 | 1.49E+05 | 1.36E+01 | 1.92E+02 | 2.49E+04 | 1.79E+04 | 5.92E+03 |
| 2043 | 5.68E+01 | 4.31E+01 | 6.42E+00 | 1.36E+04 | 1.65E+02 | 2.65E+02 | 2.29E+02 | 1.98E+03 | 5.50E+02 | 5.70E+02 | 1.56E+05 | 1.38E+01 | 1.96E+02 | 2.55E+04 | 1.77E+04 | 6.06E+03 |
| 2044 | 5.55E+01 | 4.58E+01 | 6.28E+00 | 1.41E+04 | 1.71E+02 | 2.70E+02 | 2.32E+02 | 2.08E+03 | 5.72E+02 | 5.71E+02 | 1.65E+05 | 1.41E+01 | 1.99E+02 | 2.60E+04 | 1.76E+04 | 6.19E+03 |
| 2045 | 5.41E+01 | 4.85E+01 | 6.12E+00 | 1.46E+04 | 1.79E+02 | 2.74E+02 | 2.36E+02 | 2.18E+03 | 5.96E+02 | 5.72E+02 | 1.73E+05 | 1.43E+01 | 2.03E+02 | 2.66E+04 | 1.73E+04 | 6.33E+03 |
| 2046 | 5.26E+01 | 5.15E+01 | 5.96E+00 | 1.51E+04 | 1.86E+02 | 2.79E+02 | 2.40E+02 | 2.28E+03 | 6.19E+02 | 5.73E+02 | 1.81E+05 | 1.46E+01 | 2.07E+02 | 2.71E+04 | 1.71E+04 | 6.47E+03 |
| 2047 | 5.10E+01 | 5.46E+01 | 5.78E+00 | 1.56E+04 | 1.94E+02 | 2.83E+02 | 2.43E+02 | 2.39E+03 | 6.44E+02 | 5.73E+02 | 1.90E+05 | 1.49E+01 | 2.11E+02 | 2.77E+04 | 1.68E+04 | 6.60E+03 |
| 2048 | 4.93E+01 | 5.78E+01 | 5.59E+00 | 1.61E+04 | 2.01E+02 | 2.88E+02 | 2.47E+02 | 2.50E+03 | 6.69E+02 | 5.73E+02 | 1.99E+05 | 1.51E+01 | 2.14E+02 | 2.82E+04 | 1.66E+04 | 6.74E+03 |
| 2049 | 4.74E+01 | 6.12E+01 | 5.39E+00 | 1.66E+04 | 2.09E+02 | 2.92E+02 | 2.51E+02 | 2.61E+03 | 6.95E+02 | 5.72E+02 | 2.08E+05 | 1.54E+01 | 2.18E+02 | 2.88E+04 | 1.63E+04 | 6.88E+03 |
| 2050 | 4.55E+01 | 6.48E+01 | 5.18E+00 | 1.72E+04 | 2.18E+02 | 2.97E+02 | 2.54E+02 | 2.73E+03 | 7.22E+02 | 5.71E+02 | 2.17E+05 | 1.56E+01 | 2.22E+02 | 2.93E+04 | 1.59E+04 | 7.02E+03 |

## Table S33a. Estimated material demand for producing vehicles in Japan in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 3.24E+06 | 4.35E+05 | 1.35E+05 | 1.12E+03 | 3.54E+04 | 3.50E+04 | 1.12E+03 | 4.10E+04 | 3.39E+04 | 1.51E+04 | 4.11E+02 | 6.94E+04 | 2.11E+03 | 3.37E+02 | 1.21E+01 | 9.14E+01 |
| 2021 | 3.29E+06 | 4.41E+05 | 1.42E+05 | 1.23E+03 | 3.56E+04 | 3.88E+04 | 1.13E+03 | 4.17E+04 | 3.43E+04 | 1.52E+04 | 4.29E+02 | 6.97E+04 | 2.20E+03 | 3.44E+02 | 1.25E+01 | 9.36E+01 |
| 2022 | 3.35E+06 | 4.48E+05 | 1.50E+05 | 1.34E+03 | 3.59E+04 | 4.27E+04 | 1.14E+03 | 4.23E+04 | 3.46E+04 | 1.52E+04 | 4.47E+02 | 7.00E+04 | 2.29E+03 | 3.52E+02 | 1.29E+01 | 9.58E+01 |
| 2023 | 3.41E+06 | 4.54E+05 | 1.57E+05 | 1.45E+03 | 3.62E+04 | 4.66E+04 | 1.16E+03 | 4.30E+04 | 3.49E+04 | 1.52E+04 | 4.65E+02 | 7.03E+04 | 2.39E+03 | 3.59E+02 | 1.33E+01 | 9.80E+01 |
| 2024 | 3.46E+06 | 4.61E+05 | 1.65E+05 | 1.57E+03 | 3.65E+04 | 5.05E+04 | 1.17E+03 | 4.36E+04 | 3.52E+04 | 1.53E+04 | 4.83E+02 | 7.06E+04 | 2.48E+03 | 3.66E+02 | 1.36E+01 | 1.00E+02 |
| 2025 | 3.52E+06 | 4.67E+05 | 1.73E+05 | 1.68E+03 | 3.67E+04 | 5.44E+04 | 1.18E+03 | 4.43E+04 | 3.55E+04 | 1.53E+04 | 5.01E+02 | 7.09E+04 | 2.58E+03 | 3.73E+02 | 1.40E+01 | 1.02E+02 |
| 2026 | 3.58E+06 | 4.74E+05 | 1.80E+05 | 1.79E+03 | 3.70E+04 | 5.82E+04 | 1.20E+03 | 4.49E+04 | 3.58E+04 | 1.53E+04 | 5.20E+02 | 7.12E+04 | 2.67E+03 | 3.80E+02 | 1.44E+01 | 1.05E+02 |
| 2027 | 3.63E+06 | 4.80E+05 | 1.88E+05 | 1.91E+03 | 3.73E+04 | 6.21E+04 | 1.21E+03 | 4.56E+04 | 3.62E+04 | 1.54E+04 | 5.38E+02 | 7.15E+04 | 2.76E+03 | 3.87E+02 | 1.48E+01 | 1.07E+02 |
| 2028 | 3.69E+06 | 4.87E+05 | 1.95E+05 | 2.02E+03 | 3.75E+04 | 6.60E+04 | 1.22E+03 | 4.62E+04 | 3.65E+04 | 1.54E+04 | 5.56E+02 | 7.18E+04 | 2.86E+03 | 3.95E+02 | 1.51E+01 | 1.09E+02 |
| 2029 | 3.74E+06 | 4.93E+05 | 2.03E+05 | 2.13E+03 | 3.78E+04 | 6.99E+04 | 1.24E+03 | 4.68E+04 | 3.68E+04 | 1.55E+04 | 5.74E+02 | 7.21E+04 | 2.95E+03 | 4.02E+02 | 1.55E+01 | 1.11E+02 |
| 2030 | 3.80E+06 | 5.00E+05 | 2.11E+05 | 2.24E+03 | 3.81E+04 | 7.38E+04 | 1.25E+03 | 4.75E+04 | 3.71E+04 | 1.55E+04 | 5.92E+02 | 7.24E+04 | 3.05E+03 | 4.09E+02 | 1.59E+01 | 1.13E+02 |
| 2031 | 3.81E+06 | 4.99E+05 | 2.14E+05 | 2.30E+03 | 3.80E+04 | 7.55E+04 | 1.24E+03 | 4.73E+04 | 3.69E+04 | 1.54E+04 | 5.98E+02 | 7.22E+04 | 3.07E+03 | 4.09E+02 | 1.59E+01 | 1.14E+02 |
| 2032 | 3.81E+06 | 4.99E+05 | 2.16E+05 | 2.36E+03 | 3.80E+04 | 7.72E+04 | 1.24E+03 | 4.71E+04 | 3.68E+04 | 1.52E+04 | 6.04E+02 | 7.20E+04 | 3.09E+03 | 4.10E+02 | 1.60E+01 | 1.14E+02 |
| 2033 | 3.82E+06 | 4.99E+05 | 2.19E+05 | 2.42E+03 | 3.79E+04 | 7.89E+04 | 1.23E+03 | 4.69E+04 | 3.66E+04 | 1.51E+04 | 6.09E+02 | 7.17E+04 | 3.12E+03 | 4.10E+02 | 1.61E+01 | 1.14E+02 |
| 2034 | 3.82E+06 | 4.98E+05 | 2.22E+05 | 2.48E+03 | 3.79E+04 | 8.06E+04 | 1.23E+03 | 4.67E+04 | 3.65E+04 | 1.50E+04 | 6.15E+02 | 7.15E+04 | 3.14E+03 | 4.11E+02 | 1.61E+01 | 1.15E+02 |
| 2035 | 3.83E+06 | 4.98E+05 | 2.25E+05 | 2.53E+03 | 3.78E+04 | 8.23E+04 | 1.22E+03 | 4.66E+04 | 3.63E+04 | 1.48E+04 | 6.21E+02 | 7.13E+04 | 3.17E+03 | 4.11E+02 | 1.62E+01 | 1.15E+02 |
| 2036 | 3.83E+06 | 4.97E+05 | 2.28E+05 | 2.59E+03 | 3.78E+04 | 8.40E+04 | 1.21E+03 | 4.64E+04 | 3.62E+04 | 1.47E+04 | 6.27E+02 | 7.11E+04 | 3.19E+03 | 4.12E+02 | 1.62E+01 | 1.16E+02 |
| 2037 | 3.84E+06 | 4.97E+05 | 2.31E+05 | 2.65E+03 | 3.77E+04 | 8.57E+04 | 1.21E+03 | 4.62E+04 | 3.60E+04 | 1.46E+04 | 6.32E+02 | 7.08E+04 | 3.21E+03 | 4.12E+02 | 1.63E+01 | 1.16E+02 |
| 2038 | 3.85E+06 | 4.97E+05 | 2.34E+05 | 2.71E+03 | 3.76E+04 | 8.74E+04 | 1.20E+03 | 4.60E+04 | 3.58E+04 | 1.45E+04 | 6.38E+02 | 7.06E+04 | 3.24E+03 | 4.13E+02 | 1.64E+01 | 1.16E+02 |
| 2039 | 3.85E+06 | 4.96E+05 | 2.37E+05 | 2.77E+03 | 3.76E+04 | 8.91E+04 | 1.20E+03 | 4.58E+04 | 3.57E+04 | 1.43E+04 | 6.44E+02 | 7.04E+04 | 3.26E+03 | 4.13E+02 | 1.64E+01 | 1.17E+02 |
| 2040 | 3.86E+06 | 4.96E+05 | 2.39E+05 | 2.83E+03 | 3.75E+04 | 9.08E+04 | 1.19E+03 | 4.56E+04 | 3.55E+04 | 1.42E+04 | 6.49E+02 | 7.02E+04 | 3.29E+03 | 4.14E+02 | 1.65E+01 | 1.17E+02 |
| 2041 | 3.86E+06 | 4.96E+05 | 2.42E+05 | 2.88E+03 | 3.75E+04 | 9.25E+04 | 1.19E+03 | 4.55E+04 | 3.54E+04 | 1.41E+04 | 6.55E+02 | 6.99E+04 | 3.31E+03 | 4.15E+02 | 1.66E+01 | 1.18E+02 |
| 2042 | 3.87E+06 | 4.96E+05 | 2.45E+05 | 2.93E+03 | 3.74E+04 | 9.42E+04 | 1.18E+03 | 4.54E+04 | 3.53E+04 | 1.40E+04 | 6.61E+02 | 6.97E+04 | 3.33E+03 | 4.15E+02 | 1.66E+01 | 1.18E+02 |
| 2043 | 3.87E+06 | 4.96E+05 | 2.48E+05 | 2.98E+03 | 3.74E+04 | 9.59E+04 | 1.18E+03 | 4.52E+04 | 3.51E+04 | 1.38E+04 | 6.66E+02 | 6.95E+04 | 3.36E+03 | 4.16E+02 | 1.67E+01 | 1.18E+02 |
| 2044 | 3.88E+06 | 4.95E+05 | 2.51E+05 | 3.03E+03 | 3.73E+04 | 9.76E+04 | 1.17E+03 | 4.51E+04 | 3.50E+04 | 1.37E+04 | 6.72E+02 | 6.92E+04 | 3.38E+03 | 4.17E+02 | 1.68E+01 | 1.19E+02 |
| 2045 | 3.89E+06 | 4.95E+05 | 2.53E+05 | 3.09E+03 | 3.72E+04 | 9.93E+04 | 1.17E+03 | 4.50E+04 | 3.49E+04 | 1.36E+04 | 6.78E+02 | 6.90E+04 | 3.41E+03 | 4.17E+02 | 1.68E+01 | 1.19E+02 |
| 2046 | 3.89E+06 | 4.95E+05 | 2.56E+05 | 3.14E+03 | 3.72E+04 | 1.01E+05 | 1.16E+03 | 4.48E+04 | 3.47E+04 | 1.35E+04 | 6.83E+02 | 6.88E+04 | 3.43E+03 | 4.18E+02 | 1.69E+01 | 1.20E+02 |
| 2047 | 3.90E+06 | 4.95E+05 | 2.59E+05 | 3.19E+03 | 3.71E+04 | 1.03E+05 | 1.16E+03 | 4.47E+04 | 3.46E+04 | 1.34E+04 | 6.89E+02 | 6.86E+04 | 3.46E+03 | 4.18E+02 | 1.70E+01 | 1.20E+02 |
| 2048 | 3.90E+06 | 4.95E+05 | 2.62E+05 | 3.24E+03 | 3.71E+04 | 1.04E+05 | 1.15E+03 | 4.46E+04 | 3.45E+04 | 1.33E+04 | 6.95E+02 | 6.83E+04 | 3.48E+03 | 4.19E+02 | 1.70E+01 | 1.20E+02 |
| 2049 | 3.91E+06 | 4.94E+05 | 2.65E+05 | 3.29E+03 | 3.70E+04 | 1.06E+05 | 1.15E+03 | 4.44E+04 | 3.43E+04 | 1.31E+04 | 7.00E+02 | 6.81E+04 | 3.51E+03 | 4.20E+02 | 1.71E+01 | 1.21E+02 |
| 2050 | 3.91E+06 | 4.94E+05 | 2.67E+05 | 3.35E+03 | 3.69E+04 | 1.08E+05 | 1.14E+03 | 4.43E+04 | 3.42E+04 | 1.30E+04 | 7.06E+02 | 6.79E+04 | 3.53E+03 | 4.20E+02 | 1.72E+01 | 1.21E+02 |

## Table S33b. Estimated material demand for producing vehicles in Japan in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 9.27E+00 | 2.47E+00 | 1.15E+00 | 1.24E+03 | 5.24E+00 | 2.24E+01 | 2.03E+01 | 7.13E+01 | 1.94E+01 | 5.64E+01 | 2.93E+03 | 1.18E+00 | 1.68E+01 | 2.18E+03 | 2.88E+03 | 5.18E+02 |
| 2021 | 9.21E+00 | 3.03E+00 | 1.14E+00 | 1.29E+03 | 5.58E+00 | 2.26E+01 | 2.05E+01 | 7.62E+01 | 2.04E+01 | 5.57E+01 | 3.35E+03 | 1.20E+00 | 1.69E+01 | 2.21E+03 | 2.88E+03 | 5.26E+02 |
| 2022 | 9.15E+00 | 3.59E+00 | 1.14E+00 | 1.34E+03 | 5.92E+00 | 2.28E+01 | 2.06E+01 | 8.11E+01 | 2.15E+01 | 5.50E+01 | 3.76E+03 | 1.21E+00 | 1.71E+01 | 2.24E+03 | 2.88E+03 | 5.34E+02 |
| 2023 | 9.09E+00 | 4.14E+00 | 1.13E+00 | 1.40E+03 | 6.26E+00 | 2.30E+01 | 2.08E+01 | 8.60E+01 | 2.26E+01 | 5.44E+01 | 4.17E+03 | 1.22E+00 | 1.73E+01 | 2.27E+03 | 2.89E+03 | 5.43E+02 |
| 2024 | 9.03E+00 | 4.70E+00 | 1.13E+00 | 1.45E+03 | 6.61E+00 | 2.32E+01 | 2.09E+01 | 9.09E+01 | 2.37E+01 | 5.37E+01 | 4.58E+03 | 1.24E+00 | 1.75E+01 | 2.31E+03 | 2.89E+03 | 5.51E+02 |
| 2025 | 8.96E+00 | 5.26E+00 | 1.12E+00 | 1.51E+03 | 6.95E+00 | 2.34E+01 | 2.11E+01 | 9.58E+01 | 2.48E+01 | 5.31E+01 | 4.99E+03 | 1.25E+00 | 1.77E+01 | 2.34E+03 | 2.89E+03 | 5.59E+02 |
| 2026 | 8.90E+00 | 5.82E+00 | 1.12E+00 | 1.56E+03 | 7.29E+00 | 2.36E+01 | 2.12E+01 | 1.01E+02 | 2.59E+01 | 5.24E+01 | 5.41E+03 | 1.26E+00 | 1.79E+01 | 2.37E+03 | 2.89E+03 | 5.68E+02 |
| 2027 | 8.84E+00 | 6.38E+00 | 1.11E+00 | 1.62E+03 | 7.63E+00 | 2.38E+01 | 2.13E+01 | 1.06E+02 | 2.69E+01 | 5.18E+01 | 5.82E+03 | 1.28E+00 | 1.81E+01 | 2.40E+03 | 2.89E+03 | 5.76E+02 |
| 2028 | 8.78E+00 | 6.93E+00 | 1.10E+00 | 1.67E+03 | 7.97E+00 | 2.40E+01 | 2.15E+01 | 1.10E+02 | 2.80E+01 | 5.11E+01 | 6.23E+03 | 1.29E+00 | 1.82E+01 | 2.43E+03 | 2.89E+03 | 5.84E+02 |
| 2029 | 8.72E+00 | 7.49E+00 | 1.10E+00 | 1.72E+03 | 8.31E+00 | 2.42E+01 | 2.16E+01 | 1.15E+02 | 2.91E+01 | 5.04E+01 | 6.64E+03 | 1.30E+00 | 1.84E+01 | 2.47E+03 | 2.89E+03 | 5.92E+02 |
| 2030 | 8.65E+00 | 8.05E+00 | 1.09E+00 | 1.78E+03 | 8.65E+00 | 2.44E+01 | 2.18E+01 | 1.20E+02 | 3.02E+01 | 4.98E+01 | 7.06E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.89E+03 | 6.01E+02 |
| 2031 | 8.54E+00 | 8.79E+00 | 1.08E+00 | 1.79E+03 | 9.04E+00 | 2.44E+01 | 2.17E+01 | 1.22E+02 | 3.14E+01 | 4.93E+01 | 7.22E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.87E+03 | 6.01E+02 |
| 2032 | 8.43E+00 | 9.53E+00 | 1.06E+00 | 1.79E+03 | 9.42E+00 | 2.43E+01 | 2.17E+01 | 1.25E+02 | 3.26E+01 | 4.89E+01 | 7.38E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.85E+03 | 6.01E+02 |
| 2033 | 8.32E+00 | 1.03E+01 | 1.05E+00 | 1.80E+03 | 9.80E+00 | 2.43E+01 | 2.16E+01 | 1.27E+02 | 3.38E+01 | 4.84E+01 | 7.55E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.82E+03 | 6.01E+02 |
| 2034 | 8.21E+00 | 1.10E+01 | 1.04E+00 | 1.81E+03 | 1.02E+01 | 2.43E+01 | 2.16E+01 | 1.29E+02 | 3.50E+01 | 4.79E+01 | 7.71E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.80E+03 | 6.01E+02 |
| 2035 | 8.10E+00 | 1.17E+01 | 1.02E+00 | 1.82E+03 | 1.06E+01 | 2.43E+01 | 2.15E+01 | 1.32E+02 | 3.62E+01 | 4.75E+01 | 7.87E+03 | 1.31E+00 | 1.86E+01 | 2.50E+03 | 2.77E+03 | 6.02E+02 |
| 2036 | 7.99E+00 | 1.25E+01 | 1.01E+00 | 1.82E+03 | 1.09E+01 | 2.43E+01 | 2.15E+01 | 1.34E+02 | 3.74E+01 | 4.70E+01 | 8.03E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.75E+03 | 6.02E+02 |
| 2037 | 7.88E+00 | 1.32E+01 | 9.94E-01 | 1.83E+03 | 1.13E+01 | 2.42E+01 | 2.14E+01 | 1.36E+02 | 3.86E+01 | 4.65E+01 | 8.20E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.73E+03 | 6.02E+02 |
| 2038 | 7.77E+00 | 1.40E+01 | 9.80E-01 | 1.84E+03 | 1.17E+01 | 2.42E+01 | 2.14E+01 | 1.38E+02 | 3.98E+01 | 4.61E+01 | 8.36E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.70E+03 | 6.02E+02 |
| 2039 | 7.66E+00 | 1.47E+01 | 9.65E-01 | 1.85E+03 | 1.21E+01 | 2.42E+01 | 2.13E+01 | 1.41E+02 | 4.10E+01 | 4.56E+01 | 8.52E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.68E+03 | 6.02E+02 |
| 2040 | 7.55E+00 | 1.54E+01 | 9.51E-01 | 1.86E+03 | 1.25E+01 | 2.42E+01 | 2.13E+01 | 1.43E+02 | 4.22E+01 | 4.51E+01 | 8.69E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.65E+03 | 6.03E+02 |
| 2041 | 7.45E+00 | 1.60E+01 | 9.38E-01 | 1.86E+03 | 1.28E+01 | 2.41E+01 | 2.12E+01 | 1.45E+02 | 4.32E+01 | 4.46E+01 | 8.86E+03 | 1.31E+00 | 1.85E+01 | 2.50E+03 | 2.63E+03 | 6.03E+02 |
| 2042 | 7.35E+00 | 1.65E+01 | 9.25E-01 | 1.87E+03 | 1.31E+01 | 2.41E+01 | 2.12E+01 | 1.47E+02 | 4.41E+01 | 4.42E+01 | 9.03E+03 | 1.30E+00 | 1.85E+01 | 2.50E+03 | 2.61E+03 | 6.03E+02 |
| 2043 | 7.25E+00 | 1.71E+01 | 9.12E-01 | 1.88E+03 | 1.34E+01 | 2.41E+01 | 2.11E+01 | 1.49E+02 | 4.51E+01 | 4.37E+01 | 9.20E+03 | 1.30E+00 | 1.85E+01 | 2.50E+03 | 2.58E+03 | 6.03E+02 |
| 2044 | 7.14E+00 | 1.76E+01 | 8.99E-01 | 1.89E+03 | 1.37E+01 | 2.41E+01 | 2.11E+01 | 1.51E+02 | 4.60E+01 | 4.32E+01 | 9.38E+03 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.56E+03 | 6.04E+02 |
| 2045 | 7.04E+00 | 1.82E+01 | 8.86E-01 | 1.90E+03 | 1.40E+01 | 2.40E+01 | 2.10E+01 | 1.53E+02 | 4.69E+01 | 4.27E+01 | 9.55E+03 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.54E+03 | 6.04E+02 |
| 2046 | 6.94E+00 | 1.87E+01 | 8.73E-01 | 1.91E+03 | 1.43E+01 | 2.40E+01 | 2.10E+01 | 1.56E+02 | 4.79E+01 | 4.22E+01 | 9.72E+03 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.51E+03 | 6.04E+02 |
| 2047 | 6.84E+00 | 1.93E+01 | 8.60E-01 | 1.92E+03 | 1.46E+01 | 2.40E+01 | 2.09E+01 | 1.58E+02 | 4.88E+01 | 4.17E+01 | 9.89E+03 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.49E+03 | 6.04E+02 |
| 2048 | 6.73E+00 | 1.98E+01 | 8.47E-01 | 1.93E+03 | 1.49E+01 | 2.40E+01 | 2.09E+01 | 1.60E+02 | 4.98E+01 | 4.12E+01 | 1.01E+04 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.47E+03 | 6.05E+02 |
| 2049 | 6.63E+00 | 2.04E+01 | 8.35E-01 | 1.94E+03 | 1.52E+01 | 2.39E+01 | 2.08E+01 | 1.62E+02 | 5.07E+01 | 4.08E+01 | 1.02E+04 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.45E+03 | 6.05E+02 |
| 2050 | 6.53E+00 | 2.09E+01 | 8.22E-01 | 1.95E+03 | 1.55E+01 | 2.39E+01 | 2.08E+01 | 1.64E+02 | 5.16E+01 | 4.03E+01 | 1.04E+04 | 1.30E+00 | 1.84E+01 | 2.50E+03 | 2.42E+03 | 6.05E+02 |

## Table S34a. Estimated automotive urban mineral formation in China in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 6.89E+06 | 9.30E+05 | 1.81E+05 | 2.88E+02 | 8.56E+04 | 2.50E+04 | 2.44E+03 | 8.53E+04 | 7.10E+04 | 3.49E+04 | 7.02E+02 | 1.57E+05 | 2.59E+03 | 5.74E+02 | 1.76E+01 | 1.74E+02 |
| 2021 | 8.10E+06 | 1.09E+06 | 2.13E+05 | 3.45E+02 | 1.01E+05 | 2.98E+04 | 2.87E+03 | 1.00E+05 | 8.34E+04 | 4.09E+04 | 8.25E+02 | 1.85E+05 | 3.04E+03 | 6.74E+02 | 2.07E+01 | 2.05E+02 |
| 2022 | 9.47E+06 | 1.28E+06 | 2.51E+05 | 4.15E+02 | 1.17E+05 | 3.54E+04 | 3.35E+03 | 1.17E+05 | 9.74E+04 | 4.78E+04 | 9.66E+02 | 2.16E+05 | 3.57E+03 | 7.88E+02 | 2.42E+01 | 2.39E+02 |
| 2023 | 1.10E+07 | 1.48E+06 | 2.92E+05 | 5.01E+02 | 1.36E+05 | 4.21E+04 | 3.88E+03 | 1.36E+05 | 1.13E+05 | 5.53E+04 | 1.12E+03 | 2.50E+05 | 4.15E+03 | 9.14E+02 | 2.81E+01 | 2.78E+02 |
| 2024 | 1.26E+07 | 1.69E+06 | 3.36E+05 | 6.06E+02 | 1.56E+05 | 4.99E+04 | 4.43E+03 | 1.55E+05 | 1.29E+05 | 6.32E+04 | 1.29E+03 | 2.86E+05 | 4.77E+03 | 1.05E+03 | 3.23E+01 | 3.18E+02 |
| 2025 | 1.42E+07 | 1.91E+06 | 3.83E+05 | 7.32E+02 | 1.75E+05 | 5.89E+04 | 4.99E+03 | 1.74E+05 | 1.45E+05 | 7.11E+04 | 1.46E+03 | 3.22E+05 | 5.42E+03 | 1.18E+03 | 3.65E+01 | 3.59E+02 |
| 2026 | 1.57E+07 | 2.12E+06 | 4.31E+05 | 8.84E+02 | 1.95E+05 | 6.91E+04 | 5.53E+03 | 1.93E+05 | 1.61E+05 | 7.86E+04 | 1.63E+03 | 3.58E+05 | 6.06E+03 | 1.32E+03 | 4.07E+01 | 3.99E+02 |
| 2027 | 1.72E+07 | 2.31E+06 | 4.78E+05 | 1.06E+03 | 2.12E+05 | 8.07E+04 | 6.02E+03 | 2.11E+05 | 1.76E+05 | 8.56E+04 | 1.79E+03 | 3.90E+05 | 6.70E+03 | 1.44E+03 | 4.48E+01 | 4.37E+02 |
| 2028 | 1.85E+07 | 2.49E+06 | 5.25E+05 | 1.28E+03 | 2.28E+05 | 9.38E+04 | 6.46E+03 | 2.26E+05 | 1.89E+05 | 9.16E+04 | 1.94E+03 | 4.20E+05 | 7.31E+03 | 1.56E+03 | 4.85E+01 | 4.72E+02 |
| 2029 | 1.97E+07 | 2.64E+06 | 5.70E+05 | 1.53E+03 | 2.42E+05 | 1.09E+05 | 6.83E+03 | 2.39E+05 | 2.00E+05 | 9.67E+04 | 2.09E+03 | 4.45E+05 | 7.88E+03 | 1.66E+03 | 5.20E+01 | 5.03E+02 |
| 2030 | 2.07E+07 | 2.77E+06 | 6.14E+05 | 1.82E+03 | 2.53E+05 | 1.25E+05 | 7.12E+03 | 2.49E+05 | 2.09E+05 | 1.01E+05 | 2.21E+03 | 4.66E+05 | 8.42E+03 | 1.75E+03 | 5.50E+01 | 5.30E+02 |
| 2031 | 2.15E+07 | 2.86E+06 | 6.58E+05 | 2.16E+03 | 2.62E+05 | 1.44E+05 | 7.33E+03 | 2.57E+05 | 2.16E+05 | 1.03E+05 | 2.33E+03 | 4.82E+05 | 8.93E+03 | 1.82E+03 | 5.77E+01 | 5.52E+02 |
| 2032 | 2.21E+07 | 2.94E+06 | 7.02E+05 | 2.57E+03 | 2.68E+05 | 1.67E+05 | 7.46E+03 | 2.62E+05 | 2.21E+05 | 1.05E+05 | 2.44E+03 | 4.94E+05 | 9.44E+03 | 1.88E+03 | 6.02E+01 | 5.71E+02 |
| 2033 | 2.26E+07 | 3.00E+06 | 7.51E+05 | 3.08E+03 | 2.73E+05 | 1.94E+05 | 7.54E+03 | 2.65E+05 | 2.24E+05 | 1.05E+05 | 2.55E+03 | 5.03E+05 | 9.96E+03 | 1.94E+03 | 6.27E+01 | 5.88E+02 |
| 2034 | 2.31E+07 | 3.05E+06 | 8.07E+05 | 3.68E+03 | 2.77E+05 | 2.27E+05 | 7.58E+03 | 2.66E+05 | 2.27E+05 | 1.05E+05 | 2.66E+03 | 5.11E+05 | 1.06E+04 | 2.00E+03 | 6.52E+01 | 6.05E+02 |
| 2035 | 2.37E+07 | 3.10E+06 | 8.72E+05 | 4.39E+03 | 2.81E+05 | 2.65E+05 | 7.62E+03 | 2.68E+05 | 2.29E+05 | 1.05E+05 | 2.80E+03 | 5.20E+05 | 1.12E+04 | 2.06E+03 | 6.82E+01 | 6.24E+02 |
| 2036 | 2.43E+07 | 3.17E+06 | 9.47E+05 | 5.21E+03 | 2.86E+05 | 3.10E+05 | 7.66E+03 | 2.70E+05 | 2.32E+05 | 1.05E+05 | 2.95E+03 | 5.30E+05 | 1.20E+04 | 2.14E+03 | 7.16E+01 | 6.46E+02 |
| 2037 | 2.51E+07 | 3.24E+06 | 1.03E+06 | 6.12E+03 | 2.92E+05 | 3.59E+05 | 7.72E+03 | 2.72E+05 | 2.36E+05 | 1.05E+05 | 3.12E+03 | 5.42E+05 | 1.29E+04 | 2.22E+03 | 7.54E+01 | 6.72E+02 |
| 2038 | 2.59E+07 | 3.33E+06 | 1.12E+06 | 7.10E+03 | 2.99E+05 | 4.13E+05 | 7.78E+03 | 2.75E+05 | 2.40E+05 | 1.05E+05 | 3.31E+03 | 5.55E+05 | 1.38E+04 | 2.32E+03 | 7.97E+01 | 7.00E+02 |
| 2039 | 2.68E+07 | 3.42E+06 | 1.22E+06 | 8.15E+03 | 3.06E+05 | 4.70E+05 | 7.85E+03 | 2.78E+05 | 2.45E+05 | 1.05E+05 | 3.52E+03 | 5.70E+05 | 1.49E+04 | 2.42E+03 | 8.42E+01 | 7.30E+02 |
| 2040 | 2.77E+07 | 3.51E+06 | 1.32E+06 | 9.25E+03 | 3.13E+05 | 5.29E+05 | 7.92E+03 | 2.80E+05 | 2.50E+05 | 1.05E+05 | 3.73E+03 | 5.85E+05 | 1.59E+04 | 2.52E+03 | 8.88E+01 | 7.61E+02 |
| 2041 | 2.86E+07 | 3.60E+06 | 1.43E+06 | 1.04E+04 | 3.21E+05 | 5.90E+05 | 7.98E+03 | 2.83E+05 | 2.54E+05 | 1.05E+05 | 3.94E+03 | 5.99E+05 | 1.70E+04 | 2.62E+03 | 9.35E+01 | 7.92E+02 |
| 2042 | 2.95E+07 | 3.69E+06 | 1.53E+06 | 1.15E+04 | 3.28E+05 | 6.51E+05 | 8.03E+03 | 2.85E+05 | 2.58E+05 | 1.05E+05 | 4.15E+03 | 6.14E+05 | 1.80E+04 | 2.72E+03 | 9.81E+01 | 8.22E+02 |
| 2043 | 3.04E+07 | 3.77E+06 | 1.63E+06 | 1.26E+04 | 3.34E+05 | 7.10E+05 | 8.06E+03 | 2.86E+05 | 2.62E+05 | 1.04E+05 | 4.35E+03 | 6.27E+05 | 1.90E+04 | 2.82E+03 | 1.02E+02 | 8.51E+02 |
| 2044 | 3.12E+07 | 3.85E+06 | 1.72E+06 | 1.36E+04 | 3.41E+05 | 7.68E+05 | 8.09E+03 | 2.87E+05 | 2.66E+05 | 1.04E+05 | 4.54E+03 | 6.41E+05 | 2.00E+04 | 2.92E+03 | 1.07E+02 | 8.79E+02 |
| 2045 | 3.20E+07 | 3.93E+06 | 1.82E+06 | 1.46E+04 | 3.47E+05 | 8.24E+05 | 8.12E+03 | 2.88E+05 | 2.69E+05 | 1.03E+05 | 4.73E+03 | 6.54E+05 | 2.09E+04 | 3.01E+03 | 1.11E+02 | 9.06E+02 |
| 2046 | 3.28E+07 | 4.01E+06 | 1.91E+06 | 1.57E+04 | 3.54E+05 | 8.79E+05 | 8.15E+03 | 2.90E+05 | 2.73E+05 | 1.03E+05 | 4.91E+03 | 6.67E+05 | 2.19E+04 | 3.10E+03 | 1.15E+02 | 9.34E+02 |
| 2047 | 3.36E+07 | 4.08E+06 | 2.00E+06 | 1.67E+04 | 3.61E+05 | 9.34E+05 | 8.18E+03 | 2.91E+05 | 2.77E+05 | 1.03E+05 | 5.10E+03 | 6.81E+05 | 2.28E+04 | 3.19E+03 | 1.19E+02 | 9.61E+02 |
| 2048 | 3.44E+07 | 4.17E+06 | 2.10E+06 | 1.77E+04 | 3.68E+05 | 9.91E+05 | 8.21E+03 | 2.92E+05 | 2.81E+05 | 1.02E+05 | 5.29E+03 | 6.96E+05 | 2.38E+04 | 3.29E+03 | 1.23E+02 | 9.89E+02 |
| 2049 | 3.53E+07 | 4.25E+06 | 2.20E+06 | 1.88E+04 | 3.75E+05 | 1.05E+06 | 8.24E+03 | 2.93E+05 | 2.85E+05 | 1.02E+05 | 5.49E+03 | 7.11E+05 | 2.47E+04 | 3.38E+03 | 1.28E+02 | 1.02E+03 |
| 2050 | 3.62E+07 | 4.33E+06 | 2.30E+06 | 1.99E+04 | 3.82E+05 | 1.11E+06 | 8.26E+03 | 2.94E+05 | 2.89E+05 | 1.02E+05 | 5.69E+03 | 7.26E+05 | 2.57E+04 | 3.48E+03 | 1.32E+02 | 1.05E+03 |

Unit: t

## Table S34b. Estimated automotive urban mineral formation in China in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 2.38E+01 | 5.39E+00 | 2.64E+00 | 8.98E+02 | 1.45E+01 | 5.39E+01 | 4.77E+01 | 3.85E+01 | 5.21E+01 | 1.72E+02 | 1.43E+02 | 2.65E+00 | 3.75E+01 | 4.48E+03 | 6.22E+03 | 1.02E+03 |
| 2021 | 2.80E+01 | 6.32E+00 | 3.10E+00 | 1.06E+03 | 1.71E+01 | 6.33E+01 | 5.60E+01 | 4.57E+01 | 6.12E+01 | 2.01E+02 | 2.10E+02 | 3.11E+00 | 4.40E+01 | 5.26E+03 | 7.31E+03 | 1.20E+03 |
| 2022 | 3.27E+01 | 7.38E+00 | 3.62E+00 | 1.24E+03 | 2.00E+01 | 7.40E+01 | 6.54E+01 | 5.42E+01 | 7.17E+01 | 2.35E+02 | 3.23E+02 | 3.63E+00 | 5.15E+01 | 6.15E+03 | 8.54E+03 | 1.41E+03 |
| 2023 | 3.78E+01 | 8.54E+00 | 4.19E+00 | 1.45E+03 | 2.32E+01 | 8.57E+01 | 7.58E+01 | 6.43E+01 | 8.33E+01 | 2.72E+02 | 5.05E+02 | 4.21E+00 | 5.96E+01 | 7.12E+03 | 9.88E+03 | 1.63E+03 |
| 2024 | 4.31E+01 | 9.76E+00 | 4.78E+00 | 1.67E+03 | 2.67E+01 | 9.80E+01 | 8.67E+01 | 7.58E+01 | 9.56E+01 | 3.11E+02 | 7.86E+02 | 4.82E+00 | 6.83E+01 | 8.15E+03 | 1.13E+04 | 1.87E+03 |
| 2025 | 4.85E+01 | 1.10E+01 | 5.38E+00 | 1.90E+03 | 3.02E+01 | 1.10E+02 | 9.77E+01 | 8.89E+01 | 1.08E+02 | 3.50E+02 | 1.20E+03 | 5.43E+00 | 7.69E+01 | 9.20E+03 | 1.27E+04 | 2.11E+03 |
| 2026 | 5.36E+01 | 1.22E+01 | 5.95E+00 | 2.14E+03 | 3.37E+01 | 1.23E+02 | 1.08E+02 | 1.04E+02 | 1.21E+02 | 3.87E+02 | 1.79E+03 | 6.03E+00 | 8.54E+01 | 1.02E+04 | 1.40E+04 | 2.34E+03 |
| 2027 | 5.83E+01 | 1.32E+01 | 6.47E+00 | 2.38E+03 | 3.71E+01 | 1.34E+02 | 1.18E+02 | 1.20E+02 | 1.33E+02 | 4.22E+02 | 2.58E+03 | 6.58E+00 | 9.32E+01 | 1.12E+04 | 1.53E+04 | 2.56E+03 |
| 2028 | 6.24E+01 | 1.42E+01 | 6.92E+00 | 2.61E+03 | 4.03E+01 | 1.44E+02 | 1.27E+02 | 1.39E+02 | 1.44E+02 | 4.52E+02 | 3.61E+03 | 7.08E+00 | 1.00E+02 | 1.20E+04 | 1.64E+04 | 2.76E+03 |
| 2029 | 6.58E+01 | 1.50E+01 | 7.29E+00 | 2.84E+03 | 4.33E+01 | 1.53E+02 | 1.35E+02 | 1.59E+02 | 1.54E+02 | 4.77E+02 | 4.92E+03 | 7.52E+00 | 1.06E+02 | 1.28E+04 | 1.73E+04 | 2.93E+03 |
| 2030 | 6.83E+01 | 1.57E+01 | 7.58E+00 | 3.07E+03 | 4.60E+01 | 1.60E+02 | 1.41E+02 | 1.82E+02 | 1.64E+02 | 4.96E+02 | 6.54E+03 | 7.87E+00 | 1.12E+02 | 1.34E+04 | 1.80E+04 | 3.08E+03 |
| 2031 | 7.00E+01 | 1.62E+01 | 7.77E+00 | 3.29E+03 | 4.85E+01 | 1.65E+02 | 1.46E+02 | 2.08E+02 | 1.72E+02 | 5.10E+02 | 8.55E+03 | 8.16E+00 | 1.16E+02 | 1.39E+04 | 1.85E+04 | 3.20E+03 |
| 2032 | 7.09E+01 | 1.66E+01 | 7.87E+00 | 3.52E+03 | 5.09E+01 | 1.69E+02 | 1.49E+02 | 2.39E+02 | 1.80E+02 | 5.19E+02 | 1.10E+04 | 8.37E+00 | 1.19E+02 | 1.43E+04 | 1.87E+04 | 3.29E+03 |
| 2033 | 7.11E+01 | 1.69E+01 | 7.90E+00 | 3.78E+03 | 5.33E+01 | 1.72E+02 | 1.52E+02 | 2.75E+02 | 1.88E+02 | 5.23E+02 | 1.41E+04 | 8.54E+00 | 1.21E+02 | 1.46E+04 | 1.88E+04 | 3.37E+03 |
| 2034 | 7.09E+01 | 1.71E+01 | 7.88E+00 | 4.06E+03 | 5.59E+01 | 1.75E+02 | 1.54E+02 | 3.19E+02 | 1.96E+02 | 5.24E+02 | 1.79E+04 | 8.69E+00 | 1.23E+02 | 1.50E+04 | 1.89E+04 | 3.45E+03 |
| 2035 | 7.05E+01 | 1.74E+01 | 7.84E+00 | 4.40E+03 | 5.89E+01 | 1.78E+02 | 1.56E+02 | 3.71E+02 | 2.06E+02 | 5.25E+02 | 2.23E+04 | 8.85E+00 | 1.25E+02 | 1.53E+04 | 1.88E+04 | 3.53E+03 |
| 2036 | 7.00E+01 | 1.77E+01 | 7.80E+00 | 4.78E+03 | 6.25E+01 | 1.81E+02 | 1.59E+02 | 4.31E+02 | 2.18E+02 | 5.26E+02 | 2.75E+04 | 9.04E+00 | 1.28E+02 | 1.57E+04 | 1.88E+04 | 3.63E+03 |
| 2037 | 6.96E+01 | 1.81E+01 | 7.76E+00 | 5.20E+03 | 6.65E+01 | 1.85E+02 | 1.62E+02 | 4.97E+02 | 2.31E+02 | 5.28E+02 | 3.32E+04 | 9.27E+00 | 1.31E+02 | 1.61E+04 | 1.88E+04 | 3.75E+03 |
| 2038 | 6.93E+01 | 1.85E+01 | 7.73E+00 | 5.67E+03 | 7.10E+01 | 1.90E+02 | 1.66E+02 | 5.70E+02 | 2.46E+02 | 5.31E+02 | 3.94E+04 | 9.52E+00 | 1.35E+02 | 1.67E+04 | 1.88E+04 | 3.87E+03 |
| 2039 | 6.90E+01 | 1.91E+01 | 7.70E+00 | 6.16E+03 | 7.58E+01 | 1.94E+02 | 1.70E+02 | 6.48E+02 | 2.61E+02 | 5.35E+02 | 4.60E+04 | 9.79E+00 | 1.39E+02 | 1.72E+04 | 1.89E+04 | 4.01E+03 |
| 2040 | 6.85E+01 | 1.97E+01 | 7.66E+00 | 6.66E+03 | 8.09E+01 | 1.99E+02 | 1.74E+02 | 7.29E+02 | 2.78E+02 | 5.38E+02 | 5.28E+04 | 1.01E+01 | 1.43E+02 | 1.78E+04 | 1.89E+04 | 4.15E+03 |
| 2041 | 6.80E+01 | 2.04E+01 | 7.61E+00 | 7.17E+03 | 8.60E+01 | 2.04E+02 | 1.78E+02 | 8.11E+02 | 2.95E+02 | 5.41E+02 | 5.99E+04 | 1.03E+01 | 1.47E+02 | 1.83E+04 | 1.89E+04 | 4.29E+03 |
| 2042 | 6.74E+01 | 2.12E+01 | 7.55E+00 | 7.67E+03 | 9.12E+01 | 2.09E+02 | 1.82E+02 | 8.94E+02 | 3.12E+02 | 5.44E+02 | 6.69E+04 | 1.06E+01 | 1.50E+02 | 1.89E+04 | 1.89E+04 | 4.42E+03 |
| 2043 | 6.67E+01 | 2.21E+01 | 7.48E+00 | 8.15E+03 | 9.63E+01 | 2.13E+02 | 1.86E+02 | 9.75E+02 | 3.28E+02 | 5.46E+02 | 7.37E+04 | 1.09E+01 | 1.54E+02 | 1.94E+04 | 1.88E+04 | 4.55E+03 |
| 2044 | 6.61E+01 | 2.31E+01 | 7.42E+00 | 8.61E+03 | 1.01E+02 | 2.18E+02 | 1.89E+02 | 1.05E+03 | 3.45E+02 | 5.48E+02 | 8.04E+04 | 1.11E+01 | 1.57E+02 | 1.99E+04 | 1.88E+04 | 4.68E+03 |
| 2045 | 6.55E+01 | 2.41E+01 | 7.35E+00 | 9.06E+03 | 1.06E+02 | 2.22E+02 | 1.93E+02 | 1.13E+03 | 3.61E+02 | 5.50E+02 | 8.68E+04 | 1.14E+01 | 1.61E+02 | 2.04E+04 | 1.87E+04 | 4.80E+03 |
| 2046 | 6.49E+01 | 2.54E+01 | 7.29E+00 | 9.49E+03 | 1.11E+02 | 2.26E+02 | 1.96E+02 | 1.21E+03 | 3.77E+02 | 5.53E+02 | 9.32E+04 | 1.16E+01 | 1.64E+02 | 2.09E+04 | 1.87E+04 | 4.92E+03 |
| 2047 | 6.43E+01 | 2.67E+01 | 7.23E+00 | 9.93E+03 | 1.17E+02 | 2.31E+02 | 2.00E+02 | 1.28E+03 | 3.94E+02 | 5.56E+02 | 9.96E+04 | 1.18E+01 | 1.68E+02 | 2.14E+04 | 1.87E+04 | 5.05E+03 |
| 2048 | 6.38E+01 | 2.82E+01 | 7.18E+00 | 1.04E+04 | 1.22E+02 | 2.35E+02 | 2.04E+02 | 1.36E+03 | 4.12E+02 | 5.60E+02 | 1.06E+05 | 1.21E+01 | 1.71E+02 | 2.19E+04 | 1.86E+04 | 5.18E+03 |
| 2049 | 6.33E+01 | 2.97E+01 | 7.12E+00 | 1.08E+04 | 1.28E+02 | 2.40E+02 | 2.08E+02 | 1.44E+03 | 4.30E+02 | 5.64E+02 | 1.13E+05 | 1.24E+01 | 1.75E+02 | 2.25E+04 | 1.86E+04 | 5.31E+03 |
| 2050 | 6.27E+01 | 3.15E+01 | 7.06E+00 | 1.13E+04 | 1.45E+01 | 2.45E+02 | 2.12E+02 | 1.53E+03 | 4.49E+02 | 5.67E+02 | 1.20E+05 | 1.26E+01 | 1.79E+02 | 2.30E+04 | 1.86E+04 | 5.44E+03 |

Unit: t

## Table S35a. Estimated automotive urban mineral formation in Japan in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 3.49E+06 | 4.70E+05 | 1.04E+05 | 3.83E+02 | 4.21E+04 | 1.82E+04 | 1.23E+03 | 4.34E+04 | 3.61E+04 | 1.73E+04 | 3.75E+02 | 7.85E+04 | 1.52E+03 | 3.07E+02 | 9.85E+00 | 9.04E+01 |
| 2021 | 3.46E+06 | 4.67E+05 | 1.06E+05 | 4.33E+02 | 4.16E+04 | 1.94E+04 | 1.22E+03 | 4.32E+04 | 3.58E+04 | 1.71E+04 | 3.76E+02 | 7.76E+04 | 1.56E+03 | 3.08E+02 | 9.99E+00 | 9.03E+01 |
| 2022 | 3.44E+06 | 4.63E+05 | 1.08E+05 | 4.86E+02 | 4.10E+04 | 2.06E+04 | 1.21E+03 | 4.29E+04 | 3.56E+04 | 1.69E+04 | 3.78E+02 | 7.68E+04 | 1.60E+03 | 3.10E+02 | 1.01E+01 | 9.02E+01 |
| 2023 | 3.41E+06 | 4.60E+05 | 1.10E+05 | 5.42E+02 | 4.04E+04 | 2.19E+04 | 1.20E+03 | 4.26E+04 | 3.54E+04 | 1.67E+04 | 3.81E+02 | 7.60E+04 | 1.64E+03 | 3.11E+02 | 1.03E+01 | 9.01E+01 |
| 2024 | 3.39E+06 | 4.56E+05 | 1.12E+05 | 6.01E+02 | 3.98E+04 | 2.32E+04 | 1.19E+03 | 4.24E+04 | 3.52E+04 | 1.65E+04 | 3.83E+02 | 7.52E+04 | 1.69E+03 | 3.13E+02 | 1.05E+01 | 9.01E+01 |
| 2025 | 3.37E+06 | 4.53E+05 | 1.15E+05 | 6.62E+02 | 3.93E+04 | 2.47E+04 | 1.18E+03 | 4.22E+04 | 3.50E+04 | 1.64E+04 | 3.86E+02 | 7.44E+04 | 1.73E+03 | 3.16E+02 | 1.06E+01 | 9.01E+01 |
| 2026 | 3.35E+06 | 4.51E+05 | 1.18E+05 | 7.25E+02 | 3.87E+04 | 2.63E+04 | 1.17E+03 | 4.20E+04 | 3.48E+04 | 1.62E+04 | 3.90E+02 | 7.36E+04 | 1.78E+03 | 3.18E+02 | 1.08E+01 | 9.03E+01 |
| 2027 | 3.33E+06 | 4.48E+05 | 1.21E+05 | 7.91E+02 | 3.82E+04 | 2.79E+04 | 1.16E+03 | 4.19E+04 | 3.46E+04 | 1.60E+04 | 3.95E+02 | 7.29E+04 | 1.83E+03 | 3.21E+02 | 1.10E+01 | 9.05E+01 |
| 2028 | 3.32E+06 | 4.46E+05 | 1.24E+05 | 8.59E+02 | 3.77E+04 | 2.97E+04 | 1.15E+03 | 4.17E+04 | 3.45E+04 | 1.58E+04 | 3.99E+02 | 7.22E+04 | 1.89E+03 | 3.23E+02 | 1.12E+01 | 9.08E+01 |
| 2029 | 3.31E+06 | 4.45E+05 | 1.27E+05 | 9.29E+02 | 3.73E+04 | 3.16E+04 | 1.15E+03 | 4.16E+04 | 3.43E+04 | 1.57E+04 | 4.05E+02 | 7.15E+04 | 1.94E+03 | 3.26E+02 | 1.14E+01 | 9.11E+01 |
| 2030 | 3.31E+06 | 4.43E+05 | 1.31E+05 | 1.00E+03 | 3.69E+04 | 3.36E+04 | 1.14E+03 | 4.16E+04 | 3.42E+04 | 1.55E+04 | 4.11E+02 | 7.09E+04 | 2.00E+03 | 3.29E+02 | 1.16E+01 | 9.16E+01 |
| 2031 | 3.30E+06 | 4.43E+05 | 1.35E+05 | 1.08E+03 | 3.65E+04 | 3.57E+04 | 1.14E+03 | 4.16E+04 | 3.41E+04 | 1.54E+04 | 4.18E+02 | 7.04E+04 | 2.05E+03 | 3.32E+02 | 1.19E+01 | 9.22E+01 |
| 2032 | 3.30E+06 | 4.42E+05 | 1.39E+05 | 1.15E+03 | 3.62E+04 | 3.79E+04 | 1.13E+03 | 4.16E+04 | 3.41E+04 | 1.52E+04 | 4.26E+02 | 6.99E+04 | 2.11E+03 | 3.36E+02 | 1.21E+01 | 9.28E+01 |
| 2033 | 3.31E+06 | 4.42E+05 | 1.43E+05 | 1.23E+03 | 3.60E+04 | 4.03E+04 | 1.13E+03 | 4.17E+04 | 3.40E+04 | 1.51E+04 | 4.35E+02 | 6.95E+04 | 2.17E+03 | 3.39E+02 | 1.23E+01 | 9.36E+01 |
| 2034 | 3.32E+06 | 4.43E+05 | 1.48E+05 | 1.31E+03 | 3.58E+04 | 4.27E+04 | 1.13E+03 | 4.18E+04 | 3.40E+04 | 1.50E+04 | 4.44E+02 | 6.91E+04 | 2.24E+03 | 3.43E+02 | 1.25E+01 | 9.45E+01 |
| 2035 | 3.34E+06 | 4.44E+05 | 1.53E+05 | 1.39E+03 | 3.56E+04 | 4.52E+04 | 1.13E+03 | 4.20E+04 | 3.40E+04 | 1.49E+04 | 4.54E+02 | 6.88E+04 | 2.30E+03 | 3.47E+02 | 1.28E+01 | 9.55E+01 |
| 2036 | 3.35E+06 | 4.46E+05 | 1.58E+05 | 1.48E+03 | 3.55E+04 | 4.78E+04 | 1.13E+03 | 4.21E+04 | 3.41E+04 | 1.48E+04 | 4.64E+02 | 6.86E+04 | 2.36E+03 | 3.51E+02 | 1.30E+01 | 9.65E+01 |
| 2037 | 3.37E+06 | 4.48E+05 | 1.63E+05 | 1.56E+03 | 3.55E+04 | 5.05E+04 | 1.13E+03 | 4.24E+04 | 3.41E+04 | 1.48E+04 | 4.75E+02 | 6.84E+04 | 2.43E+03 | 3.55E+02 | 1.33E+01 | 9.77E+01 |
| 2038 | 3.40E+06 | 4.51E+05 | 1.68E+05 | 1.64E+03 | 3.54E+04 | 5.31E+04 | 1.14E+03 | 4.26E+04 | 3.42E+04 | 1.47E+04 | 4.86E+02 | 6.83E+04 | 2.49E+03 | 3.60E+02 | 1.35E+01 | 9.88E+01 |
| 2039 | 3.42E+06 | 4.53E+05 | 1.73E+05 | 1.73E+03 | 3.54E+04 | 5.58E+04 | 1.14E+03 | 4.28E+04 | 3.43E+04 | 1.47E+04 | 4.97E+02 | 6.82E+04 | 2.55E+03 | 3.64E+02 | 1.38E+01 | 1.00E+02 |
| 2040 | 3.45E+06 | 4.56E+05 | 1.78E+05 | 1.81E+03 | 3.55E+04 | 5.85E+04 | 1.14E+03 | 4.31E+04 | 3.43E+04 | 1.46E+04 | 5.09E+02 | 6.82E+04 | 2.61E+03 | 3.68E+02 | 1.40E+01 | 1.01E+02 |
| 2041 | 3.48E+06 | 4.59E+05 | 1.83E+05 | 1.89E+03 | 3.56E+04 | 6.11E+04 | 1.15E+03 | 4.33E+04 | 3.44E+04 | 1.46E+04 | 5.20E+02 | 6.82E+04 | 2.67E+03 | 3.72E+02 | 1.42E+01 | 1.02E+02 |
| 2042 | 3.51E+06 | 4.62E+05 | 1.88E+05 | 1.97E+03 | 3.56E+04 | 6.37E+04 | 1.15E+03 | 4.35E+04 | 3.45E+04 | 1.45E+04 | 5.31E+02 | 6.82E+04 | 2.73E+03 | 3.76E+02 | 1.44E+01 | 1.04E+02 |
| 2043 | 3.53E+06 | 4.64E+05 | 1.93E+05 | 2.05E+03 | 3.57E+04 | 6.62E+04 | 1.16E+03 | 4.38E+04 | 3.46E+04 | 1.45E+04 | 5.42E+02 | 6.83E+04 | 2.79E+03 | 3.79E+02 | 1.46E+01 | 1.05E+02 |
| 2044 | 3.56E+06 | 4.67E+05 | 1.97E+05 | 2.13E+03 | 3.58E+04 | 6.87E+04 | 1.16E+03 | 4.39E+04 | 3.47E+04 | 1.44E+04 | 5.52E+02 | 6.83E+04 | 2.84E+03 | 3.83E+02 | 1.48E+01 | 1.06E+02 |
| 2045 | 3.59E+06 | 4.69E+05 | 2.02E+05 | 2.20E+03 | 3.59E+04 | 7.12E+04 | 1.16E+03 | 4.41E+04 | 3.47E+04 | 1.44E+04 | 5.63E+02 | 6.84E+04 | 2.89E+03 | 3.86E+02 | 1.50E+01 | 1.07E+02 |
| 2046 | 3.61E+06 | 4.72E+05 | 2.06E+05 | 2.28E+03 | 3.60E+04 | 7.35E+04 | 1.16E+03 | 4.42E+04 | 3.48E+04 | 1.43E+04 | 5.72E+02 | 6.84E+04 | 2.94E+03 | 3.89E+02 | 1.52E+01 | 1.08E+02 |
| 2047 | 3.64E+06 | 4.74E+05 | 2.10E+05 | 2.35E+03 | 3.61E+04 | 7.58E+04 | 1.16E+03 | 4.44E+04 | 3.48E+04 | 1.43E+04 | 5.82E+02 | 6.84E+04 | 2.98E+03 | 3.92E+02 | 1.54E+01 | 1.09E+02 |
| 2048 | 3.66E+06 | 4.76E+05 | 2.14E+05 | 2.42E+03 | 3.61E+04 | 7.80E+04 | 1.16E+03 | 4.44E+04 | 3.48E+04 | 1.42E+04 | 5.91E+02 | 6.84E+04 | 3.03E+03 | 3.94E+02 | 1.55E+01 | 1.10E+02 |
| 2049 | 3.68E+06 | 4.77E+05 | 2.18E+05 | 2.48E+03 | 3.62E+04 | 8.02E+04 | 1.16E+03 | 4.45E+04 | 3.48E+04 | 1.41E+04 | 5.99E+02 | 6.83E+04 | 3.06E+03 | 3.97E+02 | 1.56E+01 | 1.11E+02 |
| 2050 | 3.69E+06 | 4.79E+05 | 2.22E+05 | 2.55E+03 | 3.62E+04 | 8.22E+04 | 1.16E+03 | 4.45E+04 | 3.47E+04 | 1.41E+04 | 6.07E+02 | 6.83E+04 | 3.10E+03 | 3.99E+02 | 1.58E+01 | 1.12E+02 |

Unit: t

## Table S35b. Estimated automotive urban mineral formation in Japan in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 1.16E+01 | 2.71E+00 | 1.31E+00 | 6.52E+02 | 6.96E+00 | 2.66E+01 | 2.36E+01 | 3.24E+01 | 2.51E+01 | 8.09E+01 | 7.61E+02 | 1.32E+00 | 1.88E+01 | 2.28E+03 | 3.14E+03 | 5.27E+02 |
| 2021 | 1.14E+01 | 2.68E+00 | 1.30E+00 | 6.91E+02 | 6.82E+00 | 2.62E+01 | 2.33E+01 | 3.50E+01 | 2.46E+01 | 7.90E+01 | 9.11E+02 | 1.31E+00 | 1.86E+01 | 2.27E+03 | 3.11E+03 | 5.25E+02 |
| 2022 | 1.12E+01 | 2.66E+00 | 1.28E+00 | 7.32E+02 | 6.69E+00 | 2.59E+01 | 2.31E+01 | 3.78E+01 | 2.42E+01 | 7.70E+01 | 1.07E+03 | 1.30E+00 | 1.84E+01 | 2.26E+03 | 3.09E+03 | 5.24E+02 |
| 2023 | 1.10E+01 | 2.65E+00 | 1.27E+00 | 7.75E+02 | 6.55E+00 | 2.55E+01 | 2.28E+01 | 4.07E+01 | 2.37E+01 | 7.50E+01 | 1.24E+03 | 1.29E+00 | 1.82E+01 | 2.25E+03 | 3.06E+03 | 5.22E+02 |
| 2024 | 1.08E+01 | 2.64E+00 | 1.25E+00 | 8.20E+02 | 6.42E+00 | 2.51E+01 | 2.25E+01 | 4.38E+01 | 2.33E+01 | 7.30E+01 | 1.42E+03 | 1.27E+00 | 1.80E+01 | 2.24E+03 | 3.04E+03 | 5.21E+02 |
| 2025 | 1.06E+01 | 2.66E+00 | 1.24E+00 | 8.66E+02 | 6.30E+00 | 2.48E+01 | 2.22E+01 | 4.69E+01 | 2.29E+01 | 7.10E+01 | 1.61E+03 | 1.26E+00 | 1.79E+01 | 2.23E+03 | 3.01E+03 | 5.20E+02 |
| 2026 | 1.04E+01 | 2.69E+00 | 1.22E+00 | 9.12E+02 | 6.20E+00 | 2.45E+01 | 2.19E+01 | 5.02E+01 | 2.25E+01 | 6.90E+01 | 1.80E+03 | 1.25E+00 | 1.77E+01 | 2.22E+03 | 2.99E+03 | 5.19E+02 |
| 2027 | 1.02E+01 | 2.74E+00 | 1.21E+00 | 9.59E+02 | 6.12E+00 | 2.42E+01 | 2.17E+01 | 5.35E+01 | 2.22E+01 | 6.71E+01 | 2.01E+03 | 1.24E+00 | 1.76E+01 | 2.21E+03 | 2.97E+03 | 5.18E+02 |
| 2028 | 1.00E+01 | 2.82E+00 | 1.20E+00 | 1.01E+03 | 6.05E+00 | 2.39E+01 | 2.15E+01 | 5.69E+01 | 2.20E+01 | 6.52E+01 | 2.22E+03 | 1.23E+00 | 1.74E+01 | 2.21E+03 | 2.94E+03 | 5.18E+02 |
| 2029 | 9.87E+00 | 2.93E+00 | 1.18E+00 | 1.05E+03 | 6.01E+00 | 2.36E+01 | 2.12E+01 | 6.03E+01 | 2.18E+01 | 6.34E+01 | 2.45E+03 | 1.22E+00 | 1.73E+01 | 2.20E+03 | 2.92E+03 | 5.18E+02 |
| 2030 | 9.69E+00 | 3.07E+00 | 1.17E+00 | 1.10E+03 | 5.99E+00 | 2.34E+01 | 2.10E+01 | 6.38E+01 | 2.18E+01 | 6.16E+01 | 2.69E+03 | 1.21E+00 | 1.72E+01 | 2.20E+03 | 2.90E+03 | 5.19E+02 |
| 2031 | 9.52E+00 | 3.24E+00 | 1.15E+00 | 1.15E+03 | 6.00E+00 | 2.32E+01 | 2.09E+01 | 6.74E+01 | 2.18E+01 | 6.00E+01 | 2.94E+03 | 1.21E+00 | 1.71E+01 | 2.20E+03 | 2.88E+03 | 5.20E+02 |
| 2032 | 9.36E+00 | 3.44E+00 | 1.14E+00 | 1.19E+03 | 6.04E+00 | 2.30E+01 | 2.07E+01 | 7.10E+01 | 2.19E+01 | 5.84E+01 | 3.19E+03 | 1.20E+00 | 1.70E+01 | 2.20E+03 | 2.86E+03 | 5.21E+02 |
| 2033 | 9.21E+00 | 3.68E+00 | 1.13E+00 | 1.24E+03 | 6.11E+00 | 2.28E+01 | 2.06E+01 | 7.46E+01 | 2.21E+01 | 5.69E+01 | 3.46E+03 | 1.20E+00 | 1.70E+01 | 2.21E+03 | 2.84E+03 | 5.23E+02 |
| 2034 | 9.07E+00 | 3.96E+00 | 1.12E+00 | 1.28E+03 | 6.21E+00 | 2.27E+01 | 2.05E+01 | 7.83E+01 | 2.24E+01 | 5.55E+01 | 3.74E+03 | 1.20E+00 | 1.70E+01 | 2.21E+03 | 2.83E+03 | 5.26E+02 |
| 2035 | 8.94E+00 | 4.28E+00 | 1.10E+00 | 1.33E+03 | 6.34E+00 | 2.26E+01 | 2.04E+01 | 8.20E+01 | 2.28E+01 | 5.43E+01 | 4.02E+03 | 1.20E+00 | 1.70E+01 | 2.22E+03 | 2.81E+03 | 5.29E+02 |
| 2036 | 8.82E+00 | 4.63E+00 | 1.09E+00 | 1.37E+03 | 6.50E+00 | 2.26E+01 | 2.03E+01 | 8.58E+01 | 2.33E+01 | 5.31E+01 | 4.31E+03 | 1.20E+00 | 1.70E+01 | 2.23E+03 | 2.80E+03 | 5.32E+02 |
| 2037 | 8.71E+00 | 5.02E+00 | 1.08E+00 | 1.41E+03 | 6.69E+00 | 2.26E+01 | 2.03E+01 | 8.95E+01 | 2.39E+01 | 5.21E+01 | 4.59E+03 | 1.20E+00 | 1.70E+01 | 2.24E+03 | 2.78E+03 | 5.35E+02 |
| 2038 | 8.60E+00 | 5.45E+00 | 1.07E+00 | 1.45E+03 | 6.91E+00 | 2.26E+01 | 2.03E+01 | 9.31E+01 | 2.46E+01 | 5.11E+01 | 4.88E+03 | 1.20E+00 | 1.71E+01 | 2.26E+03 | 2.77E+03 | 5.39E+02 |
| 2039 | 8.51E+00 | 5.91E+00 | 1.07E+00 | 1.49E+03 | 7.15E+00 | 2.26E+01 | 2.03E+01 | 9.68E+01 | 2.53E+01 | 5.03E+01 | 5.17E+03 | 1.21E+00 | 1.71E+01 | 2.27E+03 | 2.76E+03 | 5.43E+02 |
| 2040 | 8.42E+00 | 6.41E+00 | 1.06E+00 | 1.53E+03 | 7.41E+00 | 2.27E+01 | 2.03E+01 | 1.00E+02 | 2.62E+01 | 4.95E+01 | 5.45E+03 | 1.21E+00 | 1.72E+01 | 2.28E+03 | 2.75E+03 | 5.47E+02 |
| 2041 | 8.33E+00 | 6.93E+00 | 1.05E+00 | 1.56E+03 | 7.70E+00 | 2.27E+01 | 2.03E+01 | 1.04E+02 | 2.71E+01 | 4.89E+01 | 5.72E+03 | 1.22E+00 | 1.73E+01 | 2.30E+03 | 2.74E+03 | 5.51E+02 |
| 2042 | 8.25E+00 | 7.49E+00 | 1.04E+00 | 1.59E+03 | 8.00E+00 | 2.28E+01 | 2.04E+01 | 1.07E+02 | 2.80E+01 | 4.82E+01 | 6.00E+03 | 1.22E+00 | 1.73E+01 | 2.31E+03 | 2.73E+03 | 5.56E+02 |
| 2043 | 8.17E+00 | 8.06E+00 | 1.03E+00 | 1.62E+03 | 8.32E+00 | 2.29E+01 | 2.04E+01 | 1.11E+02 | 2.90E+01 | 4.77E+01 | 6.26E+03 | 1.23E+00 | 1.74E+01 | 2.33E+03 | 2.72E+03 | 5.60E+02 |
| 2044 | 8.09E+00 | 8.66E+00 | 1.02E+00 | 1.65E+03 | 8.65E+00 | 2.29E+01 | 2.05E+01 | 1.14E+02 | 3.01E+01 | 4.72E+01 | 6.52E+03 | 1.23E+00 | 1.75E+01 | 2.34E+03 | 2.71E+03 | 5.63E+02 |
| 2045 | 8.01E+00 | 9.27E+00 | 1.01E+00 | 1.68E+03 | 8.98E+00 | 2.30E+01 | 2.05E+01 | 1.17E+02 | 3.11E+01 | 4.67E+01 | 6.76E+03 | 1.24E+00 | 1.76E+01 | 2.36E+03 | 2.70E+03 | 5.67E+02 |
| 2046 | 7.93E+00 | 9.90E+00 | 1.00E+00 | 1.70E+03 | 9.33E+00 | 2.31E+01 | 2.05E+01 | 1.20E+02 | 3.22E+01 | 4.62E+01 | 7.00E+03 | 1.24E+00 | 1.76E+01 | 2.37E+03 | 2.69E+03 | 5.70E+02 |
| 2047 | 7.85E+00 | 1.05E+01 | 9.93E-01 | 1.72E+03 | 9.68E+00 | 2.31E+01 | 2.06E+01 | 1.23E+02 | 3.33E+01 | 4.58E+01 | 7.23E+03 | 1.25E+00 | 1.77E+01 | 2.38E+03 | 2.68E+03 | 5.73E+02 |
| 2048 | 7.76E+00 | 1.12E+01 | 9.82E-01 | 1.74E+03 | 1.00E+01 | 2.32E+01 | 2.06E+01 | 1.26E+02 | 3.44E+01 | 4.53E+01 | 7.46E+03 | 1.25E+00 | 1.77E+01 | 2.39E+03 | 2.67E+03 | 5.76E+02 |
| 2049 | 7.68E+00 | 1.18E+01 | 9.72E-01 | 1.76E+03 | 1.04E+01 | 2.32E+01 | 2.06E+01 | 1.29E+02 | 3.55E+01 | 4.49E+01 | 7.67E+03 | 1.26E+00 | 1.78E+01 | 2.40E+03 | 2.65E+03 | 5.78E+02 |
| 2050 | 7.59E+00 | 1.25E+01 | 9.61E-01 | 1.78E+03 | 1.07E+01 | 2.33E+01 | 2.06E+01 | 1.31E+02 | 3.66E+01 | 4.45E+01 | 7.88E+03 | 1.26E+00 | 1.78E+01 | 2.41E+03 | 2.63E+03 | 5.80E+02 |

Unit: t

## Table S36a. Estimated UMS of vehicles in China in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 2.15E+08 | 2.89E+07 | 5.94E+06 | 1.29E+04 | 2.65E+06 | 9.87E+05 | 7.53E+04 | 2.63E+06 | 2.20E+06 | 1.07E+06 | 2.23E+04 | 4.88E+06 | 8.34E+04 | 1.80E+04 | 5.58E+02 | 5.46E+03 |
| 2021 | 2.28E+08 | 3.07E+07 | 6.42E+06 | 1.51E+04 | 2.81E+06 | 1.13E+06 | 7.96E+04 | 2.79E+06 | 2.33E+06 | 1.13E+06 | 2.39E+04 | 5.17E+06 | 8.96E+04 | 1.91E+04 | 5.96E+02 | 5.81E+03 |
| 2022 | 2.41E+08 | 3.23E+07 | 6.93E+06 | 1.81E+04 | 2.96E+06 | 1.30E+06 | 8.36E+04 | 2.93E+06 | 2.45E+06 | 1.19E+06 | 2.55E+04 | 5.45E+06 | 9.61E+04 | 2.03E+04 | 6.34E+02 | 6.15E+03 |
| 2023 | 2.53E+08 | 3.39E+07 | 7.48E+06 | 2.17E+04 | 3.10E+06 | 1.51E+06 | 8.72E+04 | 3.05E+06 | 2.56E+06 | 1.23E+06 | 2.70E+04 | 5.70E+06 | 1.03E+05 | 2.14E+04 | 6.72E+02 | 6.48E+03 |
| 2024 | 2.65E+08 | 3.53E+07 | 8.06E+06 | 2.60E+04 | 3.23E+06 | 1.75E+06 | 9.04E+04 | 3.17E+06 | 2.66E+06 | 1.27E+06 | 2.86E+04 | 5.94E+06 | 1.10E+05 | 2.24E+04 | 7.10E+02 | 6.80E+03 |
| 2025 | 2.75E+08 | 3.66E+07 | 8.66E+06 | 3.09E+04 | 3.34E+06 | 2.03E+06 | 9.31E+04 | 3.26E+06 | 2.75E+06 | 1.31E+06 | 3.02E+04 | 6.15E+06 | 1.17E+05 | 2.34E+04 | 7.47E+02 | 7.10E+03 |
| 2026 | 2.85E+08 | 3.78E+07 | 9.33E+06 | 3.68E+04 | 3.44E+06 | 2.36E+06 | 9.53E+04 | 3.34E+06 | 2.83E+06 | 1.33E+06 | 3.18E+04 | 6.34E+06 | 1.24E+05 | 2.44E+04 | 7.84E+02 | 7.39E+03 |
| 2027 | 2.94E+08 | 3.88E+07 | 1.01E+07 | 4.37E+04 | 3.53E+06 | 2.74E+06 | 9.70E+04 | 3.41E+06 | 2.89E+06 | 1.35E+06 | 3.35E+04 | 6.52E+06 | 1.32E+05 | 2.53E+04 | 8.23E+02 | 7.67E+03 |
| 2028 | 3.03E+08 | 3.98E+07 | 1.08E+07 | 5.17E+04 | 3.61E+06 | 3.17E+06 | 9.84E+04 | 3.46E+06 | 2.95E+06 | 1.36E+06 | 3.53E+04 | 6.67E+06 | 1.41E+05 | 2.62E+04 | 8.62E+02 | 7.95E+03 |
| 2029 | 3.11E+08 | 4.07E+07 | 1.17E+07 | 6.07E+04 | 3.68E+06 | 3.66E+06 | 9.94E+04 | 3.50E+06 | 3.00E+06 | 1.37E+06 | 3.71E+04 | 6.82E+06 | 1.50E+05 | 2.72E+04 | 9.03E+02 | 8.23E+03 |
| 2030 | 3.20E+08 | 4.16E+07 | 1.26E+07 | 7.08E+04 | 3.75E+06 | 4.21E+06 | 1.00E+05 | 3.52E+06 | 3.04E+06 | 1.37E+06 | 3.90E+04 | 6.95E+06 | 1.59E+05 | 2.81E+04 | 9.46E+02 | 8.52E+03 |
| 2031 | 3.28E+08 | 4.24E+07 | 1.36E+07 | 8.14E+04 | 3.82E+06 | 4.79E+06 | 1.01E+05 | 3.55E+06 | 3.08E+06 | 1.37E+06 | 4.11E+04 | 7.09E+06 | 1.70E+05 | 2.91E+04 | 9.91E+02 | 8.81E+03 |
| 2032 | 3.37E+08 | 4.33E+07 | 1.46E+07 | 9.26E+04 | 3.89E+06 | 5.39E+06 | 1.01E+05 | 3.57E+06 | 3.12E+06 | 1.37E+06 | 4.31E+04 | 7.22E+06 | 1.80E+05 | 3.01E+04 | 1.04E+03 | 9.11E+03 |
| 2033 | 3.46E+08 | 4.41E+07 | 1.57E+07 | 1.04E+05 | 3.96E+06 | 6.02E+06 | 1.02E+05 | 3.59E+06 | 3.17E+06 | 1.36E+06 | 4.53E+04 | 7.37E+06 | 1.91E+05 | 3.12E+04 | 1.08E+03 | 9.42E+03 |
| 2034 | 3.55E+08 | 4.51E+07 | 1.68E+07 | 1.16E+05 | 4.03E+06 | 6.67E+06 | 1.02E+05 | 3.61E+06 | 3.21E+06 | 1.36E+06 | 4.75E+04 | 7.52E+06 | 2.02E+05 | 3.22E+04 | 1.13E+03 | 9.74E+03 |
| 2035 | 3.65E+08 | 4.60E+07 | 1.79E+07 | 1.28E+05 | 4.11E+06 | 7.34E+06 | 1.02E+05 | 3.63E+06 | 3.25E+06 | 1.35E+06 | 4.98E+04 | 7.67E+06 | 2.14E+05 | 3.33E+04 | 1.18E+03 | 1.01E+04 |
| 2036 | 3.75E+08 | 4.70E+07 | 1.91E+07 | 1.41E+05 | 4.18E+06 | 8.01E+06 | 1.03E+05 | 3.65E+06 | 3.30E+06 | 1.35E+06 | 5.21E+04 | 7.83E+06 | 2.25E+05 | 3.45E+04 | 1.23E+03 | 1.04E+04 |
| 2037 | 3.85E+08 | 4.79E+07 | 2.02E+07 | 1.54E+05 | 4.26E+06 | 8.70E+06 | 1.03E+05 | 3.66E+06 | 3.35E+06 | 1.35E+06 | 5.44E+04 | 7.99E+06 | 2.37E+05 | 3.56E+04 | 1.29E+03 | 1.07E+04 |
| 2038 | 3.95E+08 | 4.89E+07 | 2.14E+07 | 1.66E+05 | 4.34E+06 | 9.39E+06 | 1.04E+05 | 3.68E+06 | 3.39E+06 | 1.34E+06 | 5.68E+04 | 8.16E+06 | 2.49E+05 | 3.67E+04 | 1.34E+03 | 1.11E+04 |
| 2039 | 4.05E+08 | 4.99E+07 | 2.25E+07 | 1.79E+05 | 4.42E+06 | 1.01E+07 | 1.04E+05 | 3.69E+06 | 3.44E+06 | 1.34E+06 | 5.91E+04 | 8.32E+06 | 2.60E+05 | 3.79E+04 | 1.39E+03 | 1.14E+04 |
| 2040 | 4.15E+08 | 5.08E+07 | 2.37E+07 | 1.92E+05 | 4.50E+06 | 1.08E+07 | 1.04E+05 | 3.70E+06 | 3.48E+06 | 1.33E+06 | 6.14E+04 | 8.48E+06 | 2.72E+05 | 3.90E+04 | 1.44E+03 | 1.18E+04 |
| 2041 | 4.24E+08 | 5.17E+07 | 2.49E+07 | 2.05E+05 | 4.58E+06 | 1.15E+07 | 1.05E+05 | 3.71E+06 | 3.52E+06 | 1.32E+06 | 6.37E+04 | 8.65E+06 | 2.84E+05 | 4.01E+04 | 1.49E+03 | 1.21E+04 |
| 2042 | 4.34E+08 | 5.27E+07 | 2.61E+07 | 2.18E+05 | 4.66E+06 | 1.22E+07 | 1.05E+05 | 3.72E+06 | 3.56E+06 | 1.31E+06 | 6.61E+04 | 8.81E+06 | 2.96E+05 | 4.13E+04 | 1.54E+03 | 1.24E+04 |
| 2043 | 4.44E+08 | 5.36E+07 | 2.72E+07 | 2.31E+05 | 4.73E+06 | 1.29E+07 | 1.05E+05 | 3.72E+06 | 3.60E+06 | 1.30E+06 | 6.84E+04 | 8.97E+06 | 3.07E+05 | 4.24E+04 | 1.59E+03 | 1.28E+04 |
| 2044 | 4.54E+08 | 5.45E+07 | 2.85E+07 | 2.45E+05 | 4.81E+06 | 1.36E+07 | 1.05E+05 | 3.72E+06 | 3.64E+06 | 1.29E+06 | 7.08E+04 | 9.14E+06 | 3.19E+05 | 4.35E+04 | 1.65E+03 | 1.31E+04 |
| 2045 | 4.64E+08 | 5.54E+07 | 2.97E+07 | 2.59E+05 | 4.89E+06 | 1.44E+07 | 1.05E+05 | 3.71E+06 | 3.68E+06 | 1.28E+06 | 7.32E+04 | 9.31E+06 | 3.31E+05 | 4.47E+04 | 1.70E+03 | 1.35E+04 |
| 2046 | 4.74E+08 | 5.63E+07 | 3.09E+07 | 2.73E+05 | 4.97E+06 | 1.52E+07 | 1.04E+05 | 3.71E+06 | 3.72E+06 | 1.27E+06 | 7.56E+04 | 9.48E+06 | 3.44E+05 | 4.58E+04 | 1.75E+03 | 1.38E+04 |
| 2047 | 4.84E+08 | 5.72E+07 | 3.22E+07 | 2.87E+05 | 5.05E+06 | 1.59E+07 | 1.04E+05 | 3.69E+06 | 3.75E+06 | 1.26E+06 | 7.81E+04 | 9.65E+06 | 3.56E+05 | 4.70E+04 | 1.81E+03 | 1.42E+04 |
| 2048 | 4.94E+08 | 5.81E+07 | 3.35E+07 | 3.02E+05 | 5.13E+06 | 1.67E+07 | 1.04E+05 | 3.68E+06 | 3.79E+06 | 1.24E+06 | 8.06E+04 | 9.82E+06 | 3.69E+05 | 4.82E+04 | 1.86E+03 | 1.45E+04 |
| 2049 | 5.05E+08 | 5.90E+07 | 3.49E+07 | 3.18E+05 | 5.20E+06 | 1.76E+07 | 1.03E+05 | 3.66E+06 | 3.82E+06 | 1.22E+06 | 8.31E+04 | 9.99E+06 | 3.82E+05 | 4.94E+04 | 1.92E+03 | 1.49E+04 |
| 2050 | 5.15E+08 | 5.99E+07 | 3.63E+07 | 3.33E+05 | 5.28E+06 | 1.84E+07 | 1.02E+05 | 3.63E+06 | 3.85E+06 | 1.20E+06 | 8.57E+04 | 1.02E+07 | 3.95E+05 | 5.06E+04 | 1.97E+03 | 1.52E+04 |

## Table S36b. Estimated UMS of vehicles in China in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 7.30E+02 | 1.65E+02 | 8.09E+01 | 2.96E+04 | 4.63E+02 | 1.67E+03 | 1.48E+03 | 1.47E+03 | 1.65E+03 | 5.27E+03 | 2.97E+04 | 8.23E+01 | 1.17E+03 | 1.39E+05 | 1.91E+05 | 3.20E+04 |
| 2021 | 7.70E+02 | 1.74E+02 | 8.54E+01 | 3.20E+04 | 4.95E+02 | 1.77E+03 | 1.57E+03 | 1.67E+03 | 1.77E+03 | 5.57E+03 | 4.10E+04 | 8.73E+01 | 1.24E+03 | 1.48E+05 | 2.02E+05 | 3.40E+04 |
| 2022 | 8.06E+02 | 1.83E+02 | 8.94E+01 | 3.46E+04 | 5.28E+02 | 1.87E+03 | 1.65E+03 | 1.91E+03 | 1.88E+03 | 5.84E+03 | 5.69E+04 | 9.20E+01 | 1.30E+03 | 1.56E+05 | 2.12E+05 | 3.59E+04 |
| 2023 | 8.38E+02 | 1.90E+02 | 9.29E+01 | 3.74E+04 | 5.61E+02 | 1.95E+03 | 1.73E+03 | 2.19E+03 | 2.00E+03 | 6.09E+03 | 7.73E+04 | 9.64E+01 | 1.37E+03 | 1.64E+05 | 2.20E+05 | 3.77E+04 |
| 2024 | 8.64E+02 | 1.97E+02 | 9.59E+01 | 4.03E+04 | 5.95E+02 | 2.04E+03 | 1.80E+03 | 2.52E+03 | 2.11E+03 | 6.30E+03 | 1.02E+05 | 1.00E+02 | 1.42E+03 | 1.71E+05 | 2.28E+05 | 3.94E+04 |
| 2025 | 8.85E+02 | 2.03E+02 | 9.83E+01 | 4.34E+04 | 6.29E+02 | 2.11E+03 | 1.86E+03 | 2.90E+03 | 2.23E+03 | 6.47E+03 | 1.31E+05 | 1.04E+02 | 1.48E+03 | 1.78E+05 | 2.34E+05 | 4.10E+04 |
| 2026 | 9.01E+02 | 2.08E+02 | 1.00E+02 | 4.68E+04 | 6.64E+02 | 2.17E+03 | 1.92E+03 | 3.34E+03 | 2.35E+03 | 6.61E+03 | 1.67E+05 | 1.08E+02 | 1.52E+03 | 1.84E+05 | 2.38E+05 | 4.24E+04 |
| 2027 | 9.11E+02 | 2.13E+02 | 1.01E+02 | 5.05E+04 | 7.01E+02 | 2.23E+03 | 1.97E+03 | 3.86E+03 | 2.47E+03 | 6.72E+03 | 2.10E+05 | 1.11E+02 | 1.57E+03 | 1.90E+05 | 2.42E+05 | 4.38E+04 |
| 2028 | 9.16E+02 | 2.18E+02 | 1.02E+02 | 5.45E+04 | 7.41E+02 | 2.28E+03 | 2.01E+03 | 4.44E+03 | 2.60E+03 | 6.80E+03 | 2.59E+05 | 1.14E+02 | 1.61E+03 | 1.96E+05 | 2.44E+05 | 4.52E+04 |
| 2029 | 9.16E+02 | 2.22E+02 | 1.02E+02 | 5.89E+04 | 7.83E+02 | 2.33E+03 | 2.05E+03 | 5.11E+03 | 2.74E+03 | 6.85E+03 | 3.15E+05 | 1.16E+02 | 1.65E+03 | 2.01E+05 | 2.45E+05 | 4.65E+04 |
| 2030 | 9.12E+02 | 2.27E+02 | 1.02E+02 | 6.37E+04 | 8.28E+02 | 2.38E+03 | 2.09E+03 | 5.85E+03 | 2.88E+03 | 6.88E+03 | 3.79E+05 | 1.19E+02 | 1.68E+03 | 2.06E+05 | 2.45E+05 | 4.78E+04 |
| 2031 | 9.07E+02 | 2.32E+02 | 1.01E+02 | 6.86E+04 | 8.76E+02 | 2.42E+03 | 2.12E+03 | 6.63E+03 | 3.04E+03 | 6.90E+03 | 4.46E+05 | 1.21E+02 | 1.72E+03 | 2.11E+05 | 2.45E+05 | 4.91E+04 |
| 2032 | 9.00E+02 | 2.38E+02 | 1.00E+02 | 7.37E+04 | 9.26E+02 | 2.47E+03 | 2.16E+03 | 7.45E+03 | 3.20E+03 | 6.91E+03 | 5.16E+05 | 1.24E+02 | 1.75E+03 | 2.17E+05 | 2.45E+05 | 5.04E+04 |
| 2033 | 8.93E+02 | 2.46E+02 | 9.97E+01 | 7.89E+04 | 9.78E+02 | 2.51E+03 | 2.20E+03 | 8.31E+03 | 3.37E+03 | 6.93E+03 | 5.88E+05 | 1.27E+02 | 1.79E+03 | 2.22E+05 | 2.44E+05 | 5.18E+04 |
| 2034 | 8.86E+02 | 2.54E+02 | 9.90E+01 | 8.43E+04 | 1.03E+03 | 2.56E+03 | 2.24E+03 | 9.19E+03 | 3.55E+03 | 6.95E+03 | 6.63E+05 | 1.29E+02 | 1.83E+03 | 2.28E+05 | 2.44E+05 | 5.32E+04 |
| 2035 | 8.79E+02 | 2.63E+02 | 9.83E+01 | 8.98E+04 | 1.09E+03 | 2.61E+03 | 2.28E+03 | 1.01E+04 | 3.74E+03 | 6.98E+03 | 7.40E+05 | 1.32E+02 | 1.87E+03 | 2.34E+05 | 2.44E+05 | 5.47E+04 |
| 2036 | 8.72E+02 | 2.74E+02 | 9.76E+01 | 9.54E+04 | 1.15E+03 | 2.66E+03 | 2.33E+03 | 1.10E+04 | 3.93E+03 | 7.00E+03 | 8.18E+05 | 1.35E+02 | 1.91E+03 | 2.40E+05 | 2.43E+05 | 5.62E+04 |
| 2037 | 8.65E+02 | 2.86E+02 | 9.69E+01 | 1.01E+05 | 1.21E+03 | 2.72E+03 | 2.37E+03 | 1.20E+04 | 4.12E+03 | 7.03E+03 | 8.97E+05 | 1.38E+02 | 1.96E+03 | 2.46E+05 | 2.43E+05 | 5.77E+04 |
| 2038 | 8.57E+02 | 3.00E+02 | 9.61E+01 | 1.06E+05 | 1.27E+03 | 2.77E+03 | 2.41E+03 | 1.29E+04 | 4.33E+03 | 7.06E+03 | 9.77E+05 | 1.41E+02 | 2.00E+03 | 2.52E+05 | 2.42E+05 | 5.92E+04 |
| 2039 | 8.49E+02 | 3.15E+02 | 9.53E+01 | 1.12E+05 | 1.33E+03 | 2.82E+03 | 2.46E+03 | 1.39E+04 | 4.53E+03 | 7.09E+03 | 1.06E+06 | 1.44E+02 | 2.04E+03 | 2.58E+05 | 2.42E+05 | 6.07E+04 |
| 2040 | 8.41E+02 | 3.31E+02 | 9.44E+01 | 1.17E+05 | 1.40E+03 | 2.88E+03 | 2.50E+03 | 1.48E+04 | 4.74E+03 | 7.11E+03 | 1.14E+06 | 1.47E+02 | 2.08E+03 | 2.65E+05 | 2.41E+05 | 6.22E+04 |
| 2041 | 8.32E+02 | 3.49E+02 | 9.35E+01 | 1.23E+05 | 1.46E+03 | 2.93E+03 | 2.54E+03 | 1.58E+04 | 4.95E+03 | 7.14E+03 | 1.22E+06 | 1.50E+02 | 2.13E+03 | 2.71E+05 | 2.40E+05 | 6.37E+04 |
| 2042 | 8.23E+02 | 3.69E+02 | 9.25E+01 | 1.28E+05 | 1.53E+03 | 2.98E+03 | 2.58E+03 | 1.68E+04 | 5.17E+03 | 7.17E+03 | 1.30E+06 | 1.53E+02 | 2.17E+03 | 2.77E+05 | 2.39E+05 | 6.52E+04 |
| 2043 | 8.13E+02 | 3.90E+02 | 9.14E+01 | 1.34E+05 | 1.60E+03 | 3.03E+03 | 2.63E+03 | 1.78E+04 | 5.39E+03 | 7.19E+03 | 1.38E+06 | 1.56E+02 | 2.21E+03 | 2.83E+05 | 2.38E+05 | 6.67E+04 |
| 2044 | 8.02E+02 | 4.12E+02 | 9.03E+01 | 1.39E+05 | 1.67E+03 | 3.08E+03 | 2.67E+03 | 1.88E+04 | 5.62E+03 | 7.21E+03 | 1.47E+06 | 1.59E+02 | 2.25E+03 | 2.89E+05 | 2.37E+05 | 6.83E+04 |
| 2045 | 7.91E+02 | 4.37E+02 | 8.90E+01 | 1.45E+05 | 1.74E+03 | 3.14E+03 | 2.71E+03 | 1.99E+04 | 5.85E+03 | 7.24E+03 | 1.55E+06 | 1.62E+02 | 2.29E+03 | 2.95E+05 | 2.35E+05 | 6.98E+04 |
| 2046 | 7.78E+02 | 4.63E+02 | 8.77E+01 | 1.50E+05 | 1.81E+03 | 3.19E+03 | 2.76E+03 | 2.10E+04 | 6.09E+03 | 7.26E+03 | 1.64E+06 | 1.65E+02 | 2.34E+03 | 3.01E+05 | 2.34E+05 | 7.13E+04 |
| 2047 | 7.65E+02 | 4.91E+02 | 8.63E+01 | 1.56E+05 | 1.89E+03 | 3.24E+03 | 2.80E+03 | 2.21E+04 | 6.34E+03 | 7.27E+03 | 1.73E+06 | 1.68E+02 | 2.38E+03 | 3.08E+05 | 2.32E+05 | 7.29E+04 |
| 2048 | 7.50E+02 | 5.20E+02 | 8.47E+01 | 1.62E+05 | 1.97E+03 | 3.29E+03 | 2.84E+03 | 2.32E+04 | 6.60E+03 | 7.28E+03 | 1.83E+06 | 1.71E+02 | 2.42E+03 | 3.14E+05 | 2.30E+05 | 7.45E+04 |
| 2049 | 7.35E+02 | 5.52E+02 | 8.29E+01 | 1.68E+05 | 2.05E+03 | 3.35E+03 | 2.89E+03 | 2.44E+04 | 6.86E+03 | 7.29E+03 | 1.92E+06 | 1.74E+02 | 2.46E+03 | 3.20E+05 | 2.28E+05 | 7.60E+04 |
| 2050 | 7.17E+02 | 5.85E+02 | 8.10E+01 | 1.74E+05 | 2.14E+03 | 3.40E+03 | 2.93E+03 | 2.56E+04 | 7.14E+03 | 7.30E+03 | 2.02E+06 | 1.77E+02 | 2.51E+03 | 3.26E+05 | 2.25E+05 | 7.76E+04 |

## Table S37a. Estimated UMS of vehicles in Japan in 2022−2050 following standard scenario (Fe−Ag)

| Year | Fe | Al | Cu | Co | Pb | Ni | Sn | Zn | Mn | Mg | Sb | Cr | Ba | W | Au | Ag |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 4.09E+07 | 5.50E+06 | 1.49E+06 | 9.85E+03 | 4.67E+05 | 3.42E+05 | 1.42E+04 | 5.14E+05 | 4.26E+05 | 1.96E+05 | 4.84E+03 | 8.95E+05 | 2.27E+04 | 3.96E+03 | 1.37E+02 | 1.11E+03 |
| 2021 | 4.07E+07 | 5.47E+06 | 1.52E+06 | 1.07E+04 | 4.61E+05 | 3.61E+05 | 1.41E+04 | 5.12E+05 | 4.24E+05 | 1.94E+05 | 4.89E+03 | 8.87E+05 | 2.34E+04 | 4.00E+03 | 1.39E+02 | 1.12E+03 |
| 2022 | 4.06E+07 | 5.46E+06 | 1.57E+06 | 1.15E+04 | 4.56E+05 | 3.84E+05 | 1.41E+04 | 5.12E+05 | 4.23E+05 | 1.93E+05 | 4.96E+03 | 8.80E+05 | 2.41E+04 | 4.04E+03 | 1.42E+02 | 1.12E+03 |
| 2023 | 4.06E+07 | 5.45E+06 | 1.61E+06 | 1.24E+04 | 4.52E+05 | 4.08E+05 | 1.40E+04 | 5.12E+05 | 4.23E+05 | 1.91E+05 | 5.04E+03 | 8.75E+05 | 2.48E+04 | 4.09E+03 | 1.45E+02 | 1.13E+03 |
| 2024 | 4.07E+07 | 5.46E+06 | 1.67E+06 | 1.34E+04 | 4.49E+05 | 4.36E+05 | 1.40E+04 | 5.13E+05 | 4.23E+05 | 1.90E+05 | 5.14E+03 | 8.70E+05 | 2.56E+04 | 4.14E+03 | 1.48E+02 | 1.14E+03 |
| 2025 | 4.08E+07 | 5.47E+06 | 1.72E+06 | 1.44E+04 | 4.46E+05 | 4.65E+05 | 1.40E+04 | 5.16E+05 | 4.23E+05 | 1.89E+05 | 5.26E+03 | 8.66E+05 | 2.65E+04 | 4.20E+03 | 1.51E+02 | 1.15E+03 |
| 2026 | 4.11E+07 | 5.50E+06 | 1.79E+06 | 1.55E+04 | 4.45E+05 | 4.97E+05 | 1.40E+04 | 5.18E+05 | 4.24E+05 | 1.88E+05 | 5.39E+03 | 8.64E+05 | 2.73E+04 | 4.26E+03 | 1.55E+02 | 1.17E+03 |
| 2027 | 4.14E+07 | 5.53E+06 | 1.85E+06 | 1.66E+04 | 4.44E+05 | 5.31E+05 | 1.41E+04 | 5.22E+05 | 4.26E+05 | 1.87E+05 | 5.53E+03 | 8.63E+05 | 2.83E+04 | 4.33E+03 | 1.59E+02 | 1.18E+03 |
| 2028 | 4.17E+07 | 5.57E+06 | 1.92E+06 | 1.77E+04 | 4.43E+05 | 5.68E+05 | 1.42E+04 | 5.27E+05 | 4.28E+05 | 1.87E+05 | 5.69E+03 | 8.62E+05 | 2.92E+04 | 4.40E+03 | 1.63E+02 | 1.20E+03 |
| 2029 | 4.22E+07 | 5.62E+06 | 2.00E+06 | 1.89E+04 | 4.44E+05 | 6.06E+05 | 1.43E+04 | 5.32E+05 | 4.30E+05 | 1.87E+05 | 5.86E+03 | 8.63E+05 | 3.03E+04 | 4.47E+03 | 1.67E+02 | 1.22E+03 |
| 2030 | 4.27E+07 | 5.67E+06 | 2.08E+06 | 2.02E+04 | 4.45E+05 | 6.46E+05 | 1.44E+04 | 5.38E+05 | 4.33E+05 | 1.87E+05 | 6.04E+03 | 8.64E+05 | 3.13E+04 | 4.55E+03 | 1.71E+02 | 1.24E+03 |
| 2031 | 4.32E+07 | 5.73E+06 | 2.16E+06 | 2.14E+04 | 4.47E+05 | 6.86E+05 | 1.45E+04 | 5.43E+05 | 4.36E+05 | 1.87E+05 | 6.22E+03 | 8.66E+05 | 3.23E+04 | 4.63E+03 | 1.75E+02 | 1.26E+03 |
| 2032 | 4.37E+07 | 5.79E+06 | 2.24E+06 | 2.26E+04 | 4.48E+05 | 7.25E+05 | 1.46E+04 | 5.49E+05 | 4.39E+05 | 1.87E+05 | 6.39E+03 | 8.68E+05 | 3.33E+04 | 4.71E+03 | 1.79E+02 | 1.28E+03 |
| 2033 | 4.42E+07 | 5.84E+06 | 2.31E+06 | 2.38E+04 | 4.50E+05 | 7.64E+05 | 1.47E+04 | 5.54E+05 | 4.41E+05 | 1.87E+05 | 6.57E+03 | 8.70E+05 | 3.43E+04 | 4.78E+03 | 1.83E+02 | 1.31E+03 |
| 2034 | 4.47E+07 | 5.90E+06 | 2.39E+06 | 2.50E+04 | 4.52E+05 | 8.02E+05 | 1.48E+04 | 5.59E+05 | 4.44E+05 | 1.87E+05 | 6.74E+03 | 8.73E+05 | 3.52E+04 | 4.84E+03 | 1.86E+02 | 1.33E+03 |
| 2035 | 4.52E+07 | 5.95E+06 | 2.46E+06 | 2.61E+04 | 4.54E+05 | 8.39E+05 | 1.49E+04 | 5.64E+05 | 4.46E+05 | 1.87E+05 | 6.91E+03 | 8.75E+05 | 3.60E+04 | 4.91E+03 | 1.90E+02 | 1.35E+03 |
| 2036 | 4.57E+07 | 6.00E+06 | 2.53E+06 | 2.72E+04 | 4.57E+05 | 8.75E+05 | 1.49E+04 | 5.68E+05 | 4.48E+05 | 1.87E+05 | 7.07E+03 | 8.78E+05 | 3.69E+04 | 4.97E+03 | 1.93E+02 | 1.36E+03 |
| 2037 | 4.61E+07 | 6.05E+06 | 2.60E+06 | 2.83E+04 | 4.59E+05 | 9.10E+05 | 1.50E+04 | 5.72E+05 | 4.50E+05 | 1.86E+05 | 7.23E+03 | 8.80E+05 | 3.76E+04 | 5.03E+03 | 1.96E+02 | 1.38E+03 |
| 2038 | 4.66E+07 | 6.10E+06 | 2.66E+06 | 2.94E+04 | 4.61E+05 | 9.44E+05 | 1.51E+04 | 5.75E+05 | 4.52E+05 | 1.86E+05 | 7.38E+03 | 8.83E+05 | 3.84E+04 | 5.08E+03 | 1.99E+02 | 1.40E+03 |
| 2039 | 4.70E+07 | 6.14E+06 | 2.73E+06 | 3.04E+04 | 4.63E+05 | 9.78E+05 | 1.51E+04 | 5.78E+05 | 4.53E+05 | 1.86E+05 | 7.53E+03 | 8.85E+05 | 3.91E+04 | 5.13E+03 | 2.01E+02 | 1.42E+03 |
| 2040 | 4.74E+07 | 6.18E+06 | 2.79E+06 | 3.15E+04 | 4.65E+05 | 1.01E+06 | 1.52E+04 | 5.81E+05 | 4.55E+05 | 1.85E+05 | 7.67E+03 | 8.87E+05 | 3.98E+04 | 5.18E+03 | 2.04E+02 | 1.43E+03 |
| 2041 | 4.78E+07 | 6.22E+06 | 2.85E+06 | 3.24E+04 | 4.67E+05 | 1.04E+06 | 1.52E+04 | 5.83E+05 | 4.55E+05 | 1.85E+05 | 7.80E+03 | 8.88E+05 | 4.04E+04 | 5.22E+03 | 2.06E+02 | 1.45E+03 |
| 2042 | 4.82E+07 | 6.25E+06 | 2.91E+06 | 3.34E+04 | 4.69E+05 | 1.07E+06 | 1.52E+04 | 5.85E+05 | 4.56E+05 | 1.84E+05 | 7.93E+03 | 8.90E+05 | 4.10E+04 | 5.26E+03 | 2.09E+02 | 1.46E+03 |
| 2043 | 4.85E+07 | 6.28E+06 | 2.96E+06 | 3.43E+04 | 4.71E+05 | 1.10E+06 | 1.53E+04 | 5.86E+05 | 4.57E+05 | 1.84E+05 | 8.06E+03 | 8.91E+05 | 4.16E+04 | 5.29E+03 | 2.11E+02 | 1.48E+03 |
| 2044 | 4.88E+07 | 6.31E+06 | 3.01E+06 | 3.52E+04 | 4.72E+05 | 1.13E+06 | 1.53E+04 | 5.87E+05 | 4.57E+05 | 1.83E+05 | 8.18E+03 | 8.92E+05 | 4.21E+04 | 5.33E+03 | 2.13E+02 | 1.49E+03 |
| 2045 | 4.91E+07 | 6.34E+06 | 3.07E+06 | 3.61E+04 | 4.74E+05 | 1.16E+06 | 1.53E+04 | 5.88E+05 | 4.57E+05 | 1.82E+05 | 8.29E+03 | 8.93E+05 | 4.26E+04 | 5.36E+03 | 2.14E+02 | 1.50E+03 |
| 2046 | 4.94E+07 | 6.36E+06 | 3.12E+06 | 3.70E+04 | 4.75E+05 | 1.19E+06 | 1.53E+04 | 5.89E+05 | 4.57E+05 | 1.81E+05 | 8.40E+03 | 8.93E+05 | 4.31E+04 | 5.39E+03 | 2.16E+02 | 1.51E+03 |
| 2047 | 4.96E+07 | 6.38E+06 | 3.16E+06 | 3.78E+04 | 4.76E+05 | 1.21E+06 | 1.53E+04 | 5.89E+05 | 4.57E+05 | 1.80E+05 | 8.51E+03 | 8.93E+05 | 4.36E+04 | 5.41E+03 | 2.18E+02 | 1.52E+03 |
| 2048 | 4.99E+07 | 6.40E+06 | 3.21E+06 | 3.87E+04 | 4.77E+05 | 1.24E+06 | 1.53E+04 | 5.89E+05 | 4.57E+05 | 1.79E+05 | 8.61E+03 | 8.93E+05 | 4.41E+04 | 5.44E+03 | 2.19E+02 | 1.53E+03 |
| 2049 | 5.01E+07 | 6.42E+06 | 3.26E+06 | 3.95E+04 | 4.78E+05 | 1.27E+06 | 1.52E+04 | 5.89E+05 | 4.56E+05 | 1.78E+05 | 8.71E+03 | 8.93E+05 | 4.45E+04 | 5.46E+03 | 2.21E+02 | 1.54E+03 |
| 2050 | 5.03E+07 | 6.43E+06 | 3.30E+06 | 4.03E+04 | 4.78E+05 | 1.29E+06 | 1.52E+04 | 5.89E+05 | 4.56E+05 | 1.77E+05 | 8.81E+03 | 8.92E+05 | 4.49E+04 | 5.48E+03 | 2.22E+02 | 1.55E+03 |

## Table S37b.Estimated UMS of vehicles in Japan in 2022−2050 following standard scenario (Pd−Nb)

| Year | Pd | Pt | Rh | Nd | Y | Pr | Sm | Dy | La | Ce | Li | In | Ta | Ti | Mo | Nb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2020 | 1.25E+02 | 3.13E+01 | 1.49E+01 | 1.21E+04 | 7.30E+01 | 2.95E+02 | 2.66E+02 | 6.70E+02 | 2.67E+02 | 8.16E+02 | 2.48E+04 | 1.52E+01 | 2.15E+02 | 2.72E+04 | 3.65E+04 | 6.38E+03 |
| 2021 | 1.23E+02 | 3.17E+01 | 1.47E+01 | 1.27E+04 | 7.18E+01 | 2.92E+02 | 2.63E+02 | 7.12E+02 | 2.62E+02 | 7.93E+02 | 2.72E+04 | 1.51E+01 | 2.14E+02 | 2.71E+04 | 3.63E+04 | 6.38E+03 |
| 2022 | 1.21E+02 | 3.26E+01 | 1.46E+01 | 1.33E+04 | 7.10E+01 | 2.89E+02 | 2.60E+02 | 7.55E+02 | 2.60E+02 | 7.71E+02 | 2.99E+04 | 1.50E+01 | 2.12E+02 | 2.71E+04 | 3.61E+04 | 6.39E+03 |
| 2023 | 1.19E+02 | 3.41E+01 | 1.44E+01 | 1.39E+04 | 7.07E+01 | 2.86E+02 | 2.58E+02 | 8.00E+02 | 2.59E+02 | 7.50E+02 | 3.28E+04 | 1.49E+01 | 2.11E+02 | 2.71E+04 | 3.59E+04 | 6.41E+03 |
| 2024 | 1.17E+02 | 3.62E+01 | 1.43E+01 | 1.45E+04 | 7.09E+01 | 2.84E+02 | 2.57E+02 | 8.47E+02 | 2.59E+02 | 7.31E+02 | 3.60E+04 | 1.49E+01 | 2.11E+02 | 2.72E+04 | 3.58E+04 | 6.44E+03 |
| 2025 | 1.16E+02 | 3.88E+01 | 1.42E+01 | 1.52E+04 | 7.16E+01 | 2.83E+02 | 2.56E+02 | 8.96E+02 | 2.61E+02 | 7.13E+02 | 3.94E+04 | 1.49E+01 | 2.11E+02 | 2.73E+04 | 3.56E+04 | 6.48E+03 |
| 2026 | 1.14E+02 | 4.19E+01 | 1.41E+01 | 1.58E+04 | 7.27E+01 | 2.82E+02 | 2.55E+02 | 9.47E+02 | 2.64E+02 | 6.96E+02 | 4.30E+04 | 1.49E+01 | 2.11E+02 | 2.75E+04 | 3.55E+04 | 6.53E+03 |
| 2027 | 1.13E+02 | 4.55E+01 | 1.40E+01 | 1.65E+04 | 7.42E+01 | 2.82E+02 | 2.55E+02 | 9.99E+02 | 2.69E+02 | 6.81E+02 | 4.68E+04 | 1.49E+01 | 2.11E+02 | 2.77E+04 | 3.55E+04 | 6.59E+03 |
| 2028 | 1.12E+02 | 4.96E+01 | 1.39E+01 | 1.72E+04 | 7.61E+01 | 2.82E+02 | 2.55E+02 | 1.05E+03 | 2.75E+02 | 6.67E+02 | 5.08E+04 | 1.50E+01 | 2.12E+02 | 2.79E+04 | 3.54E+04 | 6.65E+03 |
| 2029 | 1.10E+02 | 5.42E+01 | 1.38E+01 | 1.78E+04 | 7.84E+01 | 2.82E+02 | 2.55E+02 | 1.11E+03 | 2.82E+02 | 6.54E+02 | 5.50E+04 | 1.51E+01 | 2.13E+02 | 2.82E+04 | 3.54E+04 | 6.73E+03 |
| 2030 | 1.09E+02 | 5.92E+01 | 1.37E+01 | 1.85E+04 | 8.11E+01 | 2.83E+02 | 2.56E+02 | 1.16E+03 | 2.91E+02 | 6.42E+02 | 5.93E+04 | 1.52E+01 | 2.15E+02 | 2.84E+04 | 3.54E+04 | 6.81E+03 |
| 2031 | 1.08E+02 | 6.47E+01 | 1.37E+01 | 1.91E+04 | 8.41E+01 | 2.85E+02 | 2.57E+02 | 1.22E+03 | 3.00E+02 | 6.31E+02 | 6.36E+04 | 1.53E+01 | 2.16E+02 | 2.87E+04 | 3.54E+04 | 6.89E+03 |
| 2032 | 1.07E+02 | 7.08E+01 | 1.36E+01 | 1.97E+04 | 8.75E+01 | 2.86E+02 | 2.58E+02 | 1.27E+03 | 3.11E+02 | 6.22E+02 | 6.78E+04 | 1.54E+01 | 2.18E+02 | 2.90E+04 | 3.54E+04 | 6.97E+03 |
| 2033 | 1.07E+02 | 7.74E+01 | 1.35E+01 | 2.03E+04 | 9.11E+01 | 2.88E+02 | 2.59E+02 | 1.33E+03 | 3.23E+02 | 6.13E+02 | 7.19E+04 | 1.55E+01 | 2.19E+02 | 2.93E+04 | 3.53E+04 | 7.05E+03 |
| 2034 | 1.06E+02 | 8.45E+01 | 1.34E+01 | 2.08E+04 | 9.51E+01 | 2.89E+02 | 2.60E+02 | 1.38E+03 | 3.35E+02 | 6.06E+02 | 7.59E+04 | 1.56E+01 | 2.21E+02 | 2.96E+04 | 3.53E+04 | 7.12E+03 |
| 2035 | 1.05E+02 | 9.19E+01 | 1.34E+01 | 2.13E+04 | 9.93E+01 | 2.91E+02 | 2.61E+02 | 1.43E+03 | 3.49E+02 | 5.99E+02 | 7.97E+04 | 1.57E+01 | 2.23E+02 | 2.99E+04 | 3.53E+04 | 7.20E+03 |
| 2036 | 1.04E+02 | 9.98E+01 | 1.33E+01 | 2.18E+04 | 1.04E+02 | 2.92E+02 | 2.62E+02 | 1.47E+03 | 3.63E+02 | 5.93E+02 | 8.34E+04 | 1.58E+01 | 2.24E+02 | 3.02E+04 | 3.52E+04 | 7.27E+03 |
| 2037 | 1.03E+02 | 1.08E+02 | 1.32E+01 | 2.22E+04 | 1.08E+02 | 2.94E+02 | 2.63E+02 | 1.52E+03 | 3.78E+02 | 5.87E+02 | 8.70E+04 | 1.59E+01 | 2.26E+02 | 3.04E+04 | 3.52E+04 | 7.33E+03 |
| 2038 | 1.02E+02 | 1.17E+02 | 1.31E+01 | 2.26E+04 | 1.13E+02 | 2.96E+02 | 2.64E+02 | 1.57E+03 | 3.93E+02 | 5.82E+02 | 9.05E+04 | 1.60E+01 | 2.27E+02 | 3.07E+04 | 3.51E+04 | 7.40E+03 |
| 2039 | 1.02E+02 | 1.25E+02 | 1.30E+01 | 2.29E+04 | 1.18E+02 | 2.97E+02 | 2.65E+02 | 1.61E+03 | 4.09E+02 | 5.77E+02 | 9.39E+04 | 1.61E+01 | 2.29E+02 | 3.09E+04 | 3.50E+04 | 7.45E+03 |
| 2040 | 1.01E+02 | 1.34E+02 | 1.29E+01 | 2.33E+04 | 1.23E+02 | 2.99E+02 | 2.66E+02 | 1.65E+03 | 4.25E+02 | 5.73E+02 | 9.71E+04 | 1.62E+01 | 2.30E+02 | 3.11E+04 | 3.49E+04 | 7.51E+03 |
| 2041 | 9.98E+01 | 1.43E+02 | 1.28E+01 | 2.36E+04 | 1.28E+02 | 3.00E+02 | 2.67E+02 | 1.69E+03 | 4.41E+02 | 5.69E+02 | 1.00E+05 | 1.63E+01 | 2.31E+02 | 3.13E+04 | 3.48E+04 | 7.56E+03 |
| 2042 | 9.89E+01 | 1.52E+02 | 1.27E+01 | 2.39E+04 | 1.33E+02 | 3.02E+02 | 2.68E+02 | 1.73E+03 | 4.57E+02 | 5.65E+02 | 1.03E+05 | 1.64E+01 | 2.32E+02 | 3.15E+04 | 3.47E+04 | 7.61E+03 |
| 2043 | 9.80E+01 | 1.61E+02 | 1.25E+01 | 2.41E+04 | 1.38E+02 | 3.03E+02 | 2.68E+02 | 1.77E+03 | 4.73E+02 | 5.61E+02 | 1.06E+05 | 1.65E+01 | 2.33E+02 | 3.17E+04 | 3.45E+04 | 7.65E+03 |
| 2044 | 9.70E+01 | 1.70E+02 | 1.24E+01 | 2.44E+04 | 1.43E+02 | 3.04E+02 | 2.69E+02 | 1.81E+03 | 4.89E+02 | 5.57E+02 | 1.09E+05 | 1.65E+01 | 2.34E+02 | 3.18E+04 | 3.44E+04 | 7.69E+03 |
| 2045 | 9.60E+01 | 1.79E+02 | 1.23E+01 | 2.46E+04 | 1.48E+02 | 3.05E+02 | 2.70E+02 | 1.84E+03 | 5.05E+02 | 5.53E+02 | 1.12E+05 | 1.66E+01 | 2.35E+02 | 3.20E+04 | 3.42E+04 | 7.73E+03 |
| 2046 | 9.51E+01 | 1.88E+02 | 1.22E+01 | 2.48E+04 | 1.53E+02 | 3.06E+02 | 2.70E+02 | 1.88E+03 | 5.21E+02 | 5.49E+02 | 1.15E+05 | 1.67E+01 | 2.36E+02 | 3.21E+04 | 3.40E+04 | 7.76E+03 |
| 2047 | 9.40E+01 | 1.97E+02 | 1.20E+01 | 2.50E+04 | 1.58E+02 | 3.07E+02 | 2.70E+02 | 1.91E+03 | 5.36E+02 | 5.45E+02 | 1.17E+05 | 1.67E+01 | 2.37E+02 | 3.22E+04 | 3.38E+04 | 7.79E+03 |
| 2048 | 9.30E+01 | 2.06E+02 | 1.19E+01 | 2.52E+04 | 1.63E+02 | 3.08E+02 | 2.71E+02 | 1.95E+03 | 5.51E+02 | 5.41E+02 | 1.20E+05 | 1.67E+01 | 2.37E+02 | 3.23E+04 | 3.37E+04 | 7.82E+03 |
| 2049 | 9.20E+01 | 2.14E+02 | 1.18E+01 | 2.54E+04 | 1.68E+02 | 3.08E+02 | 2.71E+02 | 1.98E+03 | 5.67E+02 | 5.36E+02 | 1.22E+05 | 1.68E+01 | 2.38E+02 | 3.24E+04 | 3.34E+04 | 7.85E+03 |
| 2050 | 9.09E+01 | 2.23E+02 | 1.16E+01 | 2.55E+04 | 1.73E+02 | 3.09E+02 | 2.71E+02 | 2.01E+03 | 5.82E+02 | 5.32E+02 | 1.25E+05 | 1.68E+01 | 2.38E+02 | 3.25E+04 | 3.32E+04 | 7.87E+03 |

## Table S38. Sensitivity of parameters

| Parameter, x | Sensitivity, S(x) |  |
| --- | --- | --- |
|  | When x +10% | When x -10% |
| Metal concentration | 109.85% | 90.72% |
| Product weight | 110.00% | 90.00% |
| Product new-sale number | 110.02% | 89.97% |
| Product lifespan distribution shape parameter | 98.37% | 101.92% |
| Product lifespan distribution scale parameter | 86.44% | 116.33% |

The parameter that has the most significant influence on the model is the scale parameter of the product lifespan distribution, which implies that the model's accuracy depends on the availability and quality of the product lifespan data. Other parameters that significantly affect the model are the number of new sales, the product, the weight of the product, and the concentration of metal in the product.

# References

1.	Kamran, M., Chapter 10 - Electric vehicles and smart grids. In Fundamentals of Smart Grid Systems, Kamran, M., Ed. Academic Press: 2023; pp 431-460.

2.	Silva, C.; Farias, T., CHAPTER SEVEN - Evaluation of Energy Consumption, Emissions, and Costs of Plug-in Hybrid Vehicles. In Electric and Hybrid Vehicles, Pistoia, G., Ed. Elsevier: Amsterdam, 2010; pp 193-210.

3.	Hosseini, S. E.; Butler, B., An overview of development and challenges in hydrogen powered vehicles. International Journal of Green Energy 2020, 17, (1), 13-37.

4.	Sakai, S.-i.; Yoshida, H.; Hiratsuka, J.; Vandecasteele, C.; Kohlmeyer, R.; Rotter, V. S.; Passarini, F.; Santini, A.; Peeler, M.; Li, J.; Oh, G.-J.; Chi, N. K.; Bastian, L.; Moore, S.; Kajiwara, N.; Takigami, H.; Itai, T.; Takahashi, S.; Tanabe, S.; Tomoda, K.; Hirakawa, T.; Hirai, Y.; Asari, M.; Yano, J., An international comparative study of end-of-life vehicle (ELV) recycling systems. Journal of Material Cycles and Waste Management 2014, 16, (1), 1-20.

5.	National Development and Reform Commission of China. Notice on construction of anthropogenic mineral demonstration base (in Chinese): http://www.gov.cn/zwgk/2010-05/27/content_1614890.htm (Accessed May 2022).

6.	Deng, T.; Fu, C.; Zhang, Y., What is the connection of urban material stock and socioeconomic factors? A case study in Chinese cities. Resources, Conservation and Recycling 2022, 185, 106494.

7.	Castro, M. B. G.; Remmerswaal, J. A. M.; Reuter, M. A., Life cycle impact assessment of the average passenger vehicle in the Netherlands. The International Journal of Life Cycle Assessment 2003, 8, (5), 297-304.

8.	Elgowainy, A.; Han, J.; Ward, J.; Joseck, F.; Gohlke, D.; Lindauer, A.; Ramsden, T.; Biddy, M.; Alexander, M.; Barnhart, S. Cradle-to-grave lifecycle analysis of US light duty vehicle-fuel pathways: a greenhouse gas emissions and economic assessment of current (2015) and future (2025-2030) technologies; Argonne National Lab.(ANL), Argonne, IL (United States): 2016.

9.	Field, F. R., III; Wallington, T. J.; Everson, M.; Kirchain, R. E., Strategic Materials in the Automobile: A Comprehensive Assessment of Strategic and Minor Metals Use in Passenger Cars and Light Trucks. Environ. Sci. Technol. 2017, 51, (24), 14436-14444.

10.	Yano, J.; Xu, G.; Liu, H.; Toyoguchi, T.; Iwasawa, H.; Sakai, S.-i., Resource and toxic characterization in end-of-life vehicles through dismantling survey. Journal of Material Cycles and Waste Management 2019, 21, (6), 1488-1504.

11.	Kosai, S.; Matsui, K.; Matsubae, K.; Yamasue, E.; Nagasaka, T., Natural resource use of gasoline, hybrid, electric and fuel cell vehicles considering land disturbances. Resources, Conservation and Recycling 2021, 166, 105256.

12.	Bhuwalka, K.; Field, F. R., III; De Kleine, R. D.; Kim, H. C.; Wallington, T. J.; Kirchain, R. E., Characterizing the Changes in Material Use due to Vehicle Electrification. Environ. Sci. Technol. 2021, 55, (14), 10097-10107.

13.	United States Geological Survey, Minerals Yearbook - Metals and Minerals. https://www.usgs.gov/centers/national-minerals-information-center/minerals-yearbook-metals-and-minerals (Accessed June, 2023）.

14.	National Bureau of Statistics of China. National data (in Chinese): https://data.stats.gov.cn/index.htm (Accessed May 2022).

15.	Japan Automobile Manufacturers Association, The motor industry of Japan 2022. https://www.jama.org/the-motor-industry-of-japan-2022/ (Accessed June, 2023）.

16.	Zeng, X.; Ali, S. H.; Tian, J.; Li, J., Mapping anthropogenic mineral generation in China and its implications for a circular economy. Nature Communications 2020, 11, (1), 1544.

17.	Xu, G.; Yano, J.; Sakai, S.-i., Recycling Potentials of Precious Metals from End-of-Life Vehicle Parts by Selective Dismantling. Environ. Sci. Technol. 2019, 53, (2), 733-742.

18.	Sharif, M. N.; Islam, M. N., The Weibull distribution as a general model for forecasting technological change. Technological Forecasting and Social Change 1980, 18, (3), 247-256.

19.	Zheng, J.; Zhou, Y.; Yu, R.; Zhao, D.; Lu, Z.; Zhang, P., Survival rate of China passenger vehicles: A data-driven approach. Energy Policy 2019, 129, 587-597.

20.	International Energy Agency, End-of-life recycling rates for selected metals. https://www.iea.org/data-and-statistics/charts/end-of-life-recycling-rates-for-selected-metals (Accessed June, 2023）.

21.	Recycling Rates of Metals: A Status Report. United Nations Environment Programme (UNEP), Nairobi, Kenya (2011).