Supplementary Information for

A sustainable electrolyte towards dendrite-free and long-lasting zinc-metal batteries

Wei Zhang1,6, Ruwei Chen1,6, Yuhang Dai1,6, Gongxun Lu2, Mengtian Zhang2, Xian Wu2, Zijuan Du1, Xuan Gao1, Fei Guo1, Chumei Ye3, Haobo Dong1, Jiexin Zhu1, Wei Zong1, Zhenming Xu4*, Peie Jiang1, Mingqiang Liu1, Yulun Wu5, Zheng Li5, Guanjie He1* & Ivan P. Parkin1*

1 Christopher Ingold Laboratory, Department of Chemistry, University College London, London WC1H 0AJ, UK

2 Tsinghua Shenzhen International Graduate School, Tsinghua University, Shenzhen 518055, P. R. China

3 Department of Materials Science and Metallurgy, University of Cambridge, Cambridge CB3 0FS, UK

4 Jiangsu Key Laboratory of Electrochemical Energy Storage Technologies, College of Materials Science and Technology, Nanjing University of Aeronautics and Astronautics, Nanjing 210016, P. R. China

5 School of Metallurgy and Environment, Central South University, Changsha 410083, P. R. China

6 These authors contributed equally: Wei Zhang, Ruwei Chen, Yuhang Dai.

*E-mail: xuzhenming@nuaa.edu.cn; g.he@ucl.ac.uk; i.p.parkin@ucl.ac.uk;

This PDF file includes:

Supplementary Figs. 1 to 23.

Supplementary Tables 1 to 2.

Supplementary Figures and Tables

Supplementary Fig. 1∣3D partial enlarged snapshots representing Zn2+ solvation structure obtained from MD simulations of a pure ZnSO4 system and b MU/ZnSO4 system (grey balls: Zn atoms; red balls: O atoms; pink balls: H atoms; yellow balls: S atoms; blue balls: N atoms; brown balls: C balls).

Supplementary Fig. 2∣Illustration of desolvation process of Zn2+ from Zn(H2O)62+ in the pure ZnSO4 electrolyte.

Supplementary Fig. 3∣Illustration of desolvation process of Zn2+ from the electrolyte with MU.

Supplementary Fig. 4∣Nyquist plots of the Zn||Zn symmetric cells in electrolytes a without MU, b with MU at various temperatures.

Supplementary Fig. 5∣Digital photographs of the electrolytes with different concentrations of MU.

Supplementary Fig. 6∣Raman spectra of the electrolytes with/without MU.

Supplementary Fig. 7∣a Local Raman spectra for 1 M ZnSO4 with/without MU additives. b Two different Zn2+ solvation structures in MU/ZnSO4 electrolyte.

Supplementary Fig. 8∣FT-IR spectra of the electrolytes with/without MU.

Supplementary Fig. 9∣Enlarged FT-IR spectra of electrolytes containing different MU additives.

Supplementary Fig. 10∣Coulombic efficiencies of Zn||Cu cells containing different contents of MU additives at 1 mA cm-2 with a capacity of 0.5 mAh cm-2.

Supplementary Fig. 11∣Electric double layer capacitance (EDLC) measurements for Zn||Zn symmetric cells with/without MU additive. CV curves within -15 mV ~ 15 mV at different scan rates in the el	ectrolyte without a with c without MU additive. The plots of capacitive currents density vs. scan rate for the cell cycled in the electrolyte b with d without MU additive.

Supplementary Fig. 12∣a In-situ electrochemical impedance spectroscopy (EIS) was carried out to study the transport kinetics of Zn||Zn symmetric cells upon continuous discharge/rest. The data were obtained after orderly discharging and standing for 4 min at 0.5 mA cm-2.1 EIS curves of Zn||Zn symmetric cells b without MU and c with MU.

Supplementary Fig. 13∣SEM image of the pristine zinc foil (top view).

Supplementary Fig. 14∣SEM images of Zn deposits on a substrate (Zn||Zn symmetric cells) at 5 mAcm-2 and 1 mA h cm-2 for 100 cycles in a 1 M ZnSO4 (BE) and b 1 M ZnSO4 + 500 mM MU (DE).

Supplementary Fig. 15∣Electrolyte potentials: a without MU b with MU.

Supplementary Fig. 16∣Zinc deposition thickness in different positions on the substrate along deposition time in the electrolyte: a without MU; b with MU.

Supplementary Fig. 17∣Rate performances of the Zn||Zn symmetric cell with MU additive at various current densities with a capacity of 1 mA h cm-2.

Supplementary Fig. 18∣XRD pattern (Mo Kα radiation) of the commercial MnO2.

Supplementary Fig. S19∣Charge/discharge curves of Zn||MnO2 full cell under different current densities with MU additive.

Supplementary Fig. 20∣Charge/discharge curves of Zn||MnO2 full cell under different current densities without MU additive.

Supplementary Fig. 21∣CV curves of Zn||MnO2 full cells with/without MU additive.

Supplementary Fig. 22∣Charge/discharge curves at different cycles of the Zn||AC capacitor with MU additive.

Supplementary Fig. 23∣Charge/discharge curves at different cycles of the Zn||I2 full cell with MU additives at 2 A g-1.

Supplementary Table 1∣Summary of application of DRT peaks from a Zn||Zn symmetric cell.

| DRT peak | Approximate time constant, τ | Assignment |
| --- | --- | --- |
| P1 | 13.2-20 μs | Double-layer relaxation |
| P2 | 21.9-44.5μs | Solid-electrolyte interphase |
| P3 | 0.11-0.5 ms | Positive electrode charge transfer |
| P4 | 1.2-3.3 ms | Positive electrode charge transfer |
| P5 | 11-56 ms | Positive electrode charge transfer |
| P6 | 0.3-0.91 s | Diffusion |
| P7 | 3.95-12.02 s |  |

Supplementary Table 2∣Comparison of the cumulative plating capacity of the ZnSO4-MU electrolyte with recently reported Zn metal anodes with electrolyte additives optimization.

| Electrolyte (M: mol L-1; m: mol kg-1) | Current Density (mA cm-2) | Capacity (mAh cm-2) |  | Cycle Life (h) | Cumulative Capacity (mAh cm-2) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 M ZnSO4+500 mM MU | 10 |  | 1 | 1600 | 8000 | This work |
| 0.5 M ZnSO4-7H2O-3DMF (H2O/DMF = 7:3 by volume) | 3 |  | 1 | 1100 | 1650 | 2 |
| 1 M ZnSO4+0.5 wt % silk fibroin | 1 |  | 1 | 1600 | 800 | 3 |
| 2 M ZnSO4+ 0.2 g L-1 CeCl3 | 2 |  | 1 | 2600 | 2600 | 4 |
| 1 M ZnSO4+10 mM glucose | 1 |  | 1 | 2000 | 1000 | 5 |
| 2 M ZnSO4+8 mg mL-1 PASP | 0.5 |  | 0.5 | 3200 | 800 | 6 |
| 2 M ZnSO4+0.0085 M La(NO3)3 | 1 |  | 1 | 1200 | 600 | 7 |
| 3 M ZnSO4+0.25 mM PFOA | 1 |  | 0.5 | 2200 | 1100 | 8 |
| 1 M ZnSO4+5 vol % NMP | 1 |  | 1 | 1500 | 750 | 9 |
| 1 M Zn(ClO4)2+10 mM β-CD | 1 |  | 1 | 1000 | 500 | 10 |
| 3 M ZnSO4+10 mM TH | 5 |  | 1 | 700 | 350 | 11 |
| 0.5 M Zn(CF3SO3)2 in DMMP and H2O (molar ratio 3:2) | 1 |  | 1 | 2500 | 1250 | 12 |
| 1 M Zn(CF3SO3)2+25 mM Zn(H2PO4)2 | 1 |  | 1 | 1200 | 600 | 13 |
| 2 M ZnSO4 in DMA/H2O (volumetric ratio: 2: 20) | 1 |  | 1 | 1900 | 950 | 14 |

*Note: Dimethylformamide (DMF); Polyaspartic Acid (PASP); Perfluorooctanoic Acid (PFOA); N-Methyl Pyrrolidone (NMP); β-Cyclodextrin (β-CD); Threonine (TH); Dimethyl Methylphosphonate (DMMP); N, N-Dimethylacetamide (DMA).

Supplementary references

1.	Wan J. et al. A Double-Functional Additive Containing Nucleophilic Groups for High-Performance Zn-Ion Batteries. ACS Nano 17, 1610−1621 (2023).

2.	Zou P. et al. Localized Hydrophobicity in Aqueous Zinc Electrolytes Improves Zinc Metal Reversibility. Nano Lett. 22, 7535-7544 (2022).

3.	Xu J. et al. In Situ Construction of Protective Films on Zn Metal Anodes via Natural Protein Additives Enabling High-Performance Zinc Ion Batteries. ACS Nano 16, 11392−11404 (2022).

4.	Hu Z. et al. A Self-Regulated Electrostatic Shielding Layer toward Dendrite-Free Zn Batteries. Adv. Mater. 34, 2203104 (2022).

5.	Sun P. et al. Simultaneous Regulation on Solvation Shell and Electrode Interface for Dendrite-Free Zn Ion Batteries Achieved by a Low-Cost Glucose Additive. Angew. Chem. Int. Ed. 60, 18247-18255 (2021).

6.	Zhou T. et al. Toward stable zinc aqueous rechargeable batteries by anode morphology modulation via polyaspartic acid additive. Energy Storage Mater. 45, 777-785 (2022).

7.	Zhao R. et al. Lanthanum nitrate as aqueous electrolyte additive for favourable zinc metal electrodeposition. Nat. Commun. 13, 3252 (2022).

8.	Zhao F. et al. Trace amounts of fluorinated surfactant additives enable high performance zinc-ion batteries. Energy Storage Mater. 53, 638-645 (2022).

9.	Wang D. et al. In Situ Formation of Nitrogen-Rich Solid Electrolyte Interphase and Simultaneous Regulating Solvation Structures for Advanced Zn Metal Batteries. Angew. Chem. Int. Ed. 61, e202212839 (2022).

10.	Qiu M. et al. Anion-Trap Engineering toward Remarkable Crystallographic Reorientation and Efficient Cation Migration of Zn Ion Batteries. Angew. Chem. Int. Ed. 61, e202210979 (2022).

11.	Miao Z. et al. Unveiling unique steric effect of threonine additive for highly reversible Zn anode. Nano Energy 97,  (2022).

12.	Liu S. et al. Monolithic Phosphate Interphase for Highly Reversible and Stable Zn Metal Anode. Angew. Chem. Int. Ed. 62, e202215600 (2023).

13.	Zeng X. et al. Electrolyte Design for In Situ Construction of Highly Zn2+-Conductive Solid Electrolyte Interphase to Enable High-Performance Aqueous Zn-Ion Batteries under Practical Conditions. Adv. Mater. 33, 2007416 (2021).

14.	Wu F. et al. Achieving Highly Reversible Zinc Anodes via N, N‐Dimethylacetamide Enabled Zn‐Ion Solvation Regulation. Small 18, 2202363 (2022).