| Entry | Catalyst (g or ml) | Conditions | Time (min) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | ChCl (0.04 g) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 15 | 25 |
| 2 | Glucose (0.04 g) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 15 | 30 |
| 3 | Glucose/ChCl (0.1 ml) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 15 | 95 |
| 4 | Glucose/ChCl (0.1 ml) | Water (0.1 ml)/Ethanol (0.1 ml)/70 °C | 15 | 94 |
| 5 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.03 g) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 10 | 95 |
| 6 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.02 g) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 10 | 89 |
| 7 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.04 g) | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 10 | 95 |
| 8 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.03 g) | Water (0.1 ml)/60 °C | 10 | 72 |
| 9 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.03 g) | Ethanol (0.1 ml)/60 °C | 10 | 75 |
| 10 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.03 g) | Water (0.1 ml)/Ethanol (0.1 ml)/50 °C | 10 | 83 |
| 11 | Fe3O4@Si-(CH2)3-ChCl/Glu (0.03 g) | Water (0.1 ml)/Ethanol (0.1 ml)/70 °C | 10 | 94 |
| 12 | --b | Water (0.1 ml)/Ethanol (0.1 ml)/60 °C | 50 | --c |
| aReaction conditions: benzaldehyde (1 mmol), ethyl acetoacetate (1 mmol ) and hydroxylamine hydrochloride (1 mmol) . bThis reaction was carried out in the absence of Fe3O4@Si-(CH2)3-ChCl/Glu . cNo product 4a observed. |  |  |  |  |

Table 1.

| Entry | Products (4a-l) | Fe3O4@Si-(CH2)3-ChCl/Glu |  | Mp (°C) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | ChCl/Glu |  | Found | Lit. |
|  |  | Yielda (%) | Time (min) |  |  |
| 4a |  | 95 | 10 | 140-141 | 140-14125 |
|  |  | 95 | 15 |  |  |
| 4b |  | 96 | 5 | 173-174 | 173-17425 |
|  |  | 95 | 10 |  |  |
| 4c |  | 90 | 10 | 138-139 | 137-13926 |
|  |  | 90 | 15 |  |  |
| 4d |  | 92 | 10 | 201-203 | 200-20127 |
|  |  | 92 | 15 |  |  |
| 4e |  | 93 | 7 | 219-220 | 220-22125 |
|  |  | 92 | 10 |  |  |
| 4f |  | 92 | 10 | 135-137 | 134-13528 |
|  |  | 92 | 15 |  |  |
| 4g |  | 90 | 10 | 134-135 | 130-13229 |
|  |  | 90 | 15 |  |  |
| 4h |  | 85 | 10 | 211-212 | 210-21127 |
|  |  | 85 | 15 |  |  |
| 4i |  | 95 | 5 | 134-135 | 134-13630 |
|  |  | 95 | 10 |  |  |
| 4j |  | 90 | 10 | 142-144 | 143-14425 |
|  |  | 90 | 15 |  |  |
| 4k |  | 92 | 10 | 195-196 | 193-19431 |
|  |  | 90 | 15 |  |  |
| 4l |  | 88 | 10 | 179-181 | 180-18232 |
|  |  | 85 | 15 |  |  |

Table 2.