SUPPLEMENTARY MATERIALS

High-performance pyrite nano-catalyst driven photothermal/chemodynamic synergistic therapy for Osteosarcoma

Meirong Li1,2,#, Minghua Wang1,#, Junfeng Huang4,#,  Shiqi Tang1, Jingyu Yang1, Zhourui Xu2, Gaixia Xu2, Xin Chen2, Jia Liu1,*, Chengbin Yang2,*

*Correspondence: liujia870702@126.com; cbyang@szu.edu.cn

1Central Laboratory, The Second Affiliated Hospital of the Chinese University of Hong Kong, Shenzhen & Longgang District People’s Hospital of Shenzhen, Shenzhen 518172, Guangdong, P. R. China

2Guangdong Key Laboratory for Biomedical Measurements and Ultrasound Imaging, School of Biomedical Engineering, Shenzhen University Medical School, Shenzhen University, Shenzhen 518060, Guangdong, P. R. China

3Pathology department, The Second Affiliated Hospital of the Chinese University of Hong Kong, Shenzhen & Longgang District People’s Hospital of Shenzhen, Shenzhen 518172, Guangdong, P. R. China

4School of Mechanical Engineering, Dongguan University of Technology, Dongguan 523808, Guangdong, P. R. China.

## Fig. S1 SEM image of FeS2 NPs, scale bar = 1 μm.

## Figure S2. Survey XPS spectrum of FeS2 NPs

## Figure S3. EDX-elemental mapping of (A) FeS2 NPs, (B) FeS2@CSS NPs and (C) FeS2@CP NPs, scale bar = 50 nm.

## Table S1. Chemical compositions of FeS2 NPs, FeS2@CSS NPs and FeS2@CP NPs via EDX analysis.

| Sample Element | k-line factor | Entry |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | FeS2 |  | FeS2@CSS |  | FeS2@CP |  |
|  |  | wt % | atom % | wt % | atom % | wt % | atom % |
| S | 0.980 | 56.32 | 69.19 | 42.03 | 38.41 | 38.97 | 35.14 |
| Fe | 1.214 | 43.68 | 30.81 | 37.84 | 19.91 | 39.51 | 20.47 |
| C | 3.115 | - | - | 8.2 | 20.01 | 9.36 | 22.53 |
| O | 1.455 | - | - | 9.96 | 19.82 | 8.75 | 15.81 |
| Na | 1.124 | - | - | 1.97 | 1.85 | 1.21 | 1.52 |
| N | 1.807 | - | - | - | - | 2.2 | 4.53 |

## Fig. S4 (A) Zeta potential values of FeS2-based NPs tested by DLS. All data were expressed as the mean ± SD, n = 3. (B) Precipitation of FeS2-based NPs in aqueous solution after overnight standing.

## Fig. S5 The catalytic activity of FeS2 NPs as Fenton reagents. (A) The concentration-, (B) pH-, and (C) temperature-dependent Fenton catalytic activity of FeS2 NPs with H2O2 substrate. All data were expressed as the mean ± SD (n = 3. Statistics were done using one-way ANOVA with Tukey multi-comparisons. *p < 0.05, **p < 0.01, ***p < 0.001 and ns, no significance).

## Fig. S6 UV-Vis absorption spectrum for FeS2 NPs, FeS2@CSS NPs and FeS2@CP NPs.

## Fig. S7  (A) Quantitative analysis of cell uptake rates and (B) the mean fluorescence intensity (MFI) analysis on U2-OS cells treated with FeS2-based NPs detected by flow cytometry. Blk: Blank. All data were expressed as the mean ± SD (n = 3. Statistics were done using one-way ANOVA with Tukey multi-comparisons. *p < 0.05, **p < 0.01, ***p < 0.001 and ns, no significance).

## Fig. S8 (A) Biodegradation of FeS2-based NPs in pH 4.5 and pH 7.4 buffer (mimicking lysosome and cytoplasm environment, respectively). (B) Hemolysis assay of FeS2-based NPs with different concentrations.

## Fig. S9 Routine blood values analysis for the BALB/c mice treated with PBS and different FeS2-based NPs for 15 days. WBC: white blood cell count, Lymph: lymphocyte count, Mid: intermediate cell count, Gran: granulose count, Lymph %: percentage of lymphocytes, Mid %: percentage of intermediate cells, Gran %: percentage of granulose, RBC: red blood cell count, HGB: Hemoglobin, HCT: hematocrit, MCV: mean corpuscular volume, MCH: mean corpuscular hemoglobin, MCHC: mean corpuscular hemoglobin concentration, RDW-CV: coefficient of variation of red cell distribution width, RDW-SD: red cell distribution width, PLT: platelet count, MPV: mean platelet volume, PDW: platelet distribution width, PCT: plateletcrit. All data were expressed as the mean ± SD (n = 4, one-way ANOVA and Tukey multi-comparisons. ns, no significance).

## Fig. S10 Blood biochemistry analysis for the BALB/c mice treated with PBS and different FeS2-based NPs for 14 days. γ-GT: gamma-glutamyl transferase, ALP: alkaline phosphatase, ALT: alanine transaminase, AST: aspartate transaminase, CK: creatine kinase, α-HBDH: α-hydroxybutyrate dhehydrogenase, LDH: lactate dehydrogenase, GLU: blood glucose, TG: triglyceride, D-BIL: direct bilirubin, UA: uric acid, TC: total cholesterol, HDL-C: high-density lipoprotein cholesterol, LDL-C: low-density lipoprotein cholesterol, ALB: albumin. All data were expressed as the mean ± SD (n = 4, one-way ANOVA and Tukey multi-comparisons. ns, no significance).

## Fig. S11 (A) Bodyweight changes of the BALB/c mice during a 15-day treatment of PBS and different FeS2-based NPs. (B) Major organ indexes of mice in each group at treatment endpoint. All data were expressed as the mean ± SD (n = 4, one-way ANOVA with Tukey multi-comparisons. ns, no significance).

## Fig. S12 Representative microphotographs of H&E staining of the sections from the major organs collected from the BALB/c mice at the treatment endpoint. Scale bar = 200 μm.

## Fig. S13 Anti-cancer efficacy of FeS2-based NPs in U2-OS cells. Intracellular ROS level assessed with (A) the percentages of cells producing ROS and (B) the MFI of ROS detected by flow cytometry with DCFH-DA probe in U2-OS cells after FeS2-based NPs treatment for 24 h. (C) Intracellular LPO level detected by flow cytometry with C11-BODIPY 581/591 in U2-OS cells after FeS2-based NPs treatment for 24 h. (D) Quantitative MFI analysis of LPO recorded in panel (C). Loss of intracellular GSH assessed with (E) the rate of GSH/total glutathione and (F) the rate of GSH/GSSG in U2-OS cells after FeS2-based NPs treatment for 24 h. (G) Western blot analysis of GPX4 expression in U2-OS cells treated with different nano-formulations for 24 h with or without laser irradiation, and (H) GPX4 protein expression was quantified and normalized with β-actin. (I) Quantitative analysis of JC-1 monomers rate to assess the mitochondrial membrane potential of U2-OS cells induced by FeS2-based NPs treatment for 24 hours. (J) Quantitative analysis U2-OS cells apoptosis induced by FeS2-based NPs treatment for 24 hours. (K) Cell viability of U2-OS cells was analyzed by a CCK-8 assay after the treatment with FeS2-based NPs for 24 h. All data were expressed as the mean ± SD (n = 3. Statistics were done using one-way ANOVA with Tukey multi-comparisons. *p < 0.05, **p < 0.01, ***p < 0.001 and ns, no significance).

## Fig. S14 Flow cytometry detection of mitochondrial membrane potential with JC-1 probe on MNNG-HOS cells treated with different concentrations of FeS2-based NPs for 24 h.

## Fig. S15 Flow cytometry detection of mitochondrial membrane potential with JC-1 probe on U2-OS cells treated with different concentrations of FeS2-based NPs for 24 h.

## Fig. S16 Flow cytometry detection of apoptosis with Annexin V/FITC and PI on MNNG-HOS cells treated with different concentrations of FeS2-based NPs for 24 h.

## Fig. S17 Flow cytometry detection of apoptosis with Annexin V/FITC and PI on U2-OS cells treated with different concentrations of FeS2-based NPs for 24 h.

## Fig. S18 (A) In vivo photothermal images of MNNG-HOS tumor-bearing mice intratumorally injected with PBS and different FeS2-based NPs dispersion activated by 1 W/cm2 1064 nm laser for 10 min. The dotted circle represents the tumor site. (B) The temperature increased curve of tumor area under laser irradiation, n = 3.

## Fig. S19. (A) Bodyweight changes of the MNNG-HOS tumor-bearing BALB/c nude mice during the treatment of the test groups (B) Main organ index of mice in each test group at treatment endpoint. All data were expressed as the mean ± SD (n = 5, one-way ANOVA with Tukey multi-comparisons. ns, no significance).

## Fig. S20. Representative microphotographs of H&E staining of the sections from the major organs collected from the MNNG-HOS tumor-bearing BALB/c nude mice in different groups at the treatment endpoint. Scale bar = 200 μm.