Supplementary Information for

High-strength and crack-free welding of unweldable aluminum alloys via novel Zr-core-Al-shell wires

Jun Jin1, Shaoning Geng1,*, Leshi Shu1, Ping Jiang1,*, Xinyu Shao1, Chu Han1, Liangyuan Ren1, Yuantai Li1, Lu Yang1 & Xiangqi Wang2

The State Key Laboratory of Digital Manufacturing Equipment and Technology, School of Mechanical Science and Engineering, Huazhong University of Science & Technology, Wuhan, Hubei, 430074, China. 2 Jihua Laboratory Testing Center, Jihua Laboratory, Foshan, PR China.

*email: sngeng@163.com; jiangping@hust.edu.cn

### 1. The phase filed (PF) modelling

Supplementary Fig. 1 shows the temperature histories of weld centre at different locations. The average cooling rate was used for phase field (PF) modelling.

Supplementary Fig. 1 Temperature histories of weld centre with experimental measurement

The phase-field (PF) model developed by Takaki and Ohno1,2 was adopted in this study. The governing equations of ϕ and u of the PF are as follows:

(1)

(2)

Eq. (1) represents the time evolution of the PF. τ0 = a2λW0/Dl is the relaxation time, W0 is the interface thickness, and λ = a1W0/d0 is the coupling constant associated with the thermodynamic driving force. The numerical constants a1 and a2 are a1= 0.8839 and a2= 0.6267. d0= kГ/m(1 - k)c0 is the chemical capillary length, where k is the partition coefficient, m is the liquidus slope, c0 is the initial concentration in the liquid, and Г is the Gibbs–Thomson coefficient. as(n) is the crystalline anisotropy, which is given as:

(3)

where ε4 is the anisotropic strength. u' = (T - Ts)/(Tl - Ts) is the nondimensional temperature undercooling. The polynomials f(ϕ) and g(ϕ) are given as df(ϕ)/dϕ = −ϕ + ϕ3 and dg(ϕ)/dϕ = (1 − ϕ2)2. According to the mixture rule, the local concentration c is given by c = [(1 + ϕ)cs + (1 - ϕ)cl]/2, where cl and cs are the solute concentration in the liquid and solid phases, respectively. cl and cs satisfy the relation k = cse/cle = cs/cl, where cse and cle are the equilibrium concentrations in the solid and liquid, respectively. Eq. (2) represents the time of the solute diffusion equation. Dimensionless supersaturation u is defined as follows:

(4)

Dl and Ds are the solute diffusivities in liquids and solids, respectively.is the anti-trapping current, which is given by jAT = -(1-kDs/Dl)(2/2)W0[1+(1-k)u](∂ϕ/∂t)∇ϕ/∇ϕ. q(ϕ) is an interpolating function given by q(ϕ) = [kDs+Dl+(kDs-Dl)]ϕ/(2Dl). J is the fluctuating current of a random Gaussian number.

### 2. Estimating the strengthening contributions

Supplementary Table 1: Estimates of the various strengthening contributions for the
fusion zone

| Materials | σ0 (MPa) | Δσgb (MPa) | Δσppt (MPa) | Δσss (MPa) | Δσdis (MPa) | ΔσyCal (MPa) |
| --- | --- | --- | --- | --- | --- | --- |
| FZ | 10 | 125 | 6 | 67.3 | 56.3 | 265 |

Supplementary Fig. 2: Engineering stress-strain curves of the base materials. (Dashed line shows their 0.2% yield point)

Supplementary Fig. 3: Engineering stress-strain curves of the different filler materials

Supplementary Fig. 4: Distribution of the GND density of the welds

Supplementary Fig. 5: TEM-EDX characteristics of precipitates in the interiors of

grains in the FQZ. a, STEM-HAADF mode. b, Corresponding EDX mapping image

Supplementary Fig. 6: SEM (BSE mode) characteristics of the fusion zone

Supplementary Fig. 7: SEM-EDS characteristics of the fusion zone. a, SEM image. b, c, d, e, f, EDS spectra of the substrate.

### Supplementary References

- Takaki, T. et al. Competitive grain growth during directional solidification of a polycrystalline binary alloy: Three-dimensional large-scale phase-field study. Materialia. 1, 104-113 (2018).

- Takaki, T. et al. Two-dimensional phase-field simulations of dendrite competitive growth during the directional solidification of a binary alloy bicrystal. Acta Mater. 81, 272-283 (2014).