Supplementary Information

A new screen-printed carbon sensor gold nanoparticles/kaolinite mineral: electrochemical analysis of Propyphenazone and the investigation of ds-DNA interaction

Ceren Yıldız, Dilek Eskiköy Bayraktepe and Zehra Yazan*

Ankara University, Faculty of Science Department of Chemistry, Ankara, Turkiye

* Corresponding author.

E-mail address: zdurmus@science.ankara.edu.tr (Z. Yazan)

Fig. S1 CV voltammograms of 0.05 mM HAuCl4 with the scan rate of 50 mVs-1 in 0.05 M H2SO4, pH 2.0. Number of cycle: 15

a

b

c

Fig. S2 Optimization of (a) HAuCl4 concentrations (b) HAuCl4 number of scans and (c) Kao content for the oxidation of 30.0 µM PRO using DPV method in ABS buffer solution, pH 4.5

Fig. S3 CV voltammograms of 5.0 mM of [Fe(CN)6]3−/4− containing 0.1 M KCl solution at a scan rate of 0.05 Vs-1 on Kao–GNPs/SPCE

Table S1 The RSD% values of the CVs given in Fig. S3

|  | RSD%* |
| --- | --- |
| Anodic peak current | 1.03 |  |
| Anodic peak potential | 1.51 |  |
| Cathodic peak current | 0.60 |  |
| Cathodic peak potential | 0.80 |  |

* RSD is the relative standard deviation of 10 replications.

Fig. S4 DPV responses of 1.0 µM PROP with interfering substances at the ratio of 1:1