Supplemental Material (Appendix)

Estimated and observed nucleation densities of electrodeposited Cu and Cu-Ag particles at n-Si(001) substrate

Yunkai Suna*, Giovanni Zangaria

a. Department of Materials Science and Engineering, University of Virginia, Charlottesville, VA, 22904, USA

* Corresponding authors. Yúnkāi Sūn, Email: ys3ej@virginia.edu; Giovanni Zangari, Email: gz3e@virginia.edu

Appendix-A: Evaluating the impact of the rate of concentration drop at the electrode/electrolyte interface under large deposition overpotentials.

All the models mentioned in the main text of this paper assume complete diffusion control behavior, that the concentration at the electrode/electrolyte interface immediately drops to 0 right after the beginning of the deposition. However, when the exchange current and the applied deposition overpotential are small, the transient concentration drop at the electrode/electrolyte interface may impact the modeling and analysis of the potentiostatic transients during the initial stage of electrodeposition. In this section, we will propose a method to estimate the timescale of such behavior.

Assuming the system follows a one-step electron transfer process and ignoring the anodic branch by assuming a large deposition overpotential (Tafel behavior) [1], we have the electrode kinetics with the local concentration (note that Ei0 is the standard electrode potential with concentration of depositing species ~10-3 mol/cm3).

For single-step electrochemical reactions, we have the relationship [1]:

ji=zFKfC0,t-Kba0,t#Eqn.A1

In which Kf and Kb are positive numbers indicating the reaction kinetics. Therefore, we use the convention ji for the reduction current of Cu(II)/Cu.

Where a0,t≈1 is the activity of the deposit at the surface of the substrate. Assuming large overpotential, we could ignore the anodic branch and have:

ji≈zFKfC0,t#Eqn.A2

For Cu electrodeposition, from the experimental results (exchange current [2] and electrode kinetics [3]), with 0.5M H2SO4, we have the exchange current and the electrode kinetics:

j0=1.58×10-3C0,t0.67exp-0.36CH2SO4  A/cm2 with Ci in mol/L #Eqn.A3

j=j0exp-αcηF/RT-expαaηF/RT,  αc=0.49,  αa=1.3 #Eqn.A4

By neglecting the anodic branch, we have:

j=1.58×10-3C0,t0.67exp-0.36CH2SO4⋅exp-αcηF/RT   A/cm2 with Ci in mol/L#Eqn.A5

Meanwhile, the overpotential is defined based on the equilibrium potential of the Cu with C0,st=1 mol/L:

η=E-Eeq=E-E0+RTzFlnC0,tC0,st#Eqn.A6

Therefore, we have the deposition current:

j=j0exp-αcFRTE-E0+RTzFlnC0,tC0,st#Eqn.A7

Simplify, with αC=0.49 and j0 from eqn.(A3), we have:

j=1.58×10-3C0,t0.915C0,st0.245exp-0.36CH2SO40⋅exp-αCFRTE-E0    A/cm2 with Ci in mol/L #Eqn.A8

Define K0=1.58×10-3zFC0,st0.245exp-0.36CH2SO40, and compare with eqn.(A2), we have:

Kf=K0exp-αCFRTE-ECuII/Cu0CCuSO4×103-0.085#Eqn.A9

Note that ECuII/Cu0 is the standard electrode potential for Cu2+/Cu with 1 mol/L Cu2+. The unit of CCuSO4 is mol/cm3 instead of mol/L.

Despite Cu electrodeposition from sulfuric acid being a multi-step reaction with the rate-limiting step of Cu(II)/Cu(I) [3], combining the measured value from the two references leads to a C0,t-0.085 difference from the theory. To apply the analytical solution from the heat-transfer problem, we assume that this value is small and decided to completely ignore such differences, leading to:

jizF=-KfC0,t,  Kf≈K0exp-αCFRTE-ECuII/Cu0#Eqn.A10

With E=-0.85 VSMSE and ECuII/Cu0=-0.313 VSMSE, we have K0=6.838×10-6 cm/s and Kf=0.229 cm/s, corresponding to a deposition current of 441 mA/cm2 with 10mM Cu(II) at the electrolyte/electrode interface.

Using the electrode kinetics as the boundary condition, we solve the following semi-infinite planar diffusion problem:

∂Cx,t∂t=D∂2Cx,t∂x2#Eqn.A11a

Cx,0=C0,  -D∂C0,t∂x=-jizF=-KfC0,t,  C+∞,t=C0 #Eqn.A11b

Note that the positive flux direction from Fick’s first law and the concentration field is defined towards +x. The positive direction of flux is opposite to our convention for current ji=zFKfC0,t, which value is positive for electrodeposition (correlated to flux towards -x).

This problem is analogous to the semi-infinite planar heat-transfer problem with Newton’s law of cooling as the boundary condition, for which an analytical solution is available [4, 5]. Translating the variables from the heat equation to Fick’s second law, the analytical solution is:

Cx,tC0=erfx2Dt+expKf2tDxDt+Kf2tDerfcx2Dt+Kf2tD#Eqn.A12

The concentration profiles with different values of Kf2/t are presented in Fig.2a in the main text.

When Kf2t≪D and Kfx≪D, we have the solution for the semi-infinite planar diffusion with surface concentration fixed at C0,t=0 (associated with the Cottrell equation for transient reaction rate) [6].

The surface concentration at a given time t is:

C0,t=C0expKf2tDerfcKf2tD#Eqn.A13

Note that for this equation C0,t→+∞=0. This is because this equation cannot be used with applied potentials close to equilibrium potential, at which potential the anodic current (neglected in our assumptions) is equal to the cathodic current. The time dependence of the surface concentration is demonstrated in Fig.2b in the main text.

We could define a characteristic time as the time when Kf2t=D:

tC≝DKf2,  C0,tCC0≈0.428#Eqn.A14

Considering the definition of the diffusion layer, we could find:

δt=DC0-C0,tKfC0,t=DKf⋅-1+exp-t/tc1-erft/tc#Eqn.A15

When t≪tC, we have δt≈1.128Dt. When t≫tC, we could find δt≈1.128Dt. Thus, if the system follows the reaction rate -D∂C0,t∂x=-KfC0,t, the diffusion layer thickness from the semi-infinite diffusion problem with C0,t=0 (associated with the Cottrell equation) is a good estimation of the diffusion layer thickness regardless of the level of transient concentration drop at the surface. The time dependence of the diffusion layer thickness is presented in Fig.2c in the main text.

a) When t≪tC, we have:

exp-Kf2t/D≈1-Kf2t/D    and  erfcKf2t/D≈1-4Kf2tπD#Eqn.A16

Therefore, the diffusion layer thickness with the reactive boundary proportional to surface concentration is:

δt=2Dt-πKf2t/Dπ-24Kf2t/D≈4Dtπ≈1.128Dt#Eqn.A17

b) When t≫tC, from Wolfram alpha, the function can be expanded with respect to t at +∞:

δt=DKf⋅-1+KfπtD+12KfπDt-12Kf3πD3t3+…#Eqn.A18

At Kf2t/D →+∞, we could find the diffusion layer thickness:

δt=πDt≈1.772Dt#Eqn.A19

Appendix-B: Tables for the fitting results with various models.

Table-B1 Fitted diffusivities and numbers of growth centers from the 1-point correlation function.

| Samples (Efficiency ~0.80) | Range of fitting | Diffusivity, fitted by the 1-point correlation function (cm2/s) | Number of growing centers, fitted by the 1-point correlation function (#/cm2) | Observed particle density (#/cm2) |
| --- | --- | --- | --- | --- |
| Cu-0.85 | [3.5s, 10.0s] | 5.293×10-6 | 2.073×104 | 4.646×109 |
| Cu-0.90 | [2.0s, 10.0s] | 5.220×10-6 | 4.656×104 | 8.314×109 |
| Cu-0.95 | [0.5s, 10.0s] | 5.386×10-6 | 1.570×105 | 1.152×1010 |
| Cu-1.00 | [0.5s, 10.0s] | 5.408×10-6 | 6.471×105 | 1.702×1010 |
| CuAg-0.85 | [2.5s, 10.0s] | 5.965×10-6 | 6.620×104 | 1.608×1010 |
| CuAg-0.90 | [1.5s, 10.0s] | 6.262×10-6 | 1.245×105 | 1.584×1010 |
| CuAg-0.95 | [0.5s, 10.0s] | 6.351×10-6 | 4.969×105 | 1.609×1010 |
| CuAg-1.00 | [0.5s, 10.0s] | 6.408×10-6 | 3.196×106 | 2.117×1010 |

Table-B2 Fitted nucleation kinetics and the particle density from the Classical model based on the potentiostatic transients. The diffusivities fitted from the 1-point correlation function were used for each sample. The particle density from the instantaneous mode of the Classical model is evaluated at the peak current and peak time of the potentiostatic transient.

| Samples (Efficiency ~0.80) | Classical model instantaneous mode (#/cm2) | Range of fitting | Classical model: fitted n | Classical model: fitted KN | Classical model estimation at 5s (#/cm2) | Observed particle density (#/cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| Cu-0.85 | 8.877×105 | [0.02s, 0.5s] | -0.457 | 6.369×105 | 2.810×106 | 4.646×109 |
| Cu-0.90 | 1.939×106 | [0.02s, 0.2s] | -0.764 | 6.752×105 | 4.180×106 | 8.314×109 |
| Cu-0.95 | 5.107×106 | [0.02s, 0.1s] | -0.771 | 2.334×106 | 1.474×107 | 1.152×1010 |
| Cu-1.00 | 9.431×106 | [0.02s, 0.08s] | -0.726 | 6.951×106 | 3.943×107 | 1.702×1010 |
| CuAg-0.85 | 1.259×106 |  |  |  |  | 1.608×1010 |
| CuAg-0.90 | 1.821×106 |  |  |  |  | 1.584×1010 |
| CuAg-0.95 | 4.668×106 |  |  |  |  | 1.609×1010 |
| CuAg-1.00 | 1.668×107 |  |  |  |  | 2.117×1010 |

Table-B3 Estimation of particle density from the observed average 1st nearest neighbor distance of the deposits with 5s deposition and the diffusion zone radius at the peak time of the potentiostatic transient (corresponds to 0.942C0 local concentration of a hemispherical diffusion field). The unit for the nucleation densities is #/cm2.

| Samples (Efficiency ~0.80) | Observed average 1st NN distance (nm) | Peak time in potentiostatic transient (s) | Size of the independently growing hemisphere particles at peak time (nm) | Characteristic diffusion length (nm, 0.942Ci0) | Particle density estimated from 1st NN distance | Particle density estimated from diffusion zone radius | Observed nucleation density |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu-0.85 | 87.01 | 1.892 | 377 | 6519 | 1.321×1010 | 5.883×105 | 4.646×109 |
| Cu-0.90 | 68.24 | 0.804 | 244 | 4220 | 2.147×1010 | 1.404×106 | 8.314×109 |
| Cu-0.95 | 60.73 | 0.296 | 150 | 2601 | 2.711×1010 | 3.695×106 | 1.152×1010 |
| Cu-1.00 | 51.12 | 0.168 | 113 | 1964 | 3.827×1010 | 6.484×106 | 1.702×1010 |
| CuAg-0.85 | 50.05 | 0.892 | 274 | 4752 | 3.992×1010 | 1.107×106 | 1.608×1010 |
| CuAg-0.90 | 50.85 | 0.624 | 235 | 4072 | 3.867×1010 | 1.508×106 | 1.584×1010 |
| CuAg-0.95 | 51.92 | 0.220 | 141 | 2435 | 3.710×1010 | 4.216×106 | 1.609×1010 |
| CuAg-1.00 | 45.87 | 0.056 | 71 | 1234 | 4.753×1010 | 1.642×107 | 2.117×1010 |

Table-B4 Fitted particle density (#/cm2) and diffusivities (cm2/s) from the instantaneous and progressive modes of the SRWBS model (identical to the S-H model). Peak current is in “A/cm2”, and peak time is in “s”.

| Samples (Efficiency ~0.80) | Peak time | Peak current | SRWBS instantaneous mode Diffusivity | SRWBS instantaneous mode nucleation density | SRWBS progressive mode Diffusivity | SRWBS progressive mode particle density at peak time | SRWBS progressive mode saturation particle density | Observed particle density |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cu-0.85 | 1.892 | -0.002688 | 1.442×10-5 | 3.468×105 | 9.040×10-6 | 9.698×105 | 1.033×106 | 4.646×109 |
| Cu-0.90 | 0.804 | -0.003749 | 1.192×10-5 | 9.875×105 | 7.473×10-6 | 2.761×106 | 2.941×106 | 8.314×109 |
| Cu-0.95 | 0.296 | -0.006278 | 1.231×10-5 | 2.597×106 | 7.717×10-6 | 7.262×106 | 7.735×106 | 1.152×1010 |
| Cu-1.00 | 0.168 | -0.008787 | 1.368×10-5 | 4.115×106 | 8.581×10-6 | 1.151×107 | 1.226×107 | 1.702×1010 |
| CuAg-0.85 | 0.892 | -0.003131 | 9.227×10-6 | 1.150×106 | 5.786×10-6 | 3.214×106 | 3.424×106 | 1.608×1010 |
| CuAg-0.90 | 0.624 | -0.004075 | 1.093×10-5 | 1.387×106 | 6.854×10-6 | 3.879×106 | 4.131×106 | 1.584×1010 |
| CuAg-0.95 | 0.220 | -0.006334 | 9.311×10-6 | 4.619×106 | 5.839×10-6 | 1.291×107 | 1.376×107 | 1.609×1010 |
| CuAg-1.00 | 0.056 | -0.011581 | 7.917×10-6 | 2.134×107 | 4.965×10-6 | 5.966×107 | 6.355×107 | 2.117×1010 |

Table-B5 Fitted nucleation site density (#/cm2), diffusivity (cm2/s). and activation frequency of each nucleation site (s-1) from the S-M model, the SRWBS model, and the H-T/M-N model.

| Samples (Efficiency ~0.80) | S-M Diffusivity | S-M nucleation site density | S-M nucleation frequency | SRWBS Diffusivity | SRWBS nucleation site density | SRWBS nucleation frequency | HT/MN Diffusivity | HT/MN nucleation site density | HT/MN nucleation frequency |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cu-0.85 | 1.947×10-5 | 3.586×106 | 0.163 | 1.947×10-5 | 3.272×106 | 0.134 | 1.446×10-5 | 1.374×106 | 0.553 |
| Cu-0.90 | 1.725×10-5 | 2.334×106 | 2.306 | 1.724×10-5 | 2.194×106 | 1.818 | 1.399×10-5 | 2.857×106 | 1.643 |
| Cu-0.95 | 1.614×10-5 | 7.984×106 | 5.927 | 1.613×10-5 | 7.500×106 | 4.682 | 1.326×10-5 | 1.038×107 | 3.706 |
| Cu-1.00 | 1.556×10-5 | 3.503×107 | 4.472 | 1.556×10-5 | 3.227×107 | 3.633 | 1.255×10-5 | 2.987×107 | 4.864 |
| CuAg-0.85 | 1.725×10-5 | 7.209×105 | 1.584×108 | 1.721×10-5 | 7.307×105 | 70.98 | 8.844×10-6 | 2.756×109 | 0.00228 |
| CuAg-0.90 | 1.745×10-5 | 1.211×106 | 5.270×103 | 1.738×10-5 | 1.250×106 | 69.44 | 9.150×10-6 | 3.425×109 | 0.00496 |
| CuAg-0.95 | 1.683×10-5 | 3.407×106 | 148.5 | 1.678×10-5 | 3.467×106 | 70.98 | 9.050×10-6 | 5.665×109 | 0.0193 |
| CuAg-1.00 | 1.633×10-5 | 1.582×107 | 75.27 | 1.634×10-5 | 1.494×107 | 58.65 | 9.031×10-6 | 3.565×1010 | 0.0296 |

Appendix-C: Details regarding the nucleation density from the SRWBS model with progressive or instantaneous nucleation kinetics (S-H model)

a) For the instantaneous mode of the SRWBS model (identical to the S-H model but with a better physical picture, with nucleation rate at free area: Itf=Nf,∞δt) [7-9]:

jt/zFjpeak/zF≡JtaprJpeakapr=tpeakt1/21-exp-1.25643t/tpeak1-exp-1.25643#Eqn.C1a

a1≝23/2π3/2VmCi01/2Di⋅Nf,∞=1.25643tpeak#Eqn.C1b

a2≝Ci0χC⋅Diπ1/2=Jpeakaprtpeak1/21-exp-1.25643#Eqn.C1c

Note that all the numbers are dimensionless. As long as the units of the variables are consistent, the value of the numbers will be the same. Therefore, the diffusivity Di and the nucleation density Nf,∞ are:

Di=πa2χCCi02=6.13953⋅tpeakχCjpeakaprzFCi02#Eqn.C2a

Nf,∞=a1Ci03/223/2π5/2Vm1/2a2χC2=0.012994VmCi01/2⋅zFCi0χCjpeakaprtpeak2#Eqn.C2b

The expression for the diffusivity is identical to equation (28) in the original work [7, 10].

b) For the progressive mode of the SRWBS model (identical to the S-H model but with a better physical picture, with nucleation rate at free area: Itf=AηNf,∞) [7-9, 11]:

jt/zFjpeak/zF≡JtaprJpeakapr=tpeakt1/21-exp-2.33664⋅t/tpeak21-exp-2.33664#Eqn.C3a

a1≝25/2π3/2VmCi01/2DiAηNf,∞3=2.33664tpeak2#Eqn.C3b

a2≝Ci0χC⋅Diπ1/2=Jpeakaprtpeak1/21-exp-2.33664#Eqn.C3c

Therefore, the diffusivity Di and the nucleation rate AηNf,∞ are:

Di=πa2χCCi02=3.84981⋅tpeakχCjpeakaprzFCi02#Eqn.C4a

AηNf,∞=3a1Ci03/22π5/2Vm1/2a2χC2=0.057806VmCi01/2tpeak⋅zFCi0χC⋅jpeakaprtpeak2#Eqn.C4b

The expression for the diffusivity is identical to the equation (27) in the original work [7, 10].

The nucleation density at a given time t is:

Ntapr=AηNf,∞25/2π1/2VmCi01/2Di1/2erft⋅2π3/2VmCi01/2DiAηNf,∞21/2#Eqn.C5

Expressing Ntapr in the peak current and peak time, we have:

Ntapr=0.03870Ci0Vm1/2⋅zFCi0χC⋅jpeakapr⋅tpeak2erf1.32381⋅ttpeak#Eqn.C6

At the peak current, for the progressive mode, the nucleation density is 93.9% of the saturation nucleation density. The saturation nucleation density at t→+∞ is:

Napr,s=Nt→∞apr =0.03870Ci0Vm1/2⋅zFCi0χC⋅jpeakapr⋅tpeak2#Eqn.C7

The estimated nucleation density from the SRWBS model with progressive and instantaneous nucleation kinetics is listed in Table-B4. Estimations are ~10-3 smaller than the observed values.

Appendix-D: Estimating the Cu(I) concentration at the electrolyte/electrode interface with deposition efficiency.

If assuming that all the side reactions are negligible, the surface concentration of Cu(I) species can be estimated if knowing the Coulombic efficiency for the deposition. The physical picture of the following model is shown in Fig.D.

Fig.D Illustration about the physical picture of the proposed model in this section. The red lines indicate the concentration profiles of Cu(II) at different deposition times, whereas the green lines indicate those of Cu(I) at the same times.

For Cu electrodeposition, the total current is:

jtot=2FJCuIIdep+FJCuIIex#Eqn.D1

In which JCuIIex indicates the flux of Cu(II) towards the substrate which does not lead to deposition. The deposition efficiency is defined as χC≝2FJCuIIdep/jtot. Therefore, we have the relationship:

JCuIIdep=χCJCuIIex21-χC#Eqn.D2

Meanwhile, at the very initial stage, the effect of convection can be neglected. Based on our analysis in section 3.2.5.1, at the deposition potentials used in this work, the Cu(II) species should be immediately depleted at the electrode/electrolyte interface. Thus, we assume that the diffusion of the Cu(II) species, either leading to Cu deposition or Cu(I) intermediate species, follows the Cottrell equation:

JCuIItot=JCuIIdep+JCuIIex=DCuIIπt1/2CCuII0#Eqn.D3

Knowing the deposition efficiency χC, we could Solve for JCuIIex:

JCuIIex=21-χC2-χCDCuIIπt1/2CCuII0#Eqn.D4

Neglect the convection, we assume that the flux of Cu(I) also follows the semi-infinite diffusion problem with fixed concentration at the substrate. The concentration of Cu(I) at the electrode/electrolyte interface CCuIs is:

DCuIπt1/2CCuIs=JCuIIex=21-χC2-χCDCuIIπt1/2CCuII0#Eqn.D5

Which means the surface concentration of Cu(I) is:

CCuIs=21-χC2-χCDCuIIDCuI1/2CCuII0#Eqn.D6

On the other hand, if the solubility limit of the reaction intermediate Cu(I) is known, if furtherly assuming that side reactions can be neglected, the minimum deposition efficiency is:

χCmin=2-11-CCuIs2CCuI0DCuIDCuII1/2#Eqn.D7

References

[1] A.J. Bard, L.R. Faulkner, 3. Kinetics of Electrode Reactions,  Electrochemical methods: fundamentals and applications, 2nd Edition. , John Wiley & Sons2000, pp. 87-136.

[2] R. Cabán, T.W. Chapman, Statistical Analysis of Electrode Kinetics Measurements‐Copper Deposition from CuSO4‐H 2 SO 4 Solutions, Journal of the Electrochemical Society, 124 (1977) 1371.

[3] E. Mattsson, J.O.M. Bockris, Galvanostatic studies of the kinetics of deposition and dissolution in the copper + copper sulphate system, Transactions of the Faraday Society, 55 (1959) 1586-1601.

[4] P.J. Schneider, Conduction heat transfer, Addison-Wesley Publishing Company1955.

[5] C.J. Geankoplis, A.A. Hersel, D.H. Lepek, 14.3B Unsteady-State Conduction in a Semi-Infinite Solid,  Transport Processes and Separation Process Principles, 5th Edition. 2003, pp. 518-522.

[6] A.J. Bard, L.R. Faulkner, 5.2.1 A Planar Electrode,  Electrochemical methods: fundamentals and applications, 2nd Edition. , John Wiley & Sons2000, pp. 161-164.

[7] Y. Sun, G. Zangari, Commentary and Notes on the Original Derivations of the Scharifker-Hills Model, Journal of The Electrochemical Society, 170 (2023) 032503.

[8] O.V. Grishenkova, A.V. Kosov, Y.P. Zaikov, V.A. Isaev, Model for the Nucleation and Diffusion-Controlled Growth of Binary Alloy Nuclei under Potentiostatic Conditions, Russian Metallurgy (Metally), 2020 (2020) 914-917.

[9] Y.D. Gamburg, Development of the electrocrystallization theory, Russian Journal of Electrochemistry, 52 (2016) 832-846.

[10] G. Gunawardena, G. Hills, I. Montenegro, B. Scharifker, Electrochemical nucleation: Part I. General considerations, Journal of Electroanalytical Chemistry and Interfacial Electrochemistry, 138 (1982) 225-239.

[11] M.E. Hyde, R.M. Jacobs, R.G. Compton, An electrodeposition study of the nucleation and growth of silver on boron-doped diamond electrodes, Journal of Electroanalytical Chemistry, 562 (2004) 61-72.