Table 1: Optimization of reaction condition for synthesis of 1, 8-dioxo-octahydroxanthenes.

| Entry | Catalyst Quantity (g) | Reaction Condition | Reaction Time (min) | Isolated Yield (%)a |
| --- | --- | --- | --- | --- |
| 1 | 0.05 | Toluene/Reflux | 40 | 28 |
| 2 | 0.05 | Chloroform/Reflux | 40 | 34 |
| 3 | 0.05 | DCM/Reflux | 40 | 40 |
| 4 | 0.05 | Acetonitrile/Reflux | 40 | 45 |
| 5 | 0.05 | EDC/Reflux | 40 | 49 |
| 6 | 0.05 | THF/Reflux | 40 | 53 |
| 7 | 0.05 | Acetone/Reflux | 40 | 57 |
| 8 | 0.01 | Ethanol/Reflux | 40 | 75 |
| 9 | 0.03 | Ethanol/Reflux | 40 | 82 |
| 10 | 0.05 | Ethanol/Reflux | 40 | 93 |

Reaction conditions: Dimedone (2 mmol), 4-Nitrobenzaldehyde (1 mmol) and SA@Cell-AEPC in solvent (5 mL) at given condition. a In all reaction 100% conversion were obtained.

Table 2: SA@Cell-AEPC catalyzed reaction between dimedone and aryl aldehydes.

| Entries | Aryl aldehyde (9) | Product (10) | Time (min) | Yield (%)a |
| --- | --- | --- | --- | --- |
| 1 | Benzaldehyde | 10a | 50 | 90 |
| 2 | 4-Nitrobenzaldehyde | 10b | 40 | 93 |
| 3 | 4-Cyanobenzaldehyde | 10c | 35 | 92 |
| 4 | 4-Bromobenzaldehyde | 10d | 50 | 86 |
| 5 | 4-Chlorobenzaldehyde | 10e | 40 | 85 |
| 6 | 4-Methylbenzaldehyde | 10f | 50 | 86 |
| 7 | 4-Hydroxybenzaldehyde | 10g | 55 | 88 |
| 8 | 4-Methoxybenzaldehyde | 10h | 45 | 85 |
| 9 | 3-Methoxybenzaldehyde | 10i | 50 | 80 |
| 10 | 2-Nitrobenzaldehyde | 10j | 45 | 84 |
| 11 | 2,5-Dimethoxybenzaldehyde | 10k | 50 | 80 |
| 12 | 3,4,5-Trimethoxybenzaldehyde | 10l | 55 | 82 |
| 13 | Furfuraldehyde | 10m | 60 | 80 |

Reaction conditions: Dimedone (2 mmol), aryl aldehyde (1 mmol), and SA@Cell-AEPC (0.05 g, 0.0075 mmol) in ethanol (5 mL) were stirred at reflux condition. a Isolated yield.

Table 3: SA@Cell-AEPC catalyzed synthesis of 2-substituted benzimidazole derivatives.

| Entries | Aryl aldehyde (9) | Product (12) | Time (min) | Yield (%)a |
| --- | --- | --- | --- | --- |
| 1 | Benzaldehyde | 12a | 70 | 88 |
| 2 | 4-Nitrobenzaldehyde | 12b | 65 | 92 |
| 3 | 4-Cyanobenzaldehyde | 12c | 60 | 92 |
| 4 | 4-Bromobenzaldehyde | 12d | 75 | 85 |
| 5 | 4-Chlorobenzaldehyde | 12e | 75 | 88 |
| 6 | 4-Hydroxybenzaldehyde | 12f | 80 | 86 |
| 7 | 4-Methylbenzaldehyde | 12g | 90 | 85 |
| 8 | 4-Methoxybenzaldehyde | 12h | 85 | 88 |
| 9 | 2-Nitrobenzaldehyde | 12i | 80 | 85 |
| 10 | Salicylaldehyde | 12j | 95 | 82 |
| 11 | 3,4,5-Trimethoxybenzaldehyde | 12k | 95 | 80 |
| 12 | Furfuraldehyde | 12l | 95 | 80 |
| 13 | Ferrocenecarboxyldehyde | 12m | 90 | 75 |

Reaction conditions: o-phenylenediamine (1 mmol), aryl aldehyde (1 mmol), and SA@Cell-AEPC (0.05 g, 0.0075 mmol) in ethanol (5 mL) were stirred at reflux condition. a Isolated yield.