Supplementary information for

Triexciton induced RGB emission of organic-inorganic zirconium halide perovskites

Chuying Wang1, Wen Meng1, Guigen Luo1, Guangyong Xu1, Min Peng1, Bin Xu1, Shuming Nie2 and Zhengtao Deng1*

1 College of Engineering and Applied Sciences, State Key Laboratory of Analytical Chemistry for Life Science, National Laboratory of Solid State Microstructures, Nanjing University Nanjing, Jiangsu 210023, P. R. China

2 Departments of Bioengineering, Chemistry, Electrical and Computer Engineering, and Materials Science and Engineering, University of Illinois at Urbana-Champaign, Urbana, IL, 61801, USA

*E-mail: dengz@nju.edu.cn

Table|  S1 The fitting results of the PL decay curves of red, green and blue, ((C2H5)4N)2ZrCl6 powders under different irradiation.

|  | Blue powder | Red powder |  |  | Green powder |  |
| --- | --- | --- | --- | --- | --- | --- |
| Excitation | 260 nm | 260 nm |  | 365 nm | 260 nm | 300 nm |
| Emission | 510 nm | 510 nm | 625 nm | 625 nm | 510 nm | 525 nm |
| A1 | 25521.77 | 107.429 | 102.351 | 97.323 | 39.793 | 116.354 |
| A1% | 100% | 96.670 | / | 86.362 | 14.318 | 76.974 |
| τ1 (μs) | 3.871 | 4.621 | 4.937 | 6.267 | 1.833 | 1.461 |
| A2 | / | 0.6086 | / | 4.451 | 65.521 | 1.270 |
| A2% | / | 3.330 | / | 13.638 | 85.682 | 23.026 |
| τ2 (μs) | / | 28.099 | / | 21.643 | 6.665 | 40.035 |
| τave (μs) | 3.871 | 5.403 | 4.937 | 8.364 | 5.973 | 10.343 |

Time-resolved PL decay curves of the perovskite are fitted by single or biexponential functions (see Eqs. 1 and 2):

| A(t) = A1 exp(-t / τ1) | (Eqs.1) |  |
| --- | --- | --- |
| A(t) = A1 exp(-t / τ1) + A2 exp(-t / τ2) | (Eqs.2) |  |

The ratio of lifetimes is calculated using

| Ai% = (Aiτi)/( A1τ1 + A2τ2) | (Eqs.3) |
| --- | --- |

The average lifetimes are calculated using

| τavg = (A1τ12 + A2τ22)/( A1τ1 + A2τ2) | (Eqs.4) |
| --- | --- |

Table|  S2 Summary of crystal data and reflection collection parameters.

| Empirical formula | C16H40Cl6N2Zr |
| --- | --- |
| Formula weight | 564.1134 |
| Crystal system | Monoclinic |
| Space group | C2/c |
| a, Å | 14.0708(17) |
| b, Å | 14.4783(19) |
| c, Å | 13.253(2) |
| α, degree | 90 |
| β, degree | 90.530(5) |
| γ, degree | 90 |
| V, Å3 | 2699.8(6) |
| Z | 4 |
| ρcalc., g cm-3 | 1.389 |
| μmm-1 | 1.006 |
| F000 | 1159.947 |
| 2θ max,deg(Completeness ) | 50.5(100%) |
| Total reflections | 21777 |
| Unique reflections | 3102 |
| Highest peak | 0.6652 |
| Deepest hole | -0.4520 |
| Rint | 0.0535 |
| R1 [obs I>4σ (I)] | 0.0429 |
| R1 (all data) | 0.0527 |
| wR2 | 0.1249 |
| Goodness-of-fit on F2 | 1.0477 |

Scheme S|  Schematic diagram of fabrication process of the ((C2H5)4N)2ZrCl6 powder samples.

Figure S1|  PL emission spectrum of green ((C2H5)4N)2ZrCl6 powder under excitation at 265 nm.

Figure S2|  SEM image and EDS mappings of ((C2H5)4N)2ZrCl6 single crystals.

Figure S3|  The crystal structures of ((C2H5)4N)2ZrCl6 viewed along a axis, b axis, and c axis.

Figure S4|  XRD patterns of ((C2H5)4N)2ZrCl6 samples.

Figure S5|  SEM images of blue, red and green ((C2H5)4N)2ZrCl6 powder samples.

Figure S6|  Photographs of green powder stored before (left) and after (right) a day at RF of 100%. The insets are the corresponding PL emission spectra of the samples.

Figure S7|  Photographs of ((C2H5)4N)2ZrCl6 samples evaporated on (a) glasses and (b) lids through different concentration of ZrCl4 precursor.

Figure S8|  Photographs of samples evaporated in tube under different irradiation.

Figure S9|  Absorption and PL emission spectra of (C13H30N)2ZrCl6 powders under different excitation.

Figure S10|  Photographs of pixelated patterns of the green and blue powders under (a) room light and (b) 375 nm irradiation.