Adsorption performance and mechanisms of mercaptans removal from gasoline oil using core-shell AC-based adsorbents: Role of intra-particles space

Pamphile Ndagijimanaa, Xuejiao Liua, *, Zhiwei Lia, Zhenjiao Xinga, Beibei Pana, Guangwei Yua, Yin Wanga, *

aCAS Key Laboratory of Urban Pollutant Conversion, Institute of Urban Environment, Chinese Academy of Sciences, Xiamen 361021, China

* Corresponding authors. E-mail address: yinwang@iue.ac.cn (Y. Wang), xjliu@iue.ac.cn (X.J. Liu)

Contents:

Table S1. Kinetics study of mercaptans adsorption by PAC and GAC-based adsorbents

Table S2. The adsorption isotherm parameters of Mercaptans adsorbed by AC-based adsorbents

Table S3. Study of mercaptans adsorbed by PAC-based adsorbents

Table S3. Study of mercaptans adsorbed by PAC-based adsorbents

Table S4. Thermodynamic study of mercaptans adsorbed by GAC-based adsorbent

Figure S1. Effect of initial concentration of mercaptans adsorbed by PAC and GAC-based adsorbents

Figure S2. Plot of ln(kc) versus 1/T of mercaptans removal by PAC and GAC-based adsorbents.

| Table S1 Kinetics study of mercaptans adsorption by PAC and GAC-based adsorbents |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Pseudo-first-order |  |  |  |  |  | Pseudo-second-order |  |  |  |  | Intraparticle diffusion |  |  |
| Sorbent | Mercaptans |  | qeexp (mgg-1) | qecal (mgg-1) | K1 | R2 | qeexp (mgg-1) |  | qecal (mgg-1) | K2 | R2 | C |  | Kdiff | R2 |
| PAC | Ethanethiol |  | 1000 | 12.50.14 | 15×10-2 | 0.423 | 1000 |  | 1000 | 28×10-2 | 1 | 995 |  | 0.190 | 0.410 |
|  | 1-Butanethiol |  | 1000 | 334.85 | 81×10-2 | 0.963 | 1000 |  | 1001 | 14×10-4 | 1 | 4.39 |  | 0.34 | 0.324 |
| PAC-core | Ethanethiol |  | 1000 | 70.09 | 27×10-2 | 0.777 | 1000 |  | 1004 | 357×10-4 | 1 | 797.37 |  | 8.67 | 0.560 |
|  | 1-Butanethiol |  | 1000 | 1011 | 42×10-2 | 0.915 | 1000 |  | 1040.75 | 104×10-4 | 0.999 | 780 |  | 17.88 | 0.62 |
| GAC | Ethanethiol |  | 1620.70 | 1036.74 | 71×10-2 | 0.853 | 1620.70 |  | 1672.13 | 29×10-4 | 0.999 | 1323 |  | 13 | 0.554 |
|  | 1-Butanethio |  | 1238.27 | 671.74 | 36×10-2 | 0.751 | 1238.27 |  | 1252.87 | 11×10-4 | 0.999 | 757 |  | 20.57 | 0.559 |
| GAC-core | Ethanethiol |  | 1666.70 | 1790.46 | 48×10-2 | 0.838 | 1666.70 |  | 1681.14 | 11×10-4 | 0.999 | 1165 |  | 21.30 | 0.623 |
|  | 1-Butanethiol |  | 1302.44 | 889.58 | 16×10-2 | 0.721 | 1302.4 |  | 1362.94 | 24×10-5 | 0.998 | 441.97 |  | 35.97 | 0.754 |

| Table S2 The adsorption isotherm parameters of Mercaptans adsorbed by AC-based adsorbents |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Langmuir isotherm |  |  | Freundlich isotherm |  |  |
| Sorbents | Temperature (oC) | Mercaptans | qm (mg/g) | kL (L/mg) | R2 | kF (mg/g)(L/mg)1/n | n | R2 |
| PAC | 25 | Ethanethiol | 1448.59 | 43×10-6 | 0.988 | 640.396 | 7.72 | 0.737 |
|  |  | 1-Butanethiol | 1251.15 | 46×10-6 | 0.998 | 695.48 | 11.02 | 0.999 |
|  | 30 | Ethanethiol | 1434.65 | 52×10-6 | 0.983 | 544.38 | 6.46 | 0.722 |
|  |  | 1-Butanethiol | 1266.19 | 46×10-6 | 0.997 | 699.14 | 0.15 | 0.978 |
|  | 40 | Ethanethiol | 1443.98 | 194×10-5 | 0.985 | 525.14 | 6.17 | 0.822 |
|  |  | 1-Butanethiol | 1290.96 | 43×10-6 | 0.997 | 766.99 | 12.56 | 0.833 |
|  | 60 | Ethanethiol | 1462.14 | 42×10-6 | 0.989 | 644.11 | 7.65 | 0.805 |
|  |  | 1-Butanethiol | 1357.15 | 43×10-6 | 0.996 | 670.52 | 9.02 | 0.991 |
| PAC-core | 25 | Ethanethiol | 1574.15 | 212×10-6 | 0.993 | 881.79 | 10.0 | 0.798 |
|  |  | 1-Butanethiol | 1421.85 | 35×10-6 | 0.997 | 686.00 | 9.03 | 0.8199 |
|  | 30 | Ethanethiol | 1520.30 | 194×10-5 | 0.7595 | 845.57 | 6.7 | 0.774 |
|  |  | 1-Butanethiol | 1434.29 | 328×10-6 | 0.997 | 709.09 | 8.95 | 0.999 |
|  | 40 | Ethanethiol | 1564.95 | 25×10-6 | 0.991 | 814.7 | 9.60 | 0.767 |
|  |  | 1-Butanethiol | 1468.79 | 314×10-6 | 0.997 | 701 | 8.46 | 0.999 |
|  | 60 | Ethanethiol | 1573.37 | 13×10-6 | 0.997 | 1119.9 | 19.6 | 0.777 |
|  |  | 1-Butanethiol | 1534.29 | 31×10-6 | 0.997 | 636.52 | 6.92 | 0.967 |
| GAC | 25 | Ethanethiol | 1711.17 | 178×10-6 | 0.999 | 1296.24 | 23.11 | 0.658 |
|  |  | 1-Butanethiol | 1325.14 | 187×10-5 | 0.999 | 688.97 | 107.98 | 0.516 |
|  | 30 | Ethanethiol | 1762.804 | 22×10-6 | 0.999 | 1284.80 | 20.73 | 0.731 |
|  |  | 1-Butanethiol | 1399.56 | 23×10-5 | 0.999 | 644.36 | 9.25 | 0.659 |
|  | 40 |  |  |  |  |  |  |  |
|  |  | Ethanethiol | 1895.02 | 22×10-6 | 0.999 | 1251.66 | 15.77 | 0.864 |
|  |  | 1-Butanethiol | 1423.123 | 186×10-5 | 0.999 | 676.97 | 9.51 | 0.685 |
|  | 60 | Ethanethiol | 2444.66 | 43×10-7 | 0.999 | 1758.83 | 19.27 | 0.975 |
|  |  | 1-Butanethiol | 1517.03 | 117×10-5 | 0.999 | 799.16 | 10.81 | 0.592 |
| GAC-core | 25 | Ethanethiol | 1938.26 | 165×10-6 | 0.998 | 1303.47 | 16.90 | 0.779 |
|  |  | 1-Butanethiol | 1539.09 | 217×10-5 | 0.999 | 588.77 | 7.38 | 0.737 |
|  | 30 | Ethanethiol | 2016.04 | 16×10-6 | 0.998 | 1248.37 | 13.78 | 0.943 |
|  |  | 1-Butanethiol | 1589.05 | 22×10-6 | 0.999 | 544.49 | 6.57 | 0.735 |
|  | 40 | Ethanethiol | 2302.14 | 91×10-7 | 0.998 | 1449.83 | 13.85 | 0.980 |
|  |  | 1-Butanethiol | 1737.97 | 243×10-5 | 0.999 | 501.54 | 5.8 | 0.908 |
|  | 60 | Ethanethiol | 2444.66 | 42×10-7 | 0.999 | 1758.83 | 19.27 | 0.975 |
|  |  | 1-Butanethiol | 1926.23 | 144×10-5 | 0.999 | 595.26 | 5.92 | 0.948 |

| Table S3 Study of mercaptans adsorbed by PAC-based adsorbents |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbents | Adsorbate | C0 (mgS L-1) | ∆H (kJ mol-1) | ∆S (J mol-1 K-1) | ∆G (kJ mol-1) |  |  |  |
|  |  |  |  |  | 298K | 303K | 313K | 333K |
| PAC | Ethanethiol | 800 | - | - | - | - | - | - |
|  | 1-Butanethiol | 800 | - | - | - | - | - | - |
| PAC | Ethanethiol | 900 | 1.44 | -2.03 | - | - | - | - |
|  | 1-Butanethiol | 900 | - | - | - | - | - | - |
| PAC | Ethanethiol | 1000 | - | - | - | - | - | - |
|  | 1-Butanethiol | 1000 | -69.824 | -160.18 | - | - | -19.69 | -16.49 |
| PAC | Ethanethiol | 1200 | - | - | -6.78 | -6.26 | -5.86 | -5.75 |
|  | 1-Butanethiol | 1200 | -5.819 | -1.96 | -525 | -5.24 | -5.14 | -5.19 |
| PAC | Ethanethiol | 1500 | -14.461 | -26.61 | -3.805 | -3.64 | -3.59 | -3.54 |
|  | 1-Butanethiol | 1500 | -2.59 | 1.52 | -3.085 | -3.37 | -3.00 | 3.13 |
| PAC | Ethanethiol | 2000 | -5.648 | -6.44 | -2.59 | -2.61 | -2.46 | -2.48 |
|  | 1-Butanethiol | 2000 | -0.57 | -2.44 | -1.30 | -1.299 | -1.34 | -1.38 |
| PAC-core | Ethanethiol | 800 | -3.77 | -69.12 | 2.89 | 2.93 | 2.91 | 2.85 |
|  | 1-Butanethiol | 800 | - | - | - | - | - | - |
| PAC-core | Ethanethiol | 900 | - | - | - | - | - | - |
|  | 1-Butanethiol | 900 |  |  |  |  |  |  |
| PAC-core | Ethanethiol | 1000 | - | - | - | - | - | - |
|  | 1-Butanethiol | 1000 |  |  | -6.69 | -7.12 | -7.61 | -9.33 |
| PAC-core | Ethanethiol | 1200 | 217.14 | 759.67 | -10.11 | -11.69 | -21.12 | - |
|  | 1-Butanethiol | 1200 | 15.393 | 74.03 | -4.39 | -4.58 | -4.99 | -6.01 |
| PAC-core | Ethanethiol | 1500 | 12.63 | 59.68 | -5.19 | -5.47 | -5.93 | -7.294 |
|  | 1-Butanethiol | 1500 | 9.53 | 46.58 |  |  |  |  |
| PAC-core | Ethanethiol | 2000 | 1.93 | 18.04 | -3.370 | -3.57 | -3.83 | -4.02 |
|  | 1-Butanethiol | 2000 | 6.726 | 30.02 | -2.241 | -2.36 | -2.67 | -3.28 |

| Table S4 Thermodynamic study of mercaptans adsorbed by GAC-based adsorbent |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbents | Adsorbate | C0 (mgS L-1) | ∆H (kJ mol-1) | ∆S (J mol-1 K-1) | ∆G (kJ mol-1) |  |  |  |
|  |  |  |  |  | 298K | 303K | 313K | 333K |
| GAC | Ethanethiol | 800 | 66.79 | 235.42 | -12.40 | -12.79 | -13.77 | -19.60 |
|  | 1-Butanethiol | 800 | 12.87 | 57.41 | -4.25 | -4.52 | -5.09 | -6.26 |
| GAC | Ethanethiol | 900 | 66.79 | 235.42 | -10.92 | -11.42 | -12.31 | -15.14 |
|  | 1-Butanethiol | 900 | 13.23 | 57.70 | -4.10 | -4.25 | -4.56 | -6.12 |
| GAC | Ethanethiol | 1000 | 66.79 | 235.42 | -10.10 | -10.43 | -11.24 | -14.20 |
|  | 1-Butanethiol | 1000 | 12.43 | 54.45 | -3.86 | -4.09 | -4.45 | -5.77 |
| GAC | Ethanethiol | 1200 | 20.32 | 80.32 | -5.08 | -5.27 | -5.82 | -8.01 |
|  | 1-Butanethiol | 1200 | 9.45 | 40.38 | -2.63 | -2.77 | -3.11 | -4.03 |
| GAC | Ethanethiol | 1500 | 14.34 | 53.87 | -2.92 | -3.12 | -3.95 | -4.90 |
|  | 1-Butanethiol | 1500 | 5.42 | 23.00 | -1.50 | -1.49 | -1.74 | -2.27 |
| GAC | Ethanethiol | 2000 | 10.54 | 35.84 | -1.41 | -1.59 | -2.03 | -2.80 |
|  | 1-Butanethiol | 2000 | 5.31 | 18.34 | -0.11 | -0.32 | -0.41 | -0.80 |
| GAC-core | Ethanethiol | 800 | - | - | - | - | - | - |
|  | 1-Butanethiol | 800 | 18.60 | 77.80 | -4.79 | -4.89 | -5.50 | -7.44 |
| GAC-core | Ethanethiol | 900 | - | - | - | - | - | - |
|  | 1-Butanethiol | 900 | 14.65 | 64.06 | -4.65 | -4.69 | -5.14 | -6.83 |
| GAC-core | Ethanethiol | 1000 | - | - | - | - | - | - |
|  | 1-Butanethiol | 1000 | 12.76 | 57.32 | -4.42 | -4.63 | -4.94 | -6.44 |
| GAC-core | Ethanethiol | 1200 | 73.25 | 263.62 | -6.16 | -6.44 | -9.54 | -14.61 |
|  | 1-Butanethiol | 1200 | 11.21 | 48.15 | -3.24 | -3.42 | -3.60 | -4.95 |
| GAC-core | Ethanethiol | 1500 | 31.90 | 118.55 | -3.67 | -3.40 | -5.76 | -7.43 |
|  | 1-Butanethiol | 1500 | 10.84 | 42.98 | -1.97 | -2.24 | -2.50 | -3.51 |
| GAC-core | Ethanethiol | 2000 | 18.04 | 67.28 | -2.13 | -1.94 | -3.44 | -4.23 |
|  | 1-Butanethiol | 2000 | 10.53 | 37.46 | -0.67 | -0.79 | -1.21 | -1.96 |

Fig. S1.

Fig. S2.