Supporting Information

Ruthenate perovskite with face-sharing motifs for sustainable alkaline hydrogen evolution

Chuanhui Zhu,a,b,c,# Hao Tian,b,c,# Pengfei Tan,a Bin Huang,a,d Shuang Zhao,a Guo-Hong Cai,a Chongyang Yuan,a Mei-Huan Zhao,a Meng Cao,b Jianfa Zhao,e Shi Luchuan,e Haili Song,a Keke Huang,f Shouhua Feng,f Mark Croft,g Chang-Qing Jin,e Shuk-Yin Tong,b,h,* Man-Rong Lia,i,*

a Key Laboratory of Bioinorganic and Synthetic Chemistry of Ministry of Education, School of Chemistry, Sun Yat-Sen University, Guangzhou 510275, P. R. China

E-mail: limanrong@mail.sysu.edu.cn

b School of Science and Engineering, The Chinese University of Hong Kong, Shenzhen 518172, P. R. China

E-mail: tongsy@cuhk.edu.cn

c School of Chemistry and Materials Science, University of Science and Technology of

China, Hefei 230026, P. R. China

d School of Computer Science and Technology, Dongguan University of Technology, Dongguan 523808, P. R. China

e Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, P. R. China

f State Key Laboratory of Inorganic Synthesis and Preparative Chemistry, International Joint Research Laboratory of Nano Micro Architecture Chemistry (NMAC), College of Chemistry, Jilin University, Changchun 130012, P. R. China

g Department of Physics and Astronomy, Rutgers, The State University of New Jersey, 136 Frelinghuysen Road, Piscataway, New Jersey 08854, USA

h Institute of Materials Science and Devices, Suzhou University of Science and Technology, Suzhou 215009, P. R. China

i School of Chemistry and Chemical Engineering, Hainan University, Haikou 570228, P. R. China

# These authors contributed equally.

Supplementary Figures

Figure S1. HRTEM images of different BaRuO3 polymorphs. (a) 9R-BRO; (b) 4H-BRO; (c) 6H-BRO.

Figure S2. Elemental-mapping of (a-d) 9R-BRO; (e-h) 4H-BRO; (i-l) 6H-BRO.

Figure S3. SEM images of (a) 9R-BRO; (b) 4H-BRO; (c) 6H-BRO.

Figure S4. Brunauer-Emmett-Teller measurements of (a) 9R-BRO; (b) 4H-BRO; (c) 6H-BRO.

Figure S5. XPS spectra showing Ba 3d and Ru 3p core level peak regions of different BaRuO3 phases.

Figure S6. Normalized Ru L3-edge XANES of the different phases of BaRuO3 compared to the Ru5+ standard Ca2YRuO6. Note the A (t2g-final state) and B (eg-final state) features.

Figure S7. Specific activity normalized to BET surface area of the different phases of BaRuO3.

Figure S8. The polarization curves of (a) 4H-, (b) 6H- and (c) 3C-BRO catalyst before and after 1000 cycles of voltammetry operation.

Figure S9. XPS spectra for Ru 3p of 9R-BRO and PXD patterns before and after the 1,000 cycles voltammetry operation and leaching in 1 M KOH and 1 M HCl for 2 weeks.

Figure S10. Ru 4d-state in BaRuO3 polymorphs. The subscript “center” and “side” denote as central atom and sideward atom in the Ru3O9 trimer for 9R-BRO, respectively. The blue and red curves indicate t2g- and eg-orbitals, respectively.

Figure S11. Temperature dependences of electrical resistivity for the different BRO-polymorphs. MIT refers to metal-insulator transition.

Figure S12. (a) Building blocks of RuO6 of BRO, the subscripts “F” and “C” denote face- and corner-shared octahedra, respectively. (b) Selected Ru-Ru bond lengths in face-shared and corner-shared octahedra for the different BRO-polymorphs.

Supplementary Tables

Table S1. Unit cell parameters, atomic coordinates and atomic displacement parameters for the 9R-, 4H-, 6H-, and 3C-polymorphs of BaRuO3 at room temperature.

| Sample | 9R-BRO | 4H-BRO | 6H-BRO | 3C-BRO |
| --- | --- | --- | --- | --- |
| Space Group | R-3mH | P63/mmc | P63/mmc | Pm-3m |
| a, Å | 5.75085(5) | 5.74197 (3) | 5.73201(10) | 4.00593(1) |
| c, Å | 21.61277(2) | 9.52340 (7) | 14.0843(3) | / |
| V, Å3 | 619.018(14) | 271.922 (4) | 400.757(16) | 64.285(1) |
| Ba1 (x, y, z) | 0, 0, 0 | 0, 0, 0 | 0, 0, 1/4 | 0, 0, 0 |
| Biso, Å2 | 1.03(2) | 1.07(4) | 0.83(8) | 0.28(1) |
| Ba2 (x, y, z) | 0, 0, 0.2181(1) | 1/3, 2/3, 1/4 | 1/3, 2/3, 0.0899(1) | / |
| Biso, Å2 | 1.03(2) | 1.07(4) | 0.94(4) | / |
| Ru1 (x, y, z) | 0, 0, 1/2 | 2/3, 1/3, 0.1161(2) | 0, 0, 0 | 1/2, 1/2, 1/2 |
| Biso, Å2 | 0.69(3) | 0.52(5) | 1.34(12) | 0.12(1) |
| Ru2 (x, y, z) | 0, 0, 0.3830(1) | / | 1/3, 2/3, 0.6586(1) | / |
| Biso, Å2 | 0.69(3) | / | 0.88(5) | / |
| O1 (x, y, z) | 1/2, 0, 0 | 1/2, 1/2, 0 | 0.5168(9), -x, 1/4 | 1/2, 1/2, 0 |
| Biso, Å2 | 1.19(6) | 1.32(12) | 1.2(2) | 0.49(5) |
| O2 (x, y, z) | 0.1561(5), 1-x, 0.5609(3) | 0.3602(7), x/2, 1/4 | 0.8355(8), -x, 0.0819(5) | / |
| Biso, Å2 | 1.19(6) | 1.32(12) | 1.89(18) | / |
| Rp/Rwp/% | 4.33/4.45 | 5.43/9.50 | 4.02/5.05 | 6.54/8.44 |

Table S2. Selected interatomic distances (Å), octahedral distortion parameter (Δ), bond valence sums (BVS) calculations, and bond angles (º) in the crystal structure for the 9R-, 4H-, 6H-, and 3C-polymorphs of BaRuO3 at room temperature.

| Sample | 9R-BRO | 4H-BRO | 6H-BRO | 3C-BRO |
| --- | --- | --- | --- | --- |
| RuO6 |  |  |  |  |
| Ru1-O | O2, 2.000(3)×6 | O1, 1.992(1)×3 | O2, 1.999(5)×6 | 2.003(1)×6 |
|  |  | O2, 1.987(4)×3 |  |  |
| < Ru1-O> | 2.000(3) | 1.989(5) | 1.999(5) | 2.003(1) |
| Δ*10-6 | 0 | 1.64 | 0 | 0 |
| BVS | 3.80 | 3.91 | 3.81 | 3.78 |
| Ru2-O | O1, 1.974(6)×3 | / | O1, 1.968(3)×3 | / |
|  | O2, 2.036(8)×3 | / | O2, 1.994(4)×3 | / |
| < Ru2-O> | 2.005(5) | / | 1.981(1) | / |
| Δ*10-6 | 239.05 | / | 43.06 | / |
| BVS | 3.76 | / | 4.01 | / |
| < Ru-O> | 2.002(5) | 1.989(5) | 1.980(1) | / |
| BaO12 |  |  |  |  |
| Ba1-O | O1, 2.879(1)×6 | O1, 2.871(1)×6 | O1, 2.871(4)×6 | 2.833(1)×12 |
|  | O2, 2.974(3)×6 | O2, 2.979(1)×6 | O2, 2.876(4)×6 |  |
| < Ba1-O> | 2.926(5) | 2.925(1) | 2.873(5) | 2.833(1) |
| BVS | 2.14 | 2.15 | 2.44 | 2.72 |
| Ba2-O | O1, 2.998(6)×3 | O1, 2.901(1)×6 | O1, 2.898(3)×3 | / |
|  | O2, 2.940(7)×3 | O2, 2.874(5)×6 | O2, 2.944(7)×3 | / |
|  | O2, 2.884(1)×6 |  | O2, 2.868(6)×6 | / |
| < Ba2-O> | 2.926(5) | 2.887(5) | 2.894(5) | / |
| BVS | 2.14 | 2.35 | 2.31 | / |
| < Ba-O> | 2.926(5) | 2.906(1) | 2.883(5) | / |
| RuF-RuF | 2.525(2) | 2.550(1) | 2.576(3) | / |
| RuC-RuC | 3.948(9) | 3.985(1) | 3.992(1) | 4.006(1) |
| RuF-O-RuF | 78.1(2) | 79.8(2) | 81.8(2) | / |
| RuC-O-RuC | 180.0(0) | 180.0(0) | 177.6(3) | 180.0(0) |

Table S3: Mass activity (A/g) and price activity (A/$) for 9R-BRO, Pt/C, RuO2 and Nano-Ni

| Sample | Mass activity (A/g) | Price ($/g) | Price activity (A/$) |
| --- | --- | --- | --- |
| 9R-BRO | 180.3 | 6.8 | 26.5 |
| Pt/C | 137.8 | 31 | 4.4 |
| RuO2 | 97.4 | 26.5 | 3.7 |
| Nano-Ni | 2.9 | 4.1 | 0.7 |