Supporting Information

Development of glucose/pH responsive smart hydrogel of carbopol and application in microneedles

Mingli Pi1, Weijun Liu1 , Beibei Huang1, Tingxuan Wu1, Tao Zhang1, Wei Wang2

Table S1. The element content of hydrogels prepared at different ratios of CP to APBA

| CP-APBA | C % | O% | N% | B% |
| --- | --- | --- | --- | --- |
| 0.2g | 61.48 | 18.76 | 10.18 | 9.58 |
| 0.4g | 41.59 | 23.11 | 18.39 | 16.91 |
| 0.6g | 30.39 | 27.04 | 23 | 19.57 |

Corresponding author, E-mail: liuwj@sit.edu.cn, Tel:  021-60877214