Supporting Information

A method of constructing highly durable conductive materials by growing metal particles inside and outside fibers through solvation and multivalent bonding forces

Yan Wena, Peibo Dua, Chao Sunb, Xiongwei Zhana, Zaisheng Caia, Fengyan Gea,c,d*

a. College of Chemistry and Chemical Engineering, Donghua University, Shanghai 201620, China

b. School of Chemical and Process Engineering, University of Leeds, Leeds LS2 9JT, UK

c. Technology Innovation Center of Hebei for fiber material, Shijiazhuang University, Shijiazhuang 050035, Hebei, China

d. National Innovation Center of Advanced Dyeing and Finishing Technology, Taian, Shandong 271000, China

*Email: DHUfyge@163.com

Figure. S1 The cross-sections of Cu/Ag/CA-PEI@Cotton FESEM.

Figure. S2 Mechanical strength of fabrics.

Figure. S3 (a,b) Molecular structure of CA and PEI, (c) Chemical reaction mechanism of phenol-amine.

SI.4 The analysis of phenol-amine reaction:

The functional groups were characterized by FTIR spectra in Fig.3d. On one hand, quinone groups were yielded by the oxidation of phenolic hydroxyl groups in mildly alkaline conditions (Zhang, et al. 2021). Subsequently, the quinone group readily reacts with the -NH2 group, as evidenced by the new peaks of 1634.9 cm-1 (-C=N), 1382.7 cm-1 (-C-N). On the other hand, -CONH- could be generated through the amidation reaction between the redundant -COOH groups of CA and -NH2 groups of PEI, which is supported by peak at 1505.2 cm-1 (-NH) and 1261.3 cm-1 (C=O). Beyond, the occurrence of the crosslinking reaction between CA and PEI were characterized by XPS in Fig.3e. The C 1s peak (Fig.2f) could be deconvoluted into five peaks: C-C at 284.6 eV, C=C at 284.8 eV, C-N at 285.5 eV (Michael addition reaction) (Liu, et al. 2013), C=N at 286.6 eV, and C=O at 288.1 eV (Schiff base reaction) (Cheng, et al. 2018). From the resolution XPS of the N 1s, the peak at 398.7 eV belongs to the C-N bond from PEI. The peak around 399.4 eV is assigned to C=N (Bang, et al. 2015) and N-H bond which are contributed from Schiff-base reaction and the original bond (N-H) in PEI, respectively. The peak at 400.9 eV is attributed to the -NH3+, which is contributed from the reaction between -COOH in CA and -NH2 in PEI (Chen, et al. 2014). The results of XPS indicate that the Michael addition, Schiff base reaction of CA and PEI occurred.

Figure. S5 Effect of CA and PEI reaction conditions on the Cu/Ag/CA-PEI@Cotton sheet resistance. The resistance value 6.09×10-3 Ω/sq of the composite fabric can be achieved at a concentration of 0.1 mol/L, at 40 ℃, in a ratio for 4 h reaction conditions.

Figure. S6 object images of the samples. (a) original cotton, (b) modified fabric with CA and PEI and (c) CA-PEI/Ag/Cu composite fabric, indicating relatively well uniform after treatment.

Figure. S7 The EDS mapping of the copper-plated cotton fibers showing the high content distribution which insured their high conductivity.

Figure. S8 The XRD spectra of samples.

The XRD spectra of the modified cotton by CA and PEI was consistent with the original cotton, while new peaks at 43.43°, 50.55° and 74.24° presented in Cu/Ag/CA-PEI@Cotton sample are corresponding to typical crystal structures of Cu (111), (200), and (220) planes, respectively(Guo, et al. 2021).

Figure. S9 TGA of samples.

The thermal retention of the cotton after CA and PEI modification increased from 7.5 % to 8.3 %, indicating that the deposits are thermally stable. Further Cu/Ag/CA-PEI@Cotton had a thermal retention of 61.1 % achieved by the formation of a dense and stable composite structure of Cu on cotton faber, which does not disintegrate at high temperatures. The rate of thermal decomposition of the sample has a corresponding variation shown in Fig.S9.

Figure. S10 DTG of samples.

Table. S1 Comparison of the performances of the composite fabric with those of other reported samples in the literature.

| Reference | materials | Sheet resistance(Ω/sq) | Heating performance | Washing times |
| --- | --- | --- | --- | --- |
| This work | Cu NPs | 6.09×10-3 | 140℃ (1 V) | 100 |
| (Guo, et al. 2021) | Cu nanowire | 0.16 | 142.2℃ (1.8 V) | 10 |
| (Jia, et al. 2020) | AgNPs | 861.3 | 63.6 ℃ (1.2 V) | -- |
| (Wang, et al. 2019) | AgNWs | 17.6–14.3 | 110 ℃ (10 V) |  |
| (Ma, et al. 2021) | PPy | 10 | 85℃ (6.0 V) | 20 |
| (Gong, et al. 2023) | PDMS/PPy-Ag/Graphene/PET | 6.32 | 53 ℃ (2.0 V) | -- |
| (Yang, et al. 2023) | MXene | 8.80 | 75 ℃ (13.0 V) | 5 |
| (Cai, et al. 2018) | CNT | 680 | 105 ℃ (10.0 V) | 10 |
| (Guo, et al. 2021) | CNT | 0.3 | 70 ℃ (1.8 V) | -- |
| (Qiu, et al. 2020) | SiO2/TiO2/carbon nanofibers | -- | 43 ℃ (30 V) | -- |
| (Li, et al. 2019) | Ceramic precursors fired cotton | 43.2 | 120.4 ℃ (8 V) | -- |

Figure. S11 Friction resistance of the composite fabric.

Reference:

Zhang Q, Qiao Y, Li C et al (2021) Chitosan/gelatin-tannic acid decorated porous tape suture with multifunctionality for tendon healing. Carbohydrate Polymers 268:118246. https://doi.org/10.1016/j.carbpol.2021.118246

Liu Z, Duan X, Qian G et al (2013) Eco-friendly one-pot synthesis of highly dispersible functionalized graphene nanosheets with free amino groups. Nanotechnology 24(4):045609. http://doi.org/10.1088/0957-4484/24/4/045609

Cheng X Q, Wang Z X, Guo J et al (2018) Designing Multifunctional Coatings for Cost-Effectively Sustainable Water Remediation. ACS Sustainable Chemistry & Engineering 6(2):1881-1890. http://doi.org/10.1021/acssuschemeng.7b03296

Bang J, Sun Y-Y, West D et al (2015) Molecular doping of ZnO by ammonia: a possible shallow acceptor. Journal of Materials Chemistry C 3(2):339-344. http://doi.org/10.1039/C4TC02209B

Chen S, Li X, Yang Z et al (2014) A simple one-step modification of various materials for introducing effective multi-functional groups. Colloids and Surfaces B: Biointerfaces 113:125-133. https://doi.org/10.1016/j.colsurfb.2013.08.041

Guo Z, Sun C, Wang J et al (2021) High-Performance Laminated Fabric with Enhanced Photothermal Conversion and Joule Heating Effect for Personal Thermal Management. ACS Applied Materials & Interfaces 13(7):8851-8862. http://doi.org/10.1021/acsami.0c23123

Guo Z, Sun C, Zhao J et al (2021) Low-Voltage Electrical Heater Based on One-Step Fabrication of Conductive Cu Nanowire Networks for Application in Wearable Devices. Advanced Materials Interfaces 8(3):2001695. https://doi.org/10.1002/admi.202001695

Jia L-C, Sun W-J, Xu L et al (2020) Facile Construction of a Superhydrophobic Surface on a Textile with Excellent Electrical Conductivity and Stretchability. Industrial & Engineering Chemistry Research 59(16):7546-7553. http://doi.org/10.1021/acs.iecr.9b06990

Ma J, Zhao Q, Zhou Y et al (2021) Hydrophobic wrapped carbon nanotubes coated cotton fabric for electrical heating and electromagnetic interference shielding. Polymer Testing 100:107240. https://doi.org/10.1016/j.polymertesting.2021.107240

Gong X, Yu H, Chen X et al (2023) Superhydrophobic PDMS/PPy-Ag/Graphene/PET films with highly efficient electromagnetic interference shielding, UV shielding, self-cleaning and electrothermal deicing. Materials Today Physics 34:101076. https://doi.org/10.1016/j.mtphys.2023.101076

Yang H, Cheng L, Yang Q et al (2023) Multifunctional and durable thermal management coating from sericin-MXene biohybrid on silk fabric micro-etched by deep eutectic solvent. Applied Surface Science 623:156962. https://doi.org/10.1016/j.apsusc.2023.156962

Cai G, Yang M, Pan J et al (2018) Large-Scale Production of Highly Stretchable CNT/Cotton/Spandex Composite Yarn for Wearable Applications. ACS Applied Materials & Interfaces 10(38):32726-32735. http://doi.org/10.1021/acsami.8b11885

Qiu K, Elhassan A, Tian T et al (2020) Highly Flexible, Efficient, and Sandwich-Structured Infrared Radiation Heating Fabric. ACS Applied Materials & Interfaces 12(9):11016-11025. http://doi.org/10.1021/acsami.9b23099

Li D, Wang J, Lu X et al (2019) One-step firing of cellulose fiber and ceramic precursors for functional electro-thermal composites. Materials & Design 181:107941. https://doi.org/10.1016/j.matdes.2019.107941