In-situ growth of SiCw on the surface of C/C composite materials and different influencing factors on the morphology control of SiCw transition layer

Chen Xie, Yun Jiang, Jingtao Chen, Jiahua Min , Jijun Zhang*, Xiaoyan Liang* and Pengfei Hu*

School of Materials Science and Engineering, Shanghai University, Shanghai 200444, China

Corresponding authors. telephone/Fax:+86-18301825160

E-mail：zhangjijun222@shu.edu.cn(J.J.Zhang), xxlyy@shu.edu.cn(X.Y.Liang), hpf-hqx@shu.edu.cn (P.F. Hu)

Table S1 Spectrum information EDS-point scan mode

| Element | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| C | 57.16 | 66.45 | 64.71 | 64.75 | 38.48 | 90.75 |
| O | 0.35 | 0.30 | 0.37 | 0.43 | 2.15 | 4.31 |
| Ni | 41.95 | 32.59 | 33.89 | 33.08 | 59.36 | 4.94 |
| Total | 100 | 100 | 100 | 100 | 100 | 100 |

Table S2 Thermodynamic calculation of Ni salt reduction process

| (1) | Ni(NO3)2·6H2O→ Ni(NO3)2·2H2O→ Ni(NO3)(OH)1.5O0.25·H2O(Basic Salt)→ Ni2O3 + NiO→ NiO(<600 ℃) |  |  |
| --- | --- | --- | --- |
| (2) | NiO + Si = Ni + SiO(g) | ΔG= 134.756 KJ-172.425 J*T | T>781.53 K |
| (3) | NiO + SiO(g) = Ni + SiO2(g) | ΔG= -572.305 KJ+178.377 J*T | T<3208.40 K |
| (4) | NiO + C = Ni + CO(g) | ΔG= 126.616 KJ-178.870 J*T | T>707.86 K |
| (5) | NiO + CO(g) = Ni + CO2(g) | ΔG= -43.112 KJ- 8.361 J*T | ΔG<0 |
| (6) | 2C + O2(g) = 2CO(g) | ΔG= -221.402 KJ- 177.572 J*T | ΔG<0 |
| (7) | 2Si + O2(g) = 2SiO(g) | ΔG= -197.460 KJ- 181.191 J*T | ΔG<0 |

Figure S1.TEM images and EDS spectrum of the Ni-SiCw interface

Figure S2. Morphological structure of beaded SiCw: a-c) TEM and HRTEM images of bead-like SiCw; d) HAADF-STEM and EDS-mapping scan patterns of bead-like SiCw