Supplementary Information

Ιn vitro RNA delivery in breast cancer cells using polysaccharide functionalized SPIONs

Olga Tsave1, Maria Psarrou2,3, Georgia Kastrinaki1,4, Eleni Papachristou5, Rigini Papi5, Vassilios Zaspalis1,4, Lori Nalbandian4†, Charalampos Sarafidis6, Andreas Ouranidis1 Theodora Choli-Papadopoulou5, Maria Vamvakaki2,3, Christos Chatzidoukas1*

1 Department of Chemical Engineering, Aristotle University of Thessaloniki (AUTH), Thessaloniki, 54124, Greece.

2 Department of Materials Science and Technology, University of Crete, Vasilika Vouton, 70013, Heraklion, Crete, Greece.

3Institute of Electronic Structure and Laser, Foundation of Research and Technology-Hellas, Vasilika Vouton, 70013, Heraklion, Crete, Greece.

4 Chemical Process & Energy Resources Institute (CPERI), Centre for Research & Technology Hellas (CERTH), Thessaloniki, Thermi, Greece.

5 Department of Chemistry, Aristotle University of Thessaloniki, GR-54124 Thessaloniki, Greece.

6 Department of Physics, Aristotle University of Thessaloniki, 54124 Thessaloniki, Greece.

Corresponding author. (Assist. Professor. C. Chatzidoukas)

Tel.: +30 2310 99 6167

E-mail address: chatzido@auth.gr

| (a) | (b) |
| --- | --- |
| (c) | (d) |
| (e) | (f) |
| Fig. S1: Raman spectra with the deconvolution curves attributed to magnetite and maghemite for (a) NPs, (b) NPs-CA, (c) NPs-CA-Ch, (d) NPs-CA-Dex, (e) NPs-Ch and (f) NPs-Dx. |  |

Fig. S2: 1H NMR spectrum of Q-chitosan in D2O.

The appearance of the characteristic chemical shift at 3.15 ppm in the 1H NMR spectrum of Q-chitosan, assigned to the protons of the newly incorporated trimethyl ammonium groups (Fig. S2), verified the successful quaternization of the polymer.

Fig. S3: (a) FTIR spectra of chitosan (black solid line) and Q-chitosan (red dashed line) and (b) TGA curves of chitosan (black solid line) and Q-chitosan (red dashed line).

The ATR-FTIR spectra of chitosan (black solid line) before quaternization, showed the vibration band at 1588 cm-1, attributed to the amino groups and the shoulder at 1652 cm-1, attributed to the amide bonds of the chitin units of chitosan []. After quaternization (Q-chitosan, red dashed line), a strong vibration band at 1476 cm-1, which corresponds to the C-H bonds of the newly incorporated trimethyl ammonium groups, appeared, confirming the successful quaternization of the biopolymer. Moreover, a peak at 1650 cm-1, which corresponds to the primary amine groups of chitosan, which were not modified, was evident.

Fig. S4: 1H NMR spectra of dextran and Ox-dextran in d6-DMSO.

The appearance of a new peak at 9.3 ppm in the 1H NMR spectrum of Ox-dextran denoted the successful modification of the polymer.

Fig. S5: (a) FTIR spectra of dextran (black solid line) and Ox-dextran (red dashed line) and (b) TGA curves of dextran (black solid line) and Ox-dextran (red dashed line).

The ATR-FTIR spectrum of Ox-dextran showed the bands at 1019 and 1634 cm-1, which are attributed to the vibrations of the C-O bonds and a characteristic vibration band of the carbonyl bond of the aldehyde group at 1738 cm-1, verifying the successful oxidation of the polymer.

Fig. S6: TEM images of the (a) NPs-CA-Ch and (b) NPs-CA-Dx.

Fig. S7: XRD diagram of the bare Fe3O4 SPIONs.

Fig. S8: (a) TEM image depicting agglomerates of NPs; the dashed line image shows a primary (single) particle defining with white outline the particle perimeter, (b) a high resolution TEM image of a primary particle defining with while outline the crystal planes of a cubic monocrystalline NP; superparamagnetic nanoparticles are monocrystalline

Fig. S8(a) illustrates the agglomerates of nanoparticles as observed in the TEM image. In Fig. S8(b), a primary cubic nanoparticle is depicted, revealing its monocrystalline nature through the orientation of planes in the three-dimensional structure. This observation aligns with the anticipated expectation, as superparamagnetic nanoparticles are known to be monocrystalline.

(b)

(b)

(a)

(a)

(d)

(d)

(c)

(c)

Fig. S9: (a), (b) Cell spheroid formation on days 3 and 12. (c) The hanging drop method. (d) Schematic representation of the diameter of each aggregate obtained as an average of 5 measurements.

Fig. S10: Representative micrographs of cell adhesion of T47D cells following their treatment with SPIONs (photographs obtained using a LEICA inverted microscope, with a 10x phase contrast. Images were captured at several time points).

NPs

NPs

NPs-CA

NPs-CA

NPs-Ch

NPs-Ch

NPs-CA-Ch

NPs-CA-Ch

NPs-Dx

NPs-Dx

NPs-CA-Dx

NPs-CA-Dx

Fig. S11: Representative micrographs of cell morphology of T47D cells following treatment with the SPIONs (photographs obtained using a LEICA inverted microscope, with a 10x phase contrast. Images were captured at several time points).

(a) (a)

(b) (b)

(c) (c)

(d) (d)

Fig. S12: Percentage change of cell survival of the T47D cells (2D monolayers), following treatment with various concentrations (1-1000 μM) of a) NPs, b) NPs-CA, c) NPs-Dx, and NPs-Ch for 24 h in the presence or absence of a magnetic field.

Wan, Y.; Creber, K.A.M.; Peppley, B.; Bui, V.T. Ionic conductivity of chitosan membranes. Polymer (Guildf). 2003, 44, 1057–1065, doi:10.1016/S0032-3861(02)00881-9.