Supporting information

Theoretical Simulation of TADF Character of 9'-Bicarbazole Modified 2,4,6-Triphenyl-1,3,5-triazine

Shuyuan Zhaoa,#, Zhengwen Linb,#, Fang Wangb, Zhenjun Sia,b *, Zhe Chena,*

a School of Materials Science and Technology, Jilin Institute of Chemical Technology, Jilin City, P. R. China

b School of Materials Science and Technology, Changchun University of Science and Technology, Changchun City, P. R. China

# Authors contributed to this article equally.

Fig. S1 Distribution of HOMO-3 ~ LUMO+3 orbitals of o-Trz-DCz, m-Trz-DCz, p-Trz-DCz in toluene solvents.

Table. S1 Energies of S1 and T1 states of p-Trz-DCz calculated by different functionals

|  | B3LYP | PBE0 | BMK | M06-2X | CAM-BLYP | Exp. |
| --- | --- | --- | --- | --- | --- | --- |
| HF% | 20 | 25 | 42 | 54 | 19/65 |  |
| S1/T1 (eV) | 2.89/2.72 | 3.10/2.77 | 3.66/3.14 | 3.91/3.35 | 4.00/2.90 | 3.09/2.86[18] |
| ΔEST (eV) | 0.17 | 0.33 | 0.52 | 0.56 | 1.10 | 0.23[17](0.32)[18] |

Table. S2 Values of θ1, θ2, θ3 and θ4 of o-Trz-DCz, m-Trz-DCz and p-Trz-DCz in S0, S1 and T1 states calculated by G09

| Molecule | State | θ1 | θ2 | θ3 | θ4 |
| --- | --- | --- | --- | --- | --- |
| o-Trz-DCz | S0 | 66.93 | 40.55 | 1.94 | 0.92 |
|  | S1 | 75.54 | 15.84 | 18.86 | 2.80 |
|  | T1 | 62.76 | 15.87 | 14.64 | 3.13 |
| m-Trz-DCz | S0 | 53.33 | 5.60 | 1.53 | 1.21 |
|  | S1 | 63.56 | 0.03 | 1.37 | 0.03 |
|  | T1 | 44.01 | 0.50 | 0.14 | 0.32 |
| p-Trz-DCz | S0 | 52.25 | 1.39 | 0.33 | 0.92 |
|  | S1 | 89.22 | 0.02 | 0.08 | 0.61 |
|  | T1 | 44.94 | 0.37 | 0.16 | 0.33 |

Table. S3 Values of B1, B2, B3 and B4 of o-Trz-DCz, m-Trz-DCz and p-Trz-DCz in S0, S1 and T1 states calculated by G09

| Molecule | State | B1 | B2 | B3 | B4 |
| --- | --- | --- | --- | --- | --- |
| o-Trz-DCz | S0 | 1.41 | 1.48 | 1.47 | 1.48 |
|  | S1 | 1.43 | 1.43 | 1.49 | 1.48 |
|  | T1 | 1.42 | 1.43 | 1.49 | 1.48 |
| m-Trz-DCz | S0 | 1.41 | 1.48 | 1.48 | 1.48 |
|  | S1 | 1.44 | 1.43 | 1.49 | 1.49 |
|  | T1 | 1.39 | 1.42 | 1.48 | 1.48 |
| p-Trz-DCz | S0 | 1.41 | 1.48 | 1.48 | 1.48 |
|  | S1 | 1.43 | 1.43 | 1.49 | 1.49 |
|  | T1 | 1.40 | 1.42 | 1.48 | 1.48 |

Table. S4 Contribution of B, A and  to the  during the S0  S1 process and the SOC constants (cm-1) between S1 and T1 of o-Trz-DCz, m-Trz-DCz and p-Trz-DCz.

| Molecule | (meV) |  |  |  |  | <S1¦ĤSO¦T1> |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | B | A |  | Total |  | S1 | T1 |
| o-Trz-DCz | 214.40 | 60.56 | 119.50 | 394.46 |  | 0.1345 | 0.2520 |
| m-Trz-DCz | 212.62 | 65.58 | 54.45 | 332.65 |  | 0.1819 | 0.4869 |
| p-Trz-DCz | 209.18 | 34.76 | 261.91 | 505.85 |  | 0.0173 | 0.2934 |

* Corresponding authors: Zhenjun Si (sizhenjun@jlict.edu.cn), Zhe Chen (chenzhe0809@foxmail.com)