Supporting Information

REMOVAL OF RHODAMINE B AND METHYLENE BLUE USING RESIDUAL Onecarpus bacaba Mart FIBERS AS BIOSORBENT: KINETIC AND THERMODYNAMIC PARAMETERS

Eberlanny Moraes Rolim1, Andreza Miranda Barata da Silva1, Joel dos Santos Batista1, Naiany Oliveira Serrão1, Leticia Layer Oliver2, Flávio Augusto de Freitas3, Gustavo Frigi Perotti1, Dominique Fernandes de Moura do Carmo1, Gustavo de Gusmão Celestino4, Paulo José Sousa Maia2

1Instituto de Ciências Exatas e Tecnologia, Universidade Federal do Amazonas, Itacoatiara, Amazonas 69103128, Brasil

2 Universidade Federal do Rio de Janeiro, Campus Macaé Professor Aloísio Teixeira, Polo Universitário, 27930-560, Macaé, Rio de Janeiro, Brasil

3Centro de Biotecnologia da Amazônia –CBA, Av. Gov. Danilo de Matos Areosa, 690 - Distrito Industrial I, Manaus - AM, 69075-351, Brasil

4Universidade Federal do Rio de Janeiro, Programa de Engenharia Metalúrgica e de Materiais/COPPE/LADPOL, Av. Horácio Macedo, 2030, Bloco F, 21941598 Rio de Janeiro, RJ, Brasil

*To whom correspondence should be addressed:

Paulo José Sousa Maia (pmldcb@gmail.com)

orcid.org/0000-0003-3101-3712

Figure S1. FTIR spectra for OBMi and OBMm.

Figure S2. pH × pHf; point of zero charge for OBMi/OBMm at pH 4.34 and 6.06, respectively (200 mg of the adsorbent, 25 mL of solution at 25 ºC).

Figure S3. Effect of initial on adsorption of (A) RhB and (B) MB onto in natura (OBMi) and NaOH-modified (OBMm) Onecarpus bacaba Mart fibers.

Figure S4. Effect of ionic strength on (A) MB and (B) RhB for OBMi and OBMm (adsorbent dosage = 200 mg, solution volume = 50 mL; contact time = 3 h; temperature = 298 K).

Figure S5. Adsorption kinetics for pseudo-first-order model and pseudo-second-order model analyses and experimental results: (A) OBMm:RhB and (B) OBMm:MB, and for the interparticle diffusion model: (C) OBMm:RhB and (D) OBMm:MB  at 25 °C and pH 6.

Figure S6: Adsorption isotherms and model fit for adsorption isotherm with adsorption isotherms at optimized conditions: (A) OBMm:MB and B) RhB on OBMm at 25 ºC.

Figure S7. Adsorption isotherms and model fit for adsorption isotherm with adsorption isotherms at optimized conditions: (A) OBMm:MB and (B) OBMm:RhB at 25 ºC