Supporting Information

Ultrathin, ultralight dual-scale fibrous networks with high infrared transmittance for high-performance, comfortable and sustainable PM0.3 air filter

Yuchen Yang 1, 2, 3, Xiangshun Li 3, Zhiyong Zhou 3, Qiaohua Qiu 3, 4, Wenjing Chen 3, Jianying Huang 1, 2, Weilong Cai 1, 2, Yuekun Lai 1, 2, *, Xiaohong Qin 3, *

1 Qingyuan Innovation Laboratory, Quanzhou 362801, P. R. China;

2 College of Chemical Engineering, Fuzhou University, Fuzhou 350116, P. R. China;

3 Key Laboratory of Textile Science & Technology of Ministry of Education, College of Textiles, Donghua University, Shanghai 201620, P. R. China;

4 College of Textile Science and Engineering, Zhejiang Sci-Tech University, Hangzhou 310018, P. R. China

*Corresponding authors. E-mails: yklai@fzu.edu.cn (Yuekun Lai), xhqin@dhu.edu.cn (Xiaohong Qin)

Figure S1. SEM images of PA6 fiber mats produced by (a) 3 wt%, (b) 4 wt%, (c) 5 wt% and (d) 5.5 wt% PA6 solutions.

Figure S2. SEM images of PA6/DTAC fiber mats produced by (a) 1 wt%, (b) 3 wt%, (c) 6 wt% and (d) 12 wt% DTAC ratios.

Figure S3. (a) Filtration efficiency, filtration resistance and (b) quality factor of various PA6 and PA6/DTAC fiber filters with different electrospinning time.

Figure S4. Optical images of KN95, N95 (MBM) and medical (MM) masks.

Table S1. Preparation parameters for various electrospun fiber mats.

| Samples | PA6 Concentration (wt%) | Mass ratio of DTAC to PA6 (wt%) | Voltage (kV) | Liquid supply rate (mm/s) | Distance (cm) |
| --- | --- | --- | --- | --- | --- |
| PA6 | 5.5 | 0 | 15 kV | 0.05 | 10 |
| PA6/DTAC-1 | 5.5 | 1 | 20 kV | 0.03 | 10 |
| PA6/DTAC-2 | 5.5 | 3 | 20 kV | 0.018 | 10 |
| PA6/DTAC-3 | 5.5 | 6 | 20 kV | 0.014 | 10 |
| PA6/DTAC-4 | 5.5 | 12 | 20 kV | 0.01 | 10 |