Supporting Information

Multifunctional cellulose composite films with dual-continuous CNT/BN networks for synchronously enhanced electromagnetic interference shielding effectiveness and thermal conductivity

Liang-Qing Zhang1,3* · Fang Zhou1 · Qin Shi1 · Zheng-Yang Zhang1 · Shu-Gui Yang2 · Ding-Xiang Yan3

1 College of Materials Science and Engineering, Xi’an University of Science and Technology, Xi’an, 710054, China

2 Shaanxi International Research Center for Soft Matter, State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, China

3 College of Polymer Science and Engineering, State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu 610065, China

*Corresponding Author: Liang-Qing Zhang

E-mail: liangqingzhang@xust.edu.cn

Figure S1. SEM images of the morphology of CNT/BN-x composites before hot pressing (A-E), and corresponding local enlarged image (A1-E1)

Table S1. Thickness of CNT/BN-x composites before and after hot pressing

| Samples | Before hot pressing | After hot pressing |
| --- | --- | --- |
|  | Thickness (mm) | Thickness (mm) |
| CNT/BN-5 | 2 | 0.417 |
| CNT/BN-10 | 2 | 0.393 |
| CNT/BN-15 | 2 | 0.439 |
| CNT/BN-20 | 2 | 0.403 |
| CNT/BN-30 | 2 | 0.489 |

Table S2. Comparison of EMI shielding performances for different materials

| Materials | Thickness (mm) | σ (S/m) | EMI SE (dB) | Ref |
| --- | --- | --- | --- | --- |
| rGO/PEI | 2.3 | 0.001 | 22 | (Ling et al. 2013) |
| S-doped rGO/PS | 2 | 33 | 24.5 | (Shahzad et al. 2015) |
| graphite/EP | 5 | 2.6 | 11 | (De Bellis et al. 2011) |
| CF/PP | 3.2 | 10 | 25 | (Ameli et al. 2013) |
| rGO/PS | 2.5 | 1.25 | 29 | (Yan et al. 2012) |
| SWCNTs/EP | 2 | 20 | 25 | (Huang et al. 2007) |
| rGO/Fe2O3/PVA | 0.36 | 3 | 20.3 | (Yuan et al. 2014) |
| CF/CNT/PS | 1 | 0.215 | 21.9 | (Yang et al. 2007) |
| SWCNTs/PU | 2 | 2.2×10-4 | 17 | (Liu et al. 2007) |
| rGO/Fe3O4/PVC | 1.8 | 7.7×10-4 | 13 | (Yao et al. 2015) |
| CNT/cellulose-BN/PVA | 0.39 | 78.1 | 29.8 | This work |

Table S3. Comparison of EMI SE and λ for different materials

| Materials | Thickness (mm) | EMI SE (dB) | λ// (W/mK) | λ⊥ (W/mK) | Ref |
| --- | --- | --- | --- | --- | --- |
| PVDF/CNT/Co-flower | 0.3 | 32 | 1.3 | / | (Li et al. 2018) |
| RGO@Fe3O4/epoxy | 1 | 13 | 1.2 | 0.08 | (Liu et al. 2019) |
| MWCNT-Fe3O4@Ag/epoxy | 2 | 35 | 0.46 | / | (Wang et al. 2019) |
| PVDF/Fe3O4/CNT | 1.1 | 33 | 0.62 | / | (Cheng et al. 2019) |
| PVDF/Fe3O4/GNP | 1.1 | 36 | 0.68 | / | (Cheng, Wei et al. 2019) |
| PVDF@5MWCNT/40BN | 2 | 8.86 | 0.83 | / | (Zhang et al. 2019) |
| rGO/NR | 2 | 26 | 1.53 | / | (An et al. 2023) |
| LLDPE/BN@GNPs | 1.75 | 27 | 3.11 | 1.02 | (Peng et al. 2023) |
| CNT/cellulose-BN/PVA | 0.39 | 29.8 | 3.567 | 1.025 | This work |

Reference

Ameli A, Jung P U and Park C B (2013) Electrical properties and electromagnetic interference shielding effectiveness of polypropylene/carbon fiber composite foams. Carbon 60: 379-391. http://10.1016/j.carbon.2013.04.050

An D, et al. (2023) The polymer-based thermal interface materials with improved thermal conductivity, compression resilience, and electromagnetic interference shielding performance by introducing uniformly melamine foam. Adv Compos Hybrid Mater 6: 136. http://10.1007/s42114-023-00709-1

Cheng H, Wei S, Ji Y, Zhai J, Zhang X, Chen J and Shen C (2019) Synergetic effect of Fe3O4 nanoparticles and carbon on flexible poly(vinylidence fluoride) based films with higher heat dissipation to improve electromagnetic shielding. Compos Part A Appl Sci Manuf. 121: 139-148. http://10.1016/j.compositesa.2019.03.019

De Bellis G, Tamburrano A, Dinescu A, Santarelli M L and Sarto M S (2011) Electromagnetic properties of composites containing graphite nanoplatelets at radio frequency. Carbon 49: 4291-4300. http://10.1016/j.carbon.2011.06.008

Huang Y, et al. (2007) The influence of single-walled carbon nanotube structure on the electromagnetic interference shielding efficiency of its epoxy composites. Carbon 45: 1614-1621. http://10.1016/j.carbon.2007.04.016

Li X, et al. (2018) Quick heat dissipation in absorption-dominated microwave shielding properties of flexible poly(vinylidene fluoride)/carbon nanotube/Co composite films with anisotropy-shaped Co (flowers or chains). ACS Appl Mater Interfaces 10: 40789-40799. http://10.1021/acsami.8b14733

Ling J, Zhai W, Feng W, Shen B, Zhang J and Zheng W (2013) Facile preparation of lightweight microcellular polyetherimide/graphene composite foams for electromagnetic interference shielding. ACS Appl Mater Interfaces 5: 2677-2684. http://10.1021/am303289m

Liu Y, et al. (2019) Anisotropic thermal conductivity and electromagnetic interference shielding of epoxy nanocomposites based on magnetic driving reduced graphene oxide@Fe3O4. Compos Sci Technol 174: 1-10. http://10.1016/j.compscitech.2019.02.005

Liu Z, et al. (2007) Reflection and absorption contributions to the electromagnetic interference shielding of single-walled carbon nanotube/polyurethane composites. Carbon 45: 821-827. http://10.1016/j.carbon.2006.11.020

Peng Z, Lv Q, Jing J, Pei H, Chen Y and Ivanov E (2023) FDM-3D printing LLDPE/BN@GNPs composites with double network structures for high-efficiency thermal conductivity and electromagnetic interference shielding. Compos Part B Eng 251: 110491. http://10.1016/j.compositesb.2022.110491

Shahzad F, Yu S, Kumar P, Lee J-W, Kim Y-H, Hong S M and Koo C M (2015) Sulfur doped graphene/polystyrene nanocomposites for electromagnetic interference shielding. Compos Struct 133: 1267-1275. http://10.1016/j.compstruct.2015.07.036

Wang L, et al. (2019) Electromagnetic interference shielding MWCNT-Fe3O4@Ag/epoxy nanocomposites with satisfactory thermal conductivity and high thermal stability. Carbon 141: 506-514. http://10.1016/j.carbon.2018.10.003

Yan D-X, Ren P-G, Pang H, Fu Q, Yang M-B and Li Z-M (2012) Efficient electromagnetic interference shielding of lightweight graphene/polystyrene composite. J Mater Chem 22: 18772. http://10.1039/c2jm32692b

Yang Y, Gupta M C and Dudley K L (2007) Towards cost-efficient EMI shielding materials using carbon nanostructure-based nanocomposites. Nanotechnology 18: 345701. http://10.1088/0957-4484/18/34/345701

Yao K, et al. (2015) Flammability properties and electromagnetic interference shielding of PVC/graphene composites containing Fe3O4 nanoparticles. RSC Adv 5: 31910-31919. http://10.1039/c5ra01046b

Yuan B, Bao C, Qian X, Song L, Tai Q, Liew K M and Hu Y (2014) Design of artificial nacre-like hybrid films as shielding to mitigate electromagnetic pollution. Carbon 75: 178-189. http://10.1016/j.carbon.2014.03.051

Zhang P, et al. (2019) Segregated double network enabled effective electromagnetic shielding composites with extraordinary electrical insulation and thermal conductivity. Compos Part A Appl Sci Manuf 117: 56-64. http://10.1016/j.compositesa.2018.11.007