Design on Modified Glass Fiber Separator by Ball-milled Tin Fluoride (SnF2) particles for Zn Metal Anodes with High Reversibility

Huaijun Zhanga, Hengyu Yanga, Banghui Wua, Yongle Lianga, Wentao Nia, Guobao Xub, Liwen Yang a*

a School of Physics and Optoelectronics, Xiangtan University, Hunan, 411105, China

b School of Materials Science and Engineering, Xiangtan University, Hunan, 411105,

China

Fig.S1 (a) SEM image of commercial SnF2 powder; (b) SEM images of SnF2@GF separator; (c) Digital image of GF separator (left) and SnF2@GF separator (right).

Fig.S2 The electrochemical performance tests of Zn||Zn symmetric cells with different concentration loading (0 mg cm−2, 0.5 mg cm−2, 1 mg cm−2 and 2 mg cm-2) after SnF2 modifying at the working condition of 1 mA cm-2 and 1mAh cm-2.

GF

SnF2@GF

Fig.S3 Digital photos about the contact angles test of water dropped over GF and SnF2@GF separator.

Fig.S4 The SEM images of polished Zn anodes.

Fig.S5 XRD pattern of as-prepared MnO2 cathode material.

Fig.S6 The corresponding charge/discharge curves of GF separators recorded at different current densities.

Table S1. The comparison of our results with the reported separators modified by

different materials.

| Zn anode | Current density (mA cm-2) | Areal capacity (mAh cm-2) | Cycle life (h) | Ref. |
| --- | --- | --- | --- | --- |
| VG | 1 | 1 | 250 | [1] |
|  | 5 | 5 | 80 |  |
| g-C3N4/GF separators | 1 | 1 | 600 | [2] |
|  | 5 | 1 | 870 |  |
| MXene | 1 | 1 | 1180 | [3] |
|  | 5 | 1 | 1200 |  |
| Zn@ZnF2-Sn | 1 | 1 | 700 | [4] |
|  | 5 | 1 | 700 |  |
| g-C3N4/cellulose fiber separator | 3 | 1 | 590 | [5] |
|  | 5 | 1 | 320 |  |
| SnF2@GF | 1 | 1 | 1400 | This work |
|  | 5 | 1 | 1000 |  |

Supporting References

[1]	D. Han, S. Wu, S. Zhang, Y. Deng, C. Cui, L. Zhang, Y. Long, H. Li, Y. Tao, Z. Weng, Q. H. Yang, F. Kang, Small 2020, 16, 2001736.

[2]	L. S. Wu, Y. Zhang, P. Shang, Y. F. Dong, Z. S. Wu, Journal of Materials Chemistry A 2021, 9, 27408-27414.

[3]	Y. W. Su, B. Z. Liu, Q. H. Zhang, J. Peng, C. H. Wei, S. Li, W. P. Li, Z. K. Xue, X. Z. Yang, J. Y. Sun, Advanced Functional Materials 2022, 32, 2204306.

[4]	C.-L. Xu, J.-H. Li, Y.-H. Feng, B. Yuan, J. Liu, M. Liu, F. Shen, P.-F. Wang, X. Han, Journal of Power Sources 2022, 548, 232044.

[5]	Y. Yang, T. Chen, B. Yu, M. Zhu, F. Meng, W. Shi, M. Zhang, Z. Qi, K. Zeng, J. Xue, Chemical Engineering Journal 2022, 433, 134077.