Table 1 Physical properties of reactive dyes
	
Dye
	
Molecular 
formula
	
MW
(g/mol)
	
λmax
(nm)
	Number of chemical group

	
	
	
	
	
-SO3Na
	
-OH
	
-NH2
	


	



	RB 171
	C40H23Cl2N15Na6O19S6

	1418.9 
	610
	6
	1
	1
	4
	1

	RR195
	C31H19ClN7Na5O21S6

	1168.3 
	540
	5
	-
	-
	1
	2

	RY184
	C19H18N4Na2O11S3

	620.54
	420
	2
	-
	-
	2
	-







































Table 2 Effect of DADMAC concentration on dyes adsorption
	DADMAC concentration (%)
	Red
	Blue
	Yellow

	0 (Untreated cotton fabric)
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	20
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	30
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	40
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	50
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	60
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