# Electronic Supplementary Information

for

Pyridine-mediated B–B bond cleavage of tetrahydroxydiboron to synthesize n-doped SWCNTs with long-term air stability

Naoki Tanaka*, Aoi Hamasuna, Itsuki Yamaguchi, Koichiro Kato, and Tsuyohiko Fujigaya*

Corresponding Author

Naoki Tanaka: tanaka.naoki.468@m.kyushu-u.ac.jp

Tsuyohiko Fujigaya: fujigaya.tsuyohiko.948@m.kyushu-u.ac.jp

# Figure S1 Seebeck coefficient of the doped SWCNT films using 4-CNpy (red), 4-Phpy (blue), 4-COOHpy (yellow green), and B2(OH)4 (green) in air. Black shows pristine SWCNT films.

# Figure S2. Energy levels of (4-CNpy)B(OH)2•, (4-Phpy)B(OH)2•, (4-COOHpy)B(OH)2•, and (4-Phpy)Bpin• in optimized geometries [UB3LYP/6-31G++(d,p) level of theory].

# Figure S3 XPS survey scans of the N-doped SWCNT films using B2(OH)4/4-Phpy.

# Figure S4 XPS narrow scans of B 1s for pristine SWCNT film (black) and SWCNT film after immersing in B2(OH)4 solution (red).

# Figure S5. Resonance structures of boryl radicals and dopant cations.

# Figure S6. Molecular orbital of HOMO–7 of (4-Phpy)B(OH)2+ in the optimized geometry [B3LYP/6-31G(d,p)].

# Figure S7. Thermogravimetric analysis of pristine SWCNT film (black) the n-doped SWCNT films using B2pin2/4-Phpy (red) and B2OH4/4-Phpy (blue)

# Table S1. Energy gain after doping of SWCNT using B2OH4/4-CNpy, B2OH4/4Phpy, B2pin2/4-CNpy, and B2pin2/4-Phpy.

|  | # Complex [Hartree] | # SWCNT [Hartree] | # Dopant [Hartree] | # Energy gain [Hartree] | # Energy gain [kcal/mol] |
| --- | --- | --- | --- | --- | --- |
| # (4-CNpy)B(OH)2 # /SWCNT | # –8151.952 | # –7634.718 | # –517.194 | # –0.040 | # –25.154 |
| # (4-Phpy)B(OH)2 # /SWCNT | # –8290.791 | # –7634.718 | # –656.023 | # –0.050 | # –31.290 |
| # (4-CNpy)Bpin # /SWCNT | # –8386.671 | # –7634.718 | # –751.899 | # –0.053 | # –33.223 |
| # (4-Phpy)Bpin # /SWCNT | # –8525.510 | # –7634.718 | # –890.729 | # –0.063 | # –39.413 |

# Table S2. Charge change of dopants before and after doping.

|  | # Molecular charge in isolation [e] | # Molecular charge after doping [e] |
| --- | --- | --- |
| # (4-CNpy)B(OH)2• | # 0 | # +0.02 |
| # (4-Phpy)B(OH)2• | # 0 | # +0.21 |
| # (4-CNpy)Bpin• | # 0 | # +0.10 |
| # (4-Phpy)Bpin• | # 0 | # +0.01 |