Supplementary material

Simultaneous study of different combinations of ZSM-5 templates and operating conditions in the MTP process; Designing, Modeling and Optimization by RSM-ANN-GA

Neda Kalantari a, Ali Farzi a,, Faez Hamooni a, Nagihan Çaylak Delibaş b, Ali Tarjomannejad a, Aligholi Niaei a,*, Dariush Salari c.

a Reactor & Catalyst Research Lab., Department of Chemical & Petroleum Engineering, University of Tabriz, Tabriz, Iran

b Department of Physics, Sakarya University, Sakarya, Turkey

c Department of Applied Chemistry, Faculty of Chemistry, University of Tabriz, Tabriz, Iran

Table S1 The ranges set for templates.

| Parameter | Levels and ranges |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | -1.5 | -1.0 | 0.0 | 1.0 | 1.5 |
| TPABr/SiO2 | 0.05 | 0.075 | 0.125 | 0.175 | 0.2 |
| CTAB/SiO2 | 0 | 0.0066 | 0.02 | 0.033 | 0.04 |
| F127/SiO2 | 0 | 0.0002 | 0.0006 | 0.001 | 0.0012 |

Fig. S1 Comparison of propylene selectivity and methanol conversion for RSM prediction and experimental data

a

b

Fig. S2 Comparison of propylene selectivity and methanol conversion for ANN prediction and experimental data

Fig. S3 Methanol conversion and propylene selectivity against variables;

(a) Temperature and WHSV,

(b) TPABr/SiO2 and WHSV,

(c) F127/SiO2 and WHSV,

(d) CTAB/SiO2 and WHSV,

(e) Temperature and TPABr/SiO2, (f) Temperature and CTAB/SiO2, (g) TPABr/SiO2 and CTAB/SiO2, (h) CTAB/SiO2 and F127/SiO2

a

b

c

d

f

g

e

h

Fig. S3 Methanol conversion and propylene selectivity against variables;

(a) Temperature and WHSV,

(b) TPABr/SiO2 and WHSV,

(c) F127/SiO2 and WHSV,

(d) CTAB/SiO2 and WHSV,

(e) Temperature and TPABr/SiO2, (f) Temperature and CTAB/SiO2, (g) TPABr/SiO2 and CTAB/SiO2, (h) CTAB/SiO2 and F127/SiO2

Fig. S4 XRD diffractions of HZ-GA Zeolite and reference pattern [1,2]

Fig. S5 (a) N2 adsorption-desorption isotherm and (b) BJH pore size distribution of HZ-GA

Fig. S6 NH3-TPD profile of HZ-GA sample

Fig. S7 Comparison of product yields on HZ-GA catalyst at temperatures of 300 ºC and 419 ºC after 2 h and 34 h of reaction time

Corresponding Author(s) E-mail: a-farzi@tabrizu.ac.ir, Phone: +98 4133392420 , Fax: +98 4133338497

aniaei@tabrizu.ac.ir, Phone: +98 4133392417 , Fax: +98 4133338497