Investigation of the release rate of biocide and corrosion resistance of vinyl-, acrylic-, and epoxy-based antifouling paints on steel in marine infrastructures

Adel Jalaiea, Abdolah Afshaara*, Seyed Borhan Mousavib**, Mohammad Heidaric

a Department of Materials Science and Engineering, Sharif University of Technology, Tehran, Iran

b Department of Materials Science and Engineering, Texas A&M University, College Station, TX 77843, USA

c Faculty of Chemical & Petroleum Engineering, University of Tabriz, Tabriz, Iran

*Corresponding 1 email: afshaar@sharif.edu

**Corresponding 2 emails:seyedborhanm@gmail.com, borhanm@tamu.edu

Table S1 Chemical composition of St-37 steel.

| Element | Mn | P | S | C | Fe |
| --- | --- | --- | --- | --- | --- |
| Percent (wt%) | 0.6 | 0.03 | 0.02 | 0.17 | 0.18 |

Table S2 Composition of Cu2O and ZnO biocide paints at different contents and the role of used additives.

| Material | Role | wt% |
| --- | --- | --- |
| Resin (binder) | Film-forming component of paint | 10, 20, 30, 40, 50, 60, and 70±0.1 |
| Cu2O particles | Biocide activity | 0, 7, 14, 20, 27, 33, and 40±0.1 |
| ZnO particles | Biocide activity | 0, 3, 6, 10, 13, 17, and 20±0.1 |
| Titanium dioxide (pigment) | Providing the color of the paint | 5±0.1 |
| Iron (III) oxide red (pigment) | Providing the color of the paint | 5±0.1 |
| Dioctyl phthalate | Providing better pigment dispersion | 5±0.1 |
| Talc | Providing the color of the paint | 5±0.1 |
| Efka FA 4644 | Dispersing agent | 2±0.1 |
| BYK310 | Providing uniform dispersion | 2±0.1 |

Table S3 Specification of artificial seawater.

| Material | Concentration (gr/liter) |
| --- | --- |
| NaCl | 24.53 |
| MgCl2.6H2O | 5.20 |
| Na2SO4 | 4.09 |
| CaCl2 | 1.16 |
| KCl | 0.695 |
| NaHCO3 | 0.201 |
| H3BO3 | 0.207 |

Fig. S1. Real photo of the designed laboratory system.

Fig. S2. Schematic of the designed laboratory system.

Fig. S3. Real photo of built setup for algae growth.

Table S4 Chemical composition of used water in the algae growth environment.

| Material | Concentration (gr/dm3) |
| --- | --- |
| K2HPO4 | 2 |
| KH2PO4 | 3.4 |
| MgSO4.7H2O | 2 |
| NaNO3 | 0.6 |
| CaCl2.2H2O | 0.6 |
| NaCl | 0.5 |
| KOH | 3 |
| FeSO4.7H2O | 0.5 |
| H2SO4 | 0.184 |
| H3BO3 | 1 |
| ZnSO4.7H2O | 0.3 |
| MnCl2.4H2O | 0.05 |
| CuSO4.5H2O | 0.06 |
| Co(NO3)2.6H2O | 0.02 |
| Na2MoO4.2H2O | 0.04 |

Fig. S4. Real photos after 3 months of sample (a) without antifouling coating, (b) with substrate and without antifouling coating, (c) 20 wt% epoxy-based antifouling coating, (d) 60 wt% epoxy-based antifouling coating, (e) 10 wt% acrylic-based antifouling coating, (f) 30 wt% acrylic-based antifouling coating, (g) 20 wt% vinyl/rosin-based antifouling coating, (h) 50 wt% vinyl/rosin-based antifouling coating.

Table S5 The pencil hardness and König pendulum hardness results of prepared antifouling paints.

| Resin | Total biocide content (wt%) | Pencil Hardness degree | König pendulum Oscillation time (s) |
| --- | --- | --- | --- |
| Acrylic | 10 | B | 65 |
|  | 30 | H | 67 |
|  | 40 | 3H | 70 |
| Epoxy | 20 | 5H | 91 |
|  | 40 | 5H | 127 |
|  | 60 | 6H | 165 |
| Vinyl/rosin | 20 | 4H | 78 |
|  | 40 | 4H | 109 |
|  | 50 | B | 65 |

(a)                                            (b)                                                  (c)

Fig. S5. Photos of (a) acrylic resin, (b) epoxy resin, (c) vinyl/rosin resin after bending test.

Table S6 Obtained dolly separation force at diverse biocides content of acrylic, epoxy, and vinyl/rosin resins.

| Resin | Total biocide content (wt%) | Pin (dolly) separation force (MPa) |
| --- | --- | --- |
| Acrylic | 30 | 12/4 |
|  | 40 | 61/4 |
| Epoxy | 40 | 58/9 |
|  | 60 | 41/8 |
| Vinyl/rosin | 40 | 61/6 |
|  | 50 | 17/7 |

(a)                                            (b)

(c)                                              (d)

(e)                                          (g)

Fig. S6. Photos of (a) 30 wt% acrylic-based antifouling coating, (b) 40 wt% acrylic-based antifouling coating, (c) 40 wt% epoxy-based antifouling coating, (d) 60 wt% epoxy-based antifouling coating, (e) 40 wt% vinyl/rosin-based antifouling coating, (g) 50 wt% vinyl/rosin-based antifouling coating after pull-off test.

Table S7 Gloss test results at diverse biocides content of acrylic, epoxy, and vinyl/rosin resins.

| Resin | Total biocide content (wt%) | Lux |
| --- | --- | --- |
| Acrylic | 30 | 26 |
|  | 40 | 20 |
| Epoxy | 40 | 42 |
|  | 60 | 40 |
| Vinyl/rosin | 40 | 45 |
|  | 50 | 38 |

Fig. S7. Photos of (a) acrylic-based antifouling coating, (b) epoxy-based antifouling coating, (c) vinyl/rosin-based antifouling coating after impact resistance test from different heights.

Table S8 Mass loss of the samples after abrasion resistance test.

| Resin | Total biocide content (wt%) | Initial weight (g) | Final weight (g) | Mass loss (g) |
| --- | --- | --- | --- | --- |
| Acrylic | 30 | 62.847 | 62.83 | 0.017 |
| Epoxy | 60 | 64.196 | 64.18 | 0.016 |
| Vinyl/rosin | 50 | 63.301 | 63.30 | 0.001 |

Fig. S8. Photos of (a) acrylic-based antifouling coating, (b) epoxy-based antifouling coating, (c) vinyl/rosin-based antifouling coating after abrasion resistance test.

Table S9 Required force for the scratch resistance of the prepared paints.

| Resin | Total biocide content (wt%) | Applied weight (g) | Photo of formed scratch |
| --- | --- | --- | --- |
| Acrylic | 30 | 1500 |  |
| Epoxy | 60 | 3000 | No scratch |
| Vinyl/rosin | 50 | 2000 |  |

Table S10 Obtained data from the polarization curve of antifouling paints and primer coating.

| Resin | Ecorr (V) | Icorr×10-6 (Acm2) | Corrosion rate (mmyear) |
| --- | --- | --- | --- |
| Primer coating | -0.83 | 79 | 3.61 |
| Acrylic 30 wt% | -0.39 | 3.2 | 0.128 |
| Epoxy 60 wt% | -0.27 | 0.082 | 0.013 |
| Vinyl/rosin 50 wt% | -0.58 | 0.47 | 0.0188 |

Fig. S9. Polarization curves of antifouling paints at different contents of polyaniline in 3.5% NaCl solution.

Table S11 Obtained data from the polarization curve of antifouling paints containing polyaniline.

| Polyaniline concentration (wt%) | Ecorr (V) | Icorr×10-6 (Acm2) | Corrosion rate (mmyear) |
| --- | --- | --- | --- |
| 0 | -0.73 | 6.3 | 0.24 |
| 10 | 0.11 | 0.0093 | 0.00035 |
| 15 | 0.23 | 0.37 | 0.0148 |
| 20 | 0.47 | 8.7 | 0.348 |
| 30 | -0.07 | 3.1 | 0.11 |

Fig. S10. Photos of sample (a) without polyaniline, (b) containing 10 wt% polyaniline after 3 months.