Supporting Information

Efficient removal of methylene blue and tetracycline hydrochloride with C60/MIL-101(Fe) as a reusable photocatalyst under visible light

Zhuyou Zhou1·Congyang Zou(corresponding author)1·Yong Wang1

·Menghe Liu1·Yufeng Ji1

- School of Environmental Science and Engineering, Suzhou University of Science and Technology, Suzhou 215009, Jiangsu, China

----------------------------------

* Corresponding author’s E-mails: ericcongyang@126.com

Tel:+8617751098666

Fig. S1 Standard curve of TCH.

Fig. S2 Standard curve of MB.

Table S1. Surface Area and Pore Structure Parameters of MIL-101(Fe) and C60/MIL-101(Fe)

| samples | BET surface area (m2·g−1) | Langmuir surface area (m2·g−1) | pore volume (cm3·g−1) | pore diameter (nm) |
| --- | --- | --- | --- | --- |
| MIL-101(Fe) | 225.7777 | 398.3818 | 0.185502 | 3.2865 |
| C60/MIL-101(Fe) | 260.2053 | 389.5439 | 0.146603 | 2.2536 |

Fig. S3 Proportion of materials with different particle sizes.

Fig. S4 Pore size distributions of the prepared MIL-101(Fe) and C60/MIL-101(Fe).