An Unprecedented Crystalline La(II)-Chalcogenide LaMg6Ga6S16 with Multifunctional Properties

Yujie Zhang, Jiale Chen, Hongping Wu, Zhanggui Hu, Jiyang Wang, Yicheng Wu and Hongwei Yu*

CONTENTS

Figure S1 (Experimental and calculated XRD patterns)	2

Figure S2 (EDS spectra)	3

Figure S3 (Powder XRD patterns of in-situ variable-temperature and different

reaction temperature)	4

Figure S4 (Moisture-stable LaMg6Ga6S16)	5

Figure S5 (Excitation-dependent PL spectrum of La2S3)	6

Figure S6 (Crystal orientation)	7

Figure S7 (Birefringence determination of LaMg6Ga6S16 crystal)	8

Figure S8 (NLO properties of LaMg6Ga6S16 and other important IR NLO crystals)	9

Table S1 (Crystallographic Data and Refinement Details)	10

Table S2 (Atomic coordinates, displacement parameters and BVS)	11

Table S3 (Selected bond distances and angles)	12

Table S4 (Induced polarizability of MgS6 and GaS4 groups)	16

Table S5 (NLO properties of LaMg6Ga6S16 and some reported chalcogenides)	17

References	18

Figure S1. Experimental and calculated XRD patterns for LaMg6Ga6S16.

Figure S2. The EDS spectra of LaMg6Ga6S16.

Figure S3. In-situ variable-temperature powder XRD (a) and variable-temperature powder XRD (b) of the LaMg6Ga6S16.

Figure S4. The moisture-stable LaMg6Ga6S16: the crystal was soaked in the water for 7d (a) before soaking; (b) soaking in the water; (c) after soaking.

Figure S5. Excitation-dependent PL spectra of La2S3 at the room temperature.

Figure S6. Thickness of LaMg6Ga6S16 crystal, inset: crystal for birefringence determination and its interference color observed in the cross-polarized light.

Figure S7. The crystal orientation of the LaMg6Ga6S16 was indexed by using a Bruker SMART APEX III.

Figure S8. The well-balanced NLO properties of LaMg6Ga6S16 (a); Comparison of SHG response and band gap of LaMg6Ga6S16 with AGS and other reported chalcogenides (b). Explanation: compared with commercial chalcopyrite-type AGS and other important IR NLO crystals, LaMg6Ga6S16 exhibits well-balanced NLO properties, including wide transmission region and band gaps, high LIDT, moderate birefringence as well as large PM SHG responses.

Table S1. Crystallographic Data and Refinement Details for LaMg6Ga6S16.

| Empirical formula | LaMg6Ga6S16 |
| --- | --- |
| Formula weight | 3648.16 |
| Temperature (K) | 297(2) |
| Crystal system | Hexagonal |
| Space group | P—6 |
| Z | 1 |
| a (Å) | 16.7154(5) |
| c (Å) | 7.4147(3) |
| V (Å3) | 1794.15(13) |
| Dc (g cm-3) | 3.376 |
| μ (mm-1) | 9.949 |
| F(000) | 1713 |
| Radiation | Mo-Kα (λ = 0.71073) |
| 2θ range(°) | 2.44 to 25.34 |
| Reflections collected | 9331 |
| Indep. Reflns/ Rint | 2340/0.0393 |
| GOOF on F2 | 1.184 |
| R1, wR2 (I >2σ(I))a | 0.0423, 0.1211 |
| R1, wR2 (all data) | 0.0495, 0.1283 |
| largest diff. peak and hole (e·Å−3) | 4.134, -2.213 |
| aR1 = Σ¦¦Fo¦—¦Fc¦¦/Σ¦Fo¦, bwR2 = Σw(Fo2—Fc2)2/Σw(Fo2)2]1/2. |  |

Table S2. Atomic coordinates (  104) and equivalent isotropic displacement parameters (Å2  103) for LaMg6Ga6S16. Ueq is defined as one-third of the trace of the orthogonalized Uij tensor.

| Atom | BVSa | Wyckoff | x | y | z | Ueq(Å) |
| --- | --- | --- | --- | --- | --- | --- |
| La(1) | 2.13 | 1c | 3333 | 6667 | 10000 | 44(1) |
| La(2) | 1.96 | 1a | 0 | 0 | 10000 | 44(1) |
| La(3) | 2.10 | 1e | 6667 | 3333 | 10000 | 46(1) |
| Mg(1) | 2.05 | 3k | 4292(9) | 1271(8) | 5000 | 30(3) |
| Mg(2) | 2.04 | 3j | 4206(10) | 1332(10) | 10000 | 39(3) |
| Mg(3) | 1.94 | 3k | 2019(7) | 2432(8) | 5000 | 25(2) |
| Mg(4) | 1.96 | 3j | 2075(8) | 2571(10) | 10000 | 35(3) |
| Mg(5) | 1.87 | 3k | 3791(7) | 4736(7) | 5000 | 28(3) |
| Mg(6) | 1.80 | 3j | 3829(7) | 4658(9) | 10000 | 42(4) |
| Ga(1) | 3.00 | 6l | 5603(2) | 7034(2) | 7482(4) | 26(1) |
| Ga(2) | 2.97 | 6l | -318(2) | 1872(2) | 7468(4) | 26(1) |
| Ga(3) | 2.97 | 6l | 4702(2) | 3573(2) | 7474(4) | 25(1) |
| S(1) | 2.05 | 6l | 5050(4) | 2450(5) | 7545(7) | 27(1) |
| S(2) | 2.18 | 6l | -106(4) | 3335(4) | 7510(20) | 27(1) |
| S(3) | 1.95 | 6l | 876(4) | 1628(5) | 7513(8) | 27(1) |
| S(4) | 1.98 | 6l | 3264(4) | 3371(4) | 7510(20) | 25(1) |
| S(5) | 1.96 | 6l | 4134(5) | 5868(5) | 7506(7) | 27(1) |
| S(6) | 1.93 | 3k | -1278(7) | 1346(7) | 5000 | 27(2) |
| S(7) | 1.82 | 3j | 5375(7) | 4503(7) | 10000 | 27(2) |
| S(8) | 2.02 | 3j | 5837(7) | 7925(7) | 10000 | 31(2) |
| S(9) | 2.02 | 3k | 5957(5) | 7963(7) | 5000 | 24(2) |
| S(10) | 2.03 | 3k | 5286(6) | 4542(7) | 5000 | 26(2) |
| S(11) | 1.84 | 3j | -1222(7) | 1237(7) | 10000 | 33(2) |
| aBond valence state was calculated using the empirical formula Vi=ΣSij=Σexp[(r0−rij)/0.37], where Sij is the bond valence associated with bond lengths rij and r0.1, 2, 3, 4 |  |  |  |  |  |  |

Table S3. Selected distances (Å) and angles (degrees) for LaMg6Ga6S16.

| La(1)-S(5)#1 | 2.963(7) | Mg(2)-S(11)#8 | 2.834(18) |
| --- | --- | --- | --- |
| La(1)-S(5) | 2.963(7) | Mg(3)-S(3)#15 | 2.522(10) |
| La(1)-S(5)#2 | 2.963(7) | Mg(3)-S(3) | 2.522(10) |
| La(1)-S(5)#3 | 2.963(7) | Mg(3)-S(6)#8 | 2.587(15) |
| La(1)-S(5)#4 | 2.963(7) | Mg(3)-S(4) | 2.643(15) |
| La(1)-S(5)#5 | 2.963(7) | Mg(3)-S(4)#15 | 2.643(15) |
| La(2)-S(3) | 2.994(7) | Mg(3)-S(9)#3 | 2.705(14) |
| La(2)-S(3)#1 | 2.994(7) | Mg(4)-S(4) | 2.548(16) |
| La(2)-S(3)#6 | 2.994(7) | Mg(4)-S(4)#1 | 2.548(16) |
| La(2)-S(3)#7 | 2.994(7) | Mg(4)-S(3) | 2.597(11) |
| La(2)-S(3)#8 | 2.994(7) | Mg(4)-S(3)#1 | 2.597(11) |
| La(2)-S(3)#9 | 2.994(7) | Mg(4)-S(11)#8 | 2.635(17) |
| La(3)-S(1)#10 | 2.967(6) | Mg(4)-S(8)#3 | 2.650(17) |
| La(3)-S(1)#11 | 2.967(6) | Mg(5)-S(5) | 2.505(10) |
| La(3)-S(1)#1 | 2.967(6) | Mg(5)-S(5)#15 | 2.505(10) |
| La(3)-S(1) | 2.967(6) | Mg(5)-S(9)#3 | 2.607(14) |
| La(3)-S(1)#12 | 2.967(6) | Mg(5)-S(10) | 2.675(16) |
| La(3)-S(1)#13 | 2.967(6) | Mg(5)-S(4)#15 | 2.727(15) |
| Mg(1)-S(10)#13 | 2.508(13) | Mg(5)-S(4) | 2.727(15) |
| Mg(1)-S(2)#14 | 2.552(16) | Mg(6)-S(5) | 2.596(12) |
| Mg(1)-S(2)#8 | 2.552(16) | Mg(6)-S(5)#1 | 2.596(12) |
| Mg(1)-S(1) | 2.560(10) | Mg(6)-S(8)#3 | 2.597(18) |
| Mg(1)-S(1)#15 | 2.560(10) | Mg(6)-S(4)#1 | 2.627(16) |
| Mg(1)-S(6)#8 | 2.793(15) | Mg(6)-S(4) | 2.627(16) |
| Mg(2)-S(1)#1 | 2.482(11) | Mg(6)-S(7) | 2.723(18) |
| Mg(2)-S(1) | 2.482(11) | Ga(1)-S(5) | 2.245(6) |
| Mg(2)-S(2)#8 | 2.572(16) | Ga(1)-S(2)#5 | 2.278(6) |
| Mg(2)-S(2)#7 | 2.572(16) | Ga(1)-S(9) | 2.287(7) |
| Mg(2)-S(7)#13 | 2.628(16) | Ga(1)-S(8) | 2.297(7) |
| Ga(2)-S(3) | 2.228(6) | S(1)#10-La(3)-S(1)#11 | 75.7(2) |
| Ga(2)-S(2) | 2.290(6) | S(1)#10-La(3)-S(1)#1 | 86.30(16) |
| Ga(2)-S(6) | 2.299(7) | S(1)#11-La(3)-S(1)#1 | 133.49(8) |
| Ga(2)-S(11) | 2.309(7) | S(1)#10-La(3)-S(1) | 133.49(7) |
| Ga(3)-S(1) | 2.226(7) | S(10)#13-Mg(1)-S(2)#14 | 88.1(3) |
| Ga(3)-S(4) | 2.253(6) | S(10)#13-Mg(1)-S(2)#8 | 88.1(3) |
| Ga(3)-S(10) | 2.315(7) | S(2)#14-Mg(1)-S(2)#8 | 93.8(7) |
| Ga(3)-S(7) | 2.333(6) | S(10)#13-Mg(1)-S(1) | 95.6(4) |
| S(5)#1-La(1)-S(5) | 77.2(3) | S(2)#14-Mg(1)-S(1) | 176.2(5) |
| S(5)#1-La(1)-S(5)#2 | 85.18(19) | S(2)#8-Mg(1)-S(1) | 85.5(3) |
| S(5)-La(1)-S(5)#2 | 134.00(9) | S(10)#13-Mg(1)-S(1)#15 | 95.6(4) |
| S(5)#1-La(1)-S(5)#3 | 134.00(9) | S(2)#14-Mg(1)-S(1)#15 | 85.5(3) |
| S(5)-La(1)-S(5)#3 | 85.18(19) | S(2)#8-Mg(1)-S(1)#15 | 176.2(5) |
| S(5)#2-La(1)-S(5)#3 | 134.00(9) | S(1)-Mg(1)-S(1)#15 | 94.9(5) |
| S(5)#1-La(1)-S(5)#4 | 85.18(19) | S(10)#13-Mg(1)-S(6)#8 | 162.5(6) |
| S(5)-La(1)-S(5)#4 | 134.00(9) | S(2)#14-Mg(1)-S(6)#8 | 80.0(3) |
| S(5)#2-La(1)-S(5)#4 | 85.17(19) | S(2)#8-Mg(1)-S(6)#8 | 80.0(3) |
| S(5)#3-La(1)-S(5)#4 | 77.2(3) | S(1)-Mg(1)-S(6)#8 | 96.2(3) |
| S(5)#1-La(1)-S(5)#5 | 134.00(9) | S(1)#15-Mg(1)-S(6)#8 | 96.2(3) |
| S(5)-La(1)-S(5)#5 | 85.18(19) | S(1)#1-Mg(2)-S(1) | 94.3(6) |
| S(5)#2-La(1)-S(5)#5 | 77.2(3) | S(1)#1-Mg(2)-S(2)#8 | 174.2(6) |
| S(5)#3-La(1)-S(5)#5 | 85.17(19) | S(1)-Mg(2)-S(2)#8 | 86.7(3) |
| S(5)#4-La(1)-S(5)#5 | 134.00(9) | S(1)#1-Mg(2)-S(2)#7 | 86.7(3) |
| S(3)-La(2)-S(3)#1 | 76.0(2) | S(1)-Mg(2)-S(2)#7 | 174.2(6) |
| S(3)-La(2)-S(3)#6 | 86.04(18) | S(2)#8-Mg(2)-S(2)#7 | 91.6(7) |
| S(3)#1-La(2)-S(3)#6 | 133.60(8) | S(1)#1-Mg(2)-S(7)#13 | 88.8(4) |
| S(3)-La(2)-S(3)#7 | 133.60(8) | S(1)-Mg(2)-S(7)#13 | 88.8(4) |
| S(3)#1-La(2)-S(3)#7 | 86.04(18) | S(2)#8-Mg(2)-S(7)#13 | 85.5(4) |
| S(3)#6-La(2)-S(3)#7 | 133.60(8) | S(2)#7-Mg(2)-S(7)#13 | 85.5(4) |
| S(3)-La(2)-S(3)#8 | 86.05(18) | S(1)#1-Mg(2)-S(11)#8 | 103.2(4) |
| S(3)#1-La(2)-S(3)#8 | 133.60(8) | S(1)-Mg(2)-S(11)#8 | 103.2(4) |
| S(3)#6-La(2)-S(3)#8 | 86.04(18) | S(2)#8-Mg(2)-S(11)#8 | 82.1(4) |
| S(3)#7-La(2)-S(3)#8 | 76.0(2) | S(2)#7-Mg(2)-S(11)#8 | 82.1(4) |
| S(3)-La(2)-S(3)#9 | 133.60(8) | S(7)#13-Mg(2)-S(11)#8 | 162.1(6) |
| S(3)#1-La(2)-S(3)#9 | 86.05(18) | S(3)#15-Mg(3)-S(3) | 95.2(4) |
| S(3)#6-La(2)-S(3)#9 | 76.0(2) | S(3)#15-Mg(3)-S(6)#8 | 94.4(4) |
| S(3)#7-La(2)-S(3)#9 | 86.04(18) | S(3)-Mg(3)-S(6)#8 | 94.4(4) |
| S(3)#8-La(2)-S(3)#9 | 133.60(8) | S(3)#15-Mg(3)-S(4) | 176.4(5) |
| S(1)#11-La(3)-S(1) | 86.30(16) | S(3)-Mg(3)-S(4) | 87.6(3) |
| S(1)#1-La(3)-S(1) | 75.7(2) | S(6)#8-Mg(3)-S(4) | 87.6(3) |
| S(1)#10-La(3)-S(1)#12 | 86.30(16) | S(3)#15-Mg(3)-S(4)#15 | 87.6(3) |
| S(1)#11-La(3)-S(1)#12 | 133.49(8) | S(3)-Mg(3)-S(4)#15 | 176.4(5) |
| S(1)#1-La(3)-S(1)#12 | 86.30(16) | S(6)#8-Mg(3)-S(4)#15 | 87.6(3) |
| S(1)-La(3)-S(1)#12 | 133.49(8) | S(4)-Mg(3)-S(4)#15 | 89.5(6) |
| S(1)#10-La(3)-S(1)#13 | 133.49(8) | S(3)#15-Mg(3)-S(9)#3 | 98.6(4) |
| S(1)#11-La(3)-S(1)#13 | 86.30(16) | S(3)-Mg(3)-S(9)#3 | 98.6(4) |
| S(1)#1-La(3)-S(1)#13 | 133.49(8) | S(6)#8-Mg(3)-S(9)#3 | 160.6(5) |
| S(1)-La(3)-S(1)#13 | 86.30(16) | S(4)-Mg(3)-S(9)#3 | 78.8(3) |
| S(1)#12-La(3)-S(1)#13 | 75.7(2) | S(11)#8-Mg(4)-S(8)#3 | 167.4(6) |
| S(4)-Mg(4)-S(4)#1 | 92.9(7) | S(5)#1-Mg(6)-S(8)#3 | 90.0(4) |
| S(4)-Mg(4)-S(3) | 88.1(3) | S(5)-Mg(6)-S(4)#1 | 171.6(6) |
| S(4)#1-Mg(4)-S(3) | 174.9(7) | S(5)#1-Mg(6)-S(4)#1 | 89.3(3) |
| S(4)-Mg(4)-S(3)#1 | 174.9(7) | S(8)#3-Mg(6)-S(4)#1 | 81.5(4) |
| S(4)#1-Mg(4)-S(3)#1 | 88.1(3) | S(5)-Mg(6)-S(4) | 89.3(3) |
| S(3)-Mg(4)-S(3)#1 | 90.5(5) | S(5)#1-Mg(6)-S(4) | 171.5(6) |
| S(4)-Mg(4)-S(11)#8 | 89.4(4) | S(8)#3-Mg(6)-S(4) | 81.5(4) |
| S(4)#1-Mg(4)-S(11)#8 | 89.4(4) | S(4)#1-Mg(6)-S(4) | 89.3(7) |
| S(3)-Mg(4)-S(11)#8 | 85.7(4) | S(5)-Mg(6)-S(7) | 104.4(4) |
| S(3)#1-Mg(4)-S(11)#8 | 85.7(4) | S(5)#1-Mg(6)-S(7) | 104.4(4) |
| S(4)-Mg(4)-S(8)#3 | 82.0(4) | S(8)#3-Mg(6)-S(7) | 159.3(7) |
| S(4)#1-Mg(4)-S(8)#3 | 82.0(4) | S(4)#1-Mg(6)-S(7) | 83.8(4) |
| S(3)-Mg(4)-S(8)#3 | 103.1(4) | S(4)-Mg(6)-S(7) | 83.8(4) |
| S(3)#1-Mg(4)-S(8)#3 | 103.1(4) | S(5)-Ga(1)-S(2)#5 | 113.7(2) |
| S(5)-Mg(5)-S(5)#15 | 95.8(5) | S(5)-Ga(1)-S(9) | 113.3(3) |
| S(5)-Mg(5)-S(9)#3 | 96.6(4) | S(2)#5-Ga(1)-S(9) | 105.2(4) |
| S(5)#15-Mg(5)-S(9)#3 | 96.6(4) | S(5)-Ga(1)-S(8) | 108.3(3) |
| S(5)-Mg(5)-S(10) | 102.5(4) | S(2)#5-Ga(1)-S(8) | 108.0(5) |
| S(5)#15-Mg(5)-S(10) | 102.5(4) | S(9)-Ga(1)-S(8) | 108.1(3) |
| S(9)#3-Mg(5)-S(10) | 151.3(6) | S(3)-Ga(2)-S(2) | 121.4(3) |
| S(5)-Mg(5)-S(4)#15 | 173.9(5) | S(3)-Ga(2)-S(6) | 117.4(3) |
| S(5)#15-Mg(5)-S(4)#15 | 89.0(3) | S(2)-Ga(2)-S(6) | 97.2(4) |
| S(9)#3-Mg(5)-S(4)#15 | 79.0(3) | S(3)-Ga(2)-S(11) | 110.1(3) |
| S(10)-Mg(5)-S(4)#15 | 80.2(4) | S(2)-Ga(2)-S(11) | 101.3(5) |
| S(5)-Mg(5)-S(4) | 89.0(3) | S(6)-Ga(2)-S(11) | 107.5(3) |
| S(5)#15-Mg(5)-S(4) | 173.9(5) | S(1)-Ga(3)-S(4) | 125.6(3) |
| S(9)#3-Mg(5)-S(4) | 79.0(3) | S(1)-Ga(3)-S(10) | 114.3(3) |
| S(10)-Mg(5)-S(4) | 80.2(4) | S(4)-Ga(3)-S(10) | 99.2(4) |
| S(4)#15-Mg(5)-S(4) | 86.0(7) | S(1)-Ga(3)-S(7) | 107.5(3) |
| S(5)-Mg(6)-S(5)#1 | 90.9(5) | S(4)-Ga(3)-S(7) | 102.3(5) |
| S(5)-Mg(6)-S(8)#3 | 90.0(4) | S(10)-Ga(3)-S(7) | 106.0(3) |
| Symmetry transformations used to generate equivalent atoms: #1 x,y,-z+2 #2 -y+1,x-y+1,-z+2 #3 -x+y,-x+1,z #4 -x+y,-x+1,-z+2 #5 -y+1,x-y+1,z #6 -y,x-y,z #7 -x+y,-x,-z+2 #8 -x+y,-x,z #9 -y,x-y,-z+2 #10 -x+y+1,-x+1,-z+2 #11 -x+y+1,-x+1,z #12 -y+1,x-y,-z+2 #13 -y+1,x-y,z #14 -x+y,-x,-z+1 #15 x,y,-z+1 |  |  |  |

Table S4 The space groups and the flexibility indices (F) of GaS4 and MgS6 groups in AgGaS2, LiGaS2, α-BaGa4S7, CaMg6Ga6S16, and LaMg6Ga6S16.

| Compounds | Space groups | GaS4/MgS6 groups | F |
| --- | --- | --- | --- |
| AgGaS2 | I—42d | GaS4 | 0.212 |
| LiGaS2 | Pna21 | GaS4 | 0.220 |
| α-BaGa4S7 | Pmn21 | GaS4 | 0.216 |
| CaMg6Ga6S16 | P—6 | GaS4 | 0.220-0.224 |
|  |  | MgS6 | 0.140-0.149 |
| LaMg6Ga6S16 | P—6 | GaS4 | 0.220-0.222 |
|  |  | MgS6 | 0.138-0.149 |

As the SHG response of a material is relevant to the polarizability of the NLO-active anionic groups, the induced polarizability of [MgS6] and [GaS4] groups were quantified based on the calculation of empirical “flexibility index” F by the bond valence method.4 As displayed in Table 6, the magnitudes of the induced dipole moment of [GaS4] groups are comparable with other chalcogenides with large SHG responses, e.g., AgGaS2, LiGaS2, BaGa4S7, and CaMg6Ga6S16. Meanwhile, the [MgS6] octahedra make also non-negligible contributions to the induced dipole moments in LaMg6Ga6S16. These illustrate that these NLO-active groups will induce large polarizations under the external field perturbation, thereby making a positive contribution to the SHG response.

Table S5. NLO properties in LaMg6Ga6S16 and other reported chalcogenides.

| Compound | Space group | dij (× AGS, pm/V) | LIDT(× AGS) | PM/NPM | ∆n@1064 nm | Band gap (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| Ga2S35 | Cc | 0.3 | 30 | NPM | 0.025@1064 nm | 2.80 |
| AgGaS26 | I_42m | d36 = 13.4 | 1 | PM | 0.044@1064 nm | 2.56 |
| α-BaGa4S77 | Pmn21 | 0.9 | 3 | PM | 0.111@1064 nm | 3.54 |
| PbGa4S78 | Pc | 1.2 |  | PM |  | 3.08 |
| SnGa4S79 | Pc | 1.3 | 19 | PM |  | 3.10 |
| MgGa2Se410 | I_4 | 0.9 | 3 | PM | 0.048@546 nm | 2.96 |
| AgGaGeS411 | Fdd2 | 0.9 | 2.5 | PM |  | 2.78 |
| Na2ZnGe2S612 | Cc | 0.9 | 6 | PM |  | 3.25 |
| Na2BaGeS413 | R3c | 0.3 | 8 | PM | 0.037@1064 nm | 3.70 |
| Na2BaSnS413 | I_42d | 0.5 | 5 | PM | 0.070@1064 nm | 3.27 |
| Li2Ga2GeS614 | Fdd2 | 0.8 |  | PM |  | 2.95 |
| KYGeS415 | P21 | 1.0 |  | PM | 0.120@1064 nm | 3.15 |
| RbMn3Ga5S1116 | Pc | 0.7 | 31.1 | PM | 0.017@2050 nm | 3.27 |
| CsMn3Ga5S1116 | Pc | 0.8 | 29.1 | PM | 0.016@2050 nm | 3.23 |
| Sr5ZnGa6S1517 | Ama2 | 1.2 | 16 | PM | 0.047@2090 nm | 3.15 |
| Ba6Zn7Ga2S1618 | R3 | 0.5 | 28 | PM |  | 3.50 |
| Ba2Ga8GeS1619 | P63mc | 1.0 | 22 | PM |  | 3.00 |
| BaGa2GeS620 | R3 | 1.0 |  |  |  | 3.23 |
| LaMg6Ga6S16 | P—6 | 0.8 | 5 | PM | 0.041@1064 nm | 3.50 |

References

1.	Wang, J.; Cheng, Y.; Wu, H.; Hu, Z.; Wang, J.; Wu, Y.; Yu, H. Sr3[SnOSe3][CO3]: A Heteroanionic Nonlinear Optical Material Containing Planar pi-conjugated [CO3] and Heteroleptic [SnOSe3] Anionic Groups. Angew. Chem. Int. Ed. 61, e202201616 (2022).

2.	Brown I, Altermatt D. Bond-valence parameters obtained from a systematic analysis of the Inorganic Crystal Structure Database. Acta Crystallogr. A 41, 244-247 (2010).

3.	Brown I. Recent Developments in the Methods and Applications of the Bond Valence Model. Chem. Rev. 109, 6858-6919 (2009).

4.	Jiang X, et al. The role of dipole moment in determining the nonlinear optical behavior of materials: ab initio studies on quaternary molybdenum tellurite crystals. J. Mater. Chem. C 2, 530-537 (2014).

5.	Zhang M, Jiang X, Zhou L, Guo G. Two phases of Ga2S3: promising infrared second-order nonlinear optical materials with very high laser induced damage thresholds. J. Mater. Chem. C 1, 4754-4760 (2013).

6.	Okorogu A, et al. Tunable middle infrared downconversion in GaSe and AgGaS2. Opt. Commun. 155, 307-312 (1998).

7.	Lin X, Zhang G, Ye N. Growth and Characterization of BaGa4S7: A New Crystal for Mid-IR Nonlinear Optics. Cryst. Growth. Des. 9, 1186-1189 (2009).

8.	Li X, Kang L, Li C, Lin Z, Yao J, Wu Y. PbGa4S7: a wide-gap nonlinear optical material. J. Mater. Chem. C 3, 3060-3067 (2015).

9.	Luo Z, et al. SHG Materials SnGa4Q7 (Q = S, Se) Appearing with Large Conversion Efficiencies, High Damage Thresholds, and Wide Transparencies in the Mid-Infrared Region. Chem. Mater. 26, 2743-2749 (2014).

10.	Wang P, et al. The Combination of Structure Prediction and Experiment for the Exploration of Alkali-Earth Metal-Contained Chalcopyrite-Like IR Nonlinear Optical Material. Adv. Sci. 9, 2106120 (2022).

11.	Petrov V, Badikov V, Shevyrdyaeva G, Panyutin V, Chizhikov V. Phase-matching properties and optical parametric amplification in single crystals of AgGaGeS4. Opt. Mater. 26, 217-222 (2004).

12.	Li G, Wu K, Liu Q, Yang Z, Pan S. Na2ZnGe2S6: A New Infrared Nonlinear Optical Material with Good Balance between Large Second-Harmonic Generation Response and High Laser Damage Threshold. J. Am. Chem. Soc. 138, 7422-7428 (2016).

13.	Wu K, Yang Z, Pan S. Na2BaMQ4 (M=Ge, Sn; Q=S, Se): Infrared Nonlinear Optical Materials with Excellent Performances and that Undergo Structural Transformations. Angew. Chem. Int. Ed. 55, 6713-6715 (2016).

14.	Kim Y, et al. Characterization of New Infrared Nonlinear Optical Material with High Laser Damage Threshold, Li2Ga2GeS6. Chem. Mater. 20, 6048-6052 (2008).

15.	Mei D, et al. Breaking through the “3.0 eV wall” of energy band gap in mid-infrared nonlinear optical rare earth chalcogenides by charge-transfer engineering. Mater. Horiz. 8, 2330-2334 (2021).

16.	Chen M, Zhou S, Wei W, Wu X, Lin H, Zhu Q. Phase Matchability Transformation in the Infrared Nonlinear Optical Materials with Diamond-Like Frameworks. Adv. Opt. Mater. 10, 2102123 (2022).

17.	Lin H, et al. Sr5ZnGa6S15: a new quaternary non-centrosymmetric semiconductor with a 3D framework structure displaying excellent nonlinear optical performance. Inorg. Chem. Front. 5, 1458-1462 (2018).

18.	Li Y, Liu P, Wu L. Ba6Zn7Ga2S16: A Wide Band Gap Sulfide with Phase-Matchable Infrared NLO Properties. Chem. Mater. 29, 5259-5266 (2017).

19.	Liu B, et al. Syntheses, Structures, and Nonlinear-Optical Properties of Metal Sulfides Ba2Ga8MS16 (M = Si, Ge). Inorg. Chem. 54, 976-981 (2015).

20.	Yin W, et al. BaGa2MQ6 (M = Si, Ge; Q = S, Se): a new series of promising IR nonlinear optical materials. Dalton. Trans. 41, 5653-5661 (2012).