Supplementary information

Bionic Nanotheranostic for Multimodal Imaging-Guided NIR-II-Photothermal Therapy of Lung Cancer

Meng Zhang1, 2†, Yuxuan Zhang1, 3, 4†, Lifeng Hang2†,Tao Zhang5, Chuangcai Luo1, 4, Wuming Li2, Yiqiang Sun6, Hua Wen2, Yiyu Chen2, Guihua Jiang1, 2* and Xiaofen Ma2*

1 The Second School of Clinical Medicine, Southern Medical University, Guangzhou 510282, China.

2 The Department of Medical Imaging, Guangzhou Key Laboratory of Molecular Functional Imaging and Artificial Intelligence for Major Brain Diseases, Guangdong Second Provincial General Hospital, Guangzhou 510317, China

3 Department of Neurosurgery, Institute of Neuroscience, The Second Affiliated Hospital of Guangzhou Medical University, Guangzhou, 510260, China.

4 The National Key Clinical Specialty, Department of Neurosurgery, Zhujiang Hospital, Southern Medical University, Guangzhou 510282, China.

5 School of Physical and Mathematical Sciences, Nanyang Technological University, 21 Nanyang Link, Singapore 637371, Singapore.

6 School of Chemistry and Chemical Engineering, University of Jinan, Jinan 250022, China

†Meng Zhang, Yuxuan Zhang and Lifeng Hang have contributed equally to this work.

*Correspondence: jianggh@gd2h.org.cn, xiaofenma12@163.com

Figure S1. TEM image of gold decahedron (scale bar: 20 nm).

Figure S2. TEM image of Au NBP (scale bar: 500 nm).

Figure S3. TEM image of Au@MnO2 (scale bar: 50 nm).

Figure S4. Digital image of Au NBP (left), Au@MnO2 (middle) and Au@MnO2@PM (right).

Figure S5. Calculation of photothermal conversion efficiency (η) of AMP.

Calculation of the Photothermal Conversion Efficiency.

Following Roper’s report (J. Phys. Chem. C 2007, 111, 3636), the total energy balance for the system can be expressed by Eq. 1:

ΣimiCp,idTdt=QNC+QDis−Qsurr                                                 (1)

Where m and Cp are the mass and heat capacity of water, respectively, T is the solution temperature, QNC is the energy inputted by NCs, QDis is the baseline energy inputted by the sample cell, and Qsurr is heat conduction away from the system surface by air.

The laser-induced source term, represents heat dissipated by electron-phonon relaxation of the plasmons on the AMP surface under the irradiation of 1064 nm laser:

QNC=I(1−A−1064)η                                                          (2)

Where I is incident laser power, η is the conversion efficiency from incident laser energy to thermal energy, and A1064 is the absorbance of the AMP at wavelength of 1064 nm. In addition, source term, QDis, expresses heat dissipated from light absorbed by the quartz sample cell itself, and it was measured independently to be 113.75 mW using a quartz cuvette cell containing pure water without any AMP. Qsurr is linear with temperature for the outgoing thermal energy, as given by Eq. 3

Qsurr=hS(T−Tsurr)                                                          (3)

Where h is heat transfer coefficient, S is the surface area of the container, and TSurr is ambient temperature of the surroundings.

Once the laser power is defined, the heat input (QNC + QDis) will be finite. Since the heat output (QSurr) is increased along with the increase of the temperature according to the Eq. 3, the system temperature will rise to a maximum when the heat input is equal to heat output:

QNC+QDis=Qsurr−max=hS(Tmax−Tsurr)                                       (4)

Where the Qsurr-max is heat conduction away from the system surface by air when the sample cell reaches the equilibrium temperature, and Tmax is the equilibrium temperature. The 1064 nm laser heat conversion efficiency (η) can be determined by substituting Eq. 2 for QNC into Eq. 4 and rearranging to get

η=hSTmax−Tsurr−QDisI(1−10−A1064)                                                         (5)

Where QDis was measured independently to be 113.75 mW, the (Tmax-TSurr) was 24.4 °C according to Figure 1G and 1H, I is 785 mW, A1064 is the absorbance (1) of AMP at 1064 nm (Figure 1F). Thus, only the hS remains unknown for calculating η.

In order to get the hS, a dimensionless driving force temperature, θ is introduced using the maximum system temperature, Tmax

θ=T−TsurrTmax−Tsurr                                                                 (6)

and a sample system time constant τs,

τs=ΣimiCp,ihS                                                                   (7)

which is substituted into Eq. 1 and rearranged to yield

dθdt=1τs[QNC+QDishSTmax−Tsurr−θ]                                                       (8)

At the cooling stage of the aqueous dispersion of the AMP, the light source was shut off, the QNC +QDis = 0, reducing the Eq. 9

dt=−τsdθθ                                                                   (9)

and integrating, giving the expression

τ=−τslnθ                                                                  (10)

finally, find the value of photothermal conversion efficiency (η)

η=hSTmax−Tsurr−QDisI(1−10−A1064)= (20.16×24.4 mW−113.7 mW)(785mW×(1−10−1.0804)= 52.07%

Figure S6. Optical microscopy images were taken 24 hours after the addition of PBS (left) and AMP (right) to A549 cell culture medium. Scale bar: 100 μm

Figure S7. Corresponding infrared thermal images (1064 nm laser doses: 1.0 W cm−2)

Figure S8. CT images of different concentrations of AMP at 120kV (left) and corresponding CT value (right).

Table S1. Photothermal performance of recently reported photothermal agents employed in NIR-II window.

| Photothermal agents | PTCE | Photothermal agents | PTCE |
| --- | --- | --- | --- |
| AMPs (this work) | 0.520 | Ti3C2/CA4@PLEL nanohydrogel1 | 0.414 |
| Au/Ag NRs2 | 0.288 | Au-Au nanocoral3 | 0.672 |
| Au NPL@TiO24 | 0.420 | anti-STR-CO-GNSs5 | 0.319 |
| Au@MOF-DOX6 | 0.302 | PLNP-Bi2S37 | 0.44 |
| Au NSs8 | 0.130 | TA-Si-Au9 | 0.241 |

PTCE, photothermal conversion efficiency.

1	Tao, N. et al. Minimally Invasive Antitumor Therapy Using Biodegradable Nanocomposite Micellar Hydrogel with Functionalities of NIR-II Photothermal Ablation and Vascular Disruption. ACS Appl Bio Mater 3, 4531-4542, doi:10.1021/acsabm.0c00465 (2020).

2	Mei, Z. et al. Activatable NIR-II photoacoustic imaging and photochemical synergistic therapy of MRSA infections using miniature Au/Ag nanorods. Biomaterials 251, 120092, doi:10.1016/j.biomaterials.2020.120092 (2020).

3	Jia, J. et al. Fine‐Tuning the Homometallic Interface of Au‐on‐Au Nanorods and Their Photothermal Therapy in the NIR‐II Window. Angewandte Chemie International Edition 59, 14443-14448, doi:10.1002/anie.202000474 (2020).

4	Gao, F. et al. Titania-coated 2D gold nanoplates as nanoagents for synergistic photothermal/sonodynamic therapy in the second near-infrared window. Nanoscale 11, 2374-2384, doi:10.1039/c8nr07188h (2019).

5	Manivasagan, P. et al. Antibody-conjugated and streptomycin-chitosan oligosaccharide-modified gold nanoshells for synergistic chemo-photothermal therapy of drug-resistant bacterial infection. J Adv Res 48, 87-104, doi:10.1016/j.jare.2022.08.009 (2023).

6	Deng, X. et al. Yolk–Shell Structured Au Nanostar@Metal–Organic Framework for Synergistic Chemo-photothermal Therapy in the Second Near-Infrared Window. Nano Letters 19, 6772-6780, doi:10.1021/acs.nanolett.9b01716 (2019).

7	Meng, Y. et al. Photothermal conversion performance and acid-induced aggregation of PLNP-Bi(2)S(3) composite nanoplatforms. Dalton Trans 51, 5285-5295, doi:10.1039/d1dt04215g (2022).

8	Song, C. et al. Gold nanostars for cancer cell-targeted SERS-imaging and NIR light-triggered plasmonic photothermal therapy (PPTT) in the first and second biological windows. Journal of Materials Chemistry B 7, 2001-2008, doi:10.1039/c9tb00061e (2019).

9	Sun, L. N. et al. Silicon nanowires decorated with gold nanoparticles via in situ reduction for photoacoustic imaging-guided photothermal cancer therapy. Journal of Materials Chemistry B 7, 4393-4401, doi:10.1039/c9tb00147f (2019).