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                                  Figure S1 Wooden tips coated with PAN-MIP mixtures in different proportions
  
                     Table S1 The adsorption rates of 14 β-agonists by four SPME tips
	Tips
	Adsorption rates (%, n=3)

	
	Salbutamol
	Ractopmine
	Clenbuterol
	Terbutaline
	Marpentello
	Penbuterol
	Brobuterol
	Phenethanolamine A
	Clorprenaline
	Formoterol
	Tobuterol
	Bambuterol
	Mabuterol
	Cibuterol

	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	a
	67
	69
	72
	68
	69
	60
	66
	62
	68
	63
	65
	64
	67
	66
	

	b
	71
	79
	82
	69
	78
	81
	72
	76
	78
	69
	70
	71
	73
	74
	

	c
	84
	82
	79
	73
	82
	80
	88
	84
	89
	70
	73
	78
	71
	73
	

	d
	83
	82
	87
	78
	79
	75
	83
	85
	87
	84
	80
	82
	75
	77
	



                         Table S2 The desorption rates of 14 β-agonists on c in solvent (acetic acid: methanol= 1:9)
	Tips
	Adsorption rates (%, n=3)

	
	Salbutamol
	Ractopmine
	Clenbuterol
	Terbutaline
	Marpentello
	Penbuterol
	Brobuterol
	Phenethanolamine A
	Clorprenaline
	Formoterol
	Tobuterol
	Bambuterol
	Mabuterol
	Cibuterol

	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	a
	95.0
	95.5
	85.6
	89.2
	97.0
	96.2
	89.7
	93.3
	89.2
	91.4
	93.6
	86.6
	89.8
	93.3
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