Table 1. Results of visible-light mediated ATRP of MMA using MIL-100(Fe) photocatalyst.a

| entry | MIL-100(Fe) [mg] | notes | initiator | solvent | t [h] | conv. [%]b | Mn, theoc | Mn, GPCd | Đd |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 6 | - | EBiB | THF | 20 | 86 | 26000 | 26900 | 1.14 |
| 2 | 0 | - | EBiB | THF | 72 | - | - | - | - |
| 3 | 6 | In dark | EBiB | THF | 72 | - | - | - | - |
| 4 | 6 | - | - | THF | 72 | 5 | 1700 | 4000 | 1.52 |
| 5 | 6 | TEA (1 equiv) | EBiB | THF | 20 | 65 | 19700 | 22000 | 1.47 |
| 6 | 6 | CuBr2/PMDETA | EBiB | THF | 20 | 20 | 6200 | 9900 | 1.40 |
| 7 | 6 | - | EBiB | DMAc | 20 | 85 | 25 700 | 24 200 | 1.25 |
| 8 | 6 | - | EBiB | DMSO | 20 | 80 | 24 200 | 32 800 | 1.33 |
| 9 | 6 | - | EBiB | DMF | 20 | 82 | 24 800 | 27 300 | 1.19 |
| 10 | 6 | - | EBiB | MeCN | 20 | 72 | 21 800 | 47 000 | 1.06 |
| 11 | 6 | - | EBiB | Dioxane | 20 | 78 | 23 600 | 37 900 | 1.15 |
| 12 | 6 | - | EBiB | EA | 20 | 72 | 21 800 | 35 700 | 1.11 |
| 13 | 6 | - | EBiB | Toluene | 20 | 64 | 19 400 | 27 900 | 1.17 |
| 14 | 6 | - | EBiB | Neat | 20 | 82 | 24 800 | 42 200 | 1.09 |
| 15 | 6 | - | EBPA | THF | 10 | 93 | 27 900 | 32 500 | 1.21 |
| 16 | 6 | - | PhBiB | THF | 10 | 98 | 29 700 | 29 400 | 1.12 |
| 17 | 10 | - | PhBiB | THF | 10 | 98 | 29 700 | 27 900 | 1.17 |
| 18 | 8 | - | PhBiB | THF | 10 | 97 | 29 400 | 27 300 | 1.14 |
| 19 | 4 | - | PhBiB | THF | 10 | 98 | 29 700 | 31 700 | 1.09 |
| 20 | 3 | - | PhBiB | THF | 12 | 94 | 28 500 | 34 700 | 1.08 |
| 21 | 2 | - | PhBiB | THF | 12 | 92 | 27 900 | 38 200 | 1.09 |
| 22 | 1 | - | PhBiB | THF | 12 | 89 | 27 000 | 40 700 | 1.07 |
| 23 | 4 | No deoxygenation | PhBiB | THF | 10 | 88 | 26 400 | 35 700 | 1.21 |
| 24 | 4 | sunlight | PhBiB | THF | 10 | 84 | 25 200 | 29 800 | 1.18 |

aReaction conditions: MMA (0.5 mL, 300 equiv.) and initiator (1 equiv.) in 0.5 mL solvent under visible light irradiation (λ = 450 nm, 2.2 mW/cm−2) at rt. bMonomer conversions were determined gravimetrically. cMn,theo = MI + [MMA]0/[I]0 × MMMA × conversion. dNumber-average molecular weight (Mn,GPC) and dispersity (Đ) were determined  by gel permeation chromatography (GPC) in THF using polystyrene standards.

Table 2. Synthesis of homopolymers via photo-ATRP using MIL-100(Fe)a.

| entry | monomer | conv. [%]b | Mn, theo [g/mol]c | Mn, GPC [g/mol]d | Đd |
| --- | --- | --- | --- | --- | --- |
| 1 | MMA | 98 | 29 700 | 31 700 | 1.09 |
| 2 | t-BMA | 92 | 39 200 | 36 900 | 1.06 |
| 3 | SMA | 95 | 96 600 | 66 500 | 1.15 |
| 4 | PhMA | 94 | 45 700 | 28 800 | 1.14 |
| 5 | FMA | 76 | 37 800 | 17 300 | 1.40 |
| 6 | DMAEMA | 91 | 42 800 | 30 080 | 1.08 |
| 7 | DCTMA | 82 | 68 400 | 45 100 | 1.20 |
| 8 | St | 70 | 21 800 | 22 500 | 1.27 |
| 9 | 4-VP | 67 | 21 100 | 18 600 | 1.31 |

aReaction conditions: Monomer (300 equiv), MIL-100(Fe)  (4 mg) and PhBiB (1 equiv) in 50 vol % THF under visible light (λ = 450 nm, 2.2 mW/cm−2) at rt for 10 h. bMonomer conversions were determined gravimetrically. cMn,Theo = MPhBiB + [Monomer]0/[PhBiB]0 × MMonomer × conversion. dMn and Đ were determined  by GPC in THF using polystyrene standards.

Table 3.  Preparation of random copolymers via photo-ATRP using MIL-100(Fe)a.

| entry | monomer B | random copolymers | conv. [%]b | Mn, GPC [g/mol]c | Đc |
| --- | --- | --- | --- | --- | --- |
| 1 | t-BMA | P(MMA-r-BMA) | 96 | 22 500 | 1.05 |
| 2 | SMA | P(MMA-r-SMA) | 95 | 40 600 | 1.13 |
| 3 | PhMA | P(MMA-r-PhMA) | 90 | 22 900 | 1.10 |
| 4 | FMA | P(MMA-r-FMA) | 82 | 22 000 | 1.21 |
| 5 | DMAEMA | P(MMA-r-DMAEMA) | 92 | 23 200 | 1.14 |
| 6 | DCTMA | P(MMA-r-DCTMA) | 85 | 33 100 | 1.26 |
| 7 | St | P(MMA-r-St) | 86 | 31 400 | 1.40 |
| 8 | 4-VP | P(MMA-r-VP) | 84 | 18 400 | 1.34 |

aReaction conditions: MMA (100 equiv) and Monomer B (100 equiv), MIL-100(Fe) (4 mg) and PhBiB (1 equiv) in 50 vol % THF under visible light (λ = 450 nm, 2.2 mW/cm−2) at rt for 10 h. bMonomer conversions were determined gravimetrically. cMn and Đ were determined  by GPC in THF using polystyrene standards.