Supplementary information

Spectrum-dependent image convolutional processing via a 2D polarization-sensitive photodetector

Yali Yu1,2, Tao Xiong1,2, Ziqi Zhou1,2, Duanyang Liu1, Yue-Yang Liu1, Juehan Yang1, Zhongming Wei1,2,*

1State Key Laboratory of Superlattices and Microstructures, Institute of Semiconductors, Chinese Academy of Sciences, Beijing 100083, China

2Center of Materials Science and Optoelectronic Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

*Correspondence: zmwei@semi.ac.cn

Fig. S1 The projected atomic models of GaTe0.5Se0.5 in different planes. a a-b plane. b a-c planes. c b-c plane.

Fig. S2 The theoretical calculated energy band structure of bulk GaTe0.5Se0.5.

Fig. S3 Iso-plots of the charge density distribution of GaTe0.5Se0.5 within the b-c plane. a CBM state. b VBM state.

Table S1 The optoelectrical performance of GaTe0.5Se0.5-based photodetector under illumination within the range of 255-1064 nm.

| Wavelength (nm) | Power density (mW/cm2) | Responsivity (mA/W) | Detectivity (*108 Jones) |
| --- | --- | --- | --- |
| 255 | 22.5 | 150 | 3.42 |
| 360 | 22.5 | 164 | 3.73 |
| 450 | 22.5 | 82 | 1.91 |
| 520 | 22.5 | 40 | 0.92 |
| 638 | 22.5 | 30 | 0.71 |
| 808 | 22.5 | 20 | 0.49 |
| 1064 | 22.5 | 4 | 0.09 |

Fig. S4 Ids-Vds curves tested under both dark condition and the illumination of 1064 nm laser.

Fig. S5 Polarization-sensitive photoresponse captured under 450 nm laser illumination, with the polarization angle systematically adjusted from 0° to 360°.

Table S2 The relationship between the polarization-sensitive photocurrent values corresponding to the convolution kernels utilized for image convolutional processing and their corresponding color-coded schematic.