# Electronic Supplementary Information (ESI) for

# VO2 Nanowires Based Composite Films with Broadband and High Tunable Electromagnetic Interference Shielding Performance

# Shuhui Lianga, Huan Guanb, Hainan Zhanga, Xiangge Han, Sue Haoa, Shuliang Doub*, Haoxin Zhoub, Chenchen Gengb, Tao Zhaob, Jinxin Gua, Hang Weib, Yao Lib

# a School of Chemical Engineering and Technology, Harbin Institute of Technology, 150001 Harbin, China

# b Center for Composite Materials and Structure, Harbin Institute of Technology, 150001 Harbin, China

Fig. S1 (a) XRD pattern, (b) Raman spectrum, (c) DSC curve of VO2(M)

Fig. S2 SEM images of surface for PVDF-HFP and VO2/PVDF-HFP composite films: (a) PVDF-HFP, (b) VP-2, (c) VP-4

Fig. S3 SEM images of cross-fracture of various films: (a) PVDF-HFP, (b) VP-1, (c) VP-2, (d) VP-3, (e) VP-4 and (f) VP-5

Fig. S4 Conductivity of VO2/PVDF-HFP composite films at a different temperature: (a) VP-1, (b) VP-2, (c) VP-3, and (d) Relative conductivity change versus temperature

Fig. S5 (a) SER, (b) SEA and (c) SET in X-band of PVDF -HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures.

Fig. S6 Power coefficient (a) A, (b) R and (c) T in X-band of PVDF -HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S7 Density of PVDF -HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S8 (a) SET/t, (b) SSET/t in X-band of PVDF-HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S9 (a) tensile stress-strain curves (b) Tensile strength and (c) fracture strain of pure PVDF-HFP and VO2/PVDF-HFP composite films

Fig. S10 (a) SER, (b) SEA, (c) the average SET, SER, and SEA and (d) SET in Ku-band of PVDF -HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S11 Power coefficient (a) A, (b) R and (c) T, and (d) average power coefficients in Ku-band of PVDF-HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S12 (a) SET/t, (b) SSET/t in Ku-band of PVDF-HFP and VO2/PVDF-HFP composite films (thickness of 1.8 mm) under different temperatures

Fig. S13 (a) SER, (b) SEA in X-band; (c) SER, (d) SEA in Ku-band of VP-5 film under different temperatures

Fig. S14 Power coefficient (a) A, (b) R and (c) T in X-band of VP-5 film under different temperatures; (d) A, (e) R and (f) T in Ku-band of VP-5 film under different temperatures

Fig. S15 Cyclicity of ‘‘off’’ and ‘‘on’’ states of EMI shielding for the VO2/PVDF-HFP composite films with different thicknesses in X and Ku band (a, b) 5 times, (c) 1000 times

Fig. S16 Effect of the temperature on (a) EMI SE, (b) reflection EMI SE, (c) absorption EMI SE in X-band of VP-5 film; Effect of the temperature on (d) EMI SE, (e) reflection EMI SE, (f) absorption EMI SE in Ku-band of VP-5 film

Fig.S17 Effect of the temperature on (a) SET in X band, (b) SET in Ku band of VP-5 film

Fig.S18 Effect of the temperature on power coefficient (a) absorption, (b) reflection and (c) transmission in X-band of VP-5 film; (d) absorption, (e) reflection and (f) transmission in Ku-band of VP-5 film

Fig.S19 Complex permittivity and of impedance matching of VP-5 film (thickness of 1.02 mm) at different temperatures: (a, c) X-band, (b, d) Ku-band

Fig.S20 Cole-Cole plots of ε" versus ε′ of VP-5 film (thickness of 1.02 mm): (a, c) before and (b, d) after phase transition

Table S1 Conductivity of VP composite films at 30℃ and 100℃

| Samples | VP-1 | VP-2 | VP-3 | VP-4 | VP-5 |
| --- | --- | --- | --- | --- | --- |
| 30℃ (S m-1) | 2.99E-08 | 2.76E-07 | 1.24E-06 | 0.07 | 0.13 |
| 100℃ (S m-1) | 5.02E-04 | 0.00501 | 0.0946 | 32.73 | 199.90 |

Table S2 Average EMI SE, SET, thickness and temperature range of existing variable EMI shielding materials with temperature responsiveness

| Composites | EMI SE (dB) | SET (dB) | Thickness (mm) | Range | Ref. |
| --- | --- | --- | --- | --- | --- |
| CF/SiO2 | 11.7-12.4 | 0.7 | 2.5 | 30-600 ℃ | [1] |
| r-GO/SiO2 | 34.5-37.5 | 3 | 1.5 | 50-200 ℃ | [2] |
| GN/Al2O3 | 22.8-37.4 | 14.6 | 1.5 | 25-400 ℃ | [3] |
| PDMS/TSM/CNT | 42.3-36.5 | -5.8 | 1.9 | RT-120 ℃ | [4] |
| Sb2Te3 | 55.5-74.8 | 19.3 | 1.36 | 40-300 ℃ | [5] |
| SiC/Ti3SiC2 | 20-46 | 26 | 3.0 | 25-600 ℃ | [6] |
| Ti3C2Tx MXene/aramid nanofiber | 49.7-63.2 | 13.5 | 0.07 | 25-300 ℃ | [7] |
| SiO2/MWCNT | 23.5-24.5 | 1 | 2.5 | 100-500 ℃ | [8] |
| ZrB2/Al2O3 | 31-44 | 13 | 1.2 | 25-600 ℃ | [9] |
| G@MgO/PVA | 20.6-27.5 | 5.9 | 1 | 30-120 ℃ | [10] |
| β-MnO2 | 20.9-21.5 | 0.6 | 2.18 | 20-500 ℃ | [11] |
| VO2/CNF | 18.7-53.6 | 35.2 | 1.9 | 25-70 ℃ | [12] |
| This work | 1.9-18.4 (X) 3.3-22.0 (Ku) | 16.5 18.7 | 0.15 | RT-100 ℃ | / |
|  | 4.0-24.4 (X) 4.8-27.2 (Ku) | 20.4 22.4 | 0.29 |  |  |
|  | 8.2-37.4 (X) 9.5-34.2 (Ku) | 29.2 24.7 | 0.60 |  |  |
|  | 9.8-40.6 (X) 10.6-37.7 (Ku) | 30.8 27.1 | 0.83 |  |  |
|  | 8.7-51.0 (X) 9.0-53.3 (Ku) | 42.3 44.3 | 1.02 |  |  |
|  | 12.3-57.1 (X) 10.5-69.9 (Ku) | 44.8 59.4 | 1.80 |  |  |

Table S3 Comparison of average EMI SEand maximumSET, of existing variable EMI shielding materials

| Composites | EMI SE (dB) | SET (dB) | Stimuli | Range | Ref. |
| --- | --- | --- | --- | --- | --- |
| PANI/MXene/cotton fabrics | 24-15 | 9 | Acid/Alkali | / | [13] |
| graphene/non-woven spacer | 20-35 | 15 | Humidity | 0-6 wt% | [14] |
| polyimide/CNT foam | 17.7-37.8 | 20.1 | Humidity | 0-35 wt% | [15] |
| CNT/CNF foam | 72-33.5 | 38.5 | Angle | 0-90 ° | [16] |
| CNF/MXene aerogel | 63.1-36.5 | 26.6 | Angle | 0-90 ° | [17] |
| MXene@AgNW/PEG | 30.5-12.4 | 18.1 | compression | 0 - 50% | [18] |
| wood/CNT sponge | 1.4-27.6 | 26.2 | compression | 0 - 75% | [19] |
| WF/CNT foam | 40.1-13.9 | 26.2 | compression | 0-75% | [20] |
| liquid metal/PDMS | 20.6-80.7 | 60.1 | Stretching | 0-400% | [21] |
| MXene organohydrogel | 32.8-37 37-20 | 4.2 17 | Stretching | 0-0% 30%-100% | [22] |
| PU@Cu Film | 52.31-0 | 52.31 | Stretching | 0-50% | [23] |
| liquid metal/EcoFlex | 41.5 - 81.6 | 40.1 | Stretching | 0-400% | [24] |
| CNT | 38-25 | 13 | Stretching | 0-30% | [25] |
| TPU/CNT | 34.57-12.8 | 21.77 | Stretching | 0-200% | [26] |
| This work | 12.3-57.1 (X) 10.5-69.7 (Ku) | 44.8 59.2 | Temperature | RT-100℃ | / |

# References:

1. Cao M, Song W, Hou Z, Wen B, Yuan J (2010) The effects of temperature and frequency on the dielectric properties, electromagnetic interference shielding and microwave-absorption of short carbon fiber/silica composites. Carbon 48(3):788-796. https://doi.org/10.1016/j.carbon.2009.10.028

2. Wen B, Cao M, Lu M, Cao W, Shi H, Liu J, Wang X, Jin H, Fang X, Wang W, Yuan J (2014) Reduced Graphene Oxides: Light-Weight and High-Efficiency Electromagnetic Interference Shielding at Elevated Temperatures. Adv Mater 26(21):3484-3489. https://doi.org/10.1002/adma.201400108

3. Qing Y, Wen Q, Luo F, Zhou W (2016) Temperature dependence of the electromagnetic properties of graphene nanosheet reinforced alumina ceramics in the X-band. J Mater Chem C 4(22):4853-4862. https://doi.org/10.1039/c6tc01163b

4. Cai J, Tang X, Chen X, Wang M (2021) Temperature and strain-induced tunable electromagnetic interference shielding in polydimethylsiloxane/multi-walled carbon nanotube composites with temperature-sensitive microspheres. Compos Part A-Appl S 140(106188):106188. https://doi.org/10.1016/j.compositesa.2020.106188

5. Chen X, Zhang J, Du K, Xie Q, Hou Z (2021) Sb2Te3 nanosheets: Topological insulators with extraordinary electromagnetic response behaviors. Chem Eng J 414:128036. https://doi.org/10.1016/j.cej.2020.128036

6. Mu Y, Zhou W, Wan F, Ding D, Hu Y, Luo F (2015) High-temperature dielectric and electromagnetic interference shielding properties of SiCf/SiC composites using Ti3SiC2 as inert filler. Compos Part A-Appl S 77:195-203. https://doi.org/10.1016/j.compositesa.2015.07.004

7. Yao J, Zhang L, Yang F, Jiao Z, Tao X, Yao Z, Zheng Y, Zhou J (2022) Superhydrophobic Ti3C2Tx MXene/aramid nanofiber films for high-performance electromagnetic interference shielding in thermal environment. Chem Eng J 446:136945. https://doi.org/10.1016/j.cej.2022.136945

8. Wen B, Cao M, Hou Z, Song W, Zhang L, Lu M, Jin H, Fang X, Wang W, Yuan J (2013) Temperature dependent microwave attenuation behavior for carbon-nanotube/silica composites. Carbon 65:124-139. https://doi.org/10.1016/j.carbon.2013.07.110

9. Qing Y, Yao H, Li Y, Luo F (2021) Plasma-sprayed ZrB2/Al2O3 ceramics with excellent high temperature electromagnetic interference shielding properties. J Eur Ceram Soc 41(2):1071-1075. https://doi.org/10.1016/j.jeurceramsoc.2020.10.031

10. Marka SK, Srikanth VVSS, Sindam B, Hazra BK, Raju KCJ, Srinath S (2019) Graphene-Wrapped MgO/Poly(vinyl alcohol) Composite Sheets: Dielectric and Electromagnetic Interference Shielding Properties at Elevated Temperatures. ACS Appl Mater Inter 11(26):23714-23730. https://doi.org/10.1021/acsami.9b05137

11. Song W, Cao M, Hou Z, Lu M, Wang C, Yuan J, Fan L (2014) Beta-manganese dioxide nanorods for sufficient high-temperature electromagnetic interference shielding in X-band. Appl Phys a-Mater 116(4):1779-1783. https://doi.org/10.1007/s00339-014-8327-1

12. Liao S, Wang X, Huang H, Shi Y, Wang Q, Hu Y, Zhu P, Sun R, Wong C, Wan Y (2023) Intelligent shielding material based on VO2 with tunable near-field and far-field electromagnetic response. Chem Eng J 464:142596. https://doi.org/10.1016/j.cej.2023.142596

13. Li D, Liu L, Wang Q, Zhang H, Chen W, Yin G, Yu Z (2022) Functional Polyaniline/MXene/Cotton Fabrics with Acid/Alkali-Responsive and Tunable Electromagnetic Interference Shielding Performances. ACS Appl Mater Inter 14(10):12703-12712. https://doi.org/10.1021/acsami.2c00797

14. Wang Y, Cheng X, Song W, Ma C, Bian X, Chen M (2018) Hydro-sensitive sandwich structures for self-tunable smart electromagnetic shielding. Chem Eng J 344:342-352. https://doi.org/10.1016/j.cej.2018.03.097

15. Sun Z, Chen J, Jia X, Wang G, Shen B, Zheng W (2021) Humidification of high-performance and multifunctional polyimide/carbon nanotube composite foams for enhanced electromagnetic shielding. Mater Today Phys 21:100521. https://doi.org/10.1016/j.mtphys.2021.100521

16. Zeng Z, Wang C, Wu T, Han D, Luković M, Pan F, Siqueira G, Nyström G (2020) Nanocellulose assisted preparation of ambient dried, large-scale and mechanically robust carbon nanotube foams for electromagnetic interference shielding. J Mater Chem A 8(35):17969-17979. https://doi.org/10.1039/D0TA05961G

17. Zeng Z, Wang C, Siqueira G, Han D, Huch A, Abdolhosseinzadeh S, Heier J, Nueesch F, Zhang CJ, Nystroem G (2020) Nanocellulose-MXene Biomimetic Aerogels with Orientation-Tunable Electromagnetic Interference Shielding Performance. Adv Sci 7(15):2000979. https://doi.org/10.1002/advs.202000979

18. He Y, Shao Y, Xiao Y, Yang J, Qi X, Wang Y (2022) Multifunctional Phase Change Composites Based on Elastic MXene/Silver Nanowire Sponges for Excellent Thermal/Solar/Electric Energy Storage, Shape Memory, and Adjustable Electromagnetic Interference Shielding Functions. ACS Appl Mater Inter 14(4):6057-6070. https://doi.org/10.1021/acsami.1c23303

19. Liu X, Li Y, Sun X, Tang W, Deng G, Liu Y, Song Z, Yu Y, Yu R, Dai L, Shui J (2021) Off/on switchable smart electromagnetic interference shielding aerogel. Matter 4(5):1735-1747. https://doi.org/10.1016/j.matt.2021.02.022

20. Chen Y, Liu Y, Li Y, Qi H (2021) Highly Sensitive, Flexible, Stable, and Hydrophobic Biofoam Based on Wheat Flour for Multifunctional Sensor and Adjustable EMI Shielding Applications. ACS Appl Mater Inter 13(25):30020-30029. https://doi.org/10.1021/acsami.1c05803

21. Zhu R, Li Z, Deng G, Yu Y, Shui J, Yu R, Pan C, Liu X (2022) Anisotropic magnetic liquid metal film for wearable wireless electromagnetic sensing and smart electromagnetic interference shielding. Nano Energy 92:106700. https://doi.org/10.1016/j.nanoen.2021.106700

22. Yu Y, Yi P, Xu W, Sun X, Deng G, Liu X, Shui J, Yu R (2022) Environmentally Tough and Stretchable MXene Organohydrogel with Exceptionally Enhanced Electromagnetic Interference Shielding Performances. Nano-Micro Lett 14(1):15. https://doi.org/10.1007/s40820-022-00819-3

23. Xia S, Wei C, Tang J, Yan J (2021) Tensile Stress-Gated Electromagnetic Interference Shielding Fabrics with Real-Time Adjustable Shielding Efficiency. ACS Sustain Chem Eng 9(42):13999-14005. https://doi.org/10.1021/acssuschemeng.1c05589

24. Liu C, Cai J, Dang P, Li X, Zhang D (2020) Highly Stretchable Electromagnetic Interference Shielding Materials Made with Conductive Microcoils Confined to a Honeycomb Structure. ACS Appl Mater Inter 12(10):12101-12108. https://doi.org/10.1021/acsami.0c00034

25. Huang K, Chen M, He G, Hu X, He W, Zhou X, Huang Y, Liu Z (2020) Stretchable microwave absorbing and electromagnetic interference shielding foam with hierarchical buckling induced by solvent swelling. Carbon 157:466-477. https://doi.org/10.1016/j.carbon.2019.10.059

26. Feng D, Xu D, Wang Q, Liu P (2019) Highly stretchable electromagnetic interference (EMI) shielding segregated polyurethane/carbon nanotube composites fabricated by microwave selective sintering. J Mater Chem C 7(26):7938-7946. https://doi.org/10.1039/c9tc02311a

Corresponding author:

E-mail addresses: haosue@hit.edu.cn (S. Hao), dousl@hit.edu.cn, yaoli@hit.edu.cn (Y. Li).