Facile Assembly of Flexible Symmetric Micro-Supercapacitors with Wide Working Voltage Window

Xiangguang Hana, b, c, Libo Zhaoa, b, c, Min Lia, b, c*, Chen Jiaa, b*, Zhikang Lia, b, c, Jiaqi Xiea, b, Guoxi Luoa, b, c*, Ping Yanga, b, c, Rabah Boukherroubd, Yurdanur Türkere, Mert Umut Özkaynake, f, Koray Bahadır Dönmeze, Zhuangde Jianga, b, c

a State Key Laboratory for Manufacturing Systems Engineering, International Joint Laboratory for Micro/Nano Manufacturing and Measurement Technologies, Xi’an Jiaotong University (Yantai) Research Institute for Intelligent Sensing Technology and System, Xi’an Jiaotong University, Xi’an 710049, China

b School of Instrument Science and Techonology, Xi’an Jiaotong University, Xi’an, 710049, China

c Shandong Laboratory of Advanced Materials and Green Manufacturing at Yantai, Yantai, 264000, China

d Univ. Lille, CNRS, Centrale Lille, Univ. Polytechnique Hauts-de-France, UMR 8520 - IEMN, F-59000 Lille, France

e Sabanci University Nanotechnology Research and Application Center (SUNUM), Istanbul, Turkey

f Department of Materials Science and Engineering, Istanbul Technical University, Istanbul, Turkey

*To whom correspondence should be addressed: limin@xjtu.edu.cn (M. Li), jiachen0224@stu.xjtu.edu.cn (C. Jia), luoguoxi@mail.xjtu.edu.cn (G. Luo).

EXPERIMENTAL SECTION

Materials and reagents. Phosphoric acid (H3PO4.H2O; PA) with a purity of 99.99% was obtained from Sigma-Aldrich (China). Lauryl ether 23 was procured from JK Scientific (Turkey) with a purity of 100% and used as a non-ionic surfactant (NI). Polyimide (PI) film was purchased from Zhongshan Chenxi Technology Co., Ltd (China). Polydimethylsiloxane (PDMS) was bought from Sigma-Aldrich (China).

Preparation of the PA-NI LC gel electrolyte. The preparation of the phosphoric acid-non-ionic surfactant liquid crystal (PA-NI LC) gel electrolyte was performed according to our previous workS1. Firstly, 1.0 g of lauryl ether 23 was heated at its melting point of 50 oC. Then, it was mixed with 7.6 g of phosphoric acid (PA, 85.0% wt/wt) in a 20 mL glass vial. This mixture was homogenized at 80 oC for 15 min to obtain the LC gel phases.

Characterization. The crystal structure was characterized by X-ray diffraction (XRD; D8 Advanced, Bruker) using Cu Kα radiation in the 2θ range of 10° to 80°. Raman spectroscopy measurements were performed on a Laser Raman spectrometer (HORIBA) using a 532-nm laser diode as excitation source. Visible light was focused by a 50× objective. The scattered light was collected by the same objective in backscattering configuration, dispersed by an 800 mm focal length monochromator and detected by a CCD camera. X-ray photoelectron spectra (XPS) were recorded on a photoelectron spectrometer (ESCALAB Xiþ, ThermoFisher Scientific) with Al Kα as the X-ray source. The laser confocal scanning microscope (LCSM) images were obtained by using OLS4000 microscope. SEM images were acquired to observe the morphology and structure of as-prepared samples using a field-emission scanning electron microscope (FESEM; Gemini SEM 500, Zeiss, 15 kV). Transmission electron microscopy (TEM) and high-resolution TEM (HRTEM) micrographs, and selected area electron diffraction (SAED) were recorded with a transmission electron microscope (TEM; JEM-F200, JEOL) operating at 200 kV. Elemental characterization was conducted with an energy dispersive X-ray spectrometer (EDS) through areal elemental mapping and analysis.

Electrochemical measurements. CV curves were collected at different scan rates (100 - 500 mV·s-1). GCD measurements were recorded at various current densities ranging from 0.08 to 0.4 mA·cm-2. Electrochemical impedance spectroscopy (EIS) was performed in the frequency range from 10-2 Hz to 105 Hz.

Figure S1. CV plots of LG-based MSCs devices with electrode widths of (a) 400 μm, (b) 500 μm and (c) 600 μm measured in PA-NI LC gel electrolyte at 500 mV·s-1.

Figure S2. ‘Platform phenomenon’ in galvanostatic charging curve at 0.06 mA cm-2.

Figure S3. GCD profiles of LG-based MSCs devices with electrode widths of (a) 400 μm, (b) 500 μm and (c) 600 μm measured in PA-NI LC gel electrolyte at various current densities.

Figure S4. Electrochemical impedance spectra of LG-based MSCs with PA-NI LC gel electrolyte. The insert in upper-right corner is the corresponding equivalent circuit of the EIS results.

Table S1. Resistance values of as-prepared MSCs.

| Electrode width (μm) | Intrinsic resistance (Rs) / ohm cm-2 | Charge transfer resistance (Rct) / ohm cm-2 |
| --- | --- | --- |
| 300 | 0.03 | 1121.0 |
| 400 | 0.07 | 1143.2 |
| 500 | 0.13 | 1163.2 |
| 600 | 0.18 | 1256 |

Reference

S1. Li, M. et al. An efficient cobalt-nickel phosphate positive electrode for high-performance hybrid microsupercapacitors. J. Energy Storage 64, 107144 (2023).