SUPPLEMENTARY INFORMATION

Simple, sensitive, and cost-effective voltammetric determination of salbutamol at a pencil graphite electrode modified with Nafion and functionalized multi-walled carbon nanotubes

Didem Giray Dilgin1,*, Kader Vural1, Serkan Karakaya2,*, Yusuf Dilgin2

1Department of Secondary Science and Mathematics Education, Faculty of Education, Çanakkale Onsekiz Mart University, Çanakkale, Turkey

2Department of Chemistry, Faculty of Science and Art, Çanakkale Onsekiz Mart University, Çanakkale, Turkey

*Corresponding author:

didemgiray@comu.edu.tr

skarakaya@comu.edu.tr

Fig. S1 (A) CVs (Potential scan range is -500 mV – +1200 mV at a scan rate of 50 mV/s) and (B) ICs (Frequency range: 1×105 – 1×10-1 Hz and the inside figure is electrochemical IS circuit model; W: Warburg impedance; Rs: Ohmic resistance; WE: Working electrode; C: Double layer capacitance) of 5.0 mM Fe(CN)63-/4- + 0.10 M KCl recorded at bare PGE, Nf/PGE, f-MWCNTs/PGE and Nf/f-MWCNTs/PGE.

Fig. S2 SEM micrographs (30000 ×100 nm) recorded for (A) PGE, (B) Nf/PGE, (C) f-MWCNTs/PGE, and (D) Nf/f-MWCNTs/PGE.

Fig. S3 EDX spectra recorded for (A) PGE, (B) Nf/PGE, (C) f-MWCNTs/PGE ve (D) Nf/f-MWCNTs/PGE.

Fig. S4 (A) DPVs of increased concentrations (0 → 150 µM) of SBT recorded at PGE under optimized conditions (v= 25 mV/s; tpulse= 10 ms; EStep= 10 mV; EAmp= 150 mV), (B) the I(µA) vs. [SBT](µM) plots and (C) the calibration plots generated from the Fig. 5A.

Table S1. The effect of the interferences on the DPV response of SBT at Nf/f-MWCNTs/PGE (Stable concentration of SBT is 5.0 µM and n=3).

| Interference | Fold | Percentage Change in DPV response (%) | SD (±) |
| --- | --- | --- | --- |
| Cu2+ | 5.0 | -5.32 | 1.32 |
| Mg2+ | 5.0 | -4.61 | 2.03 |
| Ca2+ | 5.0 | -3.67 | 1.25 |
| K+ | 100 | +3.12 | 0.70 |
| Cl- | 100 | +1.20 | 0.68 |
| Na+ | 100 | +2.77 | 1.70 |
| SO42- | 50 | +3.50 | 1.30 |
| Fructose | 50 | -2.16 | 0.44 |
| Glucose | 100 | -2.10 | 0.73 |
| Maltose | 5.0 | -5.20 | 1.40 |
| Mannose | 50 | -0.93 | 0.52 |
| Sucrose | 100 | -5.23 | 1.67 |
| Uric acid | 10 | -2.78 | 0.91 |
| Ascorbic acid | 10 | -1.50 | 0.80 |
| Dopamine | 2.5 | -2.64 | 0.53 |