Supplementary Figure F1：

Fig. 1 SEM and EDS analysis diagram of carbide slag

Supplementary Figure F2：

Fig. 4   PCA of total heavy metals and available heavy metals in soil under different treatments

Supplementary Figure F3：

Fig. 6 Adsorption model of Cu2+ by BC and Fe-BC

Supplementary Table S1：

Table 5 Langmuir and Freundlich model parameters of adsorption of Cu2+ by BC and Fe-BC

| Adsorption material | Heavy Metal | Langmuir isotherm |  |  | Freundlich isotherm |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Qm(mg/g) | KL | R2 | KF | 1n | R2 |
| Fe-BC | Cu2+ | 276.12 | 0.00120 | 0.9936 | 20.746 | 0.3894 | 0.9370 |
| BC | Cu2+ | 190.48 | 0.01904 | 0.9940 | 7.871 | 0.5038 | 0.9372 |

Supplementary Table S2：

Table 6 Data parameters of in-particle diffusion kinetics of adsorption of Cu2+ by BC and Fe-BC

| Adsorption material | Heavy Metal | Stage 1 |  |  |  | Stage 2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | C1 | Kp,1/[mg/(g·min0.5)] | R2 | C2 |  | Kp,2/[mg/(g·min0.5)] | R2 |
| Fe-BC | Cu2+ | 3.1583 | 2.6571 | 0.9357 | 15.2360 |  | 0.5489 | 0.8561 |
| BC | Cu2+ | 1.2379 | 1.8360 | 0.8070 | 11.4824 |  | 0.2535 | 0.8176 |

Supplementary Table S3：

Table 7 Data parameters of the Elovich model of BC and Fe-BC on Cu2+

| Adsorption material | Heavy Metal | Elovich model |  |  |
| --- | --- | --- | --- | --- |
|  |  | α | β | R2 |
| Fe-BC | Cu2+ | 1.6237 | 0.1754 | 0.9870 |
| BC | Cu2+ | 1.6292 | 0.3037 | 0.9537 |

Supplementary Figure F4：

Fig. 7 SEM of Fe-BC(a) and Fe-BC adsorbing Cu(b)

Supplementary Figure F5：

Fig. 8 Scanning electron microscopy and energy spectrum analysis before and after Fe-BC adsorption of Cu2+

Supplementary Figure F6：

Fig. 9 FTIR spectra of Fe-BC before and after adsorption of Cu2+

Supplementary Figure F7:

Fig. 11. Adsorption mechanism of Fe-BC on Cu2+