Supplementary Information

Carrier-free low molecular weight heparin and lipid conjugate-based nano-anticoagulant with an albumin shuttling effect

Jae-Hyeon Lee1¶, Hansol Lim2¶, Gaeun Ma2, Minho Seo1, Jun-Hyuck Lee2, Seong-Bin Yang2, Han-Gil Jeong3, Seho Kweon4*, Jooho Park2*

1Department of Biomedical Chemistry, College of Biomedical and Health Science, Konkuk University, Republic of Korea 2Department of Applied Life Science, BK21 Program, Konkuk University, Chungju 27478, Republic of Korea, 3Department of Neurology, Seoul National University Bundang Hospital, Seoul National University College of Medicine, Seongnam-si, 08826, Republic of Korea. 4Department of Molecular Medicine and Biopharmaceutical Science, Graduate School of Convergence Science and Technology, Seoul National University, Seoul 08826, Republic of Korea

¶These authors contributed equally to this work

*Corresponding author: 
Jooho Park (Phone) +82-43-843-3574, (E-mail) pkjhdn@kku.ac.kr

Seho Kweon (Phone) +82-61-450-6063, (E-mail) sayhokweon@snu.ac.kr

Supplementary Fig. 1 | a, b Schematic structure of low molecular weight heparin (LMWH) (a) and synthesis of LMWH conjugation with fatty amines (b): [LMWH–hexylamine (LMWH–C6), LMWH–octylamine (LMWH–C8), LMWH–decylamine (LMWH–C10), LMWH–dodecylamine (LMWH–C12), and LMWH–octadecylamine (LMWH–C18, LMHO)]

Supplementary Fig. 2 | a, b 1D 1H-NMR results of fatty amines (hexylamine, octylamine, decylamine, and dodecylamine) (a) and the LMWH–lipid conjugates after conjugation on the reducing sugar end of LMWH (b).

Supplementary Fig. 3 | UV-vis spectroscopic analysis of low molecular weight heparin (LMWH), octadecylamine, and LMHO.

Supplementary Fig. 4 | The number of hydrophobic interaction bonds calculated from molecular dynamic (MD) simulations for self-assembly LMHO nanoparticle.

Supplementary Fig. 5 | The stability of LMHO nanoparticles in DMEM and distilled water (DW) for a duration of 24 hours (n = 3).

Supplementary Fig. 6 | The stability of LMWH–lipid conjugates (LMWH–C6, LMWH–C8, LMWH–C10, and LMWH–C12) nanoparticles in serum for a duration of 24 hours (n = 3).

Supplementary Fig. 7 | a, b The cytotoxic effects of LMWH and LMHO with the concentration range of 0.01-100 µg/mL (n = 6) on MRC-5 (MRC-5 cells were fibroblast cells isolated from lung tissue of a 14-week-old male embryo of Caucasian origin) (a) and MDCK (MDCK cells were isolated from normal kidney tissue from a normal, adult, female cocker spaniel) (b).

Supplementary Fig. 8 | The particle size distribution of human serum albumin (HSA) in aqueous condition using Dynamic Light Scattering (DLS).

Supplementary Fig. 9 | The stability and interaction characteristics of LMWH and LMHO molecules after albumin sequential docking simulation with human serum albumin.

Supplementary Fig. 10 | The transmission electron microscopy (TEM) image of human serum albumin.

Supplementary Table 1. Pharmacokinetic parameters of LMHO and LMHO through the time course of anti-Xa activity measured in the rat plasma (n = 3).

|  | Administration route | Dose (mg/kg) | AUC0-inf (h·µg·mL-1) | CL (mL·h-1) | t1/2 (h) |
| --- | --- | --- | --- | --- | --- |
| LMWH | Intravenous | 5 | 33.06 ± 3.84 | 38.16 ± 4.51 | 2.15 ± 0.89 |
| LMHO | intravenous | 5 | 334.15 ± 159.48 | 4.33 ± 1.93 | 41.17 ± 19.15 |

*AUC; area under the curve, CL; clearance, t1/2; half life; Data are presented as mean ± S.D.

Supplementary Fig. 11 | Biodistribution of low-molecular-weight heparin (LMWH). a, b In vivo biodistribution of Cy5.5-labeled LMWH in BALC/c nude mice after subcutaneous administration (a) and the integrated density of each time point (b) (n = 3). c Fluorescence analysis of LMWH–Cy5.5 distributed in organs (the heart, liver, kidney, lung, and spleen) at 1 h, day 1, and day 14.

Supplementary Fig. 12 | a-c Quantification of fluorescence in major organs (the heart, liver, kidney, lung, and spleen) over time for Cy5.5-labeled LMWH and LMHO biodistribution at 1 h (a) day 1 (b), and day 14 (c) (n = 3).

Supplementary Fig. 13 | Electrolyte (Na, K, Cl) percentage in serum versus control value as renal function parameters (n = 3).

Supplementary Fig. 14 | Histological TUNEL staining on injection site tissues in BALB/c mice following saline, LMWH, and LMHO treatment.