Supplementary data

O1 s

Figure 1s  XPS spectra of CNC, cCNC and various Ag-cCNC concentrtaions

Table S1 Silver particles size of various Ag-cCNC concentration

| Composite material | Ag % | Minimum Silver particle size (nm) | Maximum Silver particle size (nm) | Average Silver particles size (nm) |
| --- | --- | --- | --- | --- |
| 0.5%wt Ag-cCNC | 17.0 | 7.72 | 51.81 | 21.96 ± 8.04 |
| 1.0%wt Ag-cCNC | 23.2 | 5.31 | 43.15 | 18.92 ± 7.80 |
| 1.5%wt Ag-cCNC | 28.0 | 4.87 | 37.31 | 15.79 ± 6.59 |