Supplemental Material: A stable and low loss oxide layer on α-Ta (110) film for superconducting qubits

Zengqian Ding1,a), Boyi zhou1,a), Tao Wang1,a),Lina Yang1, Yanfu Wu1, Xiao Cai1, Kanglin Xiong1,2,b), Jiagui Feng1,2,c)

1 Gusu Laboratory of Materials, Suzhou, 215123

2 Suzhou Institute of Nano-Tech and Nano-Bionics, CAS, Suzhou, 215123

a) Zengqian Ding, Boyi Zhou, and Tao Wang contributed equally to this work

b) E-mail: klxiong2008@sinano.ac.cn

c) E-mail: jgfeng2017@sinano.ac.cn

1. XRD measurements of α-Ta (110) film

Figure S1 shows three XRD curves of α-Ta (110) film, two of which were immersed in fresh piranha solution 6 and 12 times for 20 minutes each, and the other one, as a comparison, was not immersed in the piranha solution. θ‐2θ scans were performed on the films in the range from 30° to 110°. In addition to the substrate peaks, we see two prominent peaks corresponding to the α-Ta (110) and α-Ta (220). We estimated the grain size of the three spectra to be roughly 45nm based on the FWHM of the α-Ta (110) peaks. The structure and grain size of the α-Ta (110) films remain stable under the influence of corrosion and the high temperature of the piranha solution.

Fig. S1 θ‐2θ XRD scans of α-Ta (110) films, colors indicate the film without immersion in piranha solution, and with immersion in piranha solution once and twelve times, respectively.

2. XRD measurements of α-Ta (111) film

Fig. S2 θ‐2θ XRD scans of α-Ta (111) films

Fig. S2 shows that there are three sharp peaks, two of which are substrate peaks, and the one at around 107° is the peak of α-Ta (111), which indicates that the sample is a pure α-Ta (111) film.

3. AFM and TEM images of α-Ta (111)

Fig. S3 (a) AFM image of α-Ta (111) film oxidized by air measured over a 2μm×2μm area. (b) The oxide layer thickness of α-Ta (111) in air.

Fig. S3 (a) shows the surface morphology of α-Ta (111) oxidized in air with fine and dense grains in triangular. Fig. S3 (b) is the TEM image of the oxide layer on α-Ta (111) film which shows the thickness of about 2 nm.

4. Angle-resolved XPS spectra of α-Ta (110)

Figure S4 shows the fitting data and angle-resolved XPS spectra from 0° to 75°of α-Ta (110) films. The angle is defined as the angle between the normal direction of the wafer surface and the direction of the signal acceptance. Ta2O5 is the major chemical composition of the α-Ta (110) film surface. In air, the oxidized layer on the surface of α-Ta (110) contains a small amount of Ta3+[Fig.S4 (a)], and after oxidation by piranha, it contains only Ta5+ [Fig.S4 (b)].

Fig. S4 (a) XPS fitting data of α-Ta (110) oxidized in air at θ=0°. (b) XPS fitting data of α-Ta (110) oxidized in piranha at θ=0°. (c) and (d) are angle-resolved XPS spectra of α-Ta (110) films. The colors indicate the angle in degrees between sample and detector. The two peaks at low binding energy belong to 4f7/2 and 4f5/2 orbitals of Ta metal, and the two peaks at higher binding energy correspond to the same orbitals of Ta2O5.

5. Angle-resolved XPS spectra of α-Ta (111)

Figure S5 shows the fitting data and angle-resolved XPS spectra from 30° to 85°of α-Ta (111) films. The angle is defined as the angle between the normal direction of the wafer surface and the direction of the signal acceptance. The α-Ta (111) surface oxide layer consists of Ta2O5 and other sub-oxidation states (Fig. S5 (a)). After the oxidation with piranha solution, its chemical composition was redistributed, with a significant increase in Ta2O5, but small amounts of sub-oxidation states remained (Fig. S5 (b)).

Fig. S5 (a) XPS fitting data of α-Ta (111) oxidized in air at θ=30°. (b) XPS fitting data of α-Ta (111) oxidized in piranha at θ=30°. (c) The spectra vs. angle of α-Ta (111) film in atmosphere. (d) The spectra vs. angle of α-Ta (111) film after once oxidation of piranha solution. The colors indicate the angle in degrees between sample and detector.

6. Structure of the CPW

Figure S6 shows the structure of one CPW on the chip. The CPW were designed with center conductor and insulating gap widths of w = 10 µm and g = 6 µm, respectively.

Fig. S6 Optical microscopy image of one CPW