Supporting Information for:

Well-constructed a water stable Cu-BTC@TpPa-1 binary composite with excellent capture ability toward malachite green

Jiaying Zou1·Yan Li2·Haotian Dong2· Na Ma2·and Wei Dai 1,*

1Key Laboratory of the Ministry of Education for Advanced Catalysis Materials, College of Chemistry and Materials Science, Zhejiang Normal University, Jinhua 321004, People’s Republic of China

2College of Geography and Environmental Sciences, Zhejiang Normal University, Jinhua 321004, People’s Republic of China

Corresponding author:

Prof. Wei Dai

E-mail: daiwei@zjnu.edu.cn

Section I

Chemicals and instruments

Reagents required include 1, 3, 5-triformylphloroglucinol (TP, 98%) ethanol, p-phenylenediamine (Pa，99%), acetic acid(CH3COOH, ≥99.5%), dioxane(≥99.5%), anhydrous THF(≥99.5%), anhydrous acetone(≥99.5%), and anhydrous CH2Cl2(≥99.5%), anhydrous CH3OH(≥99.5%), mesitylene (99%) CH3CH2OH (≥99.7%), 1,3,5-benzenetricarboxylic acid (H3BTC, 98%), malachite green (MG), which were supplied by Sinopharm Chemical Regent Co., Ltd. Copper nitrate hydrate (Cu(NO3)2·3H2O, 99%), which was supplied by Shanghai Aladdin Biochemical Technology Co., Ltd. All chemicals selected for this work are not purified in any way.

The N2 adsorption isotherms at -196 oC were calculated using the physical adsorption device (ASAP 2020), and the total surface area and pore size of the prepared adsorbents were calculated. Isotherms were measured using samples heated for 6 hours in a vacuum at 120 oC. SEM images were obtained by electron microscope (SEM, Gemini 300). XRD (D2 Phaser, Bruker, Cu Kα radiation) was used to analyze the crystal phase of the samples. FT-IR data of potassium bromide particles were recorded by Nicolet Nexus 470 spectrometer. Thermogravimetric analysis (TG-DSC) is performed on a NETZSCH STA-449C thermal analyzer in the atmosphere of nitrogen. Elemental analysis was performed by heating the Elementar vario elcube instrument to 1150 oC。

Scheme S1 Structure of malachite green

Characterization and adsorption performance tests.

The Nitrogen adsorption isotherms were recorded at -196 °C with a surface area and porosity analyzer (Micromeritics, ASAP2020) after evacuation of the adsorbents at 150 °C for 12 h. The specific surface areas were calculated using the Brunauer-Emmett-Teller (BET) equation by assuming a section area of nitrogen molecule to be 0.162 nm 2 . The total pore volume was estimated to be the liquid N2 volume at a relative pressure of 0.99. The sample phases were determined using X-ray diffraction (XRD, D2 Phaser, Bruker, Cu K αradiation). The compositions of the samples were examined using field-emission scanning electron microscopy (SEM, Hitachi S-4800). FT-IR spectra were recorded on a Bio-Rad FTS 155 FTIR spectrometer at room temperature in KBr pellets under atmospheric conditions. Thermo-gravimetric analysis was performed using a Net- zsch STA 449 C instrument and experiments were conducted with a constant heating rate of 5 °C/min in nitrogen atmosphere.

Adsorption performance evaluation

Prior to the adsorption test, the adsorbents were dried at 150 °C in vacuum for 24 h to remove the organic solvent and organic ligand residues. For the adsorption test of malachite green (MG), the dosage of different adsorbents was 10 mg dispersed in 50 mL solution with the required initial concentration of MG (0-60 mg/L). All experiments were carried out in a set of 250 mL glass flakers containing different adsorbents. Put in the constant temperature shaker 150 r/min at 25 oC. At the end of the reaction, the supernatant of the solution was taken after standing for 5 min and centrifuged at 9000 r/min for 3 min in a centrifuge (TAS-990PlusII, Beijing Puxi Co., Ltd). The obtained solution was filtered through a 0.22 µm filter membrane and the maximum absorbance was recorded at 617 nm using a UV spectrophotometer. The tests were rerun at least three times and averaged for data recording and analysis. The equilibrium time of adsorption kinetics experiment was 2 h. The regeneration of the adsorbent was achieved by using absolute ethanol as the eluent.

The MG absorption capacity qe (mg/g) at equilibrium was calculated by the following equation (1)

(1)

The adsorption capacity of MG by the adsorbent was obtained. Where C0 and Ce (mg/L) are the initial and equilibrium concentrations of MG, V(L) is the volume of MG, and W(g) is the mass of adsorbent added.

Section II

Table S1 Textural properties of different materials, respectively

| Sample | SBET (m2/g) | Vtotal (cm3/g) | Average pore diameter (nm) |
| --- | --- | --- | --- |
| Cu-BTC | 1356.45 | 0.581 | 1.712 |
| TpPa-1 | 104.89 | 0.136 | 7.015 |
| Cu-BTC@ TpPa-1(12) | 1030.77 | 0.582 | 2.441 |
| Cu-BTC@ TpPa-1(24) | 961.29 | 0.571 | 2.571 |
| Cu-BTC@ TpPa-1(36) | 411.49 | 0.444 | 4.646 |

Table S2. The content of elements in different materials

| Sample | N (%) | C (%) | H (%) | C/N |
| --- | --- | --- | --- | --- |
| Cu-BTC | 0.05 | 26.02 | 4.43 | 530.55 |
| TpPa-1 | 10.93 | 60.72 | 5.13 | 5.557 |
| Cu-BTC@ TpPa-1(12) | 0.99 | 33.46 | 3.78 | 33.94 |
| Cu-BTC@ TpPa-1(24) | 1.59 | 32.76 | 3.45 | 20.63 |
| Cu-BTC@ TpPa-1(36) | 3.42 | 40.62 | 4.11 | 11.89 |

Table S3 MG uptake capacities of different adsorbents

| Adsorbents | Uptake capacities (mg/g) | References |
| --- | --- | --- |
| C–HA–CO2 | 26 | (Jedynak and Repelewicz, 2017) |
| Cellulose | 2 | (Goswami et al., 2023) |
| UiO-66-NH2 nanocrystals | 1 | (Yao et al., 2016) |
| M3 nanocomposite adsorbent | 42 | (Sekhar et al., 2009) |
| Carbon nanotubes | 31 | (Wu, 2007) |
| (Zn0.24Cu0.76)O particles | 32 | (Jacob et al., 2013) |
| SHU-1 | 19 | (Li et al., 2017) |
| SHU-1a | 15 | (Li et al., 2017) |
| SHU-1b | 35 | (Li et al., 2017) |
| AFLP | 52 | (Gebreslassie, 2020) |
| γ-Fe2O3/MWCNTs/Cellulose | 48 | (khalatbary et al., 2022) |
| GO | 27 | (Robati et al., 2016) |
| rGO | 14 | (Robati et al., 2016) |
| CuFe2O4 | 22 | (Vergis et al., 2017) |
| MMT/PVDF/PEO membrane | 33 | (Ali and Ismail, 2021) |
| Cu-BTC | 48 | This work |
| TpPa-1 | 26 | This work |
| Cu-BTC@TpPa-1 | 64 | This work |

References

Ali HIsmail AM（2021）Developing montmorillonite/PVDF/PEO microporous membranes for removal of malachite green: adsorption, isotherms, and kinetics.Journal of Polymer Research 28 (11),

Gebreslassie YT（2020）Equilibrium, Kinetics, and Thermodynamic Studies of Malachite Green Adsorption onto Fig (Ficus cartia) Leaves.J Anal Methods Chem 2020, 7384675

Goswami R，Mishra A，Prasad BBhatt N（2023）Development of Nanocellulose-Chitosan-Based Nanocomposite for Adsorption of Malachite Green: Isotherms and Kinetic Study.Water, Air, & Soil Pollution 234 (5),

Jacob NM，Kuruva P，Madras GThomas T（2013）Purifying Water Containing Both Anionic and Cationic Species Using a (Zn, Cu)O, ZnO, and Cobalt Ferrite Based Multiphase Adsorbent System.Industrial & Engineering Chemistry Research 52 (46), 16384-16395

Jedynak KRepelewicz M（2017）Adsorption of methylene blue and malachite green on micro-mesoporous carbon materials.Adsorption Science & Technology 35 (5-6), 499-506

Khalatbary M，Sayadi MH，Hajiani MNowrouzi M（2022）Adsorption studies on the removal of malachite green by γ-Fe2O3/MWCNTs/Cellulose as an eco-friendly nanoadsorbent.Biomass Conversion and Biorefinery,

Li H，Fang X，Ma S，Niu Y，Zhao X，Xu JDuan Z（2017）A two-dimensional porous framework: solvent-induced structural transformation and selective adsorption towards malachite green.Dalton Trans 46 (26), 8350-8353

Robati D，Rajabi M，Moradi O，Najafi F，Tyagi I，Agarwal SGupta VK（2016）Kinetics and thermodynamics of malachite green dye adsorption from aqueous solutions on graphene oxide and reduced graphene oxide.Journal of Molecular Liquids 214, 259-263

Sekhar CP，Kalidhasan S，Rajesh VRajesh N（2009）Bio-polymer adsorbent for the removal of malachite green from aqueous solution.Chemosphere 77 (6), 842-7

Vergis BR，Hari Krishna R，Kottam N，Nagabhushana BM，Sharath RDarukaprasad B（2017）Removal of malachite green from aqueous solution by magnetic CuFe2O4 nano-adsorbent synthesized by one pot solution combustion method.Journal of Nanostructure in Chemistry 8 (1), 1-12

Wu CH（2007）Adsorption of reactive dye onto carbon nanotubes: equilibrium, kinetics and thermodynamics.J Hazard Mater 144 (1-2), 93-100

Yao BJ，Jiang WL，Dong Y，Liu ZXDong YB（2016）Post-Synthetic Polymerization of UiO-66-NH2 Nanoparticles and Polyurethane Oligomer toward Stand-Alone Membranes for Dye Removal and Separation.Chemistry 22 (30), 10565-71

Table S4. Adsorption isotherm models used in this study and their linear forms

| Isotherm | Nonlinear form | Linear form | Plot |
| --- | --- | --- | --- |
| Langmuir-I | qe=qLKLCe1+KLCe |  | versus Ce |
| Freundlich |  |  | versus |
| D–R |  |  | lnqe versus ε2 |

Where qe is the maximum capacity of adsorption in mg/g; KL is a constant related to the affinity of the binding sites in L/mg; ‘Kf’ and ‘n’ are the measures of adsorption capacity and intensity of adsorption; qs is the D-R isotherm constant in mg/g; KD stands for the constant that is relevant with the adsorption energy in mol2/kJ2; ε represents the Polanyi potential constant in kJ/mol;

Table S5. Adsorption isothermal model fitting parameters of Cu-BTC, TpPa-1, Cu-BTC@TpPa-1(12), Cu-BTC@TpPa-1(24), and Cu-BTC@TpPa-1(36)

| Samples | Langmuir Model |  |  | Freundlich Model |  |  | D-R Model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qL (mg/g) | KL (L/mg) | R2 | Kf (L/g) | n | R2 | qs (mg/g) | KD (mol2/kJ2) | R2 |
| Cu-BTC | 47.77 | 0.0196 | 0.9911 | 7.1751 | 2.01 | 0.9111 | 41.51 | 10.6414 | 0.9216 |
| TpPa-1 | 25.94 | 0.0025 | 0.9993 | 7.2569 | 2.73 | 0.7298 | 26.95 | 9.5765 | 0.9663 |
| Cu-BTC@ TpPa-1(12) | 54.69 | 0.0376 | 0.9963 | 10.5157 | 2.34 | 0.9141 | 47.33 | 8.0022 | 0.9192 |
| Cu-BTC@ TpPa-1(24) | 58.93 | 0.0163 | 0.9984 | 12.6362 | 2.32 | 0.8287 | 56.6503 | 7.7706 | 0.9801 |
| Cu-BTC@ TpPa-1(36) | 68.17 | 0.0298 | 0.9918 | 14.6415 | 2.31 | 0.8419 | 62.71 | 5.3532 | 0.9394 |

Table S6. Kinetic isotherm models used in this study and their linear forms

| Name | equations |
| --- | --- |
| Pseudo-first order model |  |
| Pseudo-second order model |  |
| Intra-particle diffusion model |  |
| Normalized standard deviation |  |

Where qe and qt (mg/g) are the uptakes of thiophene at equilibrium and at time t (min), respectively, K1 (1/min) is the adsorption rate constant, K2 (g/mg.min) is the rate constant for the second-order equation, and K3 (mg/g.min1/2) is the intra-particle diffusion rate constant.

Where qe,exp and qe,cal are the experimental and calculation uptakes of MG, respectively.

Table S7. Kinetic parameters of MG adsorbed onto Cu-BTC, TpPa-1, Cu-BTC@TpPa-1(12), Cu-BTC@TpPa-1(24), and Cu-BTC@TpPa-1(36)

| Samples | Pseudo-first-order rate equation |  |  |  |  |  | Pseudo-second-order rate equation |  |  |  |  |  | Intra-particle diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe,exp (mg/g) | qe,cal (mg/g) | K1 (1/min) | R2 | △q (mg/g) | △q (%) | qe,exp (mg/g) | qe,cal (mg/g) | K2 (g·mg-1·min-1) | R2 | △q (mg/g) | △q (%) | C (mg/g) | K3 (mg·g-1·min-1/2) | R2 |
| Cu-BTC | 43.19 | 42.28 | 0.0492 | 0.9862 | 0.91 | 2.11 | 43.19 | 50.80 | 0.0011 | 0.9981 | -7.61 | -17.61 | 8.23 | 3.7097 | 0.3901 |
| TpPa-1 | 25.26 | 14.64 | 0.0439 | 0.9235 | 10.62 | 42.04 | 25.26 | 28.71 | 0.0035 | 0.9903 | --3.45 | -13.66 | 10.66 | 1.6779 | 0.7374 |
| Cu-BTC@ TpPa-1(12) | 49.11 | 59.29 | 0.0551 | 0.8710 | -10.18 | -20.72 | 49.11 | 54.12 | 0.0014 | 0.9938 | -5.01 | -10.20 | 13.53 | 3.8807 | 0.8312 |
| Cu-BTC@ TpPa-1(24) | 64.28 | 74.00 | 0.0692 | 0.8183 | -9.72 | -15.12 | 64.28 | 68.14 | 0.0015 | 0.9909 | -3.86 | -5.66 | 27.37 | 4.9728 | 0.7887 |
| Cu-BTC@ TpPa-1(36) | 56.22 | 70.94 | 0.0623 | 0.9171 | -14.72 | -26.18 | 56.22 | 60.32 | 0.0017 | 0.9939 | -4.10 | -7.29 | 18.24 | 4.2483 | 0.8246 |

Table S8. Diffusion coefficients of RhB adsorbed onto Cu-BTC and Cu-BTC@SPC

| Samples | K (s-1) | Diq (cm2/s) |
| --- | --- | --- |
| TpPa-1 | 0.1422 | 1.4233E-08 |
| Cu-BTC | 0.0122 | 4.1221E-11 |
| Cu-BTC@TpPa-1(24) | 0.0214 | 1.6324E-10 |

Fig. S1 Intra-particle diffusion model for MG adsorption onto Cu-BTC, TpPa-1, Cu-BTC@TpPa-1(12), Cu-BTC@TpPa-1(24), Cu-BTC@TpPa-1(36)