Supplementary Material for

Chloride Electrode Composed of Ubiquitous Elements for High-Energy-Density All-Solid-State Sodium-Ion Batteries

Naoto Tanibata,* Naoki Nonaka, Keisuke Makino, Hayami Takeda, and Masanobu Nakayama

Department of Advanced Ceramics, Nagoya Institute of Technology, Gokiso, Showa, Nagoya, Aichi 466-8555, Japan

*Correspondence should be addressed to tanibata.naoto@nitech.ac.jp

Supplementary Material 1　Investigation of Solid Electrolyte Materials for Separator Layer

Figure S1. AC impedance plots of NaFeCl4 compressed pellet at 298 K and 333 K.

Figure S2 shows the characterization results of the NaFeCl4 electrode using the Na3PS4 sulfide electrolyte, which is the most commonly used solid electrolyte in all-solid-state batteries (ASSBs). The charge–discharge curve (Figure S2a) reveals a low capacity of approximately 30% of the theoretical capacity (121.5 mAh g-1), although it operated at a high average working potential of approximately 3.45 V (vs. Na/Na+). The impedance plot after charging and discharging (Figure S2b) shows two semicircles. The resistance R1 on the high-frequency side is the resistance of Na10Sn4/Na3PS4 obtained from the results of the Na10Sn4/Na3PS4 symmetric cell. R2 on the low-frequency side is the resistance of the Na3PS4/NaFeCl4 interface because the capacitance is 8.3 × 10-6 F after discharge and 1.6 × 10-6 F after charge. The resistance is larger than that of Na10Sn4/Na3PS4, particularly after charging, showing a significant increase. This may be attributed to the poor oxidation resistance of Na3PS4 sulfide. Therefore, we fabricated and evaluated an ASSB using Na2.25Y0.25Zr0.75Cl6 as a separator, which reportedly exhibits the highest ionic conductivity in an oxidation-resistant chloride electrolyte.

Figure S2. Characteristics of all-solid-state sodium-ion batteries (Na10Sn4+AB | Na3PS4 | NaFeCl4+KB) using a NaFeCl4 electrode without an electrolyte (NaFeCl4:KB = 90:10 wt.%) and with Na3PS4 sulfide solid electrolyte. (a) Constant current charge–discharge curves. (b) Impedance plots before and after the charge–discharge process.

In the charge–discharge curve (Figure S3), the average working potential was approximately 0.3 V lower, 3.2 V (vs. Na/Na+) when only Na2.25Y0.25Zr0.75Cl6 was used as the separator. The Na2.25Y0.25Zr0.75Cl6 electrolyte is known to increase the resistance with each cycle, even when Na–Sn alloys are used. These results suggest that the Na2.25Y0.25Zr0.75Cl6 electrolyte is less resistant to reduction than Na3PS4 and reacts with Na10Sn4. Therefore, in this study, we used an electrolyte bilayer all-solid-state cell with Na3PS4 electrolyte on the Na10Sn4 negative electrode side and Na2.25Y0.25Zr0.75Cl6 electrolyte on the NaFeCl4 positive electrode side.

Figure S3. Constant current charge–discharge curves of the all-solid-state sodium-ion battery (Na10Sn4+AB | Na2.25Y0.25Zr0.75Cl6 | NaFeCl4+KB) with NaFeCl4 electrode without electrolyte (NaFeCl4:KB = 90:10 wt.%) and chloride electrolyte Na2.25Y0.25Zr0.75Cl6.

Figure S4. XRD patterns of the NaFeCl4 electrode before and after charging.