Rationalizing the efficiency of Cu-based MOF for the Capture and biomimetic Sequestration of Carbon dioxide

Dana Susan Abrahama, Athul K.Va, Shamna Ia, MargandanBhagiyalakshmia* and Soon Kwan Jeongb*

aDepartment of Chemistry, Central University of Kerala, India

bFine Dust Research Center, Korea Institute of Energy Research, Daejeon 34129, Republic of Korea

Corresponding author: mbhagiya@gmail.com; bhagiyalakshmi@cukerala.ac.in; jeongsk@kier.re.kr

Table S1 : Kinetic analysis of p-NPA hydrolysis on spectrophotometer with CA/Cu-MOF

| Concentration of p-NPA (mM) | Absorbance at 403 nm |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Trail 1 | Trail 2 | Trail 3 | mean | Standard Deviation |
| 5 | 0.171 | 0.190 | 0.205 | 0.189 | 0.017039171 |
| 10 | 0.279 | 0.314 | 0.302 | 0.298 | 0.017785762 |
| 20 | 0.382 | 0.376 | 0.370 | 0.376 | 0.006 |
| 40 | 0.689 | 0.750 | 0.732 | 0.724 | 0.031342197 |
| 60 | 1.052 | 1.049 | 1.052 | 1.051 | 0.001732051 |
| 80 | 1.372 | 1.387 | 1.371 | 1.377 | 0.008962886 |
| 100 | 1.729 | 1.724 | 1.751 | 1.735 | 0.014364308 |
|  |  |  | Average | 0.821 | 0.013889482 |

Uncertainty associated with precession from one-way Anova Test

| Anova: Single Factor |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| SUMMARY |  |  |  |  |  |  |
| Groups | Count | Sum | Average | Variance |  |  |
| Column 1 | 7 | 5.674 | 0.810571 | 0.351179 |  |  |
| Column 2 | 7 | 5.79 | 0.827143 | 0.34096 |  |  |
| Column 3 | 7 | 5.783 | 0.826143 | 0.346786 |  |  |
| ANOVA |  |  |  |  |  |  |
| Source of Variation | SS | df | MS | F | P-value | F crit |
| Between Groups | 0.00120886 | 2 | 0.000604 | 0.001745 | 0.998256 | 3.554557 |
| Within Groups | 6.23354943 | 18 | 0.346308 |  |  |  |
| Total | 6.23475829 | 20 |  |  |  |  |

Since F<F criteria  Uncertainty associated with precession = sx√n

Where S= Average standard deviation; x is average mean  and n  is no of measurement of analysts

For our results S =0.01 ; x = 0.82 and n =7

Therefore Uncertainty associated with precession = 0.010.82√7

= 0.0046= 0.005

Table S2a: Experimental data for the adsorption isotherms for CO2.

| CO2 isotherm at 298 K |  |  |  | CO2 isotherm at 308 K |  |  |  | CO2 isotherm at 318 K |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorption Pressure (bar) | Amount of CO2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CO2 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of CO2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CO2 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of CO2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CO2 desorbed (mmol/g) |
| 0.00 | 0.00 | 29.80 | 8.25 | 0.00 | 0.00 | 29.83 | 8.02 | 0.00 | 0.00 | 29.84 | 7.79 |
| 0.10 | 0.19 | 28.97 | 8.25 | 0.12 | 0.24 | 29.02 | 8.04 | 0.10 | 0.21 | 29.00 | 7.78 |
| 0.21 | 0.58 | 27.52 | 8.22 | 0.20 | 0.59 | 27.50 | 8.02 | 0.20 | 0.45 | 27.53 | 7.75 |
| 0.40 | 1.20 | 25.05 | 8.19 | 0.41 | 1.15 | 25.06 | 7.97 | 0.40 | 0.92 | 25.05 | 7.68 |
| 0.52 | 1.64 | 22.54 | 8.16 | 0.50 | 1.41 | 22.52 | 7.89 | 0.50 | 0.99 | 22.54 | 7.58 |
| 0.60 | 1.98 | 20.04 | 8.10 | 0.61 | 1.57 | 20.04 | 7.86 | 0.60 | 1.31 | 20.03 | 7.48 |
| 0.80 | 2.44 | 17.53 | 8.02 | 0.81 | 1.98 | 17.53 | 7.67 | 0.81 | 1.59 | 17.53 | 7.33 |
| 1.00 | 2.85 | 15.00 | 7.90 | 1.01 | 2.45 | 14.99 | 7.53 | 1.00 | 1.86 | 15.00 | 7.16 |
| 2.50 | 4.79 | 12.50 | 7.74 | 2.50 | 4.38 | 12.50 | 7.37 | 2.50 | 3.67 | 12.50 | 6.93 |
| 5.00 | 6.33 | 10.00 | 7.50 | 5.00 | 5.94 | 10.00 | 7.14 | 4.99 | 5.36 | 10.00 | 6.58 |
| 7.50 | 7.10 | 7.50 | 7.14 | 7.50 | 6.66 | 7.50 | 6.73 | 7.50 | 6.17 | 7.50 | 6.08 |
| 10.00 | 7.46 | 5.02 | 6.49 | 10.00 | 7.06 | 5.00 | 5.98 | 10.00 | 6.49 | 5.00 | 5.26 |
| 12.50 | 7.74 | 2.50 | 5.02 | 12.50 | 7.32 | 2.50 | 4.40 | 12.49 | 6.82 | 2.50 | 3.57 |
| 15.00 | 7.90 | 1.00 | 2.95 | 15.00 | 7.49 | 1.01 | 2.45 | 15.00 | 7.16 | 1.01 | 1.90 |
| 17.50 | 8.00 | 0.80 | 2.55 | 17.49 | 7.64 | 0.80 | 2.06 | 17.48 | 7.42 | 0.80 | 1.55 |
| 19.99 | 8.10 | 0.60 | 2.04 | 19.99 | 7.76 | 0.60 | 1.68 | 20.00 | 7.44 | 0.60 | 1.19 |
| 22.38 | 8.16 | 0.50 | 1.77 | 22.38 | 7.89 | 0.50 | 1.32 | 22.39 | 7.61 | 0.50 | 1.15 |
| 24.85 | 8.21 | 0.40 | 1.48 | 24.89 | 7.95 | 0.40 | 1.16 | 24.86 | 7.69 | 0.40 | 0.85 |
| 27.33 | 8.24 | 0.20 | 0.83 | 27.35 | 8.02 | 0.20 | 0.67 | 27.34 | 7.74 | 0.20 | 0.46 |
| 29.80 | 8.25 | 0.10 | 0.46 | 29.83 | 8.02 | 0.10 | 0.35 | 29.84 | 7.79 | 0.10 | 0.29 |

Table S2b: Experimental data for the adsorption isotherms forCH4

| CH4 isotherm at 298 K |  |  |  | CH4 isotherm at 308 K |  |  |  | CH4 isotherm at 318 K |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorption Pressure (bar) | Amount of CH4 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CH4 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of CH4 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CH4 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of CH4 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of CH4 desorbed (mmol/g) |
| 0.00 | 0.00 | 49.75 | 5.64 | 0.00 | 0.00 | 49.74 | 5.39 | 0.00 | 0.00 | 49.75 | 5.13 |
| 0.10 | 0.05 | 48.87 | 5.63 | 0.10 | 0.05 | 48.83 | 5.37 | 0.10 | 0.05 | 48.85 | 5.12 |
| 0.20 | 0.12 | 44.97 | 5.57 | 0.20 | 0.13 | 44.96 | 5.30 | 0.20 | 0.12 | 44.95 | 5.02 |
| 0.40 | 0.27 | 39.96 | 5.50 | 0.40 | 0.27 | 39.95 | 5.18 | 0.40 | 0.21 | 40.01 | 4.88 |
| 0.50 | 0.36 | 34.97 | 5.37 | 0.50 | 0.32 | 34.95 | 5.03 | 0.50 | 0.26 | 34.95 | 4.69 |
| 0.60 | 0.45 | 29.98 | 5.18 | 0.60 | 0.38 | 29.98 | 4.83 | 0.60 | 0.32 | 29.97 | 4.47 |
| 0.80 | 0.58 | 27.48 | 5.10 | 0.80 | 0.48 | 27.48 | 4.71 | 0.80 | 0.39 | 27.47 | 4.34 |
| 1.00 | 0.69 | 24.99 | 4.96 | 1.00 | 0.58 | 24.99 | 4.56 | 1.00 | 0.48 | 24.98 | 4.18 |
| 2.50 | 1.35 | 22.49 | 4.77 | 2.50 | 1.14 | 22.49 | 4.39 | 2.50 | 0.98 | 22.52 | 4.01 |
| 5.00 | 2.17 | 19.99 | 4.61 | 5.00 | 1.90 | 19.99 | 4.19 | 5.00 | 1.66 | 19.99 | 3.81 |
| 7.50 | 2.81 | 17.50 | 4.41 | 7.50 | 2.49 | 17.50 | 3.97 | 7.50 | 2.16 | 17.50 | 3.58 |
| 10.00 | 3.33 | 15.00 | 4.14 | 10.00 | 2.92 | 15.00 | 3.69 | 10.00 | 2.63 | 15.00 | 3.31 |
| 12.50 | 3.75 | 12.50 | 3.81 | 12.50 | 3.37 | 12.50 | 3.37 | 12.50 | 2.98 | 12.50 | 3.00 |
| 15.00 | 4.09 | 10.00 | 3.39 | 15.00 | 3.66 | 10.00 | 2.97 | 15.00 | 3.31 | 10.00 | 2.63 |
| 17.50 | 4.38 | 7.50 | 2.87 | 17.50 | 3.94 | 7.50 | 2.50 | 17.50 | 3.58 | 7.50 | 2.18 |
| 20.00 | 4.61 | 5.00 | 2.23 | 20.00 | 4.20 | 5.00 | 1.91 | 20.00 | 3.80 | 5.00 | 1.66 |
| 22.43 | 4.77 | 2.50 | 1.39 | 22.42 | 4.35 | 2.50 | 1.18 | 22.44 | 4.00 | 2.50 | 1.00 |
| 24.91 | 4.91 | 1.00 | 0.72 | 24.91 | 4.55 | 1.00 | 0.60 | 24.92 | 4.18 | 1.00 | 0.50 |
| 27.40 | 5.07 | 0.80 | 0.61 | 27.39 | 4.68 | 0.80 | 0.51 | 27.41 | 4.33 | 0.80 | 0.41 |
| 29.89 | 5.20 | 0.60 | 0.48 | 29.90 | 4.82 | 0.60 | 0.40 | 29.90 | 4.47 | 0.60 | 0.33 |

Table S2c: Experimental data for the adsorption isotherms for N2.

| N2 isotherm at 298 K |  |  |  | N2 isotherm at 308 K |  |  |  | N2 isotherm at 318 K |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorption Pressure (bar) | Amount of N2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of N2 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of N2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of N2 desorbed (mmol/g) | Adsorption Pressure (bar) | Amount of N2 adsorbed (mmol/g) | Desorption Pressure (bar) | Amount of N2 desorbed (mmol/g) |
| 0.07 | 0.02 | 49.79 | 3.63 | 0.00 | 0.00 | 49.81 | 3.25 | 0.00 | 0.00 | 49.80 | 3.02 |
| 0.10 | 0.06 | 48.90 | 3.63 | 0.10 | 0.02 | 48.87 | 3.24 | 0.10 | 0.02 | 48.89 | 2.99 |
| 0.20 | 0.11 | 44.97 | 3.53 | 0.20 | 0.04 | 44.97 | 3.11 | 0.20 | 0.03 | 44.98 | 2.89 |
| 0.40 | 0.21 | 39.99 | 3.39 | 0.40 | 0.08 | 39.98 | 2.99 | 0.40 | 0.06 | 40.02 | 2.75 |
| 0.50 | 0.28 | 35.00 | 3.22 | 0.50 | 0.09 | 34.99 | 2.80 | 0.50 | 0.08 | 35.00 | 2.57 |
| 0.60 | 0.32 | 30.01 | 3.02 | 0.60 | 0.12 | 30.01 | 2.61 | 0.60 | 0.10 | 29.99 | 2.39 |
| 0.80 | 0.41 | 27.51 | 2.90 | 0.80 | 0.15 | 27.46 | 2.51 | 0.80 | 0.13 | 27.49 | 2.27 |
| 1.00 | 0.49 | 25.01 | 2.77 | 1.00 | 0.20 | 25.03 | 2.38 | 1.00 | 0.16 | 25.00 | 2.16 |
| 2.50 | 0.94 | 22.51 | 2.63 | 2.50 | 0.46 | 22.51 | 2.25 | 2.50 | 0.39 | 22.51 | 2.02 |
| 5.00 | 1.37 | 20.02 | 2.47 | 5.00 | 0.81 | 20.02 | 2.08 | 5.00 | 0.69 | 20.01 | 1.89 |
| 7.49 | 1.64 | 17.52 | 2.29 | 7.49 | 1.10 | 17.50 | 1.94 | 7.49 | 0.94 | 17.45 | 1.73 |
| 9.99 | 1.87 | 15.01 | 2.09 | 9.99 | 1.35 | 15.01 | 1.76 | 9.98 | 1.21 | 15.01 | 1.57 |
| 12.48 | 2.09 | 12.50 | 1.87 | 12.48 | 1.59 | 12.50 | 1.53 | 12.49 | 1.38 | 12.50 | 1.38 |
| 14.97 | 2.29 | 10.00 | 1.62 | 14.97 | 1.81 | 10.00 | 1.32 | 14.96 | 1.57 | 10.00 | 1.17 |
| 17.46 | 2.47 | 7.50 | 1.33 | 17.47 | 1.95 | 7.50 | 1.09 | 17.47 | 1.77 | 7.50 | 0.93 |
| 19.95 | 2.63 | 5.00 | 0.99 | 19.95 | 2.09 | 5.00 | 0.79 | 19.96 | 1.88 | 5.00 | 0.67 |
| 22.43 | 2.76 | 2.50 | 0.58 | 22.44 | 2.27 | 2.50 | 0.43 | 22.44 | 2.06 | 2.50 | 0.37 |
| 24.92 | 2.88 | 1.00 | 0.28 | 24.94 | 2.37 | 1.00 | 0.20 | 24.93 | 2.15 | 0.99 | 0.16 |
| 27.42 | 2.98 | 0.80 | 0.23 | 27.41 | 2.51 | 0.80 | 0.18 | 27.43 | 2.30 | 0.80 | 0.13 |
| 29.91 | 3.07 | 0.60 | 0.19 | 29.92 | 2.63 | 0.60 | 0.13 | 29.90 | 2.38 | 0.60 | 0.10 |

Table S3: Selectivity data for CO2/CH4 and CO2/N2

| CO2 isotherm at 298 K |  | CH4 isotherm at 298 K |  | N2 isotherm at 298 K |  | Selectivity |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorption Pressure (bar) | Amount of CO2 adsorbed (mmol/g) | Adsorption Pressure (bar) | Amount of CH4 adsorbed (mmol/g) | Adsorption Pressure (bar) | Amount of N2 adsorbed (mmol/g) | Adsorption Pressure (bar) | CO2/CH4 | CO2/N2 |
| 0.00 | 0.00 | 0.00 | 0.00 | 0.07 | 0.02 |  |  |  |
| 0.10 | 0.19 | 0.10 | 0.05 | 0.10 | 0.06 | 0.10 | 4.04 | 3.39 |
| 0.21 | 0.58 | 0.20 | 0.12 | 0.20 | 0.11 | 0.20 | 4.79 | 5.52 |
| 0.40 | 1.20 | 0.40 | 0.27 | 0.40 | 0.21 | 0.40 | 4.49 | 5.83 |
| 0.52 | 1.64 | 0.50 | 0.36 | 0.50 | 0.28 | 0.50 | 4.57 | 5.96 |
| 0.60 | 1.98 | 0.60 | 0.45 | 0.60 | 0.32 | 0.60 | 4.43 | 6.11 |
| 0.80 | 2.44 | 0.80 | 0.58 | 0.80 | 0.41 | 0.80 | 4.18 | 5.98 |
| 1.00 | 2.85 | 1.00 | 0.69 | 1.00 | 0.49 | 1.00 | 4.12 | 5.82 |
| 2.50 | 4.79 | 2.50 | 1.35 | 2.50 | 0.94 | 3.00 | 3.56 | 5.10 |
| 5.00 | 6.33 | 5.00 | 2.17 | 5.00 | 1.37 | 5.00 | 2.92 | 4.62 |
| 7.50 | 7.10 | 7.50 | 2.81 | 7.49 | 1.64 | 8.00 | 2.52 | 4.34 |
| 10.00 | 7.46 | 10.00 | 3.33 | 9.99 | 1.87 | 10.00 | 2.24 | 3.99 |
| 12.50 | 7.74 | 12.50 | 3.75 | 12.48 | 2.09 | 13.00 | 2.07 | 3.71 |
| 15.00 | 7.90 | 15.00 | 4.09 | 14.97 | 2.29 | 15.00 | 1.93 | 3.46 |
| 17.50 | 8.00 | 17.50 | 4.38 | 17.46 | 2.47 | 18.00 | 1.83 | 3.24 |
| 19.99 | 8.10 | 20.00 | 4.61 | 19.95 | 2.63 | 20.00 | 1.76 | 3.08 |
| 22.38 | 8.16 | 22.43 | 4.77 | 22.43 | 2.76 | 22.00 | 1.71 | 2.96 |
| 24.85 | 8.21 | 24.91 | 4.91 | 24.92 | 2.88 | 25.00 | 1.67 | 2.85 |
| 27.33 | 8.24 | 27.40 | 5.07 | 27.42 | 2.98 | 27.00 | 1.62 | 2.77 |
| 29.80 | 8.25 | 29.89 | 5.20 | 29.91 | 3.07 | 29.00 | 1.59 | 2.68 |
|  |  | 34.85 | 5.34 | 34.87 | 3.25 |  |  |  |
|  |  | 39.82 | 5.49 | 39.84 | 3.40 |  |  |  |
|  |  | 44.77 | 5.59 | 44.81 | 3.52 |  |  |  |
|  |  | 49.75 | 5.64 | 49.79 | 3.63 |  |  |  |

Figure S1	: Schematic of Cu-MOF framework for surface excess adsorption of CO2

Figure S2 : Isosteric enthalpy Qst,n for CO2 adsorption on Cu-MOF at surface excess values of 3.5,4.5,5.5,6.5,7.5 and 8 mmol g-1 from Clausius−Clapeyron graphs for different temperatures studied.

Figure S3 : Isosteric enthalpy Qst,n for N2 and CH4 adsorption on Cu-MOF from Clausius−Clapeyron graphs.

Figure S4	: Freundlich-Langmuir isotherm fit for CO2 adsorption on Cu-MOF at 298 K and 313 K.

CO2 adsorption/desorption isotherms on Cu-MOF represents an isotherm of the Freundlich-Langmuir model; the two isotherms recorded at two different temperatures (298 and 318K) are considered and fitted with the Freundlich-Langmuir equation to obtain at derived pressure through the following equation (1):

n=a.b.pc1+b. pc                                                                                                 (1)

Where n is the amount of CO2 adsorbed by Cu-MOF in mmol/g, p is pressure in bar, a is the maximum amount adsorbed, b is the affinity constant, and c is the heterogeneity exponent. Equation (1) can be rearranged to obtain derived p values

pn= cna.b-n.b                                                                                       (2)

From the derived pressure, ∆Hads is evaluated using the equation (3).

∆Hads= -R. lnp2p1. T1.T2(T2- T1)                                                                  (3)

Figure S5: Reaction scheme for CO2 sequestration as CaCO3 using CA/Cu-MOF.

Figure S6	: FE-SEM image of precipitated CaCO3.

Figure S7	: XRD pattern of precipitated CaCO3.

Figure S8	: Reusability of CA/Cu-MOF for CaCO3 precipitation

Calculations:

Estimation of immobilization yield from Bradford Assay

| 1mg/ml of CA contains 946.13 µg of protein. |  |
| --- | --- |
| Amount of protein present in 4ml of CA solution | = 946.13 × 4 = 3784.52 µg of protein |
| Amount of protein left in the buffer after immobilization in 4ml | = 784.52 µg of protein |
| Amount of protein-bound on 100mg of Cu-MOF | = 3784.52-784.52 = 3000 µg of protein |
| Immobilization Yield (%) | = 30003784.52× 100 = 79% |
| Amount of CA loaded per mg of CA/Cu-MOF | = 3000 µg/100mg CA/Cu-MOF = 30µg/mg CA/Cu-MOF |

Reference:

- Jcgm, J. C. G. M. Evaluation of measurement data—Guide to the expression of uncertainty in measurement. Int. Organ. Stand. Geneva ISBN, 50, 134. (2008). http://dx.doi.org/10.1088/0026-1394/43/4/S01.