Targeted Chemoimmunotherapy for Hepatocellular Carcinoma: Dual-Stimulus Nanocarrier for Enhanced Antitumor Responses

Jinxiao Song†1, Zhenghui Jing†1, You Wu2, Jingyi Zhou1, Deteng Zhang2* Xinlong Zang1*

- School of basic medicine, Qingdao medical college, Qingdao University, Qingdao, PR China

- Institute of Neuroregeneration and Neurorehabilitation, Qingdao University, Qingdao 266071, China.

*Corresponding author:

Xinlong Zang, E-mail: zangxinlong@126.com; Deteng Zhang, E-mail: zhangbio137@qdu.edu.cn

†These authors contributed equally to this work.

Supporting information

Figure S1. Schematic illustration of PGla-PEG-PPBP (A) and PEG-PBA (B) synthesis.

Figure S2. 1H NMR of MAGlaAc.

Figure S3. 1H NMR of MAPBP.

Figure S4. 1H NMR of PGlaAc.

Figure S5. 1H NMR of PGlaAc-PEG.

Figure S6. 1H NMR of PGlaAc-PEG-PPBP.

Table S1. Particle sizes of nanoparticles at different pHs and redox conditions (n=3).

| Formulations | Particle sizes (nm) |  | Zeta potential (mV) |
| --- | --- | --- | --- |
|  | Without H2O2 | With H2O2 |  |
| PN@GPB NPs | 103.36 ± 2.31 | 873.3 ± 50.3 | -14.7 ± 0.67 |
| PN@GPB-PEG NPs at pH6.5 | 99.44 ± 3.46 | 906.9 ± 51.32 | -11.7 ± 1.06 |
| PN@GPB-PEG NPs at pH7.4 | 87.83 ± 5.61 | 735 ± 100.1 | -3.73 ± 0.24 |

Table S2. The encapsulation and drug loading efficiency of different formulations.

| Formulations | PTX |  | NLG919 |  |
| --- | --- | --- | --- | --- |
|  | EE (%) | DLE (%) | EE (%) | DLE (%) |
| PN@GPB NPs | 75 | 2.9 | 48.77 | 0.94 |
| PN@GPB-PEG NPs at pH6.5 | 77.5 | 2.98 | 41.04 | 0.79 |
| PN@GPB-PEG NPs at pH7.4 | 69.5 | 2.67 | 55.6 | 1.07 |

Figure S7. Body weight of mice received different treatments.

Figure S8. HE staining of main organs (heart, liver, spleen, lung and kidney) obtained from mice in different treatment groups.