

Table 1. The stiffness of PEG/SF/HAp scaffolds with different HAp concentration 
		        
	HAp 25mg
	HAp 50mg
	HAp 75mg
	HAp 100mg

	Stiffness(kPa)
	80.98±17.45
	127.31±12.55
	165.32±9.63
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