Electronic Supplementary Material

Synthesis of lanthanum and waste lye modified-zeolite from fly ash and its application in constructed wetland for nitrogen and phosphorus removal

Zhimei Liu 1,2,3, Zhen Liang 4 , Shengju Wu 2,3

(1.Chongqing University , Chongqing,400044, China

2.College of Resources and Environment, Chongqing School, University of Chinese Academy of Sciences, Chongqing,400714, China

3.Chongqing Institute of Green and Intelligent Technology, Chinese Academy of Sciences, Chongqing,400714, China

4.College of Fisheries , Southwest University, Chongqing,402460, China)

Corresponding author E-mails: liangzh2004@163.com

# Table S1 Design and results of BBD factors

| Numbers | LaCl3 concentration（mM） | pH | Roasting temperature （℃） | P Removal （%） |
| --- | --- | --- | --- | --- |
| 1 | 10.8 | 12 | 300 | 86.06 |
| 2 | 16.2 | 6 | 200 | 93.43 |
| 3 | 10.8 | 9 | 200 | 96.34 |
| 4 5 | 16.2 5.4 | 12 6 | 200 200 | 92.81 89.59 |
| 6 | 10.8 | 12 | 100 | 83.05 |
| 7 | 10.8 | 9 | 200 | 96.86 |
| 8 | 16.2 | 9 | 300 | 89.28 |
| 9 | 10.8 | 6 | 300 | 86.17 |
| 10 | 5.4 | 12 | 200 | 89.49 |
| 11 | 16.2 | 9 | 100 | 86.69 |
| 12 | 5.4 | 9 | 300 | 87.72 |
| 13 | 10.8 | 9 | 200 | 96.34 |
| 14 | 5.4 | 9 | 100 | 84.71 |
| 15 | 10.8 | 9 | 200 | 96.13 |
| 16 | 10.8 | 9 | 200 | 96.44 |
| 17 | 10.8 | 6 | 100 | 83.16 |

Note：three replicates of each experimen

Table S2 Optimal optimization and validation analysis of P removal under restricted domain conditions

| Factor selection range |  |  | Response Value Limiting Conditions | Optimal conditions |  |  | Model P Predicted Value | P experimental value（%） | Deviation (%) | Experimental value of N removal of LZFA（%） | N removal of ZFA(%) | Rate of change（%） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LaCl3 concentration （mM） | pH | Roasting temperature （℃） | ＞90% | LaCl3 concentration （mM） | pH | Roasting temperature（℃） | 96.83 | 95.98 | 0.88 | 81.88 | 89.33 | -8.3 |
| 5.4-16.2 | 6-12 | 100-300 |  | 13.56 | 8.93 | 208.72 |  |  |  |  |  |  |

Table S3 Chemical composition of the substances tested by XRF

| Samples | SiO2 | Al2O3 | Fe2O3 | CaO | F | K2O | TiO2 | MgO | Na2O | La2O3 | 其余 | Si/Al |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FA | 50.28 | 25.79 | 7.25 | 4.79 | 4.05 | 2.93 | 1.45 | 0.81 | 0.71 | 0 | 1.94 | 1.8 |
| ZFA | 33.49 | 18.65 | 4.83 | 2.81 | _ | 2.01 | 0.90 | 0.43 | 36.12 | 0 | 0.76 | 1.58 |
| LZFA | 36.68 | 22.35 | 7.11 | 4.00 | _ | 0.92 | 1.25 | 0.82 | 8.53 | 17.81 | 0.53 | 1.44 |

Table S4 Specific surface and pore size distribution

| Sample | BET （m2/g） | Total Pore Volume （cm3 /g） | r ( nm) | Mircropore Area （m2/ g） | Mircropore volume （cm3 /g） | rmic ( nm) |
| --- | --- | --- | --- | --- | --- | --- |
| ZFA | 3.79 | 0.021 | 21.60 | 1.507 | 0.000768 | 2.03 |
| LZFA | 207.12 | 0.217 | 4.19 | 158.32 | 0.083 | 2.09 |

Note: r and rmic represent the total and micropore average pore diameters, respectively, and are calculated from 4V/A, where V is the pore volume and A is the Bet calculated specific surface area.

Table S5  Kinetic parameters of N and P adsorption by ZFA and LZFA

| Adsorbent | Initial concentration（mg/L） | Pseudo first-order model |  |  |  |  |  |  | Pseudo second-order model |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe,cal （mg/g） |  |  | K1 （min-1） |  | R2 |  | qe,cal （mg/g） |  |  | K2 （g/(mg.min)) |  |  | R2 |
| ZFA | N 5 | 0.433 |  |  | 0.178 |  | 0.536 |  | 0.447 |  |  | 0.495 |  |  |  |
| LZFA | N 5 | 0.404 |  |  | 0.0240 |  | 0.622 |  | 0.412 |  |  | 0.982 |  |  | 0.921 |
|  | P 5 | 0.469 |  |  | 0.0246 |  | 0.596 |  | 0.481 |  |  | 0.653 |  |  | 0.913 |
| Adsorbent | Initial concentration（mg/L） | Intra particle diffusion model |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Kd1 （mg/（g.min0.5）） | C1 | R2 |  | Kd2 （mg/（g.min0.5）） |  | C2 |  | R2 | Kd3 （mg/（g.min0.5）） |  | C3 | R2 |  |
| ZFA | N 5 | 0.0107 | 0.3297 | 0.9946 |  | 0.0033 |  | 0.3872 |  | 0.6845 | 3.680×10-4 |  | 0.4332 | 0.393 |  |
| LZFA | N 5 | 0.0103 | 0.309 | 0.935 |  | 0.00367 |  | 0.357 |  | 0.985 | 6.428×10-5 |  | 0.413 | 0.405 |  |
|  | P 5 | 0.0144 | 0.333 | 0.997 |  | 0.00498 |  | 0.407 |  | 0.944 | 1.451×10-4 |  | 0.478 | 0.291 |  |

Table S6 Isothermal parameters of N and P adsorption by ZFA and LZFA

| Adsorbent |  | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Qm(mg/g) | KL（L/mg） | R2 | KF（(mg/g)/（mg/L）1/n） | 1/n | R2 |
| ZFA | N | 21.32 | 0.118 | 0.809 | 4.302 | 0.328 | 0.649 |
| LZFA | N | 17.26 | 0.204 | 0.957 | 4.100 | 0.302 | 0.797 |
|  | P | 21.48 | 0.280 | 0.801 | 5.732 | 0.277 | 0.549 |

Table S7 Relative content of surface elements before and after adsorption of N

and P by LZFA

| Atomic ratio （%） | O | N | P | Fe | Ca | La |
| --- | --- | --- | --- | --- | --- | --- |
| LZFA | 58.41 | 0.44 | 0.51 | 1.11 | 1.86 | 3.46 |
| LZFA+N+P | 57.45 | 1.29 | 3.28 | 0.94 | 0.91 | 1.75 |

Table S8 The fitting parameters of O1s split peaks for the X-ray photoelectron spectra before and after adsorption of N and P by LZFA

| Sample | Peak | Position（eV） | Area | FWHM | Percent（%） |
| --- | --- | --- | --- | --- | --- |
| LZFA | M-OH | 533.36 | 424596.50 | 2.57 | 93.88 |
|  | M-O | 528.60 | 13882.62 | 2.57 | 3.07 |
|  | H2O | 535.16 | 13821.12 | 2.57 | 3.06 |
| LZFA+N+P | M-OH | 532.07 | 372813.05 | 2.62 | 80.48 |
|  | M-O | 530.18 | 82080.16 | 2.62 | 17.71 |
|  | H2O | 535.85 | 8331.26 | 2.62 | 1.798 |

Fig. S1 Effect of different LaCl3 concentrations(a), pH (b) and roasting temperatures (c) on phosphorus removal

Fig. S2 Scanning  electron  microscopy–energy dispersive X-ray spectroscopy (SEM–EDS) of LZFA after adsorption phosphate of 500 mg/L: (a) SEM image; (b) EDS stratified diagram; (c)–(f) Fe, Ca, P and La elemental distributions, respectively.