Extended Data. Fig. 1 | Stability of unit cell width polar domains in brownmillerite SrFeO2.5 and CaFeO2.5. a-b, Variation of unit cell width polarization in brownmillerite SrFeO2.5 with the 0° domain (a) and with the 180° domain (b). Octahedral layers have no polarizations. c, Small energy difference between domain configurations of (a) and (b) indicated as domain wall (DW)-a and DW-b, respectively. d-e, Polarization variation in CaFeO2.5 with the 0° domain (d) and with the 180° domain (e). Octahedral layers have no polarizations. f, Small energy difference between domain configurations of (d) and (e) indicated as DW-d and DW-e, respectively. Negative energy means that CaFeO2.5 favors the antiferroelectric state.

Extended Data. Fig. 2 | Space groups in SrFeO2.5 and CaFeO2.5. a, Calculated relative energy of SrFeO2.5 (blue bar) and CaFeO2.5 (purple bar) from reference 23, 26, and 27. Each atomic structure along the zone axis of [101]O is illustrated on the graph. Yellow boxed region means negligible energy difference between structures. A-site ion (Sr, Ca), Fe and O elements are represented by white, dark gray, and yellow dots, respectively. A-site buckling is indicated by θ in Pnma. In terms of the space group, three major structures, I2bm, Pnma, and Pbcm, are expected for AFeO2.5 (A = Sr, Ca). Among them, I2bm is the only polar space group with a broken inversion symmetry, where the polarization in the FeO4 tetrahedral layer is aligned towards the same direction (top of (a)). In contrast, Pnma accompanies A-site buckling (θ), resulting in antipolarized FeO4 tetrahedral layers, and the overall structure is centrosymmetric (middle of (a)). Pbcm is also centrosymmetric; however, in contrast to Pnma, up- and down-polarized FeO4 tetrahedra appear alternately through an intralayer; therefore, the projected FeO4 tetrahedra along [101]O becomes nondisplacive (bottom of (a)). b, Energy barrier between polar I2bm and anti-polar Pnma phases. Brownmillerite AFeO2.5 (A = Sr (blue), Ca (purple)) have stable polar and anti-polar structure. Energy barriers between polar I2bm and anti-polar Pnma are 1.22 eV for SrFeO2.5 and 2.25 eV for CaFeO2.5.

Extended Data. Fig. 3 | Low magnification BF-STEM images of SrFeO2.5 and CaFeO2.5 films. a, SrFeO2.5 films are grown on the Nb-doped SrTiO3 substrate. Pt and Nb-doped SrTiO3 serve as electrodes for electrical poling. b, CaFeO2.5 films are grown on the LaAlO3 substrate and (Pr,Ca)MnO3 electrode layer. Also, Pt on the top serve as an electrode. Both films are well grown without prominent defects.

Extended Data. Fig. 4 | Atomic scale structural analysis of the SrFeO2.5 and CaFeO2.5. a-b, Experimental ABF-STEM and simulation images along the zone axis of [101]O for I2bm SrFeO2.5 (a) and Pnma CaFeO2.5 films (b) with overlaid corresponding atomic structures. c-d, A-site buckling angles obtained by atomic peak position analysis in the same regions as in (a) and (b), respectively. A-site buckling angle is negligible (~ 180°) in I2bm SrFeO2.5 structure and regularly up (~ 176°) and down (~ 184°) moves in Pnma CaFeO2.5 structure. e-f, Lattice ratio obtained by atomic peak position analysis in the same regions as in (a) and (b), respectively. Ratios are calculated by height over distance between neighbor A-site atoms.

Extended Data. Fig. 5 | Displacement mapping of the SrFeO2.5 and CaFeO2.5. a-b, HAADF-STEM image and Fe displacement map along the zone axis of [101]O for pristine SrFeO2.5 (a) and poled SrFeO2.5 (b). c-d, HAADF-STEM image and Fe displacement map of pristine CaFeO2.5 (c) and poled CaFeO2.5 (d). In displacement maps, arrows indicate the direction of displacement, and the amount of displacement is illustrated by the size and color of arrows. Magnitude of polarization is also expressed as a color map.

Extended Data. Fig. 6 | Electrical biasing induced phase contrast change in a brownmillerite film. a, Electron diffraction pattern of a brownmillerite structure and green arrow indicates g110 reciprocal lattice vector. b-c, In-situ two-beam BF-TEM images with g110 and atomic structures before electrical biasing (b) and after electrical biasing (c) on films with tungsten tip. Pt electrode, top layer is positively biased. Electric field induced ferroelectric switching is shown by the diffraction contrast change inside the film, although the contrast change is not clear compared to Pb(Zr,Ti)O3 because the intensity of the relevant reflection is not significantly changed.

Extended Data. Fig. 7 | Atomic structural difference between pristine and poled CaFeO2.5. a-b, Experimental HAADF-STEM and simulation images along the zone axis of [101]O for pristine CaFeO2.5 (a) and poled CaFeO2.5 (b). Yellow line indicates significant difference of A-site buckling angle. c-d, A-site buckling angles obtained by atomic peak position analysis in the same regions as in (a) and (b), respectively. Pristine CaFeO2.5 shows alternative up (~ 176°) and down (~ 184°) A-site buckling by 2 layers indicating Pnma structure, while poled sample shows random and almost 180° angle of A-site buckling indicating I2bm structure. e-f, Lattice ratio obtained by atomic peak position analysis in the same regions as in (a) and (b), respectively. Although CaFeO2.5 structure changed from Pnma to I2bm, lattice ratio is preserved regularly.

Extended Data. Fig. 8 | Phonon decoupling in anti-polar CaFeO2.5. a, Phonon dispersion of CaFeO2.5. Phonon dispersion curve along the Γ-Y direction is indicated in the red line. b, Projected phonon DOS of oxygen in FeO6 octahedral and FeO4 tetrahedral sites on the Γ-Y path. Oxygen-octahedral (gray) and oxygen-tetrahedral phonons (green) are a little decoupled except around 550 cm-1, reflecting weak interaction between them. Oxygen-tetrahedral phonon is strongly localized from 350 cm-1 to 410 cm-1, resulting in the formation of flat phonon band. c, The schematic illustration of a Γ point phonon mode near 370 cm-1 (indicated in black dot in (a)) along the [101] projection view. d, The [010] projection view for the region indicated in dashed-rectangle in (c). The arrows represent the real displacement vectors of the atoms, with a magnified amplitude. The purple and pink arrows indicate the displacement vectors for the distinguishing intralayer FeO4 tetrahedra. The bold black arrows represent the direction of the polarization.

Extended Data. Fig. 9 | Phonon decoupling in polar HfO2. a, Phonon dispersion of HfO2. Phonon dispersion curve along the Γ-Y direction is indicated in the red line. b, Projected phonon DOS of oxygen in spacer and ferroelectric (FE) layers on the Γ-Y path. Spacer (gray) and ferroelectric layer phonons (green) are a little decoupled around 130 cm-1, reflecting weak interaction between them. c-d, The schematic illustration of a Γ point phonon mode near 130 cm-1 (indicated in black dot in (a)) along the [100] projection view (c) and the [001] projection view (d). The arrows represent the real displacement vectors of the atoms, with a magnified amplitude. The red arrows indicate the displacement vectors.

Extended Data. Fig. 10 | Microscopic characterization of switchable and stable polarization in AFeO2.5 (A = Sr, Ca) films. a-b, Electric field induced stable piezoelectric phase (a) and amplitude (b) in SrFeO2.5 films which show ferroelectric domains with sharp domain boundaries. c-d, Electric field induced stable piezoelectric phase (c) and amplitude (d) in CaFeO2.5 films which show ferroelectric domains with sharp domain boundaries.