Supplementary Information

Vertically asymmetric channels of graphene oxide membrane for ultrafast ion sieving

Changdao Han1, Wenhui Zhao2, Junfan Liu3, Jian Lan3, Shouyuan Hu2, Huan Yang2, Feng Zhou3,4, Yan Fan1, Xiangmei Duan2, Pei Li2,*, and Liang Chen2,*

1Department of Optical Engineering, Zhejiang Prov Key Lab Carbon Cycling Forest Ecosy, College of Environmental and Resource Sciences, Zhejiang A&F University, Hangzhou 311300, China.

2School of Physical Science and Technology, Ningbo University, Ningbo 315211, China.

3Zhejiang GuoFu Environmental Technology Co., Ltd, Hangzhou 311300, China.

4Radiation Monitoring Technical Center of Ministry of Ecology and Environment, State Environmental Protection Key Laboratory of Radiation monitoring, Key Laboratory of Radiation Monitoring of Zhejiang Province, Hangzhou 310012, China.

*Corresponding author. E-mail: liangchen@zafu.edu.cn (L. C.); lipei@nbu.edu.cn (P. L.)

Section 1: Materials and methods

Materials

Natural graphite powder, 2,3-Diaminophenazine, KMnO4, H2SO4, HCl, K2S2O8, P2O5, H2O2, Deionized (DI) water (18.2 MΩ), MCE (diameter 50mm, pore size of 0.2 μm). All the reagents were utilized as received without further purification.

Preparation of AD-rGO Suspension

GO was prepared using the modified Hummers method1, as described in our previous works2,3. First, 3 g of natural graphite powder, 2.5 g of P2O5, and 2.5 g of K2S2O8 were gradually added to 12 mL of H2SO4, then continuously sonicated and stirred for several hours. The pre-oxidation product obtained after filtration and vacuum drying was stirred with 120 mL of H2SO4 at 5°C, and then 15 g of KMnO4 was added to the mixture at 60°C for gradual oxidation. Subsequently, the product was further oxidized at 80°C by diluting with DI water and using 20 mL of H2O2. Finally, the oxidation product was diluted and washed with DI water and HCl, respectively, to obtain a 4.1 mg mL-1 GO suspension.

Next, 25.6 mL of GO suspension and 3.5 mg of 2,3-Diaminophenazine were added to DI water, with sufficient sonication and stirring applied to each, respectively. Then, the two solutions were mixed, followed by sonication and stirring. A total of 360 mL of 28% ammonia was added to the mixed system at 80°C and stirred continuously for 6 hours, followed by additional stirring at 90°C for 1 hour. Finally, an approximately 0.15 mg mL-1 AD-rGO suspension was obtained for further use.

Filtration performances experiments

AD-rGO membranes were obtained by passing 8 mL of 0.15 mg mL-1 AD-rGO suspension, which had been diluted with 32 mL of DI water, through the vacuum filtration device onto the MCE substrate. Then, 150 ml of 50 mg L-1 Pb(NO3)2, CuSO4, ZnSO4, CrCl3, and FeCl3 solutions were separately added to the feed side of the vacuum filtration device, then performed under a pressure of 1 bar. To ensure the reliability of the experiment, the experiment was repeated three times for each.

The ion rejection rates (R, %) and water permeance (JW, L m−2 h−1 bar−1) were calculated by the Eqs. (1) and (2), respectively:

R=1 - CpCf×100%     (1)

Jw=V∆t × A × P            (2)

Where Cp and Cf are the heavy metal ion solution concentrations in filtrates and feed side, respectively, which were measured by inductive coupled plasma-optical emission spectrometry(ICP-OES, iCAP 7400, Thermo Fisher Scientific, Dreieich, Germany). V is the volume of the filtrates(L), ∆t is the permeation time (h) of filtrates, A is the effective membrane area(A = 11.34 cm2), P is the pressure (bar) which keeps in 1 bar during filtration. The mean and standard deviation were calculated for the experimental data results.

Section 2: Characterization methods

The membrane surface morphology and cross-section were analyzed by scanning electron microscope (SEM, Hitachi, S-4800) at an operating voltage of 5 kV. The chemical components of the AD-rGO membrane were analyzed by X-ray photoelectron spectroscopy (XPS, Thermo fisher Nexsa, USA). The size of AD-rGO flakes were measured by nanoparticle size analyzer (Benano 180 Zeta Pro, China).

Section 3: Membranes stability test

To evaluate the long-term filtration performance of the AD-rGO membrane during continuous operation, multiple repeated cycles were performed to test the ion rejection and water permeance of 50 mg L-1 CuSO4 solution. Specifically, 150 mL of 50 mg L-1 CuSO4 solution was added to the feed side, and the salt solution was filtered through the AD-rGO membranes under a pressure of 1 bar. The filtrate was collected and recycled into the feed side to maintain the volume and concentration of salt solution in the feed side. Every 35 mL was cycled, the concentration of the filtrate was measured, with a total of 16 cycles performed.

In addition, the mechanical stability of AD-rGO membrane was also tested by ultrasonic treatment at 40 KHz for 100 minutes in aqueous solutions.

Table S1. Comparison of different nanofiltration membranes in water permeance and retention rates for multivalent ions in literatures.

| Membrane type | Membrane name | Method or technology | Salts or ions | Permeance (Lm-2h-1bar-1) | Rejection (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| NF Membranes | γ-Al2O3/α-Al2O3 hollow fiber | dip-coating and sintering | FeCl3 | 17.4 | 97.1 | Ref.4 |
|  | PAMAM grafted TFC | grafting | Pb2+/Cu2+/Zn2+ | 3.6 | 99 | Ref.5 |
|  | PPSU/carboxylated-GO | phase inversion | Pb(NO3)2 | 2.6 | 81 | Ref.6 |
|  | PEI/POSS-GO | phase inversion | Cu2+ | 7.2 | 55 | Ref.7 |
|  | CS-P/T-PEI | CIL-IP-P | Cu2+/Pb2+ | 10.9 | 91/90.4 | Ref.8 |
| 2D materials | MoS2/PEI | incorporate | Zn2+/Cu2+ | 2.8/2.5 | 94.8/90 | Ref.9 |
|  | SC-MXene | Stacking and surface-coating | MgCl2 | 9 | 82 | Ref.10 |
|  | PEI-TMC-QTHIM | synthesized and modified | MgCl2 | 33 | 92 | Ref.11 |
| GO-based Membranes | rGO-K+ | crosslinked reduced | FeCl3 | 86.1 | 99.8 | Ref.12 |
|  | GO-UR/CA | cross-linking | CuSO4 | 20 | 81.9 | Ref.13 |
|  | GO-Fe3+ | without drying | Fe3+/Cu2+ | 75.2/56.6 | 99.9/97.8 | Ref.2 |
|  | GO-IPDI | cross-linking | Cu2+ | 46.2 | 89.4 | Ref.14 |
|  | hrGO-Trp | cross-linking | FeCl3 | 191 | 98.2 | Ref.15 |
|  | AD-rGO | reduction | Pb(NO3)2 | 2603 | 99.9 | This work |
|  |  |  | ZnSO4 | 1564 | 99.9 |  |
|  |  |  | CuSO4 | 1530 | 99.9 |  |
|  |  |  | CrCl3 | 1314 | 99.9 |  |
|  |  |  | FeCl3 | 1107 | 99.9 |  |

Table S2. Normalized areas of characteristic peaks in the C1s XPS spectra of GO and AD-rGO membranes.

| Sample | Peak percentage (%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | C=C/C-C | C-O-C/C-OH | C=O | -COOH | C-N |
| GO | 51.94 | 38.67 | 6.69 | 2.70 | / |
| AD-rGO | 64.75 | 23.82 | 6.39 | 1.04 | 4.00 |

References

1.	Hummers, W. S. et al.  Preparation of Graphitic Oxide. J. Am. Chem. Soc. 80, 1339–1339 (1958).

2.	Dai, F. et al. Ultrahigh water permeation with a high multivalent metal ion rejection rate through graphene oxide membranes. J. Mater. Chem. A 9, 10672–10677 (2021).

3.	Wang, S. et al.  Realizing ultrahigh nanofiltration performance based on small flake reduced graphene oxide membranes. Desalination 528, 115601 (2022).

4.	Wang, Z. et al. Preparation, characterization and solvent resistance of γ-Al2O3/α-Al2O3 inorganic hollow fiber nanofiltration membrane. J. Membr. Sci. 503, 69–80 (2016).

5.	Zhu, W.-P. et al.  Poly(amidoamine) dendrimer (PAMAM) grafted on thin film composite (TFC) nanofiltration (NF) hollow fiber membranes for heavy metal removal. J. Membr. Sci. 487, 117–126 (2015).

6.	Shukla, A. K. et al. Removal of heavy metal ions using a carboxylated graphene oxide-incorporated polyphenylsulfone nanofiltration membrane. Environ. Sci. Water Res. Technol. 4, 438–448 (2018).

7.	Bandehali, S. et al. New mixed matrix PEI nanofiltration membrane decorated by glycidyl-POSS functionalized graphene oxide nanoplates with enhanced separation and antifouling behaviour: Heavy metal ions removal. Sep. Purif. Technol. 242, 116745 (2020).

8.	Cheng, X. et al. Highly permeable positively charged nanofiltration membranes with multilayer structures for multiple heavy metal removals. Desalination 548, 116266 (2023).

9.	Zhang, H. et al. Construction of MoS2 composite membranes on ceramic hollow fibers for efficient water desalination. J. Membr. Sci. 592, 117369 (2019).

10.	Meng, B. et al. Fabrication of surface-charged MXene membrane and its application for water desalination. J. Membr. Sci. 623, 119076 (2021).

11.	Liu, X. et al. High-permeance Mg2+/Li+ separation nanofiltration membranes intensified by quadruple imidazolium salts. J. Membr. Sci. 667, 121178 (2023).

12.	Yang, R. et al. Robust reduced graphene oxide membranes with high water permeance enhanced by K+ modification. J. Membr. Sci. 635, 119437 (2021).

13.	Zhang, Y. et al.  Graphene oxide composite membranes cross-linked with urea for enhanced desalting properties. J. Membr. Sci. 563, 718–725 (2018).

14.	Zhang, P. et al. Cross-linking to prepare composite graphene oxide-framework membranes with high-flux for dyes and heavy metal ions removal. Chem. Eng. J. 322, 657–666 (2017).

15.	Liu, J. et al. Bio-inspired graphene oxide-amino acid cross-linked framework membrane trigger high water permeance and high metal ions rejection. J. Membr. Sci. 659, 120745 (2022).