Appendix

The nonlinear behavior of elastic materials is usually modelled with hyperelastic models. These models rely on the definition of a strain energy function, in different ways according to the material and its behavior. This function is obtained from symmetry, thermodynamics and energy considerations. In the Lagrangian framework, the strain is expressed in the form of the right Cauchy-Green strain tensor C=FTF, where F=∂xi∂Xj is deformation gradient. For an isotropic material, the strain energy function U is defined as a function of the invariants of the right Cauchy-Green strain tensor I1, I2, I3:

U=UI1, I2, I3          (A1)

I1=λ12+λ22+λ32             (A2)

I2=λ12λ22+λ22λ32+λ32λ12            (A3)

I3=λ12λ22λ32=J2               (A4)

J=detF

where  λi2 are the squares of stretches in the principle directions and the eigenvalues of right Cauchy-Green strain tensor C. To consider the incompressibility, the determinant of deformation gradient (J) is set to I3=J2=1. If the incompressible hyperelastic material is subjected to uniaxial tension x1, we can write: λ1=λ , λ2=λ3=1/λ using the relation λ12λ22λ32=1, and the deformation gradient can be expressed as:

F=λ0001λ0001λ     ,    F-1=1/λ000λ000λ          (A6)

I1=λ2+2λ  , I2=2λ+1λ2  , I3=1    (A7)

The principal Cauchy stresses of an isotropic hyperelastic material can be expressed as σi=J-1λi∂U∂λi. For uniaxial tension x1, using the incompressibility assumption, this reduces to:

σ1=2λ2-1λ∂U∂I1+1λ∂U∂I2                (A8)

The first order Ogden strain energy of a fully incompressible hyperelastic isotropic material is expressed as:

U=2μα2λ1α+λ2α+λ3α-3-pJ-1    A9

The coefficients in this strain energy functions are obtained using the experimental data such as uniaxial tensile test. This strain energy function in the uniaxial stress state and for a fully incompressible material simplifies to:

U=2μα2λα+2λ-α/2-3              (A10)

The Cauchy stress in uniaxial test using Ogden model and with the help (A8) is equal to:

σ1=2λ2-1λ∂U∂I1+1λ∂U∂I2=λ∂U∂λ     (A11)

Replacing equation (A10) in (A11) gives:

σ1=λ∂U∂λ=2μαλα-λ-(α2)                         A12

Using the relationship between engineering stress (second Piola-Krichhoff stress tensor) and Cauchy stress: σENG=N=JF-1σi , we can write:

σENG=σ1λ=2μαλα-1-λ-(α2+1)         (A13)

Taking the derivative of (A13), the tangent elastic modulus is obtained as:

Eλ=dσENGdλ=2μα(α-1)λα-2+α2+1λ-(α2+2)     (A14)

Therefore, the initial tangent modulus (λ = 1) is:

E0=2μα(α-1+α2+1 = 3μ       A15

For a fully incompressible linear isotropic material, the Poisson ratio (ν) is equal to 0.5 and using the relation μ=E0/2(1+ν) shows that μ is the the initial shear modulus of a fully incompressible material.