Supporting Information

Unveiling Intrinsic Charge Transfer Dynamics in "Bone-joint" S-Scheme Heterostructures for Promoting Photocatalytic Hydrogen Peroxide Generation

Yuhui Liu1, Xiaoxu Deng2, Meiyang Song1, Henghui Song1, Yi Wang1, Peng Chen1, *, Shuang-Feng Yin3, *

1Provincial Guizhou Key Laboratory of Green Chemical and Clean Energy Technology, School of Chemistry and Chemical Engineering, Guizhou University, Guiyang 550025, Guizhou, China.

2School of Electronics and Information Engineering, Guiyang University, Guiyang, Guizhou 550025, China.

3College of Chemistry and Chemical Engineering, Advanced Catalytic Engineering Research Center of the Ministry of Education, State Key Laboratory of Chemo/Biosensing and Chemometrics, Hunan University, Changsha 410082, PR China; College of Science, Central South University of Forestry and Technology, Changsha 410004, P.R. China.

# These authors contributed equally to this work

* Correspondence: pchen3@gzu.edu.cn; sf_yin@hnu.edu.cn

Supplementary Table 1 AQY of photocatalytic production of H2O2.

| Wavelength (nm) | 405 | 420 | 450 | 500 | 520 | 550 | 575 | 600 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H2O2 yield rate (10−9 mol s−1) | 30.57 | 25.81 | 31.16 | 22.84 | 17.50 | 10.96 | 5.02 | 2.05 |
| Light intensity (W m−2) | 144.93 | 112.80 | 222.54 | 382.91 | 301.86 | 368.93 | 503.70 | 289.93 |
| Irradiation area (10−4 m2) | 18.47 | 18.47 | 18.47 | 18.47 | 18.47 | 18.47 | 18.47 | 18.47 |
| AQY (%) | 6.77 | 7.08 | 4.04 | 1.55 | 1.45 | 0.70 | 0.23 | 0.15 |

Supplementary Table 2. Zn and In contents of prepared samples based on ICP-MS Results.

| Catalyst | Zn / ωt% | In / ωt% | Mole ratio of Zn:In | Ideal mole ratio of Zn:In |
| --- | --- | --- | --- | --- |
| ZnIn2S4 | 10.21 | 34.68 | 0.52 | 0.50 |
| ZIS-1 | 12.88 | 30.68 | 0.74 | 0.75 |
| ZIS-2 | 13.78 | 29.32 | 0.82 | 0.83 |
| ZIS-3 | 14.04 | 28.95 | 0.85 | 0.88 |
| ZIS-4 | 14.57 | 28.15 | 0.91 | 0.90 |
| ZIS-5 | 14.67 | 27.99 | 0.92 | 0.92 |
| Zn2In2S5 | 15.5 | 26.75 | 1.02 | 1.00 |

Supplementary Table 3. Element molar ratio of the prepared samples calculated by XPS.

| Catalyst | S / % | In / % | Zn / % |
| --- | --- | --- | --- |
| ZnIn2S4 | 34.49 | 17.94 | 8.75 |
| Zn2In2S5 | 32.78 | 15.74 | 14.62 |
| ZIS-2 | 26.84 | 17.66 | 12.25 |
| ZIS-R | 28.76 | 17.98 | 10.23 |

Supplementary Table 4. Comparison of different catalysts for photocatalytic produce H2O2.

| Entry | Catalyst | Reaction condition | H2O2 production (μmol·gcat−1·h−1) | Reference |
| --- | --- | --- | --- | --- |
| 1 | MIL-125-NH2 | O2/water | 1111 | 1 |
| 2 | MIL-125-PDI | O2/water | 4800 | 1 |
| 3 | RF523@333 K | O2/water | ~80 | 2 |
| 4 | Cd0.5Zn0.5S | air/water | 152 | 3 |
| 5 | PEI/C3N4 | O2/water | 208 | 4 |
| 6 | α-Fe2O3/CQD@g-C3N4 | O2/water | 139 | 5 |
| 7 | CTF-BDDBN | O2/water | 887 | 6 |
| 8 | MIL-111/001 | O2/water | 917 | 7 |
| 9 | TiO2/PEI/AgNP | air/water | 1605 | 8 |
| 10 | NMT400 | O2/water | 271 | 9 |
| 11 | ORP/GCN | O2/water | 4167 | 10 |
| 12 | CDA300 | air/water | 557 | 11 |
| 13 | Bpy-TAPT | O2/water | 4038 | 12 |
| 14 | Bpt-CTF | O2/water | 3268 | 13 |
| 15 | HTCC | O2/water | 1160 | 14 |
| 16 | Furan-BILP | O2/water | 2200 | 15 |
| 17 | CdS NRs | O2/water | 5132 | 16 |
| 18 | C3N5−x-CN | O2/water | 1359 | 17 |
| 19 | Nv–CN–CN | O2/water | 137 | 18 |
| 20 | This work | O2/water | 5939 | - |

Supplementary Fig. 1. SEM images of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS-2.

Supplementary Fig. 2. AFM height images and corresponding height profiles of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, (d) ZIS-2.

Supplementary Fig. 3. The N2 adsorption-desorption isotherms of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2.

Supplementary Fig. 4. The molecular models of (a) ZnIn2S4, (b) ZnIn2S4-(006), (c) Zn2In2S5, (d) Zn2In2S5-(006), (e) ZIS-R, and (f) ZIS.

Supplementary Fig. 5. Another schematic model based on the observed HR-TEM image. The filled-blue and filled-red circles are the atoms of Zn2In2S5 and ZnIn2S4, respectively.

According to the HRTEM image, the angle between the normal vectors of the Zn2In2S5 (006) plane and the ZnIn2S4 (006) plane is about 13°. Therefore, we construct cubic lattices and rotate them by α angle. We then observe that the atoms in these lattices can be matched if α = 13°, which is consistent with our observation. Our model suggests that there is still a small mismatch between the two lattices due to interatomic distances and different crystal symmetries. The mismatches are along the (006) planes of Zn2In2S5 and ZnIn2S4, respectively: (I) Two and six cations of Zn2In2S5 and ZnIn2S4 can be matched that shows by (i.e. 1R1 || 5d006(4) blocks), and (II) The five and two cations of Zn2In2S5 and ZnIn2S4 can be matched that shows by (i.e. 4d006(5) || 1R2 blocks), where and are the dimensionless mismatches, and block means the interatomic distance. Here,

δ1 = 1 - 1R15d006(4) and δ2 =1 - 4d006(5)1R2,

where and are the interatomic distance of the cations in the corresponding planes, respectively.

R1=(4d006(5))2 + (1d006(5))2 and R2=(5d006(4))2 + (1d006(4))2.

Our calculations display that δ1 = 0.16 and δ2 = 0.20.

Supplementary Fig. 6. HAADF-STEM at the phase interface in ZIS-2.

Supplementary Fig. 7. EPR spectra of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2.

Supplementary Fig. 8. XRD patterns of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS.

As shown in Supplementary Fig. 8, the crystallographic structures of the as-obtained samples were analyzed by X-ray diﬀraction. The XRD patterns of ZnIn2S4, Zn2In2S5 and ZIS composites present similar profiles, which are ascribed to the analogous repeating structural unit.19 As seen, pure ZnIn2S4 exhibits diffraction peaks at 2θ = 21.1o, 27.7o, 47.5o, and 52.4o, which are indexed to (006), (102), (110), and (116) structural planes of the hexagonal ZnIn2S4 respectively (JCPDS No.65-2023).20 In addition, pure Zn2In2S5 presents diffraction peaks at 2θ = 21.3 o, 27.9 o, 47.5 o, and 51.7 o, which belong to the (006), (102), (112), and (0012) structural planes of the hexagonal Zn2In2S5 respectively. (PDF No.65-6907).21

Supplementary Fig. 9. Zn and In contents of prepared samples based on ICP-MS Results.

Supplementary Fig. 10. The Raman spectrum of ZnIn2S4, Zn2In2S5, ZIS-R and ZIS-2.

The Raman peaks at roughly 128, 247, 302, and 355 cm−1 for the single ZIS can be distinguished clearly, which is consistent with the featured layer structure, LO1, TO2, and LO2 modes of ZIS, and are associated to V(S-In-S)s (surface), V(S-In-S)i (interior), and V(S-Zn-S)s (surface), respectively.22 Moreover, the Raman peaks of ZIS shift to a lower wavenumber, which is assigned to the interaction between the "bone joints" of the semicoherent interface.

Supplementary Fig. 11. High-resolution XPS spectra of (a) S 2p, (b) In 3d, (c) Zn 2p for ZnIn2S4, Zn2In2S5, ZIS-R and ZIS-2.

The Zn 2p, In 3d, and S 2p doublets have been investigated as well in ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2 (Supplementary Fig. 11), which demonstrates the existence of Zn2+, In3+, and S2− in both samples.23,24 The binding energies of S 2p3/2 and S 2p1/2 of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2 (Supplementary Fig. 11a) are 162.1 and 163.3 eV, 161.7 and 162.8 eV, 161.8 and 162.9 eV, 161.9 and 163.1 eV, respectively. Simultaneously, the binding energies for In 3d5/2 and In 3d3/2 of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2 (Supplementary Fig. 11b) are 445.3 and 452.9 eV, 445.0 and 452.6 eV, 445.1 and 452.7 eV, 445.2 and 452.8 eV, respectively. The Zn 2p3/2 and Zn 2p1/2 spectrum of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2 sample displays two peaks with binding energies of 1022.3 and 1045.4 eV, 1022.0 and 1045.0 eV, 1022.1 and 1045.1 eV, 1022.2 and 1045.2 eV, respectively (Supplementary Fig. 11c). It also demonstrates the feasibility of S-scheme heterojunctions.25

Supplementary Fig. 12. (a) UV-vis diffuse reflectance spectra, and (b) calculated band structure of as prepared samples.

Supplementary Fig. 13. Mott-Schottky plots of fabricated samples: (a) ZnIn2S4 and (b) Zn2In2S5.

Supplementary Fig. 14. Energy band structure of ZnIn2S4 and Zn2In2S5.

Supplementary Fig. 15. Density of states (DOS) of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS.

Supplementary Fig. 16. The PDOS of S, In, and Zn element of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS.

Supplementary Fig. 17. The charge effective mass in the ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS.

Carrier effective mass deduced from energy band E-k curves energy band E-k curve. The value of the effective mass depends on the second derivative or curvature near the bottom and top of the energy band. For the conduction band, electrons are generally located near the bottom of the conduction band, while for the valence band, holes are generally located near the top of the valence band. Therefore, we only need to calculate the curvature of the bottom of the conduction band and the top of the valence band to obtain the curvature of the electrons and holes. Mathematically, the data from the E-k curve can be fitted with a quadratic curve E(k) = E0 + d1k + d2k2.26 Using the fitted the formula obtained from the fit it is straightforward to obtain the second order differential, i.e. ∂2E/∂k2 = 2d2.

The effective mass is then: m* = h22d2a2

Among them, the energy E unit for the electron volt (eV = 1.602 × 10-19 J), the lattice constant a unit for the Egyptian (10-10 m), Planck's constant is 6.626 × 10-34 J·s, the static mass of the electron is 9.108 × 10-31 kg. Considering that the effective mass is generally expressed in terms of the rest mass of the electron, then the above equation can be transformed into:

m*m0 = 3.01×1022d2a2

Supplementary Fig. 18. The surface potential was detected with KPFM of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS-2.

Supplementary Fig. 19. The zeta potential of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS.

Supplementary Fig. 20. The relative built-in electric field of as prepared samples.

Supplementary Fig. 21. Differential charge density of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS.

Supplementary Fig. 22. The charge at the active site on the surface of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS.

Supplementary Fig. 23. Photogenerated carrier dynamics examined by fs-TA spectroscopy. Pseudocolor TA spectra of ZIS-R (a) and ZIS-2 (d) in the initial time window of 100 ps. The representative TA spectra at several probe delays for ZIS-R (b) and ZIS-2 (e). The typical TA kinetics probed at 700 nm for ZIS-R (c) and ZIS-2 (f).

During the TA conduction, a femtosecond UV pump/white-light continuous probe was used, in which a pump laser with a center wavelength of 400 nm was used to stimulate electron exciton from the valence band to the conduction band. Because the WLC probes at 550–750 nm could almost always acquire the same TA kinetics for each sample, the data was obtained at 700 nm. The delay process of the electrons in pure ZIS-R can be fitted by a two-exponential function, and the time constants are τ1 = 56.10 ps and τ2 = 575.26 ps (Supplementary Fig. 23c), where the τ1 reflects the stage where the electron goes from the conduction band to the trap state, and the τ2 is the migration to the valence band.27 While ZIS-2 values are τ1 = 9.51 ps, τ2 = 10.14 ps, and τ3 = 550.72 ps (Supplementary Fig. 23f), which are assigned to the stage where the electron goes from the conduction band to the trap state, the charge recombination on the semicoherent interface, and the migration to the valence band.27 The results demonstrate that the intermediate transition state provides a composite platform for electron holes.

Supplementary Fig. 24. HRTEM images of the ZIS-2 composite after Pt and Mn3O4 nanoparticles photodeposition experiments.

To further investigate the electron migration path, a metal nanoparticle photodeposition experiment was carried out. 28 In the procedure, Pt4+ in aqueous hexachloroplatinic acid (H2PtCl6) was converted to Pt0 through the use of light irradiation, and Pt0 was subsequently deposited as nanoparticles on the surface of the composite. In addition, Mn2+ is oxidized from MnCl2 to Mn3O4. The HR-TEM image of the composite after Pt and Mn3O4 photodeposition experiment (Supplementary Fig. S24) show different lattice spacings of around 0.20, 0.27, 0.41 and 0.42 nm, which match the lattice fringes of Pt (200), Mn3O4 (103), ZnIn2S4 (006) and Zn2In2S5 (006), respectively. 21,29,30,31 Pt nanoparticles are deposited on the edge of Zn2In2S5 lattice and Mn3O4 nanoparticles are deposited on the edge of ZnIn2S4 lattice, indicating that the reduction reaction occurs on the Zn2In2S5 conduction band where electrons are aggregated and the oxidation reaction occurs on the ZnIn2S4 valence band where holes are aggregated. Confirming that the transition layer (006) acts as the charge recombination sites.

Supplementary Fig. 25. (a) PL spectroscopy and (b) transient fluorescence of as prepared samples.

The I(t) and τave can be calculated by the following equation:

I(t) = A1exp(−t/τ1) + A2exp(−t/τ2)

τave = (A1τ12 + A2τ22)/(A1τ1 + A2τ2)

Supplementary Fig. 26. Temperature-dependent PL spectra of (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS-2.

Supplementary Fig. 27. (a) i-t curves (b) and electrochemical impedance spectroscopy of the photocatalyst.

Supplementary Fig. 28. The XRD (a) and XPS (b) spectra of ZIS-2 before or after the recycling test.

Supplementary Fig. 29. Contact-angle of water on the surface of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2.

Supplementary Fig. 30. Contact-angle of H2O2 on the surface of ZnIn2S4, Zn2In2S5, ZIS-R, and ZIS-2.

Supplementary Fig. 31. O2-temperature programmed desorption spectra of fabricated samples.

Supplementary Fig. 32. Photocatalytic produce H2O2 on ZIS-2 with or without scavengers (initial). ammonium oxalate (AO), tert-butyl alcohol (TBA), p-benzoquinone (PBQ), L-Tryptophan (LT) and Potassium persulfate (KSO), were used as trapping agents for holes (h+), hydroxyl radicals (·OH), superoxide radical (·O2−), Singlet oxygen (1O2) and electrons (e−), respectively.

During the experiment, the addition of tert-butanol had almost no effect on the yield of H2O2, ruling out the role of hydroxyl radicals; when ammonium oxalate, L-tryptophan, and p-benzoquinone were added, the yield decreased by nearly half, proving that electron hole, single-linear oxygen, and superoxide radicals are influential; The addition of potassium persulfate resulted in a very severe drop in yield, proving that electrons were the main player. The addition of p-benzoquinone and L-tryptophan at the same time gave another half of the yield, proving that O2 can be directly converted to H2O2. The possible reaction pathways are as follows:32

2H2O+4h+→O2+4H+ (+1.23 V vs. NHE)

O2+2H++2e-→H2O2 (+0.68 V vs. NHE) (major)

O2+e-→·O2- (-0.33 V vs. NHE)

·O2-+h+→ 1O2

·O2-+2H++e-→H2O2 (+1.44 V vs. NHE)

1O2+2H++e-→H2O2

Supplementary Fig. 33. Comparison of chemical bond lengths and charge density before and after O2 adsorption.

Supplementary Fig. 34 DFT structure of the two-step H2O2 formation process for (a) ZnIn2S4, (b) Zn2In2S5, (c) ZIS-R, and (d) ZIS.

Reference

1	Bai, P. et al. Junction of ZnmIn2S3+m and bismuth vanadate as Z-scheme photocatalyst for enhanced hydrogen evolution activity: The role of interfacial interactions. J. Colloid Interface Sci. 628, 488-499 (2022).

2	Chong, W.-K. et al. Non-metal doping induced dual p-n charge properties in a single ZnIn2S4 crystal structure provoking charge transfer behaviors and boosting photocatalytic hydrogen generation. Appl. Catal. B Environ. 325, 122372 (2023).

3	Du, C. et al. π-π conjugation driving degradation of aromatic compounds with in-situ hydrogen peroxide generation over Zn2In2S5 grown on nitrogen-doped carbon spheres. Appl. Catal. B Environ. 310, 121298 (2022).

4	Yang, W. et al. Minimized external electric field on asymmetric monolayer maximizes charge separation for photocatalysis. Appl. Catal. B Environ. 295, 120266 (2021).

5	Zhang, G. et al. Preparation of ZnIn2S4 nanosheet-coated CdS nanorod heterostructures for efficient photocatalytic reduction of Cr(VI). Appl. Catal. B Environ. 232, 164-174 (2018).

6	Cao, S. et al. H2-production and electron-transfer mechanism of a noble-metal-free WO3@ZnIn2S4 S-scheme heterojunction photocatalyst. J. Mater. Chem. A 10, 17174−17184 (2022).

7	Zhang, L. Y. et al. Emerging S-Scheme photocatalyst. Adv. Mater. 34, 2107668 (2022).

8	Supka, A. et al. Two-layer high-throughput: effective mass calculations including warping. Eng. 10, 74-80 (2022).

9	Jiao, X. et al. Defect-mediated electron–hole separation in one-unit-cell ZnIn2S4 layers for boosted solar-driven CO2 reduction. J. Am. Chem. Soc. 139, 7586-7594 (2017).

10	Sabbah, A. et al. Boosting photocatalytic CO2 reduction in a ZnS/ZnIn2S4 heterostructure through strain-induced direct Z-scheme and a mechanistic study of molecular CO2 interaction thereon. Nano Energy 93, 106809 (2022).

11	Hua, S. et al. Highly efficient p-type Cu3P/n-type g-C3N4 photocatalyst through Z-scheme charge transfer route. Appl. Catal. B Environ. 240, 253−261 (2019).

12	Li, N. et al. Efficient removal of chromium from water by Mn3O4@ZnO/Mn3O4 composite under simulated sunlight irradiation: Synergy of photocatalytic reduction and adsorption. Appl. Catal. B Environ. 214, 126−136 (2017).

13	Dang, X. et al. The in situ construction of ZnIn2S4/CdIn2S4 2D/3D nano hetero-structure for an enhanced visible-light-driven hydrogen production. J. Mater. Chem. A 9, 14888−14896 (2021).

14	Chen, X. et al. Visible-light-driven hydrogen peroxide production from water and dioxygen by perylenetetracarboxylic diimide modified titanium-based metal–organic frameworks. J. Mater. Chem. A 9, 26371−26380 (2021).

15	Shiraishi, Y. et al. Resorcinol-formaldehyde resins as metal-free semiconductor photocatalysts for solar-to-hydrogen peroxide energy conversion. Nat. Mater. 18, 985-993 (2019).

16	Lin, S. et al. Piezocatalytic and photocatalytic hydrogen peroxide evolution of sulfide solid solution nano-branches from pure water and air. Small 18, 2200914 (2022).

17	Zeng, X. et al. Simultaneously tuning charge separation and oxygen reduction pathway on graphitic carbon nitride by polyethylenimine for boosted photocatalytic hydrogen peroxide production. ACS Catal. 10, 3697−3706 (2020).

18	Chen, X. et al. Sacrificial agent-free photocatalytic H2O2 evolution via two-electron oxygen reduction using a ternary α-Fe2O3/CQD@g-C3N4 photocatalyst with broad-spectrum response. J. Mater. Chem. A 8, 18816−18825 (2020).

19	Chen, L. et al. Acetylene and Diacetylene Functionalized Covalent Triazine Frameworks as Metal-Free Photocatalysts for Hydrogen Peroxide Production: A New Two-Electron Water Oxidation Pathway. Adv. Mater. 32, 1904433 (2020).

20	Zheng, Y. et al. Photocatalytic production of H2O2 over facet-dependent Ti-MOF. Catal. Sci. Technol. 12, 969−975 (2022).

21	Li, X. et al. Boosting photocatalytic H2O2 production in pure water over a plasmonic photocatalyst with polyethylenimine modification. J. Mater. Chem. A 11, 1503−1510 (2023).

22	Yang, C. et al Calcination-regulated Microstructures of Donor-Acceptor Polymers towards Enhanced and Stable Photocatalytic H2O2 Production in Pure Water. Angew. Chem. Int. Ed. 61, e202208438 (2022).

23	Zhang, J. et al. Efficient photocatalytic H2O2 production from oxygen and pure water over graphitic carbon nitride decorated by oxidative red phosphorus. Appl. Catal. B Environ. 298, 120522 (2021).

24	Chu, C. et al. Photocatalytic H2O2 production driven by cyclodextrin-pyrimidine polymer in a wide pH range without electron donor or oxygen aeration. Appl. Catal. B Environ. 314, 121485 (2022).

25	Liu, Y. et al. Substoichiometric covalent organic frameworks with uncondensed aldehyde for highly efficient hydrogen peroxide photosynthesis in pure water. Appl. Catal. B Environ. 331, 122691 (2023).

26	Wu, C. B. et al. Polarization engineering of covalent triazine frameworks for highly efficient photosynthesis of hydrogen peroxide from molecular oxygen and water. Adv. Mater. 34, 2110266 (2022).

27	Xu, L. et al. Fabrication of a photocatalyst with biomass waste for H2O2 synthesis. ACS Catal. 11, 14480−14488 (2021).

28	Yang, T. et al. Covalent furan-benzimidazole-linked polymer hollow fiber membrane for clean and efficient photosynthesis of hydrogen peroxide. Adv. Funct. Mater. 33, 2300714 (2023).

29	Zhang, Y. et al. Water flow induced piezoelectric polarization and sulfur vacancy boosting photocatalytic hydrogen peroxide evolution of cadmium sulfide nanorods. Appl. Catal. B Environ. 331, 122714 (2023).

30	Fu, C. et al. Unraveling the dual defect effects in C3N5 for piezo-photocatalytic degradation and H2O2 generation. Appl. Catal. B Environ. 332, 122752 (2023).

31	Zhang, X. et al. Unraveling the dual defect sites in graphite carbon nitride for ultra-high photocatalytic H2O2 evolution. Energy Environ. Sci. 15, 830-842 (2022).

32	Yong, Z. et al. Solar-to-H2O2 catalyzed by covalent organic frameworks. Angew. Chem. Int. Ed., e202308980 (2023).