Supporting Information

Ultrastrong Light-Matter Coupling in

2D Metal-Organic Chalcogenolates

Surendra B. Anantharaman1,*,†, Jason Lynch1,†, Mariya Aleksich2,3, Christopher E. Stevens4,5, Christopher Munley6, Bongjun Choi1, Sridhar Shenoy1, Thomas Darlington7, Arka Majumdar6,8, P. James Shuck7, Joshua Hendrickson5, J. Nathan Hohman2,3, Deep Jariwala1,*

1 Department of Electrical and Systems Engineering, University of Pennsylvania, Philadelphia, Pennsylvania 19104, United States

### 2 Institute of Materials Science, University of Connecticut, Storrs CT 06269

3 Department of Chemistry, University of Connecticut, Storrs CT 06269

4 KBR Inc., Beavercreek, Ohio 45431, United States

5 Air Force Research Laboratory, Sensors Directorate, Wright-Patterson Air Force Base, Ohio 45433, United States

6 Department of Physics, University of Washington, Seattle, Washington 98195, United States

7 Department of Mechanical Engineering, Columbia University, New York, new York 10027, United States

8 Department of Electrical and Computer Engineering, University of Washington, Seattle, Washington 98195, United States

* Corresponding authors: sba@iitm.ac.in, dmj@seas.upenn.edu

† These authors contributed equally to this work.

Figure S1. Complex refractive index of mithrene (a) Ψ and (b) Δ spectra that were measured using a J. A. Woollam M2000 spectroscopic ellipsometer and fitted to a multi-Lorentzian to extract the complex refractive index of mithrene. The model yielded a root-mean-square-error (RMSE = 12p-qiΨiExp-ΨiModel2+ΔiExp-ΔiModel2 where p is the number of wavelengths measured, q is the number of fit parameters, and the sum is over all wavelengths) of 1.96 showing excellent agreement between experiment and model.

Section 1. Weak-, Strong-, and Ultrastrong Light-Matter Coupling in Exciton-Polaritons

(1)

The Hamiltonians of exciton-polaritons can be described as the sum of the Hamiltonian of the unperturbed exciton (Hexciton = 12Exσz where Ex is the exciton energy and σz is the exciton transition operator), the unperturbed cavity (Hcavity = Eca†a where Ec is the cavity energy and a† (a) is the creation (destruction) operator for a photon in the cavity), and the interaction Hamiltonian (Hint)1. In the cases of weak coupling (WC) and strong coupling (SC), only the first-order effects of an exciton absorbing and emitting a photon have to be considered for Hint. Therefore, the interaction Hamiltonian for WC and SC can be expressed as1:

Hint=g(σ+a+a†σ-)

Where g is the coupling parameter and σ+ (σ-) is the absorption (emission) operator of the exciton. It is clear then that the coupling parameter can be interpretted as the rate at which energy oscillates between the exciton and cavity modes. When solving this Hamiltonian, called the Jaynes-Cummings Hamiltonian, under the condition of zero detuning (∆ =Ex-Ec), the complex eigenenergies are found to be2:

E±= Ex-iΓx+Γc4 ±g2-Γx-Γc216

(2)

Where Γx (Γc) is the loss rate of the exciton (cavity). Through inspection of Eq. 2, the WC regime is defined as the region where g2<Γx-Γc216. In this regime, the coupling parameter only affects the imaginary part of the eigenenergy, and therefore, it only affects the decay rate of the states and does not affect their energies. However, when g2>Γx-Γc216, the system enters the SC regime, and the states become hybrized as the coupling parameter shifts the energies of the two eigenstates.

(3)

Weakly and strongly coupled systems can both be accurately modelled while only considering the first order effects. However, as the coupling parameter increases, and energy oscillates between the exciton and cavity more rapidly, higher-order effects such as the fast-rotating components of the exciton-cavity interactions must be considered to accurately model the system. Although these effects are always present in exciton-polaritons, their effects are not significant until the coupling parameter is 10% of the exciton energy. Therefore, by convention, the ultrastrong coupling (USC) regime is when gEx>0.1 . In the USC regime, the polariton energies are the positive solutions to the bi-quadratic3:

E±2-Ec2E±2-Ex2-4g2E±2EcEx=0

The coupling parameter for both the SC and USC regimes can then be extracted by using the transfer matrix method (TMM) to calculate the thickness dependence of the UEP and LEP since the cavity wavelength depends linearly on the mithrene thickness. The dispersion of the UEP and LEP are then fitted to Eq. 2 for the SC regime and Eq. 3 for the USC regime using a least-squared-error method to determine the coupling parameter of the exciton-polaritons.

Figure S2. Simulated higher order (HO) and lower exciton-polariton (LEP) modes in mithrene on Au. Mithrene thickness-dependent reflectance spectra for a mithrene flake on an Au substrate. The HO mode can be seen to convert into an LEP mode as the mithrene thickness increases since the detuning between the exciton and cavity modes decreases.

Figure S3. Simulation studies on layer-dependent absorption for open-cavity polaritons. (a) Using Au substrate for open cavity polaritons results in almost 40% light absorption around the mithrene exciton peak (475 nm). (b) By using Ag with a 10 nm Al2O3, the contribution from metal absorption can be drastically reduced from 40% to ~5%. Also, the 10 nm Al2O3 layer protects the silver from oxidation and avoids unwanted reaction between Ag and mithrene.

Figure S4. Q-factor of exciton-polaritons in open and closed geometries. The deconvoluted spectra of the (a) open and (b) closed cavity systems as shown in Figure 3d. The experimental data was deconvoluted into multiple Gaussian peaks and the average Q-factors were found to be 23.6 and 44.0 for the open and closed cavity systems, respectively.

Figure S5. Dispersion of exciton-polaritons in mithrene using silver reflectors. The mithrene thickness dependence of the reflectance spectra for an (a) open and (b) closed cavity system. From top to botton, the open cavity system is mithrene/Al2O3 (10 nm)/Ag, and the closed cavity system is Ag (15 nm)/Al2O3 (10 nm)/mithrene/Al2O3 (10 nm)/Ag. The coupling parameters were extracted using the quantum Rabi model as discussed in section S1.

Figure S6. Temperature-dependent optical properties of exciton and exciton-polariton from mithrene. (a) reflectance and (b) PL spectra from the mithrene on quartz substrate shows a blue-shift in the exciton peak position upon cooling. (c) reflectance and (d) PL from the mithrene on Au substrate shows multiple polariton branches below the exciton peak due to the contribution from higher-order cavities. The line spectra at 300 K (e) and 80 K (f) shows the linewidth narrowing of the E-P peak and multiple polariton branches upon cooling to 80 K.

Figure S7. Emergence of multiple polariton branches from Mithrene in closed cavity. (a) Optical micrographs of mithrene in closed cavity (PMMA/15 nm Ag/10 nm Al2O3/PMMA/ Mithrene/10 nm Al2O3/100 nm Ag). (b) PL at 300 K showing a dominant exciton-polariton emission and (c) at 80 K the emergence of multiple polariton branches at longer wavelength can be observed. The linewidth of the most intense PL peak at 80 K were ~1 nm.

Slope correction to E-K measurements.

To correct for the slope in the E-K measurements caused by the slight tiltof the CCD array, a linear transform was performed on the raw data. By analyzing the spectral tilt, a slope was determined from the spectra and could be used as a correction value. The slope was measured on several spectra and an average value of 0.0176 sin(θ)/pixel was determined. This correlates to the spectra being tilted one vertical pixel approximately every 29 horizontal pixels. Once this was determined, a linear transform was performed on the dataset correcting the data only in the background region, outside of the E-K measurement. Before and after correction data can be seen in Figure S8, Supporting Information.

Figure S8. E-k data correction. The raw data without any data treatment (a) and correcting the drift by a slope value (b) is shown here.

Table S1. Anisotropic, complex refractive index of mithrene

| Wavelength (nm) | nord | kord | next | kext |
| --- | --- | --- | --- | --- |
| 350.9151 | 1.571173 | 0.280109 | 1.47571 | 0.088286 |
| 352.5063 | 1.574049 | 0.281995 | 1.476738 | 0.096357 |
| 354.0975 | 1.576889 | 0.283757 | 1.478456 | 0.104147 |
| 355.6887 | 1.579684 | 0.285395 | 1.480793 | 0.111581 |
| 357.2799 | 1.582424 | 0.28691 | 1.483671 | 0.1186 |
| 358.8712 | 1.5851 | 0.288304 | 1.48701 | 0.125164 |
| 360.4623 | 1.587702 | 0.289577 | 1.490733 | 0.131245 |
| 362.0535 | 1.590218 | 0.290732 | 1.494764 | 0.136829 |
| 363.6447 | 1.592637 | 0.291769 | 1.499033 | 0.141913 |
| 365.2359 | 1.594947 | 0.292691 | 1.503477 | 0.146499 |
| 366.8271 | 1.597135 | 0.2935 | 1.508036 | 0.150597 |
| 368.4183 | 1.599187 | 0.294198 | 1.512658 | 0.154222 |
| 370.0095 | 1.601087 | 0.294788 | 1.517293 | 0.157391 |
| 371.6007 | 1.602818 | 0.295273 | 1.521898 | 0.160125 |
| 373.1919 | 1.604362 | 0.295656 | 1.526432 | 0.162446 |
| 374.783 | 1.605699 | 0.29594 | 1.530859 | 0.164378 |
| 376.3742 | 1.606805 | 0.29613 | 1.535144 | 0.165947 |
| 377.9654 | 1.607654 | 0.29623 | 1.539258 | 0.167181 |
| 379.5565 | 1.608218 | 0.296245 | 1.543171 | 0.168108 |
| 381.1476 | 1.608461 | 0.296181 | 1.546858 | 0.168758 |
| 382.7388 | 1.608344 | 0.296046 | 1.550296 | 0.169163 |
| 384.3299 | 1.60782 | 0.295848 | 1.553463 | 0.169355 |
| 385.9211 | 1.606831 | 0.295597 | 1.556342 | 0.169369 |
| 387.5122 | 1.605308 | 0.295307 | 1.558918 | 0.169239 |
| 389.1033 | 1.60316 | 0.294997 | 1.561178 | 0.168997 |
| 390.6944 | 1.600273 | 0.294698 | 1.56311 | 0.168678 |
| 392.2855 | 1.596493 | 0.294465 | 1.564703 | 0.168313 |
| 393.8765 | 1.591627 | 0.294401 | 1.565946 | 0.16793 |
| 395.4676 | 1.585438 | 0.294691 | 1.566824 | 0.167553 |
| 397.0587 | 1.577678 | 0.295653 | 1.567308 | 0.167204 |
| 398.6497 | 1.568151 | 0.297783 | 1.567345 | 0.166901 |
| 400.2408 | 1.556831 | 0.301753 | 1.566839 | 0.166679 |
| 401.8318 | 1.543985 | 0.308339 | 1.565624 | 0.166635 |
| 403.4228 | 1.530261 | 0.318239 | 1.563501 | 0.167029 |
| 405.0138 | 1.516623 | 0.331817 | 1.560389 | 0.168361 |
| 406.6048 | 1.504095 | 0.348927 | 1.556575 | 0.17127 |
| 408.1957 | 1.493377 | 0.368962 | 1.552805 | 0.176184 |
| 409.7867 | 1.484573 | 0.391204 | 1.550012 | 0.182978 |
| 411.3776 | 1.477262 | 0.415348 | 1.548846 | 0.190997 |
| 412.9686 | 1.470976 | 0.441849 | 1.549418 | 0.199435 |
| 414.5595 | 1.465859 | 0.471819 | 1.551423 | 0.207695 |
| 416.1504 | 1.463119 | 0.506445 | 1.554388 | 0.21552 |
| 417.7413 | 1.46495 | 0.546182 | 1.557849 | 0.222964 |
| 419.3322 | 1.47391 | 0.590166 | 1.561461 | 0.230376 |
| 420.923 | 1.492035 | 0.636193 | 1.565181 | 0.238394 |
| 422.5139 | 1.520185 | 0.681265 | 1.569557 | 0.247783 |
| 424.1047 | 1.557893 | 0.722339 | 1.575944 | 0.258921 |
| 425.6955 | 1.603667 | 0.756908 | 1.586179 | 0.27101 |
| 427.2862 | 1.655419 | 0.783233 | 1.601455 | 0.281679 |
| 428.877 | 1.710808 | 0.800335 | 1.621014 | 0.287792 |
| 430.4678 | 1.767441 | 0.807924 | 1.641947 | 0.287228 |
| 432.0585 | 1.823002 | 0.806344 | 1.660556 | 0.280216 |
| 433.6492 | 1.875383 | 0.796555 | 1.674225 | 0.26914 |
| 435.2399 | 1.922865 | 0.780101 | 1.68241 | 0.257103 |
| 436.8305 | 1.964306 | 0.759002 | 1.686278 | 0.246446 |
| 438.4212 | 1.999361 | 0.735541 | 1.687603 | 0.238134 |
| 440.0118 | 2.028561 | 0.711942 | 1.687828 | 0.232058 |
| 441.6024 | 2.053274 | 0.689984 | 1.687746 | 0.227659 |
| 443.193 | 2.075454 | 0.670646 | 1.687621 | 0.224392 |
| 444.7835 | 2.097217 | 0.653906 | 1.687424 | 0.221898 |
| 446.3741 | 2.120349 | 0.638766 | 1.687012 | 0.220009 |
| 447.9646 | 2.145893 | 0.623543 | 1.686196 | 0.218721 |
| 449.5551 | 2.173941 | 0.606318 | 1.684783 | 0.218185 |
| 451.1456 | 2.203696 | 0.58541 | 1.682616 | 0.218731 |
| 452.736 | 2.233738 | 0.55971 | 1.679673 | 0.220888 |
| 454.3264 | 2.262382 | 0.528823 | 1.67619 | 0.225334 |
| 455.9168 | 2.287998 | 0.493026 | 1.672752 | 0.232775 |
| 457.5071 | 2.309237 | 0.45312 | 1.670309 | 0.243795 |
| 459.0975 | 2.325148 | 0.410229 | 1.670147 | 0.25876 |
| 460.6878 | 2.335189 | 0.365624 | 1.673921 | 0.277736 |
| 462.2781 | 2.339201 | 0.320592 | 1.683786 | 0.30026 |
| 463.8683 | 2.337339 | 0.276339 | 1.702363 | 0.32475 |
| 465.4586 | 2.330014 | 0.233935 | 1.732031 | 0.347754 |
| 467.0488 | 2.317833 | 0.194285 | 1.773331 | 0.363867 |
| 468.6389 | 2.301551 | 0.158107 | 1.823439 | 0.367236 |
| 470.2291 | 2.282022 | 0.12591 | 1.876279 | 0.354078 |
| 471.8192 | 2.260154 | 0.097992 | 1.924565 | 0.324384 |
| 473.4093 | 2.236852 | 0.074436 | 1.962292 | 0.281625 |
| 474.9993 | 2.212972 | 0.055119 | 1.986071 | 0.231067 |
| 476.5894 | 2.189265 | 0.039743 | 1.995016 | 0.178175 |
| 478.1794 | 2.166343 | 0.027878 | 1.99008 | 0.127858 |
| 479.7693 | 2.144657 | 0.019009 | 1.973672 | 0.084211 |
| 481.3592 | 2.124492 | 0.012592 | 1.949489 | 0.050097 |
| 482.9491 | 2.105987 | 0.008101 | 1.921966 | 0.026502 |
| 484.539 | 2.089153 | 0.005059 | 1.895155 | 0.012315 |
| 486.1288 | 2.073918 | 0.003067 | 1.87164 | 0.005002 |
| 487.7187 | 2.060149 | 0.001805 | 1.852246 | 0.001793 |
| 489.3084 | 2.047689 | 0.001031 | 1.836573 | 0.000595 |
| 490.8981 | 2.036373 | 0.000572 | 1.823773 | 0.000207 |
| 492.4879 | 2.026047 | 0.000308 | 1.813053 | 0.000091 |
| 494.0775 | 2.016572 | 0.000161 | 1.803841 | 0.000054 |
| 495.6671 | 2.007831 | 0.000082 | 1.79576 | 0.000038 |
| 497.2567 | 1.999722 | 0.000041 | 1.788564 | 0.000028 |
| 498.8463 | 1.992163 | 0.000019 | 1.782081 | 0.00002 |
| 500.4359 | 1.985087 | 0.000009 | 1.776189 | 0.000015 |
| 502.0253 | 1.978439 | 0.000004 | 1.770794 | 0.000011 |
| 503.6147 | 1.97217 | 0.000002 | 1.765825 | 0.000008 |
| 505.2042 | 1.966243 | 0.000001 | 1.761222 | 0.000006 |
| 506.7935 | 1.960625 | 0 | 1.756941 | 0.000004 |
| 508.3829 | 1.955288 | 0 | 1.752941 | 0.000003 |
| 509.9722 | 1.950207 | 0 | 1.749192 | 0.000002 |
| 511.5614 | 1.945361 | 0 | 1.745666 | 0.000002 |
| 513.1507 | 1.940731 | 0 | 1.74234 | 0.000001 |
| 514.7399 | 1.936302 | 0 | 1.739195 | 0.000001 |
| 516.329 | 1.932058 | 0 | 1.736212 | 0.000001 |
| 517.9181 | 1.927986 | 0 | 1.733379 | 0 |
| 519.5071 | 1.924075 | 0 | 1.730681 | 0 |
| 521.0961 | 1.920314 | 0 | 1.728108 | 0 |
| 522.6852 | 1.916693 | 0 | 1.725649 | 0 |
| 524.274 | 1.913204 | 0 | 1.723295 | 0 |
| 525.863 | 1.909838 | 0 | 1.721039 | 0 |
| 527.4518 | 1.906588 | 0 | 1.718873 | 0 |
| 529.0406 | 1.903448 | 0 | 1.716791 | 0 |
| 530.6294 | 1.900411 | 0 | 1.714786 | 0 |
| 532.2181 | 1.897472 | 0 | 1.712855 | 0 |
| 533.8068 | 1.894625 | 0 | 1.710992 | 0 |
| 535.3954 | 1.891866 | 0 | 1.709193 | 0 |
| 536.984 | 1.88919 | 0 | 1.707453 | 0 |
| 538.5725 | 1.886593 | 0 | 1.70577 | 0 |
| 540.161 | 1.884071 | 0 | 1.704139 | 0 |
| 541.7495 | 1.881621 | 0 | 1.702559 | 0 |
| 543.3378 | 1.879238 | 0 | 1.701025 | 0 |
| 544.9262 | 1.876921 | 0 | 1.699536 | 0 |
| 546.5145 | 1.874665 | 0 | 1.698089 | 0 |
| 548.1028 | 1.872469 | 0 | 1.696681 | 0 |
| 549.691 | 1.87033 | 0 | 1.695312 | 0 |
| 551.2792 | 1.868244 | 0 | 1.693978 | 0 |
| 552.8672 | 1.866211 | 0 | 1.692679 | 0 |
| 554.4553 | 1.864227 | 0 | 1.691412 | 0 |
| 556.0433 | 1.862291 | 0 | 1.690176 | 0 |
| 557.6313 | 1.860401 | 0 | 1.68897 | 0 |
| 559.2192 | 1.858554 | 0 | 1.687792 | 0 |
| 560.807 | 1.85675 | 0 | 1.686641 | 0 |
| 562.3949 | 1.854987 | 0 | 1.685516 | 0 |
| 563.9826 | 1.853263 | 0 | 1.684415 | 0 |
| 565.5703 | 1.851576 | 0 | 1.683338 | 0 |
| 567.158 | 1.849926 | 0 | 1.682283 | 0 |
| 568.7455 | 1.84831 | 0 | 1.68125 | 0 |
| 570.3331 | 1.846728 | 0 | 1.680238 | 0 |
| 571.9206 | 1.845179 | 0 | 1.679245 | 0 |
| 573.508 | 1.843661 | 0 | 1.678272 | 0 |
| 575.0954 | 1.842174 | 0 | 1.677316 | 0 |
| 576.6827 | 1.840715 | 0 | 1.676378 | 0 |
| 578.27 | 1.839285 | 0 | 1.675458 | 0 |
| 579.8572 | 1.837883 | 0 | 1.674553 | 0 |
| 581.4444 | 1.836506 | 0 | 1.673664 | 0 |
| 583.0315 | 1.835156 | 0 | 1.67279 | 0 |
| 584.6185 | 1.83383 | 0 | 1.671931 | 0 |
| 586.2055 | 1.832528 | 0 | 1.671085 | 0 |
| 587.7924 | 1.83125 | 0 | 1.670253 | 0 |
| 589.3793 | 1.829994 | 0 | 1.669435 | 0 |
| 590.9661 | 1.82876 | 0 | 1.66863 | 0 |
| 592.5529 | 1.827547 | 0 | 1.667836 | 0 |
| 594.1396 | 1.826355 | 0 | 1.667055 | 0 |
| 595.7262 | 1.825182 | 0 | 1.666286 | 0 |
| 597.3128 | 1.824029 | 0 | 1.665528 | 0 |
| 598.8993 | 1.822895 | 0 | 1.66478 | 0 |
| 600.4858 | 1.821779 | 0 | 1.664043 | 0 |
| 602.0721 | 1.820682 | 0 | 1.663316 | 0 |
| 603.6585 | 1.819601 | 0 | 1.6626 | 0 |
| 605.2448 | 1.818537 | 0 | 1.661892 | 0 |
| 606.8309 | 1.817489 | 0 | 1.661193 | 0 |
| 608.4171 | 1.816458 | 0 | 1.660504 | 0 |
| 610.0032 | 1.815442 | 0 | 1.659822 | 0 |
| 611.5892 | 1.81444 | 0 | 1.65915 | 0 |
| 613.1752 | 1.813454 | 0 | 1.658485 | 0 |
| 614.761 | 1.812482 | 0 | 1.657827 | 0 |
| 616.3469 | 1.811524 | 0 | 1.657178 | 0 |
| 617.9327 | 1.810579 | 0 | 1.656535 | 0 |
| 619.5184 | 1.809648 | 0 | 1.6559 | 0 |
| 621.1039 | 1.808729 | 0 | 1.655272 | 0 |
| 622.6896 | 1.807823 | 0 | 1.65465 | 0 |
| 624.275 | 1.806929 | 0 | 1.654035 | 0 |
| 625.8605 | 1.806048 | 0 | 1.653427 | 0 |
| 627.4458 | 1.805178 | 0 | 1.652824 | 0 |
| 629.0311 | 1.804319 | 0 | 1.652228 | 0 |
| 630.6163 | 1.803471 | 0 | 1.651637 | 0 |
| 632.2015 | 1.802635 | 0 | 1.651052 | 0 |
| 633.7866 | 1.801808 | 0 | 1.650473 | 0 |
| 635.3716 | 1.800993 | 0 | 1.649899 | 0 |
| 636.9565 | 1.800187 | 0 | 1.64933 | 0 |
| 638.5414 | 1.799391 | 0 | 1.648766 | 0 |
| 640.1262 | 1.798605 | 0 | 1.648208 | 0 |
| 641.711 | 1.797828 | 0 | 1.647654 | 0 |
| 643.2956 | 1.797061 | 0 | 1.647105 | 0 |
| 644.8802 | 1.796303 | 0 | 1.64656 | 0 |
| 646.4647 | 1.795554 | 0 | 1.64602 | 0 |
| 648.0492 | 1.794813 | 0 | 1.645484 | 0 |
| 649.6335 | 1.794081 | 0 | 1.644953 | 0 |
| 651.2179 | 1.793357 | 0 | 1.644425 | 0 |
| 652.8021 | 1.792641 | 0 | 1.643902 | 0 |
| 654.3862 | 1.791933 | 0 | 1.643383 | 0 |
| 655.9703 | 1.791232 | 0 | 1.642867 | 0 |
| 657.5543 | 1.79054 | 0 | 1.642356 | 0 |
| 659.1383 | 1.789854 | 0 | 1.641848 | 0 |
| 660.7221 | 1.789176 | 0 | 1.641343 | 0 |
| 662.3059 | 1.788505 | 0 | 1.640842 | 0 |
| 663.8896 | 1.787841 | 0 | 1.640345 | 0 |
| 665.4733 | 1.787183 | 0 | 1.639851 | 0 |
| 667.0568 | 1.786533 | 0 | 1.63936 | 0 |
| 668.6403 | 1.785889 | 0 | 1.638872 | 0 |
| 670.2236 | 1.785251 | 0 | 1.638387 | 0 |
| 671.8069 | 1.784619 | 0 | 1.637905 | 0 |
| 673.3902 | 1.783994 | 0 | 1.637427 | 0 |
| 674.9733 | 1.783375 | 0 | 1.636951 | 0 |
| 676.5564 | 1.782761 | 0 | 1.636478 | 0 |
| 678.1394 | 1.782153 | 0 | 1.636008 | 0 |
| 679.7223 | 1.781551 | 0 | 1.63554 | 0 |
| 681.3052 | 1.780955 | 0 | 1.635075 | 0 |
| 682.8879 | 1.780364 | 0 | 1.634613 | 0 |
| 684.4706 | 1.779778 | 0 | 1.634153 | 0 |
| 686.0532 | 1.779197 | 0 | 1.633695 | 0 |
| 687.6357 | 1.778622 | 0 | 1.63324 | 0 |
| 689.2181 | 1.778052 | 0 | 1.632788 | 0 |
| 690.8004 | 1.777486 | 0 | 1.632337 | 0 |
| 692.3827 | 1.776926 | 0 | 1.631889 | 0 |
| 693.9649 | 1.77637 | 0 | 1.631443 | 0 |
| 695.547 | 1.775819 | 0 | 1.630999 | 0 |
| 697.129 | 1.775273 | 0 | 1.630557 | 0 |
| 698.7109 | 1.774731 | 0 | 1.630118 | 0 |
| 700.2928 | 1.774193 | 0 | 1.62968 | 0 |
| 701.8745 | 1.77366 | 0 | 1.629244 | 0 |
| 703.4562 | 1.773131 | 0 | 1.62881 | 0 |
| 705.0377 | 1.772606 | 0 | 1.628378 | 0 |
| 706.6193 | 1.772086 | 0 | 1.627948 | 0 |
| 708.2006 | 1.771569 | 0 | 1.62752 | 0 |
| 709.782 | 1.771057 | 0 | 1.627093 | 0 |
| 711.3632 | 1.770548 | 0 | 1.626668 | 0 |
| 712.9443 | 1.770043 | 0 | 1.626245 | 0 |
| 714.5254 | 1.769542 | 0 | 1.625823 | 0 |
| 716.1063 | 1.769045 | 0 | 1.625403 | 0 |
| 717.6872 | 1.768551 | 0 | 1.624985 | 0 |
| 719.268 | 1.768061 | 0 | 1.624568 | 0 |
| 720.8487 | 1.767575 | 0 | 1.624152 | 0 |
| 722.4293 | 1.767092 | 0 | 1.623738 | 0 |
| 724.0098 | 1.766612 | 0 | 1.623326 | 0 |
| 725.5902 | 1.766136 | 0 | 1.622915 | 0 |
| 727.1705 | 1.765663 | 0 | 1.622505 | 0 |
| 728.7508 | 1.765193 | 0 | 1.622096 | 0 |
| 730.3309 | 1.764726 | 0 | 1.621689 | 0 |
| 731.911 | 1.764263 | 0 | 1.621283 | 0 |
| 733.4909 | 1.763802 | 0 | 1.620879 | 0 |
| 735.0708 | 1.763345 | 0 | 1.620475 | 0 |
| 736.6505 | 1.762891 | 0 | 1.620073 | 0 |
| 738.2302 | 1.762439 | 0 | 1.619672 | 0 |
| 739.8098 | 1.761991 | 0 | 1.619272 | 0 |
| 741.3893 | 1.761545 | 0 | 1.618873 | 0 |
| 742.9686 | 1.761102 | 0 | 1.618476 | 0 |
| 744.548 | 1.760662 | 0 | 1.618079 | 0 |
| 746.1271 | 1.760225 | 0 | 1.617684 | 0 |
| 747.7062 | 1.75979 | 0 | 1.617289 | 0 |
| 749.2853 | 1.759358 | 0 | 1.616895 | 0 |
| 750.8641 | 1.758929 | 0 | 1.616503 | 0 |
| 752.443 | 1.758502 | 0 | 1.616111 | 0 |
| 754.0216 | 1.758078 | 0 | 1.615721 | 0 |
| 755.6002 | 1.757656 | 0 | 1.615331 | 0 |
| 757.1788 | 1.757237 | 0 | 1.614942 | 0 |
| 758.7572 | 1.75682 | 0 | 1.614554 | 0 |
| 760.3354 | 1.756406 | 0 | 1.614167 | 0 |
| 761.9137 | 1.755994 | 0 | 1.61378 | 0 |
| 763.4918 | 1.755584 | 0 | 1.613395 | 0 |
| 765.0698 | 1.755177 | 0 | 1.61301 | 0 |
| 766.6477 | 1.754772 | 0 | 1.612626 | 0 |
| 768.2255 | 1.754369 | 0 | 1.612243 | 0 |
| 769.8032 | 1.753968 | 0 | 1.61186 | 0 |
| 771.3807 | 1.75357 | 0 | 1.611479 | 0 |
| 772.9583 | 1.753174 | 0 | 1.611098 | 0 |
| 774.5356 | 1.752779 | 0 | 1.610717 | 0 |
| 776.1129 | 1.752387 | 0 | 1.610337 | 0 |
| 777.6901 | 1.751996 | 0 | 1.609959 | 0 |
| 779.2672 | 1.751608 | 0 | 1.60958 | 0 |
| 780.8441 | 1.751221 | 0 | 1.609202 | 0 |
| 782.421 | 1.750836 | 0 | 1.608825 | 0 |
| 783.9978 | 1.750453 | 0 | 1.608449 | 0 |
| 785.5744 | 1.750072 | 0 | 1.608073 | 0 |
| 787.151 | 1.749692 | 0 | 1.607697 | 0 |
| 788.7274 | 1.749315 | 0 | 1.607322 | 0 |
| 790.3038 | 1.748939 | 0 | 1.606948 | 0 |
| 791.88 | 1.748565 | 0 | 1.606574 | 0 |
| 793.4561 | 1.748192 | 0 | 1.6062 | 0 |
| 795.0321 | 1.747822 | 0 | 1.605828 | 0 |
| 796.608 | 1.747453 | 0 | 1.605455 | 0 |
| 798.1838 | 1.747086 | 0 | 1.605083 | 0 |
| 799.7595 | 1.74672 | 0 | 1.604712 | 0 |
| 801.335 | 1.746356 | 0 | 1.604341 | 0 |
| 802.9105 | 1.745994 | 0 | 1.60397 | 0 |
| 804.4858 | 1.745633 | 0 | 1.6036 | 0 |
| 806.061 | 1.745274 | 0 | 1.60323 | 0 |
| 807.6362 | 1.744916 | 0 | 1.602861 | 0 |
| 809.2112 | 1.74456 | 0 | 1.602492 | 0 |
| 810.7861 | 1.744205 | 0 | 1.602123 | 0 |
| 812.3609 | 1.743852 | 0 | 1.601755 | 0 |
| 813.9355 | 1.7435 | 0 | 1.601387 | 0 |
| 815.5101 | 1.743149 | 0 | 1.601019 | 0 |
| 817.0846 | 1.7428 | 0 | 1.600652 | 0 |
| 818.6589 | 1.742453 | 0 | 1.600285 | 0 |
| 820.2331 | 1.742107 | 0 | 1.599918 | 0 |
| 821.8073 | 1.741762 | 0 | 1.599552 | 0 |
| 823.3812 | 1.741418 | 0 | 1.599186 | 0 |
| 824.9551 | 1.741076 | 0 | 1.59882 | 0 |
| 826.5288 | 1.740735 | 0 | 1.598455 | 0 |
| 828.1024 | 1.740395 | 0 | 1.598089 | 0 |
| 829.676 | 1.740057 | 0 | 1.597724 | 0 |
| 831.2493 | 1.73972 | 0 | 1.59736 | 0 |
| 832.8226 | 1.739384 | 0 | 1.596995 | 0 |
| 834.3958 | 1.739049 | 0 | 1.596631 | 0 |
| 835.9689 | 1.738716 | 0 | 1.596267 | 0 |
| 837.5418 | 1.738383 | 0 | 1.595903 | 0 |
| 839.1146 | 1.738052 | 0 | 1.595539 | 0 |
| 840.6873 | 1.737722 | 0 | 1.595176 | 0 |
| 842.2599 | 1.737393 | 0 | 1.594812 | 0 |
| 843.8323 | 1.737065 | 0 | 1.594449 | 0 |
| 845.4046 | 1.736738 | 0 | 1.594086 | 0 |
| 846.9769 | 1.736412 | 0 | 1.593723 | 0 |
| 848.549 | 1.736088 | 0 | 1.59336 | 0 |
| 850.1209 | 1.735764 | 0 | 1.592998 | 0 |
| 851.6927 | 1.735441 | 0 | 1.592635 | 0 |
| 853.2645 | 1.73512 | 0 | 1.592273 | 0 |
| 854.8361 | 1.734799 | 0 | 1.591911 | 0 |
| 856.4075 | 1.73448 | 0 | 1.591548 | 0 |
| 857.9788 | 1.734161 | 0 | 1.591186 | 0 |
| 859.55 | 1.733843 | 0 | 1.590824 | 0 |
| 861.1211 | 1.733526 | 0 | 1.590463 | 0 |
| 862.6921 | 1.733211 | 0 | 1.590101 | 0 |
| 864.263 | 1.732895 | 0 | 1.589739 | 0 |
| 865.8337 | 1.732581 | 0 | 1.589378 | 0 |
| 867.4043 | 1.732268 | 0 | 1.589016 | 0 |
| 868.9747 | 1.731956 | 0 | 1.588655 | 0 |
| 870.545 | 1.731644 | 0 | 1.588293 | 0 |
| 872.1152 | 1.731334 | 0 | 1.587932 | 0 |
| 873.6854 | 1.731024 | 0 | 1.58757 | 0 |
| 875.2552 | 1.730715 | 0 | 1.587209 | 0 |
| 876.8251 | 1.730407 | 0 | 1.586848 | 0 |
| 878.3948 | 1.730099 | 0 | 1.586486 | 0 |
| 879.9644 | 1.729793 | 0 | 1.586125 | 0 |
| 881.5338 | 1.729487 | 0 | 1.585764 | 0 |
| 883.1031 | 1.729182 | 0 | 1.585402 | 0 |
| 884.6724 | 1.728877 | 0 | 1.585041 | 0 |
| 886.2414 | 1.728574 | 0 | 1.58468 | 0 |
| 887.8102 | 1.728271 | 0 | 1.584318 | 0 |
| 889.3791 | 1.727969 | 0 | 1.583957 | 0 |
| 890.9478 | 1.727667 | 0 | 1.583596 | 0 |
| 892.5162 | 1.727367 | 0 | 1.583234 | 0 |
| 894.0846 | 1.727067 | 0 | 1.582873 | 0 |
| 895.6528 | 1.726767 | 0 | 1.582511 | 0 |
| 897.221 | 1.726468 | 0 | 1.58215 | 0 |
| 898.7889 | 1.72617 | 0 | 1.581788 | 0 |
| 900.3568 | 1.725873 | 0 | 1.581427 | 0 |
| 901.9245 | 1.725576 | 0 | 1.581065 | 0 |
| 903.4921 | 1.72528 | 0 | 1.580703 | 0 |
| 905.0596 | 1.724985 | 0 | 1.580341 | 0 |
| 906.6268 | 1.72469 | 0 | 1.579979 | 0 |
| 908.194 | 1.724396 | 0 | 1.579617 | 0 |
| 909.761 | 1.724102 | 0 | 1.579255 | 0 |
| 911.3279 | 1.723809 | 0 | 1.578893 | 0 |
| 912.8947 | 1.723516 | 0 | 1.578531 | 0 |
| 914.4613 | 1.723224 | 0 | 1.578168 | 0 |
| 916.0278 | 1.722933 | 0 | 1.577806 | 0 |
| 917.5941 | 1.722642 | 0 | 1.577443 | 0 |
| 919.1603 | 1.722352 | 0 | 1.57708 | 0 |
| 920.7264 | 1.722062 | 0 | 1.576717 | 0 |
| 922.2924 | 1.721773 | 0 | 1.576355 | 0 |
| 923.8582 | 1.721485 | 0 | 1.575991 | 0 |
| 925.4238 | 1.721196 | 0 | 1.575628 | 0 |
| 926.9894 | 1.720909 | 0 | 1.575265 | 0 |
| 928.5547 | 1.720622 | 0 | 1.574901 | 0 |
| 930.1199 | 1.720335 | 0 | 1.574538 | 0 |
| 931.6849 | 1.720049 | 0 | 1.574174 | 0 |
| 933.2499 | 1.719763 | 0 | 1.57381 | 0 |
| 934.8148 | 1.719478 | 0 | 1.573446 | 0 |
| 936.3794 | 1.719194 | 0 | 1.573082 | 0 |
| 937.9438 | 1.718909 | 0 | 1.572717 | 0 |
| 939.5082 | 1.718626 | 0 | 1.572353 | 0 |
| 941.0724 | 1.718342 | 0 | 1.571988 | 0 |
| 942.6365 | 1.718059 | 0 | 1.571623 | 0 |
| 944.2005 | 1.717777 | 0 | 1.571258 | 0 |
| 945.7643 | 1.717495 | 0 | 1.570893 | 0 |
| 947.3278 | 1.717214 | 0 | 1.570527 | 0 |
| 948.8914 | 1.716932 | 0 | 1.570162 | 0 |
| 950.4547 | 1.716652 | 0 | 1.569796 | 0 |
| 952.0179 | 1.716371 | 0 | 1.56943 | 0 |
| 953.5809 | 1.716091 | 0 | 1.569064 | 0 |
| 955.1439 | 1.715812 | 0 | 1.568698 | 0 |
| 956.7067 | 1.715533 | 0 | 1.568331 | 0 |
| 958.2692 | 1.715254 | 0 | 1.567964 | 0 |
| 959.8317 | 1.714975 | 0 | 1.567597 | 0 |
| 961.3939 | 1.714697 | 0 | 1.56723 | 0 |
| 962.9562 | 1.714419 | 0 | 1.566863 | 0 |
| 964.5182 | 1.714142 | 0 | 1.566495 | 0 |
| 966.08 | 1.713865 | 0 | 1.566127 | 0 |
| 967.6417 | 1.713589 | 0 | 1.565759 | 0 |
| 969.2032 | 1.713312 | 0 | 1.565391 | 0 |
| 970.7646 | 1.713036 | 0 | 1.565022 | 0 |
| 972.3259 | 1.712761 | 0 | 1.564654 | 0 |
| 973.887 | 1.712485 | 0 | 1.564284 | 0 |
| 975.4479 | 1.71221 | 0 | 1.563915 | 0 |
| 977.0087 | 1.711936 | 0 | 1.563546 | 0 |
| 978.5693 | 1.711661 | 0 | 1.563176 | 0 |
| 980.1299 | 1.711387 | 0 | 1.562806 | 0 |
| 981.6901 | 1.711114 | 0 | 1.562436 | 0 |
| 983.2504 | 1.71084 | 0 | 1.562066 | 0 |
| 984.8104 | 1.710567 | 0 | 1.561695 | 0 |
| 986.3702 | 1.710294 | 0 | 1.561324 | 0 |
| 987.93 | 1.710021 | 0 | 1.560953 | 0 |
| 989.4894 | 1.709749 | 0 | 1.560581 | 0 |
| 991.049 | 1.709477 | 0 | 1.56021 | 0 |
| 992.6081 | 1.709205 | 0 | 1.559838 | 0 |
| 994.1672 | 1.708934 | 0 | 1.559465 | 0 |
| 995.7262 | 1.708663 | 0 | 1.559093 | 0 |
| 997.2849 | 1.708392 | 0 | 1.55872 | 0 |
| 998.8434 | 1.708121 | 0 | 1.558347 | 0 |
| 1012.442 | 1.705767 | 0 | 1.555078 | 0 |
| 1015.843 | 1.705181 | 0 | 1.554257 | 0 |
| 1019.245 | 1.704595 | 0 | 1.553434 | 0 |
| 1022.646 | 1.70401 | 0 | 1.552609 | 0 |
| 1026.049 | 1.703426 | 0 | 1.551782 | 0 |
| 1029.451 | 1.702842 | 0 | 1.550954 | 0 |
| 1032.854 | 1.702259 | 0 | 1.550123 | 0 |
| 1036.257 | 1.701677 | 0 | 1.549291 | 0 |
| 1039.661 | 1.701095 | 0 | 1.548457 | 0 |
| 1043.065 | 1.700514 | 0 | 1.547621 | 0 |
| 1046.47 | 1.699933 | 0 | 1.546784 | 0 |
| 1049.874 | 1.699352 | 0 | 1.545944 | 0 |
| 1053.28 | 1.698772 | 0 | 1.545102 | 0 |
| 1056.685 | 1.698192 | 0 | 1.544259 | 0 |
| 1060.091 | 1.697613 | 0 | 1.543413 | 0 |
| 1063.497 | 1.697034 | 0 | 1.542566 | 0 |
| 1066.904 | 1.696455 | 0 | 1.541716 | 0 |
| 1070.311 | 1.695877 | 0 | 1.540864 | 0 |
| 1073.719 | 1.695298 | 0 | 1.540011 | 0 |
| 1077.126 | 1.69472 | 0 | 1.539155 | 0 |
| 1080.534 | 1.694142 | 0 | 1.538297 | 0 |
| 1083.943 | 1.693564 | 0 | 1.537437 | 0 |
| 1087.352 | 1.692986 | 0 | 1.536575 | 0 |
| 1090.761 | 1.692409 | 0 | 1.535711 | 0 |
| 1094.171 | 1.691831 | 0 | 1.534844 | 0 |
| 1097.581 | 1.691254 | 0 | 1.533976 | 0 |

References

1.	Meystre, P. The Jaynes–Cummings Model. 75–95 (2021) doi:10.1007/978-3-030-76183-7_3.

2.	Reithmaier, J. P. et al. Strong coupling in a single quantum dot–semiconductor microcavity system. Nature 2004 432:7014 432, 197–200 (2004).

3.	Baranov, D. G. et al. Ultrastrong coupling between nanoparticle plasmons and cavity photons at ambient conditions. Nature Communications 2020 11:1 11, 1–9 (2020).